## Slide 1
21st International Conference on Ion Sources, Oxford, UK, 8-12 September 2025
Impedance Characteristics and Sputtering Behaviour of Pulsed Arc Discharge H- Ion Sources
Olli Tarvainen1, Alejandro Garcia Sosa1, Rob Abel1, Dan Bollinger2, Dan Faircloth1, Erin L. Flannigan1, Daniel Jones2, Pat Karns2, Claire Talbott1
1ISIS Pulsed Spallation Neutron and Muon Facility, UK Science and Technology Facilities Council, Rutherford Appleton Laboratory, Harwell, OX11 0QX United Kingdom
2Fermi National Accelerator Laboratory (FNAL), Batavia, IL, USA
Pulsed arc discharge H- ion sources are used in large-scale accelerator facilities, the Penning source at ISIS and magnetron source at Fermilab.
These caesiated ion sources can produce current densities >10 mA/mm2 but suffer from limited lifetime due to erosion of the plasma facing components.
(a) ISIS Penning ion source
(b) Fermilab magnetron ion source
 | ISIS Penning | Fermi magnetron
H- beam current | 50-60 mA | 50-60 mA
Beam energy | 36 keV | 35 keV
Discharge pulse | 700 s | 160 s
Beam pulse | 200 s | 160 s
Repetition rate | 50 Hz | 15 Hz
Lifetime | 28 days | 9 months
The ISIS Penning and Fermilab magnetron sources operate in “low impedance mode” where increasing the discharge current decreases the voltage.
Precise characteristics of the negative impedance discharge depend on the ion source geometry and Cs/H2-ratio in the discharge volume.
ISIS Penning source
Fermilab magnetron source
Sputtering yield model
Y. Yamamura and H. Tawara, Atomic Data and Nuclear Data Tables 62, 149-253 (1996)
The yield Y of ion induced sputtering of solids at normal incidence as a function of the incident particle energy E
The yield depends on the incident ion and solid target properties, most importantly atomic numbers and masses.
Cs+ ions sputter the Mo cathode, H+ threshold energy > qVarc
Sputtering predictions and comparison of the ISIS vs. Fermilab sources
ISIS Penning source
New
36 days
Number of removed molybdenum atoms to compare predicted sputtering damage with different discharge current and voltage
ISIS Penning source: Increase of discharge current results in reduced sputtering (opposite for the magnetron). This is due to the voltage dependence of the sputtering yield.
28 days Penning lifetime translates to > 9 months magnetron lifetime, which agrees well with the operational experience.
Discharge noise affecting the sputtering of the ISIS Penning ion source
The high-frequency noise in the beginning of the discharge pulse worsens over time as the source ages.
The noise is driven by plasma instability and can be controlled by adjusting the Cs/H2-ratio of the discharge.
The noisy part of the discharge is predicted to account for almost 90% of the Mo-cathode sputtering, i.e. the erosion rate of the cathode does not scale linearly with the pulse length.
ISIS Penning source
Fermilab magnetron source