## Slide 1: FETS FFA RF STATUS
Rob Mathieson, Ian Gardner, Bradley Kirk et al.
RAL

## Slide 2
Parameter | Specification for Prototyping
Energy range | 3 –12 MeV
Harmonic | 2
RF frequency | 2.0 – 3.7 MHz
Peak RF Voltage | 6kV
Re-bunching Voltage | 20kV h=1 (0.9 MHz)
Repetition Rate (Burst) | 100Hz (+)
Acceleration Time | 8ms
Approximate Aperture | 700 x 52 mm
Accelerate in 8 ms and test beam stacking
RF Parameters
(Current work is for FETS FFA – ISIS-II is different problem)

## Slide 3: Options Considered
Drift Tube
  Resonators not in stray magnetic fields
  Higher harmonic needed
  Missing bunches & chopped injection needed
Ferrite Cavity plus Fixed Frequency re-buncher
  Low power for cavity but tuning system needs power
  Recovery time concern (2 ms) for 100 Hz operation
Magnetic Alloy Cavity plus Fixed Frequency re-buncher or possibly just 2 MA cavities
  Good recovery time
  No tuning system
  Higher power needed for cavity + Linear Amp.
Cutaway view of Nimrod RF Cavity

## Slide 4
Bias Input
Azimuthal length < 1 m
Three ferrites tested GF5, 8C15 & 4M2 - 4M2 selected
Estimated RF power with 4M2 Ferrite ~ 6 kW + tuner power
Recovery time a concern for 100Hz operation (2ms)
Two Gap Ferrite Cavity

## Slide 5
Bias Input
3kV / Gap
FETS FFA Cavity using 4M2 Ferrite
Overall length ~0.4 m

## Slide 6
4M2 Sample Ferrite Frames
  Tender Exercise November 2021
  First 8 blocks arrived December 2022
  Further blocks short lead time pending approval
Initial tests confirm material performance
  Q ≈ 100 at RF frequencies
  Some evidence of magnetisation from production
Bias winding requires peak of 2800 Amp turns for Δf/f0
  Tests confirm recovery time achievable
  Multiple bias turns may be considered
Further tests required with full frame design
FETS FFA Cavity using 4M2 Ferrite

## Slide 7
MAGNETIC ALLOY SAMPLE TESTING

## Slide 8
Beam ~12 in
MA
Cu
Al
Insulation
Gap
FETS 8 Core MA Cavity with Water Cooling Plates (initial design)
6 kV peak gap voltage over 1-6 MHz
Brf limited to 0.1 T in MA from cooling
Vacuum
0.94 m
Cu MA Cu
0.3 m
Cu may be replaced by Nickel plated mild steel.

## Slide 9
Sample Cores ordered from MagDev & Hitachi
  First Cores arrived Nov 2021
  Special agreement required from KEK for Hitachi
Hitachi core winder

## Slide 10
Low Power Test Set-Up
1K107 Potted
FT3L Epoxy coated

## Slide 11
MagDev 1K107 Core Measurements
Measured with 75 V peak per core (Design voltage 750 V per core).
RF Power for 8 core cavity at 6 kV peak 110 - 150 kW
Consider using 2 cavities at ½ voltage ~38 kW each, meaning no Tuning system and wideband for fast modulations

## Slide 12
Measured with 100 V peak per core
RF Power for 8 core cavity at 6 kV peak 50 - 65 kW
Consider using 2 cavities at ½ voltage ~16 kW each, meaning no Tuning system and wideband for fast modulations
Hitachi FT3L Core Measurements

## Slide 13
FT3L and 1K107 Test Cores
6kW Combiner & Test Cavity
3kW Test SSA

## Slide 14: Initial MA Cooling Plate Design
Cooling plates made in two pieces
Teflon sheet separators
Power tests to measure the cooling

## Slide 15
 | Ferrite | MA
RF Power req. for 6kV | 6kW | 35kW
Amplifier | Solid State Class B (or A) | Large SS/ Small Vacuum Tube Class A or AB Push-pull
Bias Required | Yes Likely ~35kW | No
Est. Wallplug Power (ignoring plant) | ~45kW (Class B) ~60kW (Class A) | ~140kW (A Vac. Tube) ~100kW (B p-p Vac. Tube)
Proximity to Magnetic Fields | µr≈140, absorbed into bias | Problematic µr≈4000
Rep Rate 100Hz+ | Possible | No recovery
Bunch Stacking | Possible 10kV burst on two cavities? | Possible 10kV burst on two cavities?
LLRF | Simple but wide band Tuning system needed | Simple (little beam loading)

## Slide 16: Concluding
Either technology looks feasible to meet cavity specification
  Two cavity option may work in both cases for Acceleration & Re-bunching
Further work
  Power tests to full flux
      750V/core for 8 core cavity -> ~6kW across single core)
  μ dependency on stray B field
  Thermal tests
  Refinement of CST simulations
      Benchmarking
      Non-isotropic permeability & permittivity
Full System Spec – ferrite & MA
  Proceed to full prototype?