## Slide 1: Stripping Foil Studies
Hayley Cavanagh
CSNS Meeting – 23rd July 2025

## Slide 2: Outline
Introduction and Motivation
Aluminium Oxide Foils
Carbon Foils
Diamond Foils
Future…

## Slide 3
Inject high intensity beam, up to 3x1013 ppp, in 200 µs (~133 turns)
Vertical painting with programmable dipole
Injection Dipole
Beam Intensity
Vertical Sweeper
200 µs
  Multi-turn charge exchange injection at 70 MeV
  Accelerator upgrades
Introduction and Motivation
65 mm horizontal bump
Horizontal painting with failing sinusoidal main magnet field

## Slide 4
Proposed 180 MeV Linac
70 MeV Linac
800 MeV RCS
Initial studies as part of 180 MeV injection project showed that aluminium oxide foils used on ISIS at 70 MeV would not withstand expected temperatures
Considered carbon foils as a good compromise material between maximising stripping efficiency and minimising beam scattering and foil temperatures
  Multi-turn charge exchange injection at 70 MeV
  Accelerator upgrades
Introduction and Motivation

## Slide 5
Aluminium Oxide Foils
The foils were very fragile and needed to be cut when installed to reduce tension
The bottom leading corner was left connected, the bottom edge and half height were released from the frame, ≈75% failure on installation
Cut during production
Cut when installed
Mounting foil
Cutting foil
Al2O3 foils were manufactured ‘in-house’, taking ≈20 hrs per foil, however ≈90% foils failed before last stage of manufacture

## Slide 6
  Other labs: J-Parc, CERN, CSNS
  Tests and developments (fibres, annealing, residual nuclei, graphene, electron gun, aerogels)
  Operations
Carbon Foils
Motor drive
Mounting pin hole
Guide slot
Communicated with other labs using DLC/HBC foils, J-Parc, CERN PSB, CSNS (2016!)
Test mounting of small CSNS foil on spare foil change mechanism
Design and manufacture new foil bracket

## Slide 7
  Other labs: J-Parc, CERN, CSNS
  Tests and developments (fibres, annealing) and operations
Carbon Foils
40 mm
60 mm
Successfully mounted larger 60 x 40 mm DLC foils for machine physics, but experienced curling under beam
Developed mounting area in R52 foil preparation laboratory
Aluminium positioning jig
Anti-static guard and anti-static gun
Perspex shield to reduce air flow

## Slide 8
DLC with fibres after 3, 15 and 117 mAh
10 µm carbon fibres, Aquadag and clamped
Varied arrangement and number of fibres
Annealed foil after 0, 1.64 and 15 mAh
70 MeV foil temperature ≈500 K so anneal at 670 K for 2 hrs (+2 hr ramp up and down)
Averaged ~100 mAh/foil, so use x2/cycle
Annealing
SiC fibres
  Other labs: J-Parc, CERN, CSNS
  Tests and developments (fibres, annealing) and operations
Carbon Foils
DLC foils annealed at Micromatter 430-510 K for 2-4 hrs depending on foil condition…

## Slide 9
  SNS small/large size
  Operations since 2019
  Cardiff/Bristol/Diamond Materials
Diamond Foils
100 lines per inch, 5 µm, 55° corrugations
17 x 30 mm, no fibres, top edge support only
17 mm
30 mm
SNS produced 200 µg cm-2 samples for ISIS machine physics
Before etching
2 hours
Etched
17 mm
38 mm
Modified frame and etched using RSE-111 (hydrofluoric, nitric and acetic acid)
35 mm
30 mm
Remaining substrate
Instead test larger 30 x 50 mm 200 µg cm-2 samples for use in operations
OK for machine physics test, but too small for optimised operation

## Slide 10
Date | mAh per foil | Notes
25th November 2019 | 610 | Tear observed top right corner
20th August 2020 | 440 | Change before start-up, new cycles added before long shutdown
8th December 2020 | 426 | Beam loss, possible foil hole? (Unnecessary - beam issue was R5VD1)
9th January 2022 | 327 | Was withdrawn to storage for long shutdown, but observed large hole on inspection before cycle
24th January 2024 | 592 | Losses fine, some curling observed. Good time to change – crew, HP and OPI changes
27th January 2025 | 717 | Losses fine, some curling observed. Good time to change – crew and HP familiarity
  SNS small/large size
  Operations since 2019
  Cardiff/Bristol/Diamond Materials
  SNS small/large size
  Operations since 2019
  Cardiff/Bristol/Diamond Materials
Diamond Foils
Average 520 mAh

## Slide 11
  SNS small/large size
  Operations since 2019
  Cardiff/Bristol/Diamond Materials
Diamond Foils
Look for other nano-crystalline foil producers…
CLF/SciTech producing corrugated silicon substrates
  Define own pattern/radius

## Slide 12
  SNS small/large size
  Operations since 2019
  Cardiff/Bristol/Diamond Materials
Diamond Foils
Sample from Diamond Materials installed on ISIS on 27th January 2025, 355 mAh total
Did SEM and Raman spectroscopy to compare samples from Cardiff/Bristol/Diamond Materials to compare to SNS sample

## Slide 13
  ISIS-II Options
Future
Extraction
Injection
1.2 GeV injection into AR
SNS mount foil at 30° to spread heat over foil and prevent graphitisation
H- injection with laser stripping?
Remove physical foil, reduce scattering
Difficult to achieve long pulse length
Optimised direct proton injection?
Curved foils?
Foil carousel?
400 MeV injection into RCS
Control temperature and lifetime by minimising re-circulations
RCS in ISIS Hall
ESS AR in ISIS Hall

## Slide 14: Summary
Introduction and Motivation
Aluminium Oxide Foils
Carbon Foils
Diamond Foils
Future…

## Slide 15
Publications and Acknowledgements
Publications
IPAC ‘11: Stripping Foil Simulations for ISIS Injection Upgrades, H.V. Smith, B. Jones, D.J. Adams, C.M. Warsop
IPAC ‘12: Simulation of Double Layer Carbon Stripping Foils For ISIS Injection Upgrades, H.V. Smith, B. Jones, D.J. Adams, C.M. Warsop, Y. Irie, T. Takeda
HB 2014: An Overview of the Preparation and Characteristics of the ISIS Stripping Foil, H.V. Smith, B. Jones
IPAC ‘16: Initial Experience with Carbon Stripping Foils at ISIS, B. Jones, H.V. Smith, D.J. Adams
IPAC ‘17: Operation with Carbon Stripping Foils at ISIS, H.V. Cavanagh, B. Jones
IPAC ‘18: Progress with Carbon Stripping Foils at ISIS, B. Jones, H.V. Cavanagh
Acknowledgements
ISIS Vacuum Section: Geoff Matthews, Sunil Patel, Mark Waite
ISIS Injector: Mark Arnold, Nick Terzino
ISIS Diagnostics: Andy Chamberlain, Tony Kershaw, Chris Wilcox
ISIS Project Engineering: Matt Kearsley, Theodore Rutter, Phil Wise
ISIS Operations Crew: All!
ISIS Health Physics: Matt Harrall, David McGarry, John Moir, Paul Wright
ISIS Accelerator Physics: Dean Adams, Peter Griffin-Hicks, Bryan Jones, Ben Pine, Chris Warsop, Rob Williamson
ISIS Experimental Operations: James Taylor, James Tellam
CLF/SciTech Precision: Graham Arthur, Chris Spindloe, Dave Haddock
University of Bristol: Paul May
University of Cardiff: Soumen Mandal, Oliver Williams
Diamond Materials: Christoph Wild
Ridgeway Technology: Richard Bodkin
Research Complex at Harwell: Michal Klosowski, Sara Mosca
CERN: Klaus Hanke, Bettina Mikulec, Wim Weterings
SNS: Sarah Cousineau, Nicholas Evans, Mike Plum, Leslie Wilson
J-Parc: Hiroyuki Harada, Hideaki Hotchi, Yoshiro Irie, Isao Sugai, Yasuhiro Takeda
CSNS: Ming-Yang Huang, Jia-Xin Chen, Jie-Bing Yu, Ling Kang
FNAL: Dave Johnson
Thank you,
Any questions?