## Slide 1: Transforming Inorganic Scintillators into Nuclear Spectrometers
Dr Joseph O'Neill
IOP Nuclear Physics Conference 2026
13th-15th April 2026 | University of Brighton

## Slide 2: Overview
PSD explanation
LaX3 introduction
AFSD explanation
Measurements at NPL low scatter facility
CeBr3 extra data!
Beamline
LaX3

## Slide 3: Waveform Analysis

## Slide 4: Pulse Shape Discrimination – Charge Integration
Charge integrated pulse shape discrimination (PSD)
Exploits the differences in the time characteristics of scintillators
E.g. two types of GAGG(Ce) scintillator’s response to a 662 keV gamma ray
= 29,000
= 34,500
= 28,300
= 39,500
Total = 63,500
PSD = 0.15
Total = 67,800
PSD = 0.28

## Slide 5: PSD – Particle Species Discrimination
Deuterated stilbene
CLYC(Ce)
Cieślak, Michał J., Kelum AA Gamage, and Robert Glover. "Critical review of scintillating crystals for neutron detection." Crystals 9.9 (2019): 480.
Gaughan, N., et al. "Characterization of stilbene-d12 for neutron spectroscopy without time of flight." Nuclear Instruments and Methods in Physics Research Section A: Accelerators, Spectrometers, Detectors and Associated Equipment 1018 (2021): 165822.
Scintillation waveforms can be dependent on the instigating radiation species

## Slide 6: LaX3(Ce) Scintillators

## Slide 7: LaX3 – Cross Sections
(n,p) and (n,α) cross sections align well with energy ranges significant for security and energy (14.1 MeV)
Recent measurements have indicated that the Cl cross sections are well overestimated (Kuvin 2020)
Br data are incomplete
NEA High Priority Request List for Nuclear Data

## Slide 8: LaX3 – Scintillators
LaX3(X = Cl, Br) scintillators doped with Ce3+ have high energy resolution (2-4% at 662 keV), fast decay time (~30 ns) and have dual mode sensitivity (γ+n)
Hygroscopic and non-trivial internal activity from La decay and Ac contamination
Used in a range of facilities and instruments e.g. FATIMA, GRIFFIN etc.

## Slide 9: PSD – Amplitude Frequency Shape Discrimination
Waveforms are passed through a fast Fourier transform
Charge integration then applied with frequency gates
For implementation “live”, this is more computationally intensive than PSD

## Slide 10: AFSD - Example
LaCl3(Ce) response to internal activity and a 137Cs source

## Slide 11: NPL Neutron Facility

## Slide 12: LaX3 – Initial Measurements
Measurements taken with "unoptimised" holder
With and without shadow cone to check scattering contribution
LaCl3 – 2.5 MeV neutrons

## Slide 13: NPL Beam Campaign - Overview
Measurements taken at the NPL low-scatter facility in July 2025
Deuteron beams impinged on deuterieum and tritium targets
A range of monoenergetic neutron energies accessed by varying the beam energy and detector position
Beamline
LaX3

## Slide 14: LaCl3 and LaBr3 NPL Neutron Facility Results

## Slide 15: LaCl3(Ce) Results
AFSD improves separation by a factor of 2
(n,p) and (n,α) peaks observed across all energies
Linear response indicates neutron spectroscopy potential

## Slide 16: LaBr3(Ce) Results
Due to lower cross section in the En=1-5 MeV energy range, no clear response
At higher energies, broad γ, proton and α distributions with α peaks
Proton distributions appear to be spread across many excited states

## Slide 17: CeBr3 NPL Neutron Facility

## Slide 18: CeBr3 AFSD Performance
CeBr3 scintillators have benefits over LaX3 materials, but have no reported PSD capability
AFSD method allows us to separate the low levels of Ac contamination in the internal spectra

## Slide 19: CeBr3 Results
Measurements taken during LaX3 beam test with CeBr3
T(d,n) measurements yield clear proton and alpha bands
CeBr3 can function as neutron detector, or neutron contributions can be accounted for

## Slide 20: Other Analysis Methods
Implementation of different methods onto FPGA systems
Optimising parameters: windowing functions, normalisation, zero padding
Principal component analysis, ML, fitting decays, combinations of different methods etc.

## Slide 21: Thanks for listening!
Thanks to everyone who assisted in this work: Jacob Heery, Jack Henderson, Naomi Gadsby, Giuseppe Lorusso, Mike Bunce, Matt Taggart, Gemma Wilson, Abdul Alshammari, Gee Bartram, Chris Cousins, Katie Garrett, Connor O’Shea, Ed O’Sullivan, Sifa Poulton, David Thomas, Toby Wolverson and Renjie Wu

## Slide 22: PhD Opportunity
Development of Scintillator-Based Neutron Detectors
Explore neutron sensitive organic and inorganic scintillators, with the opportunity to utilise the UoB’s accelerator facilities (cyclotron and neutron irradiation facility )
Investigate current waveform analysis methods, with the view of improving materials’ capability to distinguish between gamma and neutron induced scintillation
Develop the university’s capacity to produce scintillation materials and detectors
To apply, please reach out to j.oneill.3@bham.ac.uk

## Slide 23
Any questions?
LaX3 paper published recently in NIM A

## Slide 24: LaCl3(Ce) Results – Future Cross Section Work
One of the key focuses of the NEA High Priority Request List for Nuclear Data
Ratio from theory = 0.0186
Ratio from measurement = 0.085(6)
In agreement with recent work

## Slide 25: PSD – Quantifying
PSD methods are quantified via the Figure of Merit (FoM)
Improvement in FoM achieved via reducing FWHM of each population, and increasing the separation
Γg
Γa
Cg
Ca
LaCl3 internal activity

## Slide 26: PSD – Optimising
Variables currently being varied
Pre-gate
Short gate
Long gate

## Slide 27: Pileup check

## Slide 28: AFSD – More Examples
LaBr3(Ce) PSD FoM = ??? AFSD FoM = 1.130(1)
LaCl3(Ce) PSD FoM = 0.5(1) AFSD FoM = 1.41(1)

## Slide 29: AFSD – Even More Examples (SiPMs)
AFSD not always an improvement from PSD – materials do have a “limit” of separation

## Slide 30: Simulations
Geant4 – energy dependence on proton and alpha gated responses
LaCl3 response shows contributions from different states and reaction channels
LaBr3 data is dependent on ENDF-VIII – prediction less confident in p channels
LaBr3 – proton response
LaBr3 – alpha response
LaCl3 – proton response
LaCl3 – alpha response

## Slide 31: LaCl3(Ce) Results - D(d,n)
Gain optimised for high energy signals
Noticeable impact on AFSD performance, especially for lower energy signals

## Slide 32: LaCl3(Ce) Results - T(d,n)