## Slide 1: Study on the synergistic optimization of material and thickness of diffusion barrier layer based on copper-based Nb3Sn film by bronze method
Bohao Zhang*, Teng Tan
Institute of Modern Physics, Chinese Academy of Sciences
University of Chinese Academy of Sciences
Advanced Energy Science and Technology Guangdong Laboratory
TFSRF 2026 September 22, 2026
zhangbohao@impcas.ac.cn
1

## Slide 2: Outline
1. Background and motivation
2. Sample preparation
3. Results and discussion
4. Summary and outlook
2

## Slide 3: Nb3Sn and Cu Combine RF and Thermal Functions
Nb3Sn provides better superconducting properties while Cu substrate is used for heat dissipation and supporting the resonant cavity.
1.3 GHz Cu cavity
SRF surface
Nb3Sn
Tc ≈ 18 K
Potential for operation at 4.2 K
Cavity substrate
Cu
High thermal conductivity
Easy machining and lower cost
Cu provides heat removal and structural support.
Bulk Nb: Tc ≈ 9.2 K
High-performance Nb cavities typically operate near 2 K.
Background: Posen & Liepe (2014); Ilyina et al. (2019).
3

## Slide 4: Why the Bronze Route Works on Cu
Bronze method can reduce the reaction temperature，provides faster Sn transport than Nb and reduce the stability of other niobium-tin phases
Sn-vapor diffusion
Cavity ≈1100 °C
Sn source ≈1200 °C
Cu melts at 1083 °C
Cu–Nb–Sn at 700 °C
A route toward Nb3Sn
without Sn-rich intermediate phases
Sn diffusion
Cu–Sn provides faster Sn transport
than diffusion through Nb
The bronze route combines a lower reaction temperature with faster Sn transport.
Müller & Schneider (2008); Mei et al. (2009).
4

## Slide 5: First Attempt: A Sn-Rich Bronze Layer
Could a Sn-rich bronze layer supply enough Sn to form better Nb3Sn?
01
Deposit Sn on Cu
Sn
Cu
02
Anneal to form bronze
Sn-rich bronze
Cu
03
Deposit Nb
Nb
Sn-rich bronze
Cu
04
Anneal to form Nb3Sn
Nb3Sn
Cu
→
→
→
Expectation: more Sn in the bronze layer → sufficient Sn during the Nb–Sn reaction
Observed transition
Tc ≈ 11.7 K
The intended improvement
was not achieved.
Cross-section and elemental distribution
Severe
Sn deficiency
This route was abandoned due to severe Sn deficiency.
5

## Slide 6: Diffusion Barriers May Limit Cu/Sn Transport
The next question is whether a thin barrier can retain Sn while limiting Cu ingress.
No barrier layer
Thick Nb interlayer
Barrier layer
Nb3Sn
Cu substrate
Nb3Sn
Thick Nb
Cu substrate
Nb3Sn
barrier layer
Cu substrate
Sn loss
Cu ingress
Sn loss / Cu ingress
Tens of micrometres of Nb
Thin barrier to test
Red: Sn diffusion toward Cu
Blue: Cu diffusion toward the film
Goal: limit interdiffusion and maintain Nb–Sn reaction without an ultrathick Nb layer.
Conceptual 3D schematic; not to scale. Red arrows: Sn toward Cu; navy arrows: substrate Cu toward the film. Based on Ilyina et al. (2019).
6

## Slide 7: Revised Route: Added Cu/Sn Layers and a Barrier
A revised layer design retained the bronze-route advantages and gave promising preliminary results.
Revised layer design
Sn
Diffusion Cu
Nb
barrier layer
Cu substrate
↓ Anneal; remove residual bronze
Nb3Sn
barrier layer
Cu substrate
Cu/Sn layers: Sn supply via bronze.
Barrier: limit Cu/Sn interdiffusion
between substrate and coating.
Preliminary results
Tc ≈ 17.1 K
Surface morphology
These results motivated the present study of barrier-layer material and thickness.
EDS composition — Nb : Sn ≈ 3 : 1
Element | Weight (%)
O | 5.72
Cu | 0.91
Nb | 66.98
Sn | 26.39
Total | 100
7

## Slide 8: Why Optimize Barrier Material and Thickness?
Promising preliminary results still leave two issues to address.
Thick niobium interlayer
Overly thin tantalum barrier
Nb3Sn
Thick Nb
Cu substrate
Nb3Sn
Ta barrier layer
Cu substrate
A thick niobium layer may improve the
preparation pressure
An overly thin tantalum barrier cannot
effectively block tin diffusion.
Research goal
Reduce barrier thickness while maintaining
effective blocking of element diffusion.
8

## Slide 9: Outline
1. Background and motivation
2. Sample preparation
3. Results and discussion
4. Summary and outlook
9

## Slide 10: Experimental Information and Parametern
Five samples share the same Nb/Cu/Sn stack and thermal cycle; only the barrier changes.
Sample | Barrier | Nominal thickness | Comparison role
Ta 1.0 | Ta | 1.0 µm | Ta thickness reference
Ta 0.5 | Ta | 0.5 µm | Response to thinner Ta
Cr 1.0 | Cr | 1.0 µm | Cr thickness reference
Cr 0.5 | Cr | 0.5 µm | Response to thinner Cr
No barrier | — | 0 | Interdiffusion control
Magnetron sputtering and heat treatment
01 OFHC Cu substrate + Ta / Cr barrier
02 Nb 6 µm / Cu 2 µm / Sn 3 µm
03 210 °C × 40 h → 400 °C × 20 h
→ 700 °C × 50 h
04 Remove residual bronze; characterize films
Representative Ta-barrier preparation sequence
Cu substrate
→
After electropolishing
→
Ta barrier
→
Multilayer coating
→
After annealing
→
After bronze removal
Characterization: M–T, XRD, SEM/EDS and scratch testing
10

## Slide 11: Outline
1. Background and motivation
2. Sample preparation
3. Results and discussion
4. Summary and outlook
11

## Slide 12: Cr Retains Narrow Transitions at Both Thicknesses
All five films show Tc near 17 K. The superconducting transition width of Cr samples with different thicknesses is less than 2k.
Tc,onset | Ta 1.0 | Ta 0.5 | Cr 1.0 | Cr 0.5 | No barrier
K | 17.3 | 17.4 | 17.2 | 17.2 | 17.0
Cr: 1.6–1.7 K at both thicknesses
Ta 1.0 µm: 2.3 K
No barrier: >7.8 K*
Chart: Transition width (mK)
| 1.0 µm | 0.5 µm
Ta | 2300 | 8200
Cr | 1600 | 1700
12

## Slide 13: XRD Detects Nb3Sn Without Competing Nb–Sn Phases
After annealing, XRD detects Nb3Sn in all five samples and no Nb6Sn5 or NbSn2.
XRD results
The change of the barrier layer may not only affect the degree of reaction, but also affect the growth orientation of Nb3Sn
Barrier samples show stronger (200), (210) and (211) reflections.
Tantalum and no barrier layer samples have obvious NbO2, which related to the oxygen introduced during the preparation process.
Possible Cr–Nb reaction
During the annealing process, chromium and niobium may undergo interfacial reaction to form dichromium niobium.
Cr2Nb may change the blocking effect and may also affect the nucleation and growth of Nb3Sn above.
13

## Slide 14: Cr and Ta Show Opposite Layer-Thickness Trends
Reducing the barrier from 1.0 to 0.5 μm increases the reacted layer thickness for chromium but decreases it for tantalum.
Ta 1.0 µm
Ta 0.5 µm
Cr 1.0 µm
Cr 0.5 µm
No barrier
Chart: Reacted layer and residual Nb
| Ta 1.0 | Ta 0.5 | Cr 1.0 | Cr 0.5 | No barrier
Reacted layer | 3.78 | 2.39 | 3.8 | 5 | 2.29
Residual Nb | 1.87 | 3.33 | 1.73 | 0.67 | 3.58
EDS interpretation
The niobium–tin ratio is uniform within the reacted layer in all samples.
Under these conditions, the reaction is more complete with a 0.5 μm chromium barrier.
Material and thickness
A thicker barrier is not always better. Thickness and material need to be selected together.
14

## Slide 15: Barrier Layers Suppress Sn Diffusion Toward Cu
Cross-sectional SEM and EDS reveal tin redistribution and the effect of the barrier layer.
(a) Ta 1.0 µm · (b) Ta 0.5 µm · (c) Cr 1.0 µm
(d) Cr 0.5 µm · (e) No barrier
Without a barrier, during heat treatment, a part of tin enters the copper substrate and does not remain in the area where it needs to react with niobium.
Without a barrier, tin can be detected in the copper substrate region, and the tin content in the copper substrate is higher than that in the niobium layer which no reaction.
Interfacial tin enrichment is observed for tantalum but not for chromium, supporting a possible chromium–niobium interface reaction.
The element distribution gives indirect support. Whether dichromated niobium is formed and how much blocking effect it contributes, it also requires subsequent direct interface analysis.
15

## Slide 16: Cr 0.5 µm Gives the Densest Surface in This Set
All five surfaces have Nb:Sn close to 3:1. Cr 0.5 μm has clearer grain faces, a denser surface and the lowest local oxygen content (8.26 at%).
Ta 1.0 µm
Ta 0.5 µm
Cr 1.0 µm
Cr 0.5 µm
No barrier
The other four samples show finer grains and porous surfaces.
Chart: Local surface O by EDS (at%)
| Ta 1.0 | Ta 0.5 | Cr 1.0 | Cr 0.5 | No barrier
O | 15.29 | 13.92 | 12.86 | 8.26 | 10.94
Surface EDS: Nb and Sn contents and atomic ratio
Sample | Ta 1.0 µm | Ta 0.5 µm | Cr 1.0 µm | Cr 0.5 µm | No barrier
Nb (at%) | 42.40 | 39.78 | 41.56 | 44.42 | 41.92
Sn (at%) | 13.48 | 12.52 | 13.83 | 14.95 | 13.17
Nb:Sn | 3.15:1 | 3.18:1 | 3.01:1 | 2.97:1 | 3.18:1
Together with XRD, oxygen may be a factor affecting surface growth. More oxygen is conducive to the formation of oxides, and oxides may influence the normal growth of Nb3Sn grains, resulting in fine-grained and porous surfaces
the introduction of oxygen is mainly related to the preparation process.
16
For RF applications, we must continue to pay attention to the surface oxidation and surface treatment of Nb3Sn .

## Slide 17: Adhesion Is Similar Across All Five Samples
Complete film failure occurs at Lc3 = 10.7–11.7 N, with no clear trend across this sample set.
Test conditions
Linear load
0.1 → 30 N
Scratch speed
6 mm min⁻¹
Scratch length
3 mm
Criterion
Film failure: Lc3
Next: FIB–SEM sections of scratch tracks to locate the failure interface.
Chart: Critical load at complete film failure
| Ta 1.0 | Ta 0.5 | Cr 1.0 | Cr 0.5 | No barrier
Critical load | 11.5 | 11 | 10.7 | 11.1 | 11.7
Adhesion hypothesis
Barrier layers may improve film adhesion, similar to silver in copper–niobium composite cavities.
Scratch-test result
All five samples were tested under the same scratch conditions.
Failure loads were around 11 N. No clear adhesion improvement was observed with tantalum or chromium barriers.
17

## Slide 18: Outline
1. Background and motivation
2. Sample preparation
3. Results and discussion
4. Summary and outlook
18

## Slide 19: Diffusion Barriers Support Nb3Sn Growth on Cu
The small-sample results establish the barrier strategy and show how material and thickness affect performance.
01
Suitable barriers reduce interdiffusion
02
Material and thickness affect the result
Next: apply the small-sample process to a 1.3 GHz single-cell copper cavity to test its applicability.
A suitable barrier reduces copper–tin interdiffusion and supports film growth without a niobium layer tens of micrometres thick.
Aims at stable, high-quality superconducting films below 5 μm on copper after subsequent optimization of the film structure.
Chromium is more robust across 0.5–1.0 μm in this set. The 0.5 μm chromium barrier gives the best overall results.
1 μm tantalum remains a feasible choice.
19

## Slide 20: Cavity Coating Starts with Cu Coupon Tests
Cooperate with Shanghai University of Science and Technology, carry out subsequent research using their whole cavity coated magnetron sputtering platform
Cavity-wall coupon test
Full-cavity coating
Vertical test
Cu coupon-test schematic
Planned: October
Magnetron-sputtering platform
4.2 K vertical RF test
Q0(Eacc) · quench
Copper coupon tests are underway at different cavity positions, assessing uniformity, morphology, adhesion and superconducting properties.
After coupon verification: full-cavity coating in October, followed by niobium, copper and tin deposition and bronze heat treatment.
Target: a 1.3 GHz single-cell copper-based Nb3Sn cavity by the end of 2026, followed by vertical RF testing.
20

## Slide 21: Thank You
Bohao Zhang
Institute of Modern Physics, Chinese Academy of Sciences
zhangbohao@impcas.ac.cn
Questions and Discussion
21

## Slide 22: Backup: Complete Surface SEM and EDS Evidence
(a) Ta 1.0 µm · (b) Ta 0.5 µm · (c) Cr 1.0 µm · (d) Cr 0.5 µm · (e) no barrier
BACKUP
22

## Slide 23: Backup: Complete Process Parameters
Full experimental details: substrate treatment, targets, sputtering, layer deposition, annealing, and bronze removal.
Substrate preparation and common sputtering conditions
Layer deposition, annealing and residual-bronze removal
Layer / step | Thickness | Power | Time / condition
Ta | 0.5 / 1.0 µm | 160 W | 20 / 40 min
Cr | 0.5 / 1.0 µm | 160 W | 13 / 26 min
Nb | 6 µm | 160 W | 4 h
Cu diffusion layer | 2 µm | 160 W | 47 min
Sn | 3 µm | 25 W | 100 min
High-vacuum anneal | 210 °C × 40 h → 400 °C × 20 h → 700 °C × 50 h | — | Ramp: 0.5 °C min⁻¹
Residual bronze removal | Cold-mounted in epoxy; only the polishing face exposed; H3PO4:HNO3 = 3:1 | — | 10 min at room temperature; DI water → absolute ethanol → high-purity N2
Stage
Material / solution
Key parameters
Follow-up
Coupon
High-purity OFHC Cu
10 × 20 × 1.5 mm³
—
Electropolishing
85 wt.% H3PO4 :
99 wt.% n-butanol
= 55:45 by volume
OFHC Cu counter-electrode
(sample recorded as cathode)
30–50 mA cm⁻²; 5–10 min
Rinse with DI water
Acid passivation
and cleaning
Dilute sulfamic acid
5–10 min at room temperature
15–20 min ultrasonic DI-water cleaning
Absolute ethanol rinse
High-purity N2 drying
Targets
Circular targets
purity ≥99.95%
2 in (50.8 mm) diameter; 3 mm thick
Same specification for all targets
Sputtering
Ar 5 sccm
Base 1 × 10⁻⁵ Pa; working 0.5 Pa
substrate 25 °C
Target gap: 8 cm
23

## Slide 24: Backup: References and Numerical Definitions
Primary paper, Nb3Sn-on-Cu and bronze-route background, and definitions used in the figures and tables.
BACKUP
1. Zhang, B. et al. Supercond. Sci. Technol. 39, 075033 (2026). DOI: 10.1088/1361-6668/ae787f.
2. Ilyina, E. A. et al. Supercond. Sci. Technol. 32, 035002 (2019). DOI: 10.1088/1361-6668/aaf61f.
3. Posen, S. & Liepe, M. Phys. Rev. ST Accel. Beams 17, 112001 (2014). DOI: 10.1103/PhysRevSTAB.17.112001.
4. Lu, M. et al. Chinese Phys. Lett. 39, 115201 (2022).
DOI: 10.1088/0256-307X/39/11/115201.
5. Godeke, A. Nb3Sn properties review. OSTI 898943.
6. Yamanaka, M. et al. Phys. Rev. Accel. Beams 29, 033101 (2026). DOI: 10.1103/1jh5-65xh.
7. Dong Peng. Fourth National Accelerator SRF Technology Conference report, pp. 16, 20–21.
Definitions
Tc,onset: onset temperature. ΔTc: transition width. Lc3: load at complete film failure.
*For Ta 0.5 µm and no barrier, the paper estimates transition widths relative to the Nb transition at 9.2 K.
Background and figure sources are listed in the notes of the relevant slides.
24