## Slide 1: From Nb to Nb3Sn: Complexity in SRF Coating Development
presenter: Caroline Hain
12th TFSRF Workshop
21-25 September 2026
on behalf of: C. Pereira, K. Brunner, W. V. Delsolaro, G. Rosaz (and many others from TE, SY, EN)

## Slide 2: What are the challenges?
M. Ghaemi et al. Surface & Coatings Technology 476 (2024) 130199
Cu substrate challenges
low surface microroughness, with minimal surface defects (pits, dents, voids etc.)
oxide-free and free of organic or particulate contaminations
at elevated temperatures, recrystallisation and grain growth can occur
significant softening and loss of mechanical strength at ~400 °C (depending on Cu purity, prior deformation and microstructure)
Film material challenges for both Nb and Nb3Sn
high film density and low surface roughness
high purity and low defect density
Nb films deposited onto Cu substrates via DCMS (left) and HiPIMS (right)
HiPIMS the method of choice
substrate bias/ ion acceleration to tens-hundreds of eV
energetic bombardment enhances adatom mobility and film densification
excessive ion energy can induce atomic displacements and lattice defects
Additional requirements for Nb3Sn
correct Nb-to-Sn stoichiometry
formation and ordering of the A15 phase → around 750 °C to provide sufficient atomic mobility
Balance thermal activation and ion bombardment to achieve dense A15 Nb3Sn while minimising defect generation and composition shifts.
Maintaining a clean, smooth and mechanically stable Cu substrate while providing the thermal budget required for Nb3Sn growth.

## Slide 3: Let’s focus on temperature

## Slide 4: Influence of temperature: Nb3Sn films
50 µm
Sn
Nb
Cu
O
Nb3Sn deposited on Cu using the same parameters and only changing the temperature
lower substrate temperature → lower adatom mobility
clear influence on porosity level and morphology
Pt
Nb3Sn
Cu
1 µm
1 µm
Cu interdiffusion from the substrate
promotes A15 phase formation
create locally non-superconducting regions
compromises superconductive performance

## Slide 5: Influence of temperature: Nb3Sn films
Mitigating Cu interdiffusion
introduce a diffusion barrier layer (DBL) between the Cu substrate and Nb3Sn
Ta is a promising barrier material and has been shown to suppress Cu diffusion
  α-Ta: stable bcc phase, the required phase for this application
  β-Ta: metastable, tetragonal and brittle, undesirable

## Slide 6: Influence of temperature: Nb3Sn films
Cu
Ta
2.5 μm
Nb3Sn
20 μm
Nb3Sn
Ta
Mitigating Cu interdiffusion
introduce a diffusion barrier layer (DBL) between the Cu substrate and Nb3Sn
Ta is a promising barrier material and has been shown to suppress Cu diffusion
  α-Ta: stable bcc phase, the required phase for this application
  β-Ta: metastable, tetragonal and brittle, undesirable

## Slide 7: Influence of temperature: Nb films
higher temperature
→ porosities and other surface defects for Nb/Cu
500 ºC
600 ºC
100 μm
20 μm
100 μm
20 μm
150 ºC
100 μm
20 μm
Is this only happening to Nb3Sn/Ta/Cu? How do higher temperatures affect Nb/Cu?

## Slide 8: Influence of temperature: Nb films
20 μm
20 μm
500 ºC
600 ºC
Nb
Nb
750 ºC
Nb3Sn
5 μm
5 μm
O
Cu
C
Nb
2.5 μm
500 ºC
500 ºC
Is this only happening to Nb3Sn/Ta/Cu? How do higher temperatures affect Nb/Cu?
Why?

## Slide 9: Influence of temperature: Cu substrate
Schematic of the constructed surface mesh (white surface) after simulating deposition of 25000 Nb and 5000 Ar atoms on Cu(100) (T = 300 K) at conditions consistent with HiPIMS growth. Nb atoms (green), Cu atoms (orange).
M. Ghaemi (University of Helsinki) https://doi.org/10.1016/j.surfcoat.2023.130199
Cumulative fraction of sputtered Cu atoms fsp (with respect to the initial number of Cu atoms in the simulation box) as a function of number of the deposited particles for HiPIMS growth simulations.
Why is this happening?
energetic species induce collision cascades that displace Cu atoms from the substrate
local heating from ion bombardment enhances atomic rearrangement and facilitates Cu diffusion
island nucleation and coalescence, Cu adatoms can be incorporated into Nb clusters
Temperature-dependant Cu atom mobility predicted through molecular dynamic simulations

## Slide 10: Influence of temperature: Cu substrate
… and supported by experimental results!
XPS depth profile of Cu, Nb, O, and C in a 150 nm thick Nb layer deposited on Cu via HiPIMS at 420 K.
Schematic of the constructed surface mesh (white surface) after simulating deposition of 25000 Nb and 5000 Ar atoms on Cu(100) (T = 300 K) at conditions consistent with HiPIMS growth. Nb atoms (green), Cu atoms (orange).
M. Ghaemi (University of Helsinki) https://doi.org/10.1016/j.surfcoat.2023.130199
Cumulative fraction of sputtered Cu atoms fsp (with respect to the initial number of Cu atoms in the simulation box) as a function of number of the deposited particles for HiPIMS growth simulations.
Temperature-dependant Cu atom mobility predicted through molecular dynamic simulations

## Slide 11: Influence of temperature: Ta DBL
Could this high Cu mobility also be affecting the Ta diffusion barrier layer?
Cumulative fraction of sputtered Cu atoms fsp as a function of number of the deposited particles for HiPIMS growth simulations.
https://doi.org/10.1016/j.surfcoat.2023.130199
Ta at 750 ºC
Ta at 300 ºC
Still to be optimised, however, very promising initial result!
New campaign ongoing, latest XPS surface results:
Nb/Cu deposited at 300 ºC → 6 % Cu
Ta/Cu without heating (under various ion acceleration conditions) → below the detection limit!
5 μm
10 μm

## Slide 12
5 μm
10 μm

## Slide 13: from samples to cavities

## Slide 14: Upscaling: deposition system
How to move from coating samples to coating cavities?
M. Ghaemi et al. Surface & Coatings Technology 476 (2024) 130199
Nb target
Different aspects need to be considered
two materials are needed: Ta and Nb3Sn
how to move from planar to cylindrical targets?
“easy enough” for Nb, how about Nb3Sn?
coating samples using planar targets
coating cavities using a cylindrical targets

## Slide 15: Upscaling: deposition system
How to move from coating samples to coating cavities?
Different aspects need to be considered
two materials are needed: Ta and Nb3Sn
how to move from planar to cylindrical targets?
“easy enough” for Nb, how about Nb3Sn?
coating samples using planar targets
50 mm
Nb3Sn planar target
Already prone to cracking!
brittle (fragile)
can create dust upon cracking
impossible to buy as a cylinder

## Slide 16: Upscaling: target strategies
How to prevent target cracking AND coat cavities?

## Slide 17: Upscaling: target strategies
How to prevent target cracking AND coat cavities?
moving from a static cathode design to a mobile cathode one (system already available for Nb coating of 1.3 GHz cavities)
using multiple planar targets to mimic a cylindrical geometry
feasible based on simulations (through direct cooling, with the cavity at 800 ºC)

## Slide 18: Upscaling: target strategies
How to prevent target cracking AND coat cavities?
moving from a static cathode design to a mobile cathode one (system already available for Nb coating of 1.3 GHz cavities)
using multiple planar targets to mimic a cylindrical geometry
feasible based on simulations (through direct cooling, with the cavity at 800 ºC)
How to prevent target cracking AND coat cavities?
use a backing plate with a similar thermal expansion coefficient as Nb3Sn (our case Cu-W)
However:
epoxy gluing → high contamination risk
indium sealing → cross-contamination has been observed

## Slide 19: Upscaling: target strategies
Different approaches are currently under investigation:
EN-MME working on developing an in-house brazing recipe
as the backing plate contains Cu it is important to prevent it contaminating the Nb3Sn target
25 μm
Nb
Cu
Sn
Ta
Cu migration still in occurring despite the presence of the Ta layer
the brazing process takes place at 800 ºC
the Nb3Sn target is not fully dense, i.e. pores are present
New trails ongoing with substituting the Cu foil for a Nb one.
schematic of brazing stack
25 μm
bonding interface

## Slide 20: Upscaling: target strategies
Nb3Sn target
Cu-W backing plate
50 μm
Nb
Sn
Cu
W
Al
Cu, W and Al detected on the surface of Nb3Sn
further analysis needed to determine if only the surface is contaminated or also the bulk
Different approaches are currently under investigation:
EN-MME working on developing an in-house brazing recipe
trying the commercially available “nanofoil bonding” approach
https://www.indium.com/products/nanofoil/
Nb3Sn target surface
50 μm

## Slide 21: what’s next?

## Slide 22: Next steps
so far…
Nb3Sn has proven to be competitive with Nb
Ta DBL deposition has been modified to take place without additional heating
understanding Cu mobility has improved
ongoing activities:
investigating different bonding routes to enable progress on a cylindrical-like target
further optimisation on the Ta DBL, considering different ion acceleration possibilities (bipolar HiPIMS, unipolar HiPIMS + cavity/substrate biasing)
assisted process development via in situ plasma diagnostics during Nb and Nb3Sn sputtering (e.g. OES, QMS)
high temperature deposition of Nb on various substrates to further unravel the behaviour of Cu
post-deposition annealing of a Nb/Cu cavity within a vacuum furnace (furnace purity checks happening now!)
To be continued at the next TFSRF Workshop!

## Slide 23: From Nb to Nb3Sn: Complexity in SRF Coating (and Substrate!) Development
presenter: Caroline Hain
12th TFSRF Workshop
21-25 September 2026
on behalf of: C. Pereira, K. Brunner, W. V. Delsolaro, G. Rosaz (and many others from TE, SY, EN)