## Slide 1
12th International Workshop on Thin Films and New Ideas for Pushing the Limits of RF Superconductivity, 21–25 September 2026 Chester, United Kingdom
Nb₃Sn thin film development on 1.3 GHz cavities
Matteo Lazzari
INFN – Legnaro National Laboratories · Università degli Studi di Padova
on behalf of the LNL Surface Treatments & Superconductivity Team
◆ PhD scholarship fully funded by Zanon Research & Innovation
SUPPORTED BY
EU Horizon — iSAS (GA 101131435) & I.FAST (GA 101004730). INFN CSN5 SuperMAD · CSN1 SRF, RD_FCC.
PROJECTS & COLLABORATIONS

## Slide 2
ACKNOWLEDGEMENTS
LNL SRF R&D — a collaborative effort
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
02 / 24
EU HORIZON PROGRAMMES
INFN ACCELERATOR R&D
INTERNATIONAL PARTNERS
INFN–LNL
C. Pira, O. Azzolini, E. Chyhyrynets, T. M. Ezeaba, D. Ford, M. Lazzari, F. Stivanello
INFN PD · RM3 · TO · LNF
A. Pepato, P. Rebesan · N. Pompeo, E. Silva · G. Ghigo · C. Gatti, G. Maccarrone, D. Di Gioacchino
CEA
C. Z. Antoine, I. Curci, Y. Kalboussi, T. Proslier
CERN
G. Rosaz, W. Venturini
DESY
M. Wenskat
HZB
S. Keckert, O. Kugeler, J. Knobloch
HZDR
S. Prucnal, S. Zhou
Jefferson Lab
A. M. Valente Feliciano
IEE SAS
E. Seiler, R. Ries
STFC / UKRI
O. B. Malyshev, R. Valizadeh, C. Benjamin, T. Sian, L. Smith
Lancaster · Liverpool · Siegen
G. Burt, N. Leicester, S. Marks, D. Seal · W. Bradley, S. Simon · X. Jiang, T. Staedler, A. Zubtsovskii
Riga Tech. Univ. · Piccoli
A. Medvids · R. Berton, D. Piccoli, F. Piccoli, G. Squizzato, F. Telatin

## Slide 3
TECHNOLOGY READINESS LEVEL
Each EU project, a step up in TRL
Nb₃Sn-on-Cu has climbed the TRL ladder through successive European programmes.
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
03 / 24
TRL SCALE
1
Basic principles
2
Concept
3
Proof of concept
4
Lab validated
5
Relevant env.
6
Demonstrated
7
Operational prototype
8
Qualified
9
Proven in operation
proof of concept
TRL 3
Tc > 17 K on small planar samples
partial-scale prototype
TRL 4
Nb₃Sn RF performance validation on QPR
partial-scale prototype validation
TRL 5
1.3 GHz Nb₃Sn cavity coated and tested
full-scale prototype demonstration
TRL 6
Nb₃Sn Conduction Cooling Cryomodule
2021
2023
2025
2028
2030
today
EUROPEAN
COLLABORATIONS
INFN
PROJECTS

## Slide 4
Outline
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
04 / 24
OVERVIEW
01
Nb₃Sn on a cavity
Commissioning the coating system and first depositions on a mock-up cavity
02
Future improvements of the system
A rotating cavity: from design to construction
03
Possible new film interface
ALD oxide interlayers
→ Next steps — from the mock-up to an RF-tested Nb₃Sn cavity

## Slide 5
01
PART 01
Nb₃Sn on a cavity
Commissioning the coating system and first depositions on a mock-up cavity
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
05 / 24

## Slide 6
RECAP
Moving the recipe onto a 1.3 GHz cavity
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
06 / 24
The recipe — validated on flat samples & QPR *
DCMS from a single stoichiometric Nb₃Sn target, Tc > 17 K on Cu
1
Low cathode power ~250 mW/cm²
2
High deposition pressure 2×10⁻² mbar
3
Deposition temperature 600–650 °C
→ Heat the cavity in vacuum during coating, below the Cu limit
4
No post-annealing
→ A15 phase formed in situ: one single, hot deposition step
5
Nb buffer layer ~30 µm
→ Accommodation and diffusion barrier
* D. Fonnesu et al., Recipe optimization and SRF test of Cu-compatible Nb₃Sn films by DCMS, Sci. Rep. 16, 3539 (2026).
01 · Nb₃Sn on a cavity
Sample #2
Nb₃Sn on bulk Nb
17.45 K
> 85 mT
< 9 nΩ
QPR RESULTS
Tc
Bpeak
Rs

## Slide 7
RECAP
Moving the recipe onto a 1.3 GHz cavity
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
07 / 24
The recipe — validated on flat samples & QPR *
DCMS from a single stoichiometric Nb₃Sn target, Tc > 17 K on Cu
1
Low cathode power ~250 mW/cm²
2
High deposition pressure 2×10⁻² mbar
3
Deposition temperature 600–650 °C
→ Heat the cavity in vacuum during coating, below the Cu limit
4
No post-annealing
→ A15 phase formed in situ: one single, hot deposition step
5
Nb buffer layer ~30 µm
→ Accommodation and diffusion barrier
* D. Fonnesu et al., Recipe optimization and SRF test of Cu-compatible Nb₃Sn films by DCMS, Sci. Rep. 16, 3539 (2026).
THE LNL 1.3 GHz COATING SYSTEM
Magnetron inside the cavity
Full coating system
Fixed planar magnetron — rectangular target on the axis
Rotating cavity — turns around it for an even coating
Heated UHV chamber — substrate up to ~670 °C
01 · Nb₃Sn on a cavity

## Slide 8
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
08 / 24
Magnetron operating window & first depositions
CHARACTERIZATION
One curve per Ar pressure
STABLE OPERATING WINDOW
100 – 1500 mA discharge current
7.5×10⁻³ – 6×10⁻² mbar Ar pressure
up to 670 °C substrate temperature
DEPOSITIONS TO DATE
12
8 × Nb
Runs for testing the magnetron set-up
4 × Nb₃Sn
First runs for parameter scaling/optimization study
DISCHARGE V–I CURVES
01 · Nb₃Sn on a cavity

## Slide 9
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
09 / 24
A mock-up cavity with seven sample positions
TESTING PLATFORM
Seven positions studied separately
2 cut-off, 3 cell, 2 cut-off
Fast testing — samples analysed without coating a full cavity
Same target distance — films compared under equal geometry
Repeatability — controlled, identical starting conditions
Why not real cavities?
Each cavity has its own substrate conditions (grain size, machining stress, actual distance from the target, batch variations)
1
2
3
4
5
6
7
1–2, 6–7: cut-off (beam tubes), 3–5: cell
Cavity-like conditions — same pressure and temperature distribution as inside a real cavity
01 · Nb₃Sn on a cavity

## Slide 10
Magnet choice and process conditions
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
10 / 24
DEPOSITION RATE
1
MAGNET CONFIGURATION
2
RATE PROFILE vs PROCESS CONDITIONS
Two magnet configurations tested → strong field chosen: higher deposition rate.
Deposition time set for a safety thickness on the cell (≈ 10 × Nb₃Sn London penetration depth), without an overly thick, stressed film at the cut-offs.
1 µm on the cell (@ ■ 2.8 nm/min) ≈ 6 h
01 · Nb₃Sn on a cavity
8.0
2.6
3.3
4.9
CUT-OFF / EQ.

## Slide 11
Different process conditions, similar Tc
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
11 / 24
DEPOSITION PARAMETERS
Points offset along x for readability , Tc measurements: F. A. Costanzo
 | P (mbar) | Tₛ (°C) | Power (W)
◆ Run 9 | 2.0×10⁻² | 600 | 112.5
■ Run 10 | 4.5×10⁻² | 650 | 142
● Run 11 | 2.4×10⁻² | 650 | 66.4
▲ Run 12 | 1.2×10⁻² | – | 70.8
Key observations
Wide spread of process parameters (pressure, mean power), yet only small changes in Tc.
Broad, poorly defined transitions — hint at large variations of pressure and substrate temperature along the cavity.
Run 9: no transition at any position.
CRITICAL TEMPERATURE
01 · Nb₃Sn on a cavity

## Slide 12
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
12 / 24
SEM ANALYSIS
Morphology, position by position
CUT-OFF
CELL
CUT-OFF
1
2
3
4
5
6
7
Run 11
66.4 W
2.4×10⁻² mbar
Run 10
142 W
4.5×10⁻² mbar
5 µm
SEM, SE 15 kV · all images at the same scale · Tc above each image (— : no transition)
Several morphologies along the cavity
Causes under investigation: pressure gradient, temperature gradient
Same region, different structure when parameters change
Can we reach a uniform film along the whole cavity?
01 · Nb₃Sn on a cavity
—
11.9 K
12.2 K
11.0 K
12.0 K
10.4 K
—
—
11.8 K
12.8 K
11.0 K
12.4 K
10.5 K
—

## Slide 13
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
13 / 24
SEM ANALYSIS
Morphology, compared with past samples
01 · Nb₃Sn on a cavity
1 µm
1 µm
SMALL SAMPLE
Cu + 15 µm Nb buffer layer
Flat sample, 2024
SEM InLens · 10 kV · ×15k
MOCK-UP CAVITY
Sapphire
Run 10 · position 3 (cell)
SEM SE · 15 kV · ×10k
Same scale: both images cropped to a 4.9 × 4.9 µm field (originals taken at ×15k and ×10k)
Comparison in progress
Small samples we already have vs. new films deposited in the cavity
Morphology as a process indicator
Mainly for temperature and pressure consideration

## Slide 14
Similar Tc on different substrates
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
14 / 24
Circled: Run 11 on Cu + Nb BL (15 µm), all others on sapphire. Open symbols: no measurable transition
SUBSTRATE AT EACH POSITION
Position | ■ Run 10 | ● Run 11
1 | Sapphire | Sapphire
2 | Sapphire | Cu + Nb BL 15 µm
3 | Sapphire | Sapphire
4 | Sapphire | Sapphire
5 | Sapphire | Cu + Nb BL 15 µm
6 | Sapphire | Sapphire
7 | Sapphire | Sapphire
Same Tc, different substrate
Pos. 2: 11.9 K (sapphire) vs 11.8 K (Cu + Nb BL)
Pos. 5: 12.0 K (sapphire) vs 12.4 K (Cu + Nb BL)
The driver doesn’t seem to be the sputtering parameters alone, but their uniformity along the cavity axis.
CRITICAL TEMPERATURE
01 · Nb₃Sn on a cavity

## Slide 15
Tc follows the position; no transition at the ends
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
15 / 24
Circled: end positions 1 and 7 — no measurable transition in either run
Key observations
Same position → similar Tc in both runs: the target–substrate distance seems to dominate.
No transition at the ends (pos. 1, 7), likely where the magnetic field no longer closes the plasma. Same thickness in the cut-off
Plasma not closing
no-plasma region
CRITICAL TEMPERATURE
01 · Nb₃Sn on a cavity

## Slide 16
Sn content along the cavity
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
16 / 24
Sn CONTENT PER RUN
■ Run 10
19.5 at.%
mean
range 18.2 – 20.6
● Run 11
19.7 at.%
mean
range 18.0 – 22.6
▲ Run 12
20.3 at.%
mean
range 18.8 – 21.8
All within the A15 range (18–26 at.%), yet Sn-poor
COMPOSITION
Sn content measured by EDX at each of the seven positions
01 · Nb₃Sn on a cavity
Required Sn % > 24%

## Slide 17
SUMMARY
Lessons learned and further investigations
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
17 / 24
1
2
3
The system works and also the testing procedure
Stable magnetron from 0.1 to 1.5 A and 7.5×10⁻³ to 6×10⁻² mbar, up to 670 °C, 12 depositions (8 Nb, 4 Nb₃Sn).
Geometry counts
Deposition rate and Tc depend on the position along the cavity.
Substrate temperature and pressure
Uniformity has to be investigated along the cavity and also good thermal contact

## Slide 18
02
PART 02
Future improvements of the system
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
18 / 24
A rotating cavity: from design to construction

## Slide 19
Rotating the cavity: from design to construction
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
19 / 24
02 · Future improvements of the system
ROTATION SYSTEM
FOUR REQUIREMENTS
1
Clean rotation — no lubricant inside the vacuum
2
x–y adjustment and tilt — to align the rotation axis with the magnetron axis
3
Thermal shielding — of the upper parts of the system
4
Motor outside the vacuum — slow rotation, < 10 rpm
STATUS
✓
Design review — done
✓
Design phase — completed
→
Parts ordered — construction by the end of 2026
Design and mechanical calculations: T. Subasinghe

## Slide 20
03
PART 03
Possible new film interface
ALD oxide interlayers
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
20 / 24

## Slide 21
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
21 / 24
iSAS TASK 3.4 · ADAPTIVE LAYER
03 · Possible new film interface
CEA adaptive layer between Cu and the Nb buffer
SCHEMES TESTED WITH CEA
✗ No Nb buffer
✓ ALD under Nb
ALD above Nb
ALD both sides
Low Tc without the Nb buffer · Tc ≈ 17 K with the adaptive layer between Cu and Nb
Tc BY BUFFER LAYER
Buffer layer
Tc (K)
ΔTc (K)
✗ No buffer layer
13.8
0.3
16 µm Nb
16.5
0.6
30 µm Nb
16.7
0.5
✓ 30 µm Nb + 18 nm Al₂O₃
16.3
0.5
✓ 30 µm Nb + 25 nm AlZrOₓ
16.9
0.2
✓ 30 µm Nb + 5 nm Al₂O₃ + 22 nm ZrO₂
16.8
0.2
×
TWO GOALS
1
Reduce or completely avoid the thick Nb buffer layer
2
Stop the thermoelectric currents between the layers

## Slide 22
First Tc without a Nb buffer layer
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
22 / 24
ALD INTERLAYERS
03 · Possible new film interface
Sample · ALD interlayer | Tc (K) | 
Cu 30 µm (control) | 12.65 ± 0.22 | 
✓ AlZrO (1:4), 48 cycles (≈4.8 nm) | 13.93 ± 0.28 | 
✓ Al₂O₃, 180 cycles (≈18 nm) | 13.20 ± 0.57 | 
✗ Al₂O₃ 50 cy + ZrO₂ 270 cy (≈32 nm) | 11.54 ± 0.32 | 
✓ ZrO₂ · 270 cycles (≈27 nm) | 13.76 ± 0.44 | 
10
12
14
16
Tc (K), dashed: Cu control (12.65 K)
✓
Single layers perform alike
Al₂O₃, ZrO₂ and AlZrO: Tc 13.2–13.9 K, above the Cu · 30 µm control
✗
The mixed stack lags behind
Al₂O₃ + ZrO₂: 11.5 K, the lowest of the series
!
A run below par
This run went wrong — the value is not representative
Next: XRD, EDS

## Slide 23
Next steps
TFSRF 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
23 / 24
◆ we are here
ROADMAP
From the mock-up to an RF-tested Nb₃Sn cavity
2026
End 2026 – 2027
2027
End 2027 – 2028
Mock-up cavity
system commissioning and first Nb₃Sn films
Small-sample optimisation
+ construction of the rotation system
First coatings on Nb cavities
higher temperatures allowed, easy RF baseline before/after coating
First Nb₃Sn-coated Cu cavity
full RF test campaign

## Slide 24
Thank you
Matteo Lazzari · malazzar@lnl.infn.it
LNL Surface Treatments & Superconductivity Team · INFN–LNL
PhD funded by Zanon Research & Innovation
WITH THANKS TO
D. Ford, F. A. Costanzo, T. Subasinghe, G. Cassarà, E. Chyhyrynets, E. Tochukwu, F. Stivanello, O. Azzolini, C. Pira

## Slide 25
RF VALIDATION
01 · Film & technical solutions
TTC 2026 · M. Lazzari, INFN–LNL, malazzar@lnl.infn.it
11 / 17
Rₛ vs peak RF field
Q vs Eacc · reaching the FCC-ee target
Sample
Tᴄ
Quench
Rs @ 4K
vs VTD
Sample #1 · bulk Nb · BCP
17.2 K
> 70 mT
~ 25 nΩ
≈ to 40 mT
Sample #2 · bulk Nb · EP + pol.
17.45 K
> 85 mT
< 9 nΩ
better, ≤ 50 mT
Sample #3 · full Cu · NbBL30
prelim.
—
—
first on Cu
Surface preparation matters
EP (#2) cuts low-field Rₛ >2× and lifts quench vs BCP (#1); Q ≈ 10× LHC.
#3 — first full-Cu QPR coating: very preliminary.
4 K · 400 MHz · courtesy O. Kugeler, S. Keckert (HZB)
Recipe confirmed on QPR samples
Defects during NbBL deposition