## Slide 1: TITLE GOES HERE
Subtitle Goes Here
Date Goes Here
Speaker Goes Here
Gray Enid I: Record Beam Acceleration with a Nb₃Sn SRF Cryomodule at JLab
Uttar Pudasaini
12th International Workshop on Thin Films and New Ideas for Pushing the Limits of RF Superconductivity, Sep 2026
Chester, UK
Notes: Tip: Keep titles under 60 characters for readability
To change the photo: Right-click on photo and select change photo

## Slide 2: Acknowledgements
G. Ciovati, R. L. Geng
M. Poelker, R. Bachimanchi, A. Castilla, J. Creel, M. Drury, S. Dutton, J. Fischer, N. Gale, K. Hesse, L. King, S. Kuzikov, J. Latshaw, G. Marble, J. Musson, P. Owen, T. Powers, T. Plawski, H. P. Wang, S. H. Wang, Y. Wang, M. Weaks, X. Gomez
G. Eremeev, Fermilab
Work presented in this talk is the result of collective contributions from several groups at Jefferson Lab.
This material is based upon work supported by the U.S. Department of Energy, Office of Science, Office of Nuclear Physics, under Contract No. 89243126CSC000213.

## Slide 3: Outline
Motivation: Progress in Nb₃Sn cavity performance and the need for a beam-acceleration demonstration
Gray Enid I for UITF: Concept, cavity qualification, and cryomodule integration
Cryomodule Performance: Cooldown, tuning, and RF characterization
Beam Acceleration Campaigns: First beam, operational challenges, and 4 K optimization
Achievement and Outlook: 7.1 MeV beam acceleration, user beam delivery, and future directions

## Slide 4: From Nb3Sn Cavity R&D to Accelerator Demonstration
1.3/1.5 GHz single-cell
Nb3Sn cavity
1.3/1.5 GHz multi-cell
Nb3Sn cavity
Promise of Nb₃Sn: comparable RF performance at 4 K to conventional Nb cavities at 2 K
Notable performance gains over the past decade
1.3/1.5 GHz single-cell: >20 MV/m with at 4.4 K
Multicell cavities: above 10 MV/m at 4.4 K
Next step: beam acceleration with Nb₃Sn cavity/cavities integrated into a cryomodule for practical applications
U.Pudasaini et al. “Managing Sn-Supply to Tune Surface Characteristics of Vapor-Diffusion Coating of Nb3Sn”, presented at the SRF'21, East Lansing, MI, USA, Jun.-Jul. 2021, doi:10.18429/JACoW-SRF2021-TUPTEV013.
S. Posen et al. “Advances in Nb3Sn superconducting radiofrequency cavities towards first practical accelerator applications” Superconductor Science and Technology. 2021 Jan 11;34(2):025007.
D. Hall, “New Insights into the Limitations on the Efficiency and Achievable Gradients in Nb3Sn SRF Cavities”, PhD thesis, Cornell University (2017).
G. Müller et al, "Status and prospects of Nb3Sn cavities for superconducting linacs," in Proceedings of the Workshop on Thin Film Coating Methods for Superconducting Accelerating Cavities, 2000
G. Eremeev “Progress in Nb3Sn developments for CEBAF-style quarter cryomodule” TTC-2022,

## Slide 5: Nb3Sn Cryomodule development at Jefferson Lab
Started in 2018: based on G. Eremeev’s ECA
Goal: build, qualify, and beam-test the first Nb₃Sn quarter cryomodule
Cryomodule concept: based on the former CEBAF injector cryomodule with two 1.5 GHz cavities
Implementation: reused a spare injector cryostat and hardware, integrated with two new Nb₃Sn-coated C75 cavities
C. Leemann, “CEBAF design overview and project status”, in Third Workshop on RF Superconductivity, edited by K.W. Sheperd (1987)

## Slide 6: Cavity Coating & Qualification
First attempt: Two C75 cavities qualified but degraded after pair assembly → redo.
Second attempt: One cavity coated at JLab, another at Fermilab; both >13 MV/m, 4 K Q0 ~10¹⁰ @ 10 MV/m.
U.Pudasaini et al., “First cryomodule with Nb3Sn cavities for beam acceleration test at Jefferson Lab”, JLAB-TN-24-052.

## Slide 7: Pair Assembly (and Re-assembly)
Vacuum leak in the ceramic window after the pair assembly
One cavity degraded from mechanical stress during disassembly, but the other did not → Pair reassembled
Skipped the vertical test of the pair to avoid mechanical degradation.
G Eremeev and U. Pudasaini “Progress in Nb3Sn developments for CEBAF-style quarter cryomodule”, TTC 2022.

## Slide 8: Gray Enid I: From Cavity Pair to Completed Cryomodule
U. Pudasaini, "Nb3Sn SRF cavities: from R&D to real accelerator – overview of recent developments", presented at IPAC'24, Nashville, TN, May 2024,

## Slide 9: Cryomodule Qualification at Cryomodule Test Facility (CMTF)
Accelerating gradients close to the vertical test
Frequency difference between two cavities ~150 kHz
2nd cavity tuned to match the first one at 2 K– no degradation
Q0 degrades, but not the field: cooldown effect?
First demonstration of >10 MeV capable Nb3Sn cryomodule!

## Slide 10: Gray Enid I at UITF for Beam Test
Accelerator test bed for cryomodules, RF cavities, photocathodes, and polarimeters
Supports low-energy polarized electron-beam experiments up to 10 MeV
200 keV beam from a photocathode DC gun; 35 ps laser pulses at nominal 1497 MHz, with adjustable repetition rate
RF: two 5 kW klystrons connected through waveguides
Cryogenics: connected to the Cryogenic Test Facility (CTF) through supply and return lines
Upgraded Injector Test Facility (UITF)

## Slide 11: From Cooldown to Beam Acceleration at UITF

## Slide 12: Cooldown
  Cryomodule thermal shield temperature chosen to 35 K instead of 70 K
  Use the bypass valve in the supply can to improve the temperature stability at the JT valve
  Target: 300 mK delta across the pair during the superconducting transition
  Continuous monitoring of Temperature, magnetic field, and frequencies during the cooldown

## Slide 13: Cooldown
Frequency tracking consistent with CMTF: landing frequencies at UITF within a few kHz of CMTF values
Nb₃Sn transition near 17.7–18.0 K: identified from Cernox temperature and fluxgate signals
Cooldown optimization: best achieved K through the transition but challenging
Multiple cooldowns and thermal cycles: performed across two campaigns for cryomodule characterization and beam testing
Transition to Superconducting Phase
Return valve fluctuation

## Slide 14: Cavity Gradients at UITF
• Eₘₐₓ: maximum accelerating gradient reached during the test
• Eₒₚ: operating accelerating gradient
maximum accelerating gradient sustaining stable cavity operation for at least one hour with no X-rays.

## Slide 15: 4 K Eₘₐₓ Comparison: VTA, CMTF, and UITF
• Eₘₐₓ: maximum accelerating gradient reached during the test
• Eₒₚ: stable operating accelerating gradient
• Cavity 1: 13.6 → 13.3 → 11.8 MV/m
• Cavity 2: 9.0 → 7.9 → 7.4 MV/m
• CMTF → UITF change may be within measurement uncertainty and due to differing test setup
Overall: both cavities retained useful 4 K performance through cryomodule integration and UITF commissioning.

## Slide 16: Q0 Evaluation
R. Geng et al., "Beam acceleration with a Nb3Sn cryomodule at JLAB", in Proc. SRF2025, Tokyo, Japan, Sep. 2025, pp. 533-537. doi:10.18429/JACoW-SRF2025-WEA05
Q0 improved compared to the CMTF test but lower than the VTA

## Slide 17: Cavity Tuning for Beam Acceleration
Tuning amount relative to landing frequency
Target frequency
1496.500 MHz
Compression → lower f
Stretch → higher f
2.1 K
-74 kHz
+67 kHz
4.3 K
-45 kHz
+97 kHz
Cavity 1
5C75-RI-NbSn01
Cavity 2
5C75-RI-04
CMTF → UITF: Both cavities cold-tuned to a common 1496.500 MHz beam frequency
Laser repetition rate matched to the same frequency
RF performance preserved: no measurable degradation within experimental uncertainty
LLRF-controlled two-cavity synchronization: tuners actively maintained resonance while amplitude and phase were regulated for beam acceleration

## Slide 18
First Beam Acceleration with Gray Enid I
Gray Enid I Nb₃Sn cryomodule — first integrated beam demonstration
INJECTOR BEAM
200 keV
2 K BENCHMARK
7.1 MeV
4 K CW Beam
5.1 MeV, 10 µA
BUNCH RATE
1496.500 MHz
Beam energy and cavity gradients
0
2
4
6
8
10
2 K
4 K
7.1
5.1
Beam energy
(MeV)
10.0
7.0
Cavity 1 Eacc
(MV/m)
6.5
4.0
Cavity 2 Eacc
(MV/m)
Beam spot on at 2 K
Beam spot on at 4 K
R. Geng et al., "Beam acceleration with a Nb3Sn cryomodule at JLAB", in Proc. SRF2025, Tokyo, Japan, Sep. 2025, pp. 533-537. doi:10.18429/JACoW-SRF2025-WEA05

## Slide 19: Microphonics and the Pressure-Driven Detuning at 4.3 K
Observed limitation chain
He-pressure
fluctuations
45 Torr p-p @ 4 K
3.2 Torr p-p @ 2 K
Pressure-driven
detuning
df/dP ≈ 19 Hz/Torr
upstream cavity
Microphonics /
phase excursions
fast detuning remained
after pressure subtraction
Beam interruption
usable 4 K gradient
limited by stability
Diagnostic evidence from Campaign I
Pressure ↔ detuning correlation
Residual fast microphonics
Fast detuning with “slow” detuning from pressure removal: peak-to-peak 575 Hz for the upstream cavity
Fourier transform spectrum reveals the leading mode at 113 Hz
Upstream cavity

## Slide 20: Limitations / Lessons → Beam Acceleration Campaign II
Campaign I limitation / lesson (2025)
4 K operation limited by stability, not available gradient
Pressure-driven detuning caused phase excursions
45 Torr p-p @ 4 K vs. 3.2 Torr @ 2 K · df/dp ≈ 19 Hz/Torr
Cooldown likely affected Q₀ and RF reproducibility
Systematic RF-performance baseline needed before beam acceleration
Campaign II (2026)
Prioritized stable, usable 4 K acceleration and resonance control
Refined cryogenic controls: JT / return valve, heater, liquid level, and pressure settings
Controlled thermal cycle + uniform cooldown through Tc
Selected cooldown + systematic Q₀(Eacc) at 2.1 K and 4.3 K, staying below quench
Before/after tuning Q₀(Eacc) comparison under the same cooldown conditions

## Slide 21: Cooldown and RF Characterization
Gradient
(MV/m)
2.1 K
4.3 K
Cavity 1
Cavity 2
Cavity 1
Cavity 2
Eₘₐₓ
14.3
8.2
11.8
7.3
Eₒₚ
10.7
7.0
10.0
7.0
Similar gradients
Emax quench-limited; no detectable X-rays
Thermal cycle -> Q₀(Eacc) measured below quench
Q₀(Eacc)
Measured at 2.1 K and 4.3 K before/after tuning to 1496.500 MHz
No measurable RF degradation
Controlled cooldown through Tc
Solid symbols: without tuning
Empty symbol: after tuning
ΔT = 0.38 ± 0.18 K during 17.7–18.0 K transition
Gradient Verification

## Slide 22: 7.1 MeV Beam Acceleration and User Operation at 4.3 K
7.1 MeV beam spot near the target
Summary of beam test
Parameter (unit)
2.1 K
4.3 K
Beam energy (MeV)
7.3
7.1
Beam current
100 nA
5 µA
Beam mode
CW
CW
Bunch rep. rate (MHz)
1496.500
1496.500
Cavity 1 Eacc (MV/m)
10.7
10.0
Cavity 2 Eacc (MV/m)
7.0
7.0
•
4.3 K record run: 5 µA CW beam to 7.1 MeV, beam current was limited
by the available laser power
•
2.1 K benchmark: 7.3 MeV at 100 nA
•
User beam delivery: 6.3 MeV, 5 nA for >1 h at 4.3 K to
irradiate samples from a company developing radiation-hard x-ray sensors
Nb₃Sn cryomodule delivered nearly the same beam energy at 4.3 K as at 2.1 K.

## Slide 23: 4 K Beam Acceleration with Nb3Sn cavity : Comparison with Previous Results
 | Arnolds et al. (1979) | Yang et al. (2024) | Gray Enid I (2026)
Cavity configuration | 1 × 8 GHz 3-cell cavity | 1 × 650 MHz 5-cell cavity | 2 × 1.5 GHz 5-cell cavities
Eop (MV/m) | 3.6 | 2.3 | 10.0
Q0(Eop) | 7 × 10⁷ | n/a | 4 × 10⁹
Ebeam (MeV) | < 0.2 | 1.9* | 7.1
Ibeam (µA) | 1 | < 1 | 5
Field-control mode | CL | OL | CL
Gray Enid I demonstrates the highest 4.3 K CW beam energy gain using two 1.5 GHz five-cell Nb₃Sn cavities.
CL = closed-loop; OL = open-loop
* Pulsed beam injected into a CW cavity RF field with 2 µs pulse length at 1 Hz.
References:
G. Arnolds et al., “Design and status of an experimental superconducting linear accelerator for electrons”, IEEE Trans. Nucl. Sci. NS-26, 3775 (1979);
Z. Yang et al., “Stable acceleration of a LHe-Free Nb3Sn demo SRF e-linac”, Supercond. Sci. Technol. 38, 015009 (2024).
Manuscript under review in PRL — stay tuned for publication.

## Slide 24: What’s Next for Beam Acceleration with Gray Enid I?
User beam delivery: operate Gray Enid I for the user program with beam energy >5 MeV
Systematic cryomodule studies: investigate cavity performance with controlled temperature gradients across the cavity pair – plan to add U-tube transfer lines for improved helium flow and stability control
Higher beam energy: install Gray Enid II upstream of Gray Enid I to extend UITF beam energy toward 10 MeV by injecting a relativistic beam
Gray Enid II — compact cryomodule development: demonstrate a 2-cell, 1.5 GHz Nb₃Sn cavity cooled by cryocoolers and powered by a solid-state RF amplifier
Location for Gray Enid II

## Slide 25: Conclusions and Outlook
Demonstrated integrated Nb₃Sn cryomodule operation with a record CW electron beam at 4.3 K
A 5 µA CW beam was accelerated from 200 keV to 7.1 MeV at 4.3 K, nearly matching 7.3 MeV at 2.1 K
Cavity performance was preserved through integration and tuning: Cavity 1 reached 11.8 MV/m, with at 10 MV/m at 4.3 K
Campaign I identified pressure-driven detuning and microphonics as the main 4 K operational stability challenge; Campaign II improved through cryogenic and LLRF control
User beam delivery demonstrated end-to-end operation: from Nb₃Sn cavities to practical accelerator use
Next: user operation, perform controlled cooldown studies, and install Gray Enid II to extend UITF beam energy toward 10 MeV

## Slide 26: QUESTIONS?
Notes: Before sharing your presentation, confirm:
Fonts are consistent
Images meet quality standards
Charts use template colors
Footer information is current
Spell check completed
Links are working
File size is optimized