## Slide 1: Progress on Bronze-Route Nb3Sn Thin Films at HZB
Oliver Kugeler on behalf of Ming Lu
23.09.2026
TFSRF2026 Workshop, Chester, UK

## Slide 2: Outline
1. Introduction of Nb3Sn coatings via bronze route
2. Small Sample Optimization and Characterization
3. Nb3Sn QPR sample Fabrication and RF test
4. Summary and Future work

## Slide 3: Introduction of Nb3Sn/Cu by bronze route
Nb3Sn film on Cu by bronze route
Phase diagram of Nb-Cu-Sn ternary system at 700℃
Precursor structure for bronze route
It involves Nb barrier deposition, bronze electroplating, vacuum heat treatment, and final chemical etching.
The bronze route offers a promising approach for direct Nb3Sn on Cu, but film quality is strongly affected by the Sn content, Nb layer, vacuum heat treatment and etching process, etc.
At HZB, we are currently optimizing bronze route recipe to improve the RF performance of Nb₃Sn film.
Nb layer
Bronze layer
Cu substrate
Cu substrate
Nb3Sn layer
Cu substrate
Nb3Sn layer
Bohao Zhang
The optimization of Cu-based Nb3Sn coating involves combining two key aspects: Nb3Sn/Nb and Nb/Cu.
Cu substrate
Nb layer
Nb substrate
Nb3Sn layer
Cu substrate
Nb layer
Nb3Sn layer

## Slide 4: Outline
1. Introduction of Nb3Sn coatings via bronze route
2. Small Sample Optimization and Characterization
3. Nb3Sn QPR sample Fabrication and RF test
4. Summary and Future work

## Slide 5: Optimization of bronze route Nb3Sn/Cu recipe
Nb layer
Cu substrate
Cu substrate
Nb3Sn layer
Cu substrate
Nb3Sn layer
Bronze layer
Tc-oriented study of bronze route parameters:
Cu substrate: OFE, mechanical polishing and Electropolishing
Nb sputtering: HiPIMS power, pressure, substrate temperature, and ex-situ baking temperature
Bronze layer: Sn content and thickness
Vacuum heat treatment: temperature and duration
Chemical etching: etchant composition and duration
Electro-polishing Cu
Sputtering Nb
Electro-plating Bronze
Vacuum heat Treatment
Post-chemical polishing
Mechanical polishing Cu

## Slide 6: Optimization of the Nb3Sn preparation process
Optimizing HiPIMS Nb pressure, temperature, thickness, and ex-situ baking improves the Nb layer density and surface chemical state, increasing Nb3Sn Tc onset from 12.93 to 16.10 K (PPMS data).
The results showed higher Nb sputtering temperatures may lower the Nb3Sn Tc​ onset, while 750 °C bronze heat treatment gives better Tc onset than 700 °C.
After Nb film baking

## Slide 7: Optimization of the Nb3Sn preparation process
Step | Process | Original Parameters | Upgrade Parameters
1 | Mechanical polishing | Up to 100 µm removal | Up to 100 µm removal
2 | Degreasing | 1% Citranox®, 1 h | 1% Citranox®, 1 h
3 | Cu Electropolishing (EP) | ≈30 µm | ≈30 µm
4 | HiPIMS Nb (sputtering) | Tsub ≈ 180 °C, Ar = 2 Pa, Power = 600 W, Thickness ≈ 10 µm | Tsub ≈ 180 °C, Ar = 0.8 Pa, Power = 400 W, Thickness ≈ 10 µm
5 | High-temperature baking | 700 °C, 20 h | 700 °C, 20 h
6 | Bronze electroplating | ≈10 µm bronze | ≈10 µm bronze
7 | Vacuum Heat treatment | 700 °C, 30 h | 750 °C, 30 h
8 | Surface bronze removal | Aqua regia about 5 min | Aqua regia about 10 min
Optimized steps 4 (denser Nb layer), 7 (large grain size) and 8 (fewer impurities):
Bronze route at 700℃ : Original recipe, Nb3Sn/Nb/Cu ≈ 1.0 µm / 10 µm / 3 mm.
Bronze route at 750℃ : Upgrade recipe, optimized steps 4+7+8.

## Slide 8: SEM characterization of Cu-based Nb3Sn
The 750°C sample exhibits larger, better-defined Nb₃Sn grains and fewer oxide phases than 700°C sample.
However, Cu particles, P-rich nanofibers, sparse grain areas, and O-enriched regions remain, indicating surface inhomogeneity and residual impurities.
Bronze route: 700℃
Bronze route: 750℃
Cu particles
P-rich nanofibers
Sparse grains areas
O-enriched regions

## Slide 9: XRD characterization of Cu-based Nb3Sn
Bronze route: 700℃
Bronze route: 750℃
XRD results showed minor Cu and NbSn₂ are detected at both 700°C and 750°C samples.
The 750 °C samples showed sharper Nb3Sn peaks and a smaller FWHM, consistent with larger Nb3Sn grains than those at 700 °C.
Alena Prudnikava

## Slide 10: GIXRD characterization of Cu-based Nb3Sn
Both GIXRD results only detects Nb3Sn phase.
Other impurities are below the detection limit or amorphous.
Cu substrate
Nb barrier layer
Nb3Sn layer
NbSn2
Cu,CuOx
NbOx,SnOx,C-H
Bronze route: 700 ℃ and 750 ℃
GIXRD
Alena Prudnikava
Phase Composition Diagram of Nb3Sn/Cu coating

## Slide 11: Thermal current test of Cu-based Nb3Sn surface
CRAFT Test conditions: Zero field cooled, Plot trapped flux magnitude of center sensor versus temperature gradient during cooldown.
Under the 0.05 K/cm temperature gradient, flux trapping in the new sample decreased from 200 μT to 25~45 μT, indicating suppressed thermoelectric currents due to improved coating homogeneity and weaker flux pinning.
F. Kramer
CRAFT
Bronze route: 700℃
Bronze route: 750℃

## Slide 12: Outline
1. Introduction of Nb3Sn coatings via bronze route
2. Small Sample Optimization and Characterization
3. Nb3Sn QPR sample Fabrication and RF test
4. Summary and Future work

## Slide 13: Nb3Sn/Nb QPR sample fabrication process
Bronze layer
Nb substrate
Nb substrate
Nb3Sn layer
Nb substrate
Nb3Sn layer
BCP 120μm + baking
Coating bronze
Synthesized Nb3Sn
Removing bronze
Nb QPR sample
Nb₃Sn/Nb preparation via bronze route
120 μm BCP + 700 °C (20h) baking to remove hydrogen and release stress;
Before bronze electroplating, the sample need activation and tilting to avoid trapped bubbles.
Increasing annealing temperature from 700 °C to 750 °C, enlarged Nb3Sn grain size and reduced surface impurities.

## Slide 14: Nb3Sn/Cu QPR sample fabrication process
Nb layer
Bronze layer
Cu substrate
Cu substrate
Nb3Sn layer
Cu substrate
Nb3Sn layer
Nb₃Sn/Cu preparation via bronze route
30 μm EP + 700 °C (20h) baking to increase the Nb layer density and release stress;
Due to the thin Nb film at the bottom (<1 μm), the bronze layer was deposited only on the top surface.
The sample still need activation and tilting to avoid surface trapped bubbles.
Sputtering Nb
Coating bronze
700℃ Heat treatment
Removing bronze
Electropolishing Cu

## Slide 15: Nb3Sn QPR sample Rs-T test comparison
At 4 K, the Cu-substrate Nb3Sn sample exhibit an Rs value 29 nΩ higher than that of the Nb-substrate Nb3Sn sample. Both samples show severe Q-slope, and simplified BCS model fitting was performed.
Rs=46.0 nΩ @4 K, 20 mT, 413 MHz
Rs=17.1 nΩ @4 K, 20 mT, 417 MHz
Nb3Sn on Nb
Sebastian Keckert
Nb3Sn on Cu
Corresponds to

## Slide 16: Nb3Sn QPR sample Rres fitting comparison
Compared with the Nb-substrate sample, the Cu-substrate Nb3Sn shows ~20 nΩ higher Rres at 20 mT, a lower Δ across all fields, and a smaller A parameter with weaker field dependence.
Rres=36.37 nΩ @ 20 mT, 413 MHz
Rres=16.04 nΩ @ 20 mT, 417 MHz
Nb3Sn on Nb
Nb3Sn on Cu

## Slide 17: Nb3Sn QPR sample thermal cycle comparison
The both Rs​ shows only a minor dependence on the cooling rate, indicating that Rs​ via bronze route is not sensitive to the thermal cycling conditions.
ΔRs=1.5 nΩ @ 4K, 20 mT, 417 MHz
ΔRs=0.8 nΩ @ 4K, 20 mT, 413 MHz
Nb3Sn on Nb
Nb3Sn on Cu

## Slide 18: Nb3Sn QPR sample penetration depth comparison
Compared with the Nb-substrate Nb3Sn (18.0 K), the Cu-substrate sample shows a lower λ(0) and lower Tc (14.7 K).
λ(0) = 166.78 ± 3.91 nm
Tc = 18.026 ± 0.025 K
λ(0) = 123.6± 5.4nm
Tc = 14.71± 0.06 K
Nb3Sn on Nb
Nb3Sn on Cu

## Slide 19: Nb3Sn QPR sample critical field comparison
The temperature-dependent quench field data near Tc was described by a T2 fit.
The Cu-substrate Nb3Sn exhibits a lower Bc(0) (56.3 mT) compared with Nb-substrate Nb3Sn (102 mT).
Nb3Sn on Nb
Nb3Sn on Cu
B0=56.3mT
Sebastian Keckert

## Slide 20: Summary of Cu-based Nb3Sn coating recipes
Increasing the niobium barrier layer’s density or thickness improved the Nb3Sn film quality on copper, approaching the quality of Nb3Sn on high-purity Nb.
Samples type | Nb layer parameters | Treatment process | Min. growth temp. of Nb3Sn | Rs@4K, 20mT, 416MHz | 0.05 K/cm trap flux (zero field) | Nb3Sn film quality
Nb3Sn/Cu samples (Sasha) | 180℃/10μm, 2.0Pa, 600W | pre-annealing 600℃ 20h +bronze route 30h | 700℃ | 46.0 | large, 200 μT | Tc=14.6K,normal
Nb3Sn/Cu samples (Sasha) | 180℃/30μm, 0.8Pa, 400W |  | 750℃ | ? | 25~45 μT | Tc~16.3K
Nb3Sn/Nb samples (IMP, China) | Nb substrate, RRR>300 |  | 750℃ | 17.1 | Small, 5 μT | Tc=17.7K,perfect
Samples type | Nb layer parameters | Treatment process | Min. growth temp. of Nb3Sn | Rs@4K, 20mT, 416MHz | 0.05 K/cm trap flux (zero field) | Nb3Sn film quality
Nb3Sn/Cu samples (Sasha) | 180℃/10μm, 2.0Pa, 600W | pre-annealing 600℃ 20h +bronze route 30h | 700℃ |  | large, 200 μT | Tc=14.6K,normal
Nb3Sn/Cu samples (Sasha) | 180℃/30μm, 0.8Pa, 400W |  | 750℃ | ? | 25~45 μT | Tc~16.3K
Nb3Sn/Nb samples (IMP, China) | Nb substrate, RRR>300 |  | 750℃ |  | Small, 5 μT | Tc=17.7K,perfect
SUST, DOI: 10.1088/1361-6668/ae496a
Origin recipe
Upgrade recipe

## Slide 21: Work summary and future work plan
Future work plan:
  Use better Cu and Nb substrate, optimize the Nb layer to reduce strain in Nb3Sn and thereby further enhance Tc.
  Use higher Sn content (10→15 at%) bronze, and longer annealing (30→50 h), and further optimize bronze etching recipe.
  Develop laser treatment, PEP, FE treatment, high-T baking, plasma cleaning to improve the surface quality of Nb3Sn.
Work summary:
  The bronze route fabrication recipe was optimized to improve the Tc of Nb3Sn on Cu substrates.
  QPR samples with Nb3Sn on both Cu and Nb substrates were fabricated and tested, and possible strategies for further improvement were proposed.

## Slide 22
Thank you for your attention.