## Slide 1: Calibration and deposition of 1.3 GHz Nb cavity coated with Nb3Sn thin film by PVD planar magnetron sputtering
Reza Valizadeh,
Oleg Malyshev, Dan Seal, James Conlon , Afshan Ashraf (STFC),
Dan Turner, Graeme Burt (Lancaster University)

## Slide 2: Outline
Objectives & Strategy
Thin Film Testing & Validation
Cavity Deposition
Summary

## Slide 3: SRF Thin Film Objectives

## Slide 4: Aims & Objectives
  To develop and validate a novel class of SRF cavities based on Nb3Sn and NbTiN thin films: improve accelerator performance and efficiency through higher accelerating fields,
            better stability,
          reduced material costs,
  lower operational costs compared to traditional bulk niobium cavities
Development of in-house skills and capabilities to deposit, measure and test thin film cavities
Thin film cavity of high Tc tested in cryomodule with beam

## Slide 5: Nb3Sn for SRF – Potential
Tc (Nb) = 9.2 K  Tc (Nb3Sn) = 18.3 K
results in lower RBCS at a given temperature
  operation at 4.5 K
  reduce grid power to run cryo plant by factor of 3
potential demonstrated by VTD cavities (state of the art):
Q0 ~ 2 x 1010 at 20 MV/m (4.4 K, 1.3 GHz) [2]
[1]

## Slide 6: Thin Film Testing & Validation

## Slide 7: RF Test With Choke Cavity
7.8 GHz Choke Cavity
Low field measurements:
Rs vs Bs, pk
Rs vs Ts
Penetration depth vs Ts
Mass parameter optimisation prior to:
High field/low frequency tests with QPR
Cavity tests
Upgrades to increase Bs, pk:
Hall sensors for residual magnetisation
studies
Magnetic shields
TF coated Cu cavities
CI bunker
3 tests per
week!
100
90
80
70
60
50
40
30
20
10
0
0 100 200 300 400 500 600 700
Rs, 4.2 K (µΩ)
Deposition Temperature (°C)
Effect of magnetron power on Nb3Sn/Cu
Target 1 (4 hr)
Target 2 (4 hr) BCS
Effect of deposition temperature on Nb/Cu
Most importantly, how does the thin film perform under RF conditions?
D. Seal (ASTeC)
Courtesy of P. McGuinness (ASTeC)
9th September 2025
STFC Thin Films Programme – CERN Visit
29

## Slide 8: Optimisation of deposition parameters using choke cavity
Optimisation of deposition power for Nb3Sn on Cu
Surface resistance of different SC thin film on Cu
Surface resistance on Nb with different surface roughness surface preparation
Optimum deposition power for Nb3Sn is stablished at 50 W DC power
Film Thickness dependence of Nb3Sn on Cu
Best surface resistance so far is achieved on Nb substrate
For high Tc, Nb3Sn seems to be more suitable candidate for 4 K operation having lower Rs than NbTiN.
Surface resistance of different thickness on Cu

## Slide 9: Low Power Cavity Test Facility
Courtesy of O. Poynton & J. Rigby
Cryocooler based facility
P < 2.5 W, T > 4 K (est.)
Quick first cavity test
Good cavities will have high power test in LHe
4 types of cavity
1.3 GHz closed
1.3 GHz split
6 GHz closed
6 GHz split
First tests in 2025!
Feedthroughs for RF, wiring etc
1.3 GHz cavity
6 GHz split cavity
Adapter for heat links
Cold head
Cavity facility alongside Choke Cavity facility

## Slide 10: High Power Cavity Testing
Full Q0 vs Eacc test with LHe
Testing with existing STFC/DL LHe infrastructure
mainly used for ESS & PIP-II cavity tests
Upgrades now allow for:
  For thin film SRF programme
  A RF single system for 650 and 700 MHz,
and 1.3 GHz
  P ≤ 200 W, T = 2 & 4.2 K
  Capability for 9-cell tests
Existing SRF Test Facilities in SuRF Lab at Daresbury Laboratory
Commissioning in 2025!
Courtesy of T. Sian & C. Hill
However, very limited number and durations for free timeslots, i.e. only good cavities should be characterised
Coordinated by T. Sian (ASTeC)

## Slide 11: 1.3 GHz Cavity Deposition

## Slide 12: First Nb3Sn calibration on 1.3 GHz Nb Cavity
View from bottom flange
View during deposition at 650° C
uncoated area under witness sample
First trial run of Nb3Sn deposition of
1.3 GHz Nb cavity with deposition parameters established on planar samples.
The trial run proved to be successful. Tc of 17.5 K
View after deposition of Nb3Sn and
Nb3Sn on Nb Witness sample
Nb3Sn
Cu
Nb
Nb3Sn

## Slide 13: First 1.3 GHz Nb cavity deposited with Nb3Sn
Cavity heating stage
Magnetron
Sputtered material (Plasma)
Cavity is deposited using magnetron sputtering (PVD).
Deposition inside a UHV system.
Deposition at 600 oC
Custom in-house magnetron designed and tested can be positioned inside the cavity.
Two magnetron opposite each other was moved in and out during deposition total 30 hours.

## Slide 14: First Nb3Sn on Nb cavity at STFC.
Inside the cavity after deposition
After some test depositions the first 1.3 GHz Nb has been coated with Nb3Sn.
After visual inspection, the cavity was prepared for testing in an ISO 4 cleanroom environment.
The cavity transported to HZB for testing.

## Slide 15: RF Test At HZB
No thermo-currents were recorded with the azimuthally placed sensors.
While the Tc was at 18.1 K it only achieved a Q0 of 8 x 106
No Tc of Nb was detected: Possibly cavity fully coated.
Poor Q factor:
  Cu contamination at surface layer due to diminishing target
  Present of other normal conducting material due to poor cavity handling.
  Or other reasons to be determined.
  No HPR after Deposition
Frequency and loaded quality factor vs temperature
Just after venting chamber
After target removed
Rs (5.3 K) ~ 43 μΩ, Tc ~ 18 K
Q0 of 8 x 106

## Slide 16: Nb Disk deposition inside segmented Nb Cavity C
Unfortunately, this resulted in mixed composition and non superconducting phase (high Sn content) gave
May be caused:
        By low temperature deposition below 600 C
Or target non homogeneity
Chart: T (K)
 | 1
 | 1
 | 1
 | 1
 | 1
 | 1
 | 1
 | 1
Rs (5 K) ~ 1500 μΩ,
Tc ~ 18 K

## Slide 17: Pre and post Annealed targets
Pre annealed (Name) | Average Nb At% | Average Sn At % | No. of spectra
Site 4 | 70.13 | 29.87 | 10
Site 9 | 70.38 | 29.62 | 9
Post Annealed |  |  | 
Site 1 | 68.98 | 30.02 | 10
Site 2 | 66.82 | 33.18 | 9
Site 3 | 63.61 | 36.39 | 7
Nb 100 mm Holder |  |  | 
Center (Light spot) | 95.88 | 4.12 | 2
Edge (Dark) | 99.85 | 0.15 | 2

## Slide 18: Comparison of Nb3Sn deposition from two different targets two different magnetron outside cavity
Statistic Nb Sn
Max 76.43 26.83
Min 73.17 23.57
Average 75.38 24.62
Standard Deviation 0.76 0.76
Old target/Com magnetron
New target/HM magnetron
Statistic Nb Sn
Max 78.05 24.11
Min 75.89 21.95
Average 76.93 23.07
Standard Deviation 0.72 0.72

## Slide 19: Copper Cavity deposition facility
The new deposition facility currently being commissioned at Daresbury Laboratory. It will be a dedicated facility for the deposition of 1.3 GHz cavities (Both single and two-cell).
The facility will be situated in an ISO 6 cleanroom environment.
Initial deposition tests are being conducted using a Nb cylindrical target and mock Cu cavity components. Integrating the heating stage.
Cu mock cavity segments
Nb Cylindrical Magnetron

## Slide 20: HIPIMS Nb deposition at 400 C 24 Hours
F7
F5
F6
The deposition is done with fixed magnetron position with four magnet segments.
Two segments in elliptical part and two middle of each tube section,
The cavity is laser welded at Electra.
Another cavity with the same parameters is deposited for 48 Hours and sent to HZB for bronze route deposition for first trial.

## Slide 21: Summary
First 1.3 GHz Nb cavity was produced by magnetron sputtering, the major deliverable for IFAST and progression of ISAS.
Although full coverage and high Tc was achieved, it resulted in low Q0 of 8x106 and Rs (5.3 K) ~ 43 μΩ, Tc ~ 18 K
After optimising deposition parameters on flat samples further optimization is needed for cavity deposition
Additional processing may be needed to remove non-superconducting phase growth to achieve low surface resistance:
    Post thermal annealing
    Mechanical or chemical polishing
    Laser or plasma processing
The ultimate goal is to deposit Nb3Sn on copper cavity:
    Do we need suitable buffer layer
    Do we need further optimisation from Nb to Cu cavity?
    Lack of cylindrical target further complicates the process.