## Slide 1: Development of the Nb3Sn coatings on Novel Cavity Geometries Using Vapor-Diffusion Technique
Nikki Tagdulang
Research Associate
Month Day, Year
FERMILAB-SLIDES-26-0213-TD
This manuscript has been authored by Fermi Forward Discovery Group, LLC under Contract No. 89243024CSC000002 with the U.S. Department of Energy, Office of Science, Office of High Energy Physics.
Notes: The larger goal here is to understand and what needs to be done to achieve reproducible acceptable Nb3Sn coating.

## Slide 2: Acknowledgement
G. Eremeev, B. Tennis, and S. Posen
M. Kelly and T. Petersen at ANL
Charles Thangaraj, Chris Edwards, and IARC-TD team
Fermilab and ANL technical staff
Adam, Anna, Jae-Yel and Zu Hawn for the material science analysis support

## Slide 3: Outline
Introduction
The Nb3Sn coating at Fermilab
Novel cavity geometries
1.5 cell 650 MHz cavity coating and results
QWR cavity coating and results
Summary

## Slide 4: Introduction
Nb₃Sn is a viable alternative to Nb, which is operating close to its fundamental limits, for superconducting radio-frequency (SRF) cavities.
High at 4 K:
  Enables the use of cryocoolers instead of liquid helium, making compact linear accelerators possible
High superheating field → high limit on the accelerating field gradient: in a standard 1.3 GHz TESLA-type cavity
  Can reduce both the capital and operational costs of high-duty-factor accelerators
S Posen and D L Hall 2017 Supercond. Sci. Technol. 30 033004

## Slide 5: The Nb3Sn coating at Fermilab
Fermilab employs vapor diffusion technique-the mainstream Nb3Sn coating process
Sn vapor is diffused and allowed to react with Nb at about 1100 0C to form stoichiometric Nb3Sn
State-of-the-art Nb3Sn-coated cavities reached above 20 MV/m coated and tested at Fermilab
  application-ready performance
The record performance appears to have shiny coating achieved through high-temperature nucleation of the vapor diffusion technique
The opportunity of vapor-diffused Nb3Sn coating is clear, but reproducibility remains a challenge.
Fermilab established standard coating process as baseline procedure.
AI generated

## Slide 6: The Nb3Sn coating at Fermilab: Standard cavity and set-up preparations
Ensure clean Nb coating chamber.
Design and fabricate coating supports taking into account mechanical stability at elevated temperatures.
Standard Nb substrate preparation ensuring no significant degradation in RF properties associated with cavity defects.
30 V Anodization for efficient Sn nucleation
Nb3Sn coating using high-temperature nucleation recipe.
For multicell cavities, sources are placed at each ends of the cavity to help achieve uniform coating.
AI generated
Notes: Mention that it is AI generated

## Slide 7: Novel cavity geometries
QWR 145 MHz
1.5 cell 650 MHz
B15S-EZ-001
Low-power e-beam source prototype of IARC
Alternative SRF cavities for ATLAS and future ion accelerators

## Slide 8: Novel cavity geometries
QWR 145 MHz
1.5 cell 650 MHz
B15S-EZ-001
Low-power e-beam source prototype of IARC
Alternative SRF cavities for ATLAS and future ion accelerators

## Slide 9: 1.5 cell 650 MHz coating
Anodized Nb cavity
Prevents usage of additional source
1.5 cell cavity is unique with a semi-closed cavity end, intended for compact accelerator demonstration with integrated RF gun.
There was technical issue that prevents data logging, but screenshots of the program showed that it received standard coating recipe.
5.5 g of Sn and 1 g of SnCl2 was added to the Sn source

## Slide 10: 1.5 cell 650 MHz coating results
Using controlled cool down (cd) and magnetic field < 3 mG
The cavity is strongly limited by residual resistance with Q0 ~ 3e9 at low fields and Eacc,max ~ 9 MV/m.
10.18429/JACoW-NAPAC2025-WEP011
Cavity appears to be well-coated visually
Some Sn spots are observed at the adaptor and cavity flange
1st cd: meas 4 K cd  meas 2 K
2nd cd: meas 4K  ramp to 30 K  meas 2 K
Repeatable controlled cd

## Slide 11: 1.5 cell 650 MHz coating results
Analysis of the 0 and pi modes of the cavity showed that the half cell has an order of magnitude higher in surface resistance compared to the full cell.
This suggests that potentially the half cell received insufficient Sn nucleation since this part is far from the source.
In Nb3Sn coating using vapor diffusion technique, one must consider cavity design to achieve uniform coating.
Alternatively, Sn plating can be used to initially seed Sn on the hard-to-reach areas of the cavity. Fermilab has started the development of this technique too.

## Slide 12: Novel cavity geometries
QWR 145 MHz
1.5 cell 650 MHz
B15S-EZ-001
Low-power e-beam source prototype of IARC
Alternative SRF cavities for ATLAS and future ion accelerators

## Slide 13: QWR 145 MHz cavity coating
High B-field region
QWR cavity geometry is as well unique consisting of an inner rod where the B-field is highest.
It also consists of two flanges at each ends. Two sources have to be used with 8 g of Sn and 1 g of SnCl2 in each.
Three cavities were coated to address repeatability and reproducibility. QWR0 has NbTi flanges, whereas the others have Nb flanges.
Coating sources were set-up such that the B-field region is at the direct sight of Sn flow.

## Slide 14: QWR 145 MHz cavity coating results
QWR0
QWR1
QWR2
Cavity appears to be well-coated visually
Sn spots were observed at the flanges in all
QWR0 demonstrated record-breaking performance with peak magnetic field of 105 mT.
QWR0 and QWR1 showed very similar results demonstrating reproducible results (2/3).
Preliminary results
T Petersen et al 2026 Supercond. Sci. Technol. 39 045006

## Slide 15: QWR 145 MHz cavity coating materials analysis
QWR0
source
end
QWR1
QWR2
S1: 8.3 g
S2: 7.8 g
S1: 8.5 g
S2: 6.7 g
QWR0 achieved uniform coating compared to QWR1 and QWR2.
At the end sample, closest to the high B-field region, the microstructure looks similar between QWR0 and QWR1, except for the patchy regions seen in QWR1. Patchy regions has thickness of about 150 nm.
Excess Sn are observed in QWR2, potential reason of degraded performance.
To understand how this happened, we first looked at how much Sn was used. It has no correlation with the samples’ quality.
S1: 7.9 g
S2: 8.2 g
Sn used
5 um
5 um
5 um
5 um
5 um
5 um
RF performance

## Slide 16: Materials correlation with coating temperature
Coating quality
QWR0
QWR1
QWR2
consistent

## Slide 17: Materials correlation with coating temperature
Coating quality
QWR0
QWR1
QWR2

## Slide 18: Materials correlation with coating temperature
There seems to be a correlation between Sn source temperatures to the coating quality.
Sn sources configuration and precise control of their temperature are important to achieve well-performing Nb3Sn-coated QWR cavities.
Sn spots observed
Uniform coating
Coating quality
QWR0
QWR1
QWR2

## Slide 19: Summary
The complex geometry of the 1.5-cell cavity was challenging to coat. It is not possible to add source and supply Sn sufficiently at the half cell. One could reconsider the cavity design, or apply an alternative technique, such as Sn plating to seed the surface with Sn prior to coating.
QWR cavities have demonstrated repeatability: 2/3 of the cavities showed remarkable RF performance. A potential correlation between the Sn source temperature and the coating quality was found for this type of cavity.
A 1.5-cell 650 MHz cavity and QWR cavities were coated at Fermilab—the first of their kind to be coated.