## Slide 1
Thin-Film Superconductivity for SRF Cavities
Current Status & Future Challenges

## Slide 2
Why Thin Films for SRF?
SRF performance is a SURFACE phenomenon — RF penetrates only ~40 nm (Nb) to ~350 nm (NbN)
Bulk Nb is near its intrinsic limit (~50 MV/m) after decades of N-doping & processing
Thin films offer:
Higher gradient potential (Nb3Sn, multilayers)
Operation at 4.2 K (vs 2 K for Nb) -> cheaper cryogenics
Lower material cost (less Nb, Cu substrate)
Better thermal stability (Cu's high thermal conductivity)
Only the first few hundred nm 'matter' — the bulk is redundant

## Slide 3
The Materials Landscape
Nb (sputtered on Cu) — Tc 9.2 K — Deployed (HIE-ISOLDE) — Mature
Nb3Sn (A15) — Tc 18 K — Prototype cavities — Most optimised alternative
NbN / NbTiN — Tc 16-17 K — Sample + small cavity — Mid-stage
MgB2 — Tc 39 K — Sample only — Exploratory
Nb3Al, V3Si, Mo-Re — Tc 11-19 K — Sample studies — Exploratory
SIS multilayers — Concept + samples — Early R&D
Nb remains the benchmark. Nb3Sn is the clear frontrunner among alternatives.

## Slide 4
Status: Sputtered Nb on Cu
ACHIEVEMENTS
CERN HIE-ISOLDE quarter-wave cavities: >60 MV/m surface peak field, Q ~ 1e9 at 2.3 K
First production thin-film cavity to match bulk-Nb performance
Seamless spun-Cu substrates eliminated weld-seam limitations
4 cryomodules (20 cavities) installed and operational
REMAINING LIMITS
Voids, impurities, non-uniformity, adhesion issues
Large elliptical cavities still trail bulk Nb

## Slide 5
Status: Nb3Sn — The Leading Alternative
Tc ~ 18 K -> can operate at 4.2 K (no superfluid helium)
Theoretical gradient ~2x Nb
Single-cell: Q0 ~ 1e10 at ~10 MV/m; up to 3e10 at 2 MV/m (4.2 K)
Coating methods: tin vapour diffusion, magnetron sputtering (DCMS, HiPIMS)
KNOWN PROBLEMS
Sn deficiency / non-stoichiometric A15 phase
Cu interdiffusion (on Cu substrate)
Surface roughness -> major gradient limiter (Cornell)
Film cracking under mechanical strain (brittle)
Q-slope at high field

## Slide 6
Status: Other Materials
Nitrides (NbN, NbTiN):
Higher Hc than Nb, but high-field Q-slope & impurity incorporation limit performance
MgB2:
Highest Tc (~39 K) -> could operate at 15-20 K; but unstable, oxygen-sensitive
SIS multilayers (Superconductor-Insulator-Superconductor):
Theoretical path to exceed Nb superheating field (>50 MV/m)
Requires pinhole-free insulating layers — not yet at cavity scale

## Slide 7
Key Achievements Summary
WHAT WORKS TODAY
Thin-film Nb-on-Cu deployed in HIE-ISOLDE (production)
Nb3Sn demonstrates high Q at 4.2 K (prototype)
Sample-level characterisation infrastructure mature
European Thin-Film SRF Roadmap published (2025)
Active international collaboration (CERN, Fermilab, Cornell, JLab, KEK, STFC)
WHAT DOES NOT YET WORK
Reproducible high-gradient Nb3Sn at production scale
Thin films matching bulk-Nb gradient on large elliptical cavities
Multilayer/SIS at cavity scale
Stable MgB2 coatings

## Slide 8
Challenge 1: Reproducibility & Yield
THE CHALLENGE
Prototype cavities hit target performance; production runs do not
Coating uniformity over complex cavity geometry is inconsistent
Defect statistics not yet controlled enough for accelerator-grade yield
IMPACT
Thin films cannot be specified for future machines (FCC, ILC) until yield is predictable
'A single great cavity is a paper. A hundred great cavities is a technology.'

## Slide 9
Challenge 2: Defects, Stoichiometry & Interface
Nb3Sn-specific:
A15 phase requires exact 3:1 Sn:Nb stoichiometry — deviations kill performance
Sn-poor regions, voids, Cu interdiffusion create weak spots
Surface roughness nucleates vortex entry -> premature quench
General:
Particulates and pinholes -> field emission
Film-substrate adhesion & thermal interface resistance -> hot spots, quench
Impurity incorporation during sputtering (O, N, Ar)
Coating chemistry & microstructure must be controlled to nm precision over m2 of surface

## Slide 10
Challenge 3: Mechanical & Operational Robustness
MECHANICAL
Nb3Sn is brittle — cracks under handling, cooldown thermal contraction, tuning stress
Safe strain range is narrow (~ -2.3% to +0.9%)
Recoating/healing degraded cavities is an active research area
OPERATIONAL
Q-slope at high field limits useful gradient
Flux pinning and trapped flux losses (especially at 4.2 K)
Long-term field emission & gradient degradation in operation (LEP-II experience)

## Slide 11
Challenge 4: Scaling & New Architectures
SCALING TO REAL CAVITIES
Most data is from sample-level or single-cell tests
Multi-cell, full-size elliptical cavities remain rare
Cryomodule integration largely unproven for alternatives
NEW ARCHITECTURES NEEDED
HiPIMS / energetic sputtering -> denser, void-free films
Multilayer SIS -> break the Nb superheating-field limit
In-situ surface preparation compatible with coating

## Slide 12
Coordinated Programs & Roadmaps
EUROPEAN PROGRAMME CHAIN (Horizon 2020 / Europe)
ARIES (2017-2021) WP15: substrate prep & TF quality (Nb, NbN, NbTiN, Nb3Sn, SIS) — TRL 3
IFAST (2021-2025) WP9: 6 & 1.3 GHz cavities; first bulk-Nb cavity PVD-coated with Nb3Sn; EU TF-SRF roadmap; laser & FLA annealing — TRL 4-5
iSAS (2024-2028) WP3: Cu cavities + Nb3Sn coating & RF testing; flux trapping & mitigation; tunability
EPITA (2027-2031) WP4: industrialise Nb3Sn cavity production; vertical & horizontal cryostat tests; conduction cooling — TRL 6
Industrial partners: 0 (ARIES) -> 3-5 (EPITA); goal: transfer Nb3Sn production to industry
SNOWMASS 2023 (US strategy)
Next-Gen SRF via advanced thin films & innovative materials (Valente-Feliciano et al.)
Nb3Sn: maturing tech for accelerators + dark-matter / GW / quantum-sensing detectors (Posen et al.)
EXAMPLE
Aug 2025: first bulk-Nb cavity coated with Nb3Sn (Cockcroft/ASTeC), RF-tested at HZB

## Slide 13
Roadmap & Outlook
NEAR-TERM (1-3 yrs):
Improve Nb3Sn reproducibility via HiPIMS & process control
Multi-cell Nb3Sn cavity demonstrations
Recoating/healing protocols
MID-TERM (3-7 yrs):
Nb3Sn production qualification for a real accelerator
SIS multilayer cavity-scale proof-of-principle
LONG-TERM (7+ yrs):
Thin-film baseline for FCC, muon colliders, ILC upgrades
4.2 K operation as standard -> major cryogenic cost reduction
Milestone: 12th Int'l Workshop on Thin Films & RF Superconductivity — Chester UK, Sept 2026

## Slide 14
Take-Home Message
Thin-film SRF has moved from concept to demonstrated prototype. The science works. The remaining battle is engineering: reproducibility, defect control, mechanical robustness, and scaling to production cavities. Nb3Sn is the material to watch; the next 3-5 years will decide whether thin films become the future of SRF.
Thank you

## Slide 15
WELCOME
TFSRF 2026- 12th EDITION
THIN FILM AND NEW IDEAS FOR PUSHING
THE LIMITS OF RF SUPERCONDUCTIVITY
International Organising Committee:
Anne- Marie Valente
Alex Gurevich
Reza Valizadeh - Chair
Cristian Pira
Thomas Proslier
Walter Venturini Delsolaro
Takayuki Saeki

## Slide 16: The TFSRF Started in 2005 at JLab
  Has been alternatively every 2 years by Jlab and INFN Legnaro (except 2020)
  From 2024 edition
    It is organized to be shared among other community
    We propose to work at International level combining various road maps.
    Intensify R&D and accelerate the progress in TF SRF field.

## Slide 17: Sharing Ideas to create Synergy
Setting the Horizon: Global Perspectives & Technical Roadmaps
Pushing SRF Thin Films Limits: Theoretical Advances, Deposition Modeling & DFT
Latest Advances in Nb Thin Film Technology
Conventional PVD, energetic condensation from highly ionized plasmas
Nb3Sn Technology: Recent Technical Advances & Scaling Horizons
Beyond Nb & Nb3Sn: Alternate materials, multilayer SIS structures and functional layers
Tailored Substrates for Advanced Film Growth
Emerging Frontlines in Characterization Methods: Advanced Imaging & Novel Probes
Emerging Frontiers & Synergies in SRF Thin Films: From Quantum Sensing to AI-Driven Material
The primary aim of the workshop is to provide a collaborative environment as open, inclusive and diverse as possible, to foster discussion and new ideas.

## Slide 18
  Speakers
Please upload your slides the day BEFORE your talk, we need to download them in order to verify them and show on ZOOM if needed

## Slide 19
  For those who are staying at the Plaza Hotel
    Breakfast is included
  Lunch is served at restaurant adjacent .
  For Dinner there will be plenty of choices in city centre

## Slide 20
  Visit to Daresbury Laboratory:
    A dedicated bus is arranged to take all the delegates to Lab and back.
    The bus will leave from the Hotel at 2:00 pm just after the lunch on Wednesday

## Slide 21: Workshop Dinner
  Direction:
  5 minutes walk from the Plaza Hotel, Signed Posted.
Date: 23rd September 2026 Time: 7pm
Chester Cathedral

## Slide 22: Remebering Abscent Colleagues