## Slide 1
Latest Advances in Nb Thin Film Technology
General questions: do we agree that
  Anomalous non linear losses (Q-slope) reside for the main part in the temperature independent component of the surface resistance (residual resistance)? How does the temperature dependent component (aka BCS) compare between bulk Nb and Nb/Cu?
  Experience with optical inspection after test, T mapping, PCT, all indicate that the main reason (or the most frequent reason) for particularly poor performance is the presence of localised “defects” or “weak points” and that large portions of the films perform like bulk Nb?
  Thermoelectric currents can be an important source of residual resistance, but engineering solutions at the level of cavity and cryomodule design are available to suppress them?
  The presence of the two abovementioned loss mechanisms makes it nearly impossible to compare coating recipes on real cavities?
  Both bulk machined and hydroformed substrates (1.3GHz) gave good results in some cases, but failed in others: how can we achieve a perfectly reproducible copper surface prior to coating? Are the existing facilities adapted or what kind of equipment/tool would be needed?

## Slide 2
Latest Advances in Nb Thin Film Technology
Detailed questions, model dependent:
Do we know all types of substrate defects which are relevant to the RF performance and hence need to be avoided?
Hydrogen and nanohydrides: what are the differences with bulk Nb, what are the possible diagnostic tools and cures?
N doping and other thermal treatments, which push the Nb away from the clean limit, trigger a frequency dependent anti Q slope: is there a hope that we can enter in this regime from the “dirty limit” side of thin films?
To what extent can low-temperature baking in vacuum or mild nitrogen environments mitigate the high-field Q-slope in Nb thin films without triggering significant oxygen/copper interdiffusion?
How does the film morphological transition zone (Thornton model Zone T vs. Zone 2) correlate with RF critical fields and local electronic transport across inter-columnar boundaries?
What specific ion energy window during biased HiPIMS best suppresses intra-grain defect formation while avoiding compressive stress accumulation and argon gas entrapment?
What specific window of initial ion nucleation energy and growth bias in ECR and HiPIMS minimizes the facet slope angle below critical thresholds across all copper substrate crystallographic orientations?
What other microstructural features dominate the higher sensitivity of Nb/Cu films to trapped ambient magnetic flux compared to bulk Nb, and how does directional cooldown affect flux expulsion in thin films?
How do the localized density of states and Dynes sub-gap parameters measured by point-contact or scanning tunneling spectroscopy differ between bulk niobium and state-of-the-art energetic Nb coatings?