## Slide 1: Ultra-pure electroforming at Boulby deep underground laboratory
K. Johnson, P. Knights, K. Nikolopoulos, G. Rogers, P. Scovell,
E. Shoemark-Banks, D. Spathara, C. Toth, P. Walters
LRT – University of York & Boulby Underground Laboratory
24/09/2026

## Slide 2
Direct dark matter detection landscape

## Slide 3
Direct dark matter detection landscape
Increase exposure
Lower backgrounds

## Slide 4: Setup
Copper as a detector material
Copper is an attractive detector material for rare event searches
  No long-lived radio-isotopes – longest 67Cu: t1/2 = 62 h
  Commercially available at high-purity
  Good mechanical and electrical properties
  Favourable electrochemical properties – more on this later!
CUORE collaboration
https://cuoreexperiment.org
NEWS-G collaboration
https://www.snolab.ca/experiment/news-g/

## Slide 5: Setup
Copper background
Copper can still represent an important background
Commercial copper contaminated - 238U and 232Th decay chains:
  Natural ore contamination
  Implanted during manufacture and handling
  Cosmogenic activation - 63Cu(n,⍺)60Co t1/2 = 5.27 yr
Simulated backgrounds for NEWS-G’s current detector
238U decay chain

## Slide 6: Setup
Electrodeposition
Deposit ions onto a cathode by applying a voltage
Governed by oxidation and reduction reactions
Deposited mass proportional to current
Molar mass
Current
No. e-
Faraday constant
Ion

## Slide 7
Species plating tendency governed by reduction potentials
Careful control of applied potential difference allows preferential plating of copper over contaminants
Used in industry to produce copper with excellent purity
Copper electrodeposition
I

## Slide 8
Ultra-pure copper electrodeposition
How this differs from industry – prioritise purity
Cu feedstock preparation
Procedure principally developed by PNNL for Majorana Demonstrator
Additive free pure electrolyte
Prioritise purity over speed -> careful voltage selection
Cleanroom environment
Stringent radiopure material and reagent selection
Purity monitoring
Comprehensive cleaning procedures
Plating underground -> reduce cosmogenic activation
NIMA 579 (2007) 486-489
RCTR 277 (2008) 103-110

## Slide 9
Results – ICPMS
Sample of copper | 232Th [uBq/kg] | 238U [uBq/kg]
Commercial C10100 NIMA 828 (2016) 22-36 | 8.7 ± 1.6 | 27.9 ± 1.9
NEWS-G plated copper NIMA 988 (2021) 164844 | <0.24 | <0.11
Majorana demonstrator electroformed NIMA 828 (2016) 22-36 | <0.119 | <0.099
Orders of magnitude improvement over commercial copper
Purity results often limited by available assay techniques -> can only set limits

## Slide 10
How this is/can be used for experiments
Electroplating
Electroforming
Cu plated onto existing structure or components
Acts as an ultra-pure shield
Reduce radon emanation
Cu plated onto a mould (called mandrel)
Remove the mandrel leaving a pure copper structure
Construct large structures
NEWS-G electroplated Cu
NIMA 988 (2021) 164844
Majorana Demonstrator
Electroformed Cu
OSTI (2012) 1039850

## Slide 11: Setup
Electroforming facility at Boulby
1.1km underground at the UK’s deep underground laboratory Boulby
Dedicated ISO-6 cleanrooms within the larger Boulby cleanroom equipped with laminar flow, particle counter, type-1 water
XIA UltraLow-1800 + ICP-MS + HPGe on site at Boulby
Boulby underground lab
https://www.boulby.stfc.ac.uk/Pages/home.aspx
Front. Phys. 2023 11:1310146
JINST 2025 20 P06010
See posters on Boulby assay:
🪧A. Hammer
🪧 B. Green
🪧 K. Johnson

## Slide 12
0.2 µm recirculating filters
Steel cylindrical mandrel
5.5N Cu feedstock
Cu bus bar
Inlets
CuSO4 electrolyte
Electroforming bath at Boulby
Ti anodes
Pure PP/PVDF pipework leached with 6M nitric acid
Electrolyte made in house from 5.5N copper feedstock etched with acidified peroxide
Multiple setups for different geometries and sizes
Larger setup’s first goal to fully electroform a 30 cm spherical proportional counter underground: DarkSPHERE-30
Electroforming facility at Boulby
Near-future plans

## Slide 13: Setup
Copper pulse plated onto stainless ⌀30 cm stainless steel cylinder
Peeled copper off mandrel -> ICPMS and XIA results pending analysis
Recently transitioned to reverse pulse plating – better throwing power & purity
Exploring nitrogen cover gas and storage
Current status

## Slide 14
Phys. Rev. D 108, 112006
O(
)
Physics Potential
Fully electroformed spherical proportional counters will have world leading sensitivity to low-mass dark matter
DarkSPHERE-30 to begin construction
Alloys being explored to improve the properties of electroformed copper – PureAlloys and PureCuAlloys projects
  NIMA 1082 (2026) 170970
  Communications Physics (2025) 8 464
  arXiv:2059.07406
  arXiv:2606.24524
See talk on Cu alloys:
👩‍🏫 D. Spathara

## Slide 15
Summary
Copper electroforming for radio-pure detectors
Orders of magnitude improvement in radiopurity over commercial Cu
Electroforming facility constructed at Boulby
First copper produced
Work ongoing to electroform a ⌀30 cm SPC
Many experiments exploring the use of electroformed and plated Cu