## Slide 1
R. Robson, S. Kitagawa, and O. M. Yaghi
Mark Warren Senior Beamline Scientist, i19, DLS
mark.warren@diamond.ac.uk
Chemistry Noble
Prize 2025
Pioneering Development of
Metal–Organic Frameworks (MOFs)

## Slide 2
MOFs
Future Material
In the 1980s, if I told I wanted a material that could:
Pull clean drinking water out of desert air
Capture carbon dioxide like an ultra-porous sponge
Offer catalytic surface area so large that 1g equals a football field
Deliver drugs precisely to where the body needs them
Separate gases with molecular-level selectivity
Store hydrogen or methane efficiently for clean energy
Detect chemicals, pollutants, or explosives with high sensitivity
Desalinate water
But today, all these applications exist, and they fall under a single class of materials: Metal–Organic Frameworks (MOFs)
Notes: But within 40 years this has happened

## Slide 3
MOFs
2025 Chemistry Nobel Prize
Prof. Richard Robson
University of Melbourne Australia
Conception
Prof. Susumu Kitagawa
Kyoto University
Japan
Application
Prof. Omar M. Yaghi
University of California,
Berkeley, USA
Streamline

## Slide 4
Prof. Richard Robson
University of Melbourne
Richard Robson
CONCEPTION
109.5º
1.54Å
Tetrahedral geometry
Carbon
Extremely hard
Thermal conductivity High refractive index Chemical resistance
Diamond
Notes: Late 1980’s
Richard Robson was inspired by the structure of Diamond Every carbon atom is linked to four others
Tetrahedral geometry

## Slide 5
4,4,4,4,-tetracyano-tetraphenyl-methane
109.5º
8.86Å
Tetrahedral geometry
nitrile
tetraphenyl-methane
Prof. Richard Robson
University of Melbourne
Richard Robson
CONCEPTION
Notes: In collaboration with Bernard Hoskins
Rather than carbon, he used a tetrahedral geometry organic molecule (4′,4″,4''',4''''-tetracyano-tetraphenyl-methane)
Tetraphenylmethane with a nitrile group at the tips of each phenyl

## Slide 6
109.5º
8.86Å
Tetrahedral geometry
Organic linker
Copper
metal node
Prof. Richard Robson
University of Melbourne
Richard Robson
CONCEPTION
Notes: This is a orgainic compound that is attracted to copper ions.
Self assemble
When the substances were combined, they formed an ordered and very spacious crystal.

## Slide 7
Tetrahedral geometry
Prof. Richard Robson
University of Melbourne
Richard Robson
CONCEPTION
Notes: Late 1980’s 4′,4″,4''',4''''-tetracyano-tetraphenyl-methane
Richard Robson was inspired by the structure of diamond, in which every carbon atom is linked to four others in a pyramid-like shape. Rather than carbon, he used copper ions and a molecule with four arms, each with a nitrile at the end. This is a chemical compound that is attracted to copper ions. When the substances were combined, they formed an ordered and very spacious crystal. ©Johan Jarnestad/The Royal Swedish Academy of Sciences

## Slide 8
Prof. Richard Robson
University of Melbourne
Richard Robson
CONCEPTION
Notes: In the same way at the carbon in diamond,
Each copper metal node can coordinate to four other linkers forming a 3D lattice

## Slide 9
voids
Prof. Richard Robson
University of Melbourne
Richard Robson
CONCEPTION
Notes: Remarkable these contain channels void space and channels running through the crystals
These voids give MOFS a huge internal surface area
This was the metal organic framework
However at this time these were too fragile

## Slide 10
Current MOFs were too fragile to be in real life application
Introduced flexible organic frameworks Kitagawa showed that frameworks can also be stable, porous, and functional
Introducing the concept of porosity paving the way for MOFs in gas storage, CO2 capture, water purification and gas sensors
Susumu Kitagawa
Application
Prof. Susumu Kitagawa
Kyoto University, Japan
4-4-bipyridine (bpy)
Notes: Porous Coordination Polymers (PCPs) 1997 flexible frameworks
“soft porous crystals” — MOFs whose frameworks are flexible or responsive (structurally, chemically or physically).
introducing the concept of porosity to coordination polymers
paved the way for MOFs in gas storage (hydrogen, methane), CO2 capture, water purification, and gas sensors.

## Slide 11
Susumu Kitagawa
Application
Prof. Susumu Kitagawa
Kyoto University, Japan
4-4-bipyridine (bpy)
Notes: Porous Coordination Polymers (PCPs) introducing the concept of porosity to coordination polymers
paved the way for MOFs in gas storage (hydrogen, methane), CO2 capture, water purification, and gas sensors.
https://onlinelibrary.wiley.com/doi/epdf/10.1002/anie.199717251

## Slide 12
Susumu Kitagawa
Application
Prof. Susumu Kitagawa
Kyoto University, Japan
Notes: Porous Coordination Polymers (PCPs) introducing the concept of porosity to coordination polymers
paved the way for MOFs in gas storage (hydrogen, methane), CO2 capture, water purification, and gas sensors.
https://onlinelibrary.wiley.com/doi/epdf/10.1002/anie.199717251

## Slide 13
Susumu Kitagawa
Application
Prof. Susumu Kitagawa
Kyoto University, Japan
Demonstrated for the first time that MOFs can permanently maintain porosity and adsorb gases reversibly
Notes: Porous Coordination Polymers (PCPs) introducing the concept of porosity to coordination polymers
paved the way for MOFs in gas storage (hydrogen, methane), CO2 capture, water purification, and gas sensors.
Able to absorb gas molecules and release them without falling apart. https://onlinelibrary.wiley.com/doi/epdf/10.1002/anie.199717251

## Slide 14
Omar Yaghi
Streamline
Prof. Omar M. Yaghi
University of California, Berkeley, USA
O
O
-O
O-
dicarboxylic acid – organic linkers
Notes: Omar Haghi has an idea – can you make frameworks true customisable
Predictable crystalline structure - Grown up lego for the chemist
Linkers made of carboxylate groups or di-carboxylate

## Slide 15
Omar Yaghi
Streamline
Prof. Omar M. Yaghi
University of California, Berkeley, USA
O
O
-O
O-
1-4,dicarboxylic acid – organic linkers
Metal paddlewheels
MOF5
Notes: ZnO4 clusters
Paddle wheel – nodes
Combined with the dicarboxylic organic linkers
Yaghi coined the term ‘metal–organic framework’
Fantastic stability

## Slide 16
Omar Yaghi
Streamline
Prof. Omar M. Yaghi
University of California, Berkeley, USA
O. M. Yaghi, M. O’Keeffe, N. W. Ockwig, H. K. Chae, M. Eddaoudi and J. Kim, Nature, 2003, 423, 705–714
O
O
-O
O-
O
O
-O
O-
NH2
O
O-
O
-O
O
O-
O
-O
Notes: Able to adapt the linker to suit
16 types all with different properties
Different nano sized pours
Made customizable material to suit the requirements of the application
Opened up the field

## Slide 17
MOF
Properties
Image from: A. Aldhaher et al. Hybrid Advances 5 (2024) 100131
Change the metal node
Tune electronic properties - redox behaviour, charge distribution, binding strength
Change the functional groups on the linker
Control gas affinity & selectivity
Change the linker length or geometry
Adjust pore size and shape – diffusion rates, storage capacity, and gas accessibility
Instead of synthesizing a material and then discovering its properties, we can design a MOF with the exact features needed for a specific application
Notes: Change the metal – change the electronic
Change the functional groups – attraction to gas molecule and selectivity properties
Change the linker size – change the pour size
This means that we don’t synthesis framework and find out the properties,
We design the MOF to suit the application needs.

## Slide 18
Omar Yaghi
Streamline
Image from:
L. Glasby et. al. Chem. Mater. 2024, 36, 19, 9013–9030
Notes: Over 120 000 MOF in the Cambridge Structural Database

## Slide 19
MOFs
2025 Chemistry Nobel Prize
Prof. Richard Robson
University of Melbourne Australia
Conception
Prof. Susumu Kitagawa
Kyoto University
Japan
Application
Prof. Omar M. Yaghi
University of California,
Berkeley, USA
Streamline
Notes: These three scientist amongst other have pioneered a new area of chemistry
Majority of chemistry and material university departments have some who specialises in framework research

## Slide 20
Co(bpy)1.5(NO3)2
4-4-bipyridine (bpy)
nitrate
Susumu Kitagawa
i19
Gas Experiments

## Slide 21
Solvated
Vacuum
10 bar CO2
Chart: Electron in pore (platon squeeze)
| gs_100 | gs_101 | gs_102_r1-4 | gs_102_r5-8 | gs_103 | gs_104 | gs_105
 | 128 | 20 | 16 | 15 | 19 | 190 | 187
i19
Gas Experiments

## Slide 22
EH2:
Serial
GAS cELL
vac start
0.5 bar
1.0 bar
a)
400 wells x 64
25,600 welled chip
flexible framework
In collaboration with Josh Smith, Robin Owen, Anna Warren and Lee Brammer
Notes: Serial work is also making a big impact on in-situ experiments
With Josh, a joint diamond PhD student, we have developed serial gas cell used to study SHF-61 which is a flexible framework
Pours in the framework is able to contract to expand as solvent or gas is added or removed
Using the still image approach - Batch analysis 25,000 crystals - as a function of CO2 pressure
Can see the distribution of change of unit cells upon update which is affected by crystal size and defects within the crystal
This cell has it limitation in pressure and collection routine

## Slide 23
flexible framework 1
flexible framework 2
EH2:
Serial
GAS cELL
In collaboration with Josh Smith, Anna Warren, Robin Owen and Lee Brammer
Notes: 800 wells polymer grid in typical gas cell, able to go high vacuum to 40 bars
Able utilise small rotation serial methods
Able to obtain beautiful structure at pressure point.
As a comparison in the related system, we can see a much large spread as a function for pressure.
Really show that doing a gas cell experiment on single crystal sample may not be representation

## Slide 24
Notes: Nature chemistry 2017

## Slide 25
NO
activation
Notes: NO is toxic
biologically active molecule, anti-thrombotic, wound healing
and anti-microbial properties
Glucose monitor needles
Russel has used this in a MOF within a

## Slide 26
Chemistry Noble Prize 2025
Summary
MOFs and the 2025 Nobel Prize
  Prof. Richard Robson – Conception
  Prof. Susumu Kitagawa – Application
  Prof. Omar M. Yaghi – Streamlining
Why MOFs Matter:
  Ultra-porous materials enabling:
    Water harvesting from air
    CO₂ capture and gas separation
    Drug delivery and catalysis
    Hydrogen/methane storage for clean energy
    Chemical sensing and desalination
Origins:
  Inspired by diamond’s tetrahedral geometry
  Developed using organic linkers and metal nodes
Impact:
  Revolutionised material science with modular, tuneable frameworks