## Slide 1: Neutron diffraction applications
Tom Wood
Webinar: Materials studies for clean energy: how neutron and muon techniques can help
12th February 2026

## Slide 2
What is neutron diffraction?
The principle is exactly the same as X-ray diffraction, but run slightly differently
Sample
Radiation (n or hν)
Image from Physics LibreTexts
Differences are:
Neutrons scatter differently to X-rays
ISIS operates on time-of-flight
  ToF directly proportional to d-spacing
  Not so constrained by angle

## Slide 3
Neutrons scatter differently to X-rays
An example from battery materials: a straightforward measurement
Na2/3Mn2/3Ni1/3O2
Images courtesy of Dr Andy Bridger

## Slide 4
Neutrons are penetrating
Which means we can use complex sample environment
Ammonia decomposition catalysts in-situ
Images taken from:
Phys. Chem. Chem. Phys. 2018, 20, 22689.
Faraday Discuss. 2016, 188, 525
ron.smith@stfc.ac.uk

## Slide 5
Neutrons are penetrating
Iron nitriding in situ

## Slide 6
Neutrons are penetrating
Fe4N
Fe
Iron nitriding in situ

## Slide 7
SANS: looking at larger spacings
Small angles equals larger distances (1 to 100 nm)
Sample
Radiation (n or hν)

## Slide 8
SANS: looking at larger spacings
Hard carbon anodes for sodium batteries
Measurements on an in operando sodium half-cell.
gabriel.perez@stfc.ac.uk
https://doi.org/10.1039/D3TA04739C

## Slide 9
Non-exhaustive list of other energy areas
Solar cell materials
J. Phys. Chem. C 2019, 123, 14934
Solid oxide fuel cells
Nat. Energy 2017, 2, 16214
In operando pouch cells
From: “Advancing Battery Diagnostics through Operando Neutron Diffraction of Unmodified Non-deuterated Li-ion Single-layer Pouch Cells
Electrolyte structure
EES Batteries 2025, 1, 1797

## Slide 10
Addendum: A quick mention of reflectometry (not diffraction)
Organic electrode structures
ACS Appl. Mater. Interfaces 2019, 11, 13803
Image from Physics LibreTexts
Hydrogen sensors
ACS Appl. Mater. Interfaces 2023, 15, 8033