## Slide 1: Neutron Imaging and Engineering Diffraction
Sylvia Britto
Instrument Scientist, IMAT
Webinar: Material Studies for Clean Energy
12th Feb, 2026

## Slide 2
Spatial resolution
60 μm (3D)
120 μm (Bragg edge)
Flux (max)
4*107 n/cm2/s
Max Field of View
20 x 20 cm2
3 x 3 cm2 (Bragg edge)
Radiography (2D imaging)
Tomography (3D imaging)
2 - <10 hours
TOF (Bragg edge) imaging
Δ/ ~0.6 at 4Å
Diffraction
Neutron Imaging and Diffraction on IMAT
Imaging camera
Sample stack
Diffraction detectors
beam

## Slide 3
Sample
L1
Neutron Imaging
Detector
Neutron pulses (e.g. 10 Hz)
polychromatic
“white” beam
Neutron Imaging
Total cross section: )
Transmission
Attenuation coeff. 
rotation

## Slide 4
Recording the 3D image:
Collect projections: #projections = #pixel * π / 2.
Apply normalisation (flat field; dark field); filters; determine centre of rotation;
Reconstruct slices using: filtered back projection or iterative algorithms
4) Visualization and analysis tools ImageJ / Avizo / VGStudio / etc
White beam tomography
rotation
Chadwick’s neutron chamber replica

## Slide 5
A pulsed neutron source enables effective Time of Flight techniques, i.e. determination of neutron energies.
v = = h/(m*)
Energy-resolved neutron radiography on IMAT
3000 energy slices
10 Hz
sample
Detector at 57 m

## Slide 6: What’s in a pixel?
l
Bragg edges show crystal structure – how those atoms are arranged
Resonance peaks show which atoms/isotopes present
Wavelength, TOF
intensity
Height → Texture
Height → Concentration
Width → Temperature
Position → Strain
l
) ()
l
Energy-dispersive (TOF) imaging /Bragg Edge Mapping
Start
Max Field of
View
3 x 3 cm2

## Slide 7
Bragg Peaks
Bragg Edges
Diffraction / transmission analysis:
positions → residual strains
heights → phase composition
rel. heights → texture
widths → microstrain/particle size
d-spacing
Spatially resolved Diffraction/transmission analysis

## Slide 8
Clean Energy Applications of Neutron Imaging
Energy storage
Fuel Cells and Batteries
Cultural Heritage
Neutron Imaging in Life Sciences

## Slide 9
https://www.iter.org/machine/
Assessing manufacturing quality of components: Fusion divertor tungsten monoblock
T. Minniti et al, Nucl. Fusion 65, 2025, 026041
Neutron imaging useful to non-destructively characterize defects and voids in dense plasma facing components
in nuclear fusion reactors.

## Slide 10
L. L. Evans et al, Fusion Energy and Design, 134, 2018, 97-108
Assessing manufacturing quality of fusion divertor tungsten monoblock
X-ray Tomography
Neutron Tomography

## Slide 11
T. Minniti et al, Nucl. Fusion 65, 2025, 026041
Assessing manufacturing quality of fusion divertor tungsten monoblock
Strain map derived from Bragg edge imaging

## Slide 12
Hydrogen embrittlement
Review of Hydrogen Embrittlement in Metals: Hydrogen Diffusion, Hydrogen Characterization, Hydrogen Embrittlement Mechanism
and Prevention, X. Li et al, Acta Metallurgica Sinica, 33, 2020, 759-773.
Can cause catastrophic mechanical failure in H carrying pipelines, high pressure storage tanks, refuelling stations
San Francisco Bay Bridge, 2013
Neutron imaging useful to non-destructively quantify spatial distribution of hydrogen in engineering alloys.

## Slide 13
Hydrogen embrittlement in alloys
N. L. Buitrago et al, J. Nucl. Mater. 503, 2018, 98-109
Standards containing known amounts of H are used to calculate attenuation coefficients.
From this H content in unknown samples can be determined.

## Slide 14
LS14250 - Saft
Li metal / thionyl
positive tab
Li anode
SOCl2
cathode
SO2 gas
reservoir
15mm
R. F. Ziesche, J. B. Robinson, M. D. R. Kok, H. Markotter, W. Kockelmann, N. Kardjilov, I. Manke, D. J. L. Brett and P. R. Shearing, 4D Neutron and X-ray Tomography Studies of High Energy Density Primary Batteries: Part 1. Dynamic Studies of LiSOCl2 during Discharge, J. Electrochem. Soc. 167, 130545, 2020.
Lithium diffusion in Li/SOCl2 batteries
< … discharging … >
15mm
R. Ziesche, J. Electrochem. Soc. 167 (2020)
Energy Storage: Li Diffusion in Li/SOCl2 batteries
R. F. Zeische et al, J. Electrochem. Soc. 167, 2020, 130545
Neutron imaging can be used to visualize lithium ion diffusion and dynamics in Li-ion batteries.

## Slide 15: Isotope Selectivity

## Slide 16
R. Bradbury et al, Adv. Funct. Mater. 33, 2023, 2302619
Visualizing Lithium ion transport in solid state Li-S batteries
@NeXT, ILL

## Slide 17: Neutron Imaging of Fuel Cells
S. Zhou et al, Cell Reports Physical Science, 5, 2024, 102208
Neutron imaging can be used to study water management in operating fuel cells.

## Slide 18
Thank you
IMAT Contacts
Sylvia Britto sylvia.britto@stfc.ac.uk
Ranggi Ramadhan ranggi.ramadhan@stfc.ac.uk
Winfried Kockelmann winfried.kockelmann@stfc.ac.uk
Engin-X Contacts
Joe Kelleher joe.Kelleher@stfc.ac.uk
Tung-Lik Lee tung-lik.lee@stfc.ac.uk