## Slide 1
Muon applications
Peter Baker
ISIS Muon Group scientist
Notes: The abstract pattern can be removed or repositioned if required. Be careful to ‘Send to Back’ so that it does not obscure any important information.

## Slide 2: Two ways to use muons
Positive muons to study magnetic fields inside materials
Positive muons implanted into the sample
Spin polarization changes in response to static and dynamic magnetic fields
A bit like Nuclear Magnetic Resonance
Negative muons to study the elemental composition of materials
Negative muons implanted into the sample
X-rays emitted specific to the nucleus capturing each muon
A bit like X-Ray Fluorescence

## Slide 3: Ionic motion
Batteries, supercapacitors, hydrogen fuel cells and storage

## Slide 4: What information do you get from muons?

## Slide 5: Which ions can you study?
Nucleus | Moment | Abundance (%) | Chance of success | Ionic radius (pm)
1H | +4.84 | 99.9885 | Have to separate µ+, µ+e- and H+ motion | 0.0008 or 110
7Li | +4.20 | 92.41 | Excellent and well-studied | 90
19F | +2.63 | 100 | Not promising due to F-μ bonds | 119
23Na | +2.86 | 100 | Excellent and some existing work | 116
25Mg | -0.86 | 10.13 | Works but with a small signal | 86
27Al | +3.64 | 100 | Promising | 67.5
43Ca | -1.49 | 0.135 | Terrible unless enriched | 114
51V | +5.15 | 99.76 | Promising | 68-93
67Zn | +0.875 | 4.1 | Not promising | 88
127I | +2.81 | 100 | Excellent | 206
Also consider:
Do nuclei move faster than muons?
Is the environment magnetic too?
Does NMR work?
If not, why not?

## Slide 6: What information do you get from muons?
How often ions with a magnetic moment move past
  Measures the atomic-level ionic self diffusion rate
  Knowing pathways allows comparison with bulk diffusion
  Change with temperature is governed by energy barriers to motion
Field distributions inside the sample
  Probe of local structural changes – as distances between atoms change, so does the field distribution

## Slide 7: Ex-situ ion diffusion measurements – Li deficient NCA
Primary use of muons is to measure local ionic motion
  Works in paramagnetic materials
  Material doesn’t have to be in a cell
  Ion must have a nuclear magnetic moment, e.g. Li, Na, K, Mg, I
Measure the hopping rate as a function of temperature
  Extract energy barrier(s)
  Find hopping rate ~MHz and derive local diffusivity for available pathways
T.E. Ashton et al., J. Mater. Chem. A 2020, 8, 11545

## Slide 8: Li+ Diffusion in NMC811 during cycling
Changes in local structure
Li+ hopping rate
Li+ diffusion coefficient

## Slide 9: Chemical reactions
Catalysis, kinetics, supercritical water

## Slide 10
Positive muons can capture electrons to form a light hydrogen isotope: Muonium (Mu)
Mu can undergo the same reactions as a H-atom …
Muonium Chemistry
Addition: Mu + R2C=CH2 R2ĊCH2Mu
Abstraction: Mu + RX MuX + R·
Radical Combin.: Mu + ·OH MuOH
E- transfer: Mu + Xn+ µ+ + X(n-1)+

## Slide 11
Determine rate constants, kMu …
Change Benzene conc. and measure λTot
Determine kMu
From kMu …
2 – 3-fold catalytic effect from benzene on metal surface

## Slide 12: Semiconductors
Solar, power electronics, computing

## Slide 13: What muons can tell you about semiconductors
Generally studying muonium in the semiconductor
Hydrogen defect analogue
  Where it forms in the material
  What dynamics it experiences
Investigating paramagnetic centres
  e.g. NV centres in diamond
Charge carrier dynamics
  Thermal effects
  Light induced effects

## Slide 14: Charge carrier kinetics in semiconductors
Carrier-Mu interaction depolarises muon signal
  Relaxation rate tells carrier density
HIFI Laser for optically generating carriers in semiconductors
General-purpose setup for light-pump muon-probe experiments
By changing the pulse delay, one can measure carrier lifetime spectrum
  Even in completed solar cells
Depth-dependent measurements enable carrier kinetics study within a wafer
Applicable to many semiconductors. So far: Si, Ge, SiC, GaAs
Review of Scientific Instruments 87, 125111 (2016).
Phys. Rev. Lett. 119, 226601 (2017).
Appl. Phys. Lett. 115, 112101 (2019).
Appl. Phys. Lett. 118, 252105 (2021).
Journal of Applied Physics 132, 065704 (2022).
Journal of Applied Physics 136, 055707 (2024).

## Slide 15: Elemental composition
Batteries, fertilizers, cultural heritage

## Slide 16: How negative muons determine elemental composition
High Energy X-rays emitted – XRF turbocharged
Energy depends on the atom which captures the muon
0.1-10MeV – mass of the muon is 200x that of the electron so higher energy
Can measure as a function of depth up to ~ 1cm
Proof of concept imaging studies in progress

## Slide 17: Li plating on graphite anodes
Negative muon study of a pouch cell
Can use muon beam energy to tune the layer that the muons stop in
Atomic Coulomb capture from metallic Li ~50x more than for atomic Li
Very sensitive to Li plating
I. Umegaki et al., Anal. Chem. 2020, 92, 8194

## Slide 18
E. Querel et al., J. Mater. Chem. A, 2025, 13, 2275
Composition within pouch cells

## Slide 19: Elemental analysis of ‘kryptonite’
Jadarite (LiNaSiB3O7(OH)) – (Fluorine deficient) Kryptonite!
Potential Li and B ore
Only 1 known reserve
Formation and structure poorly understood
Measurements use energy-sensitive Ge detectors
Fit peaks to determine amplitudes and positions to give the Measured wt%
Correct for muon capture probably for different elements determined using standards to give the Actual wt%
Technique is effective in determining the composition of Li-containing ores
20 mm
Synthetic
Natural
M. Rhodes et al., in preparation

## Slide 20: Green fertilizer composition
Compare batches of fertilizer derived from waste materials to commercial reference materials
Understand consequences of variable feedstock on composition as a function of depth within pellets at different moisture contents
Non-destructive depth-dependence capability allows pellets to be studied in a representative form
Dry pellet
Swollen pellet -> Dry pellet exposed to moisture

## Slide 21: Conclusions
Muons are used across a wide range of clean energy materials
  Ionic motion in battery and fuel cell materials from ex-situ to in-operando
  Reaction kinetics in catalysts
  Charge carrier dynamics and defects in semiconductors
  Non-destructive elemental composition beneath the surface
Muons also used extensively in magnetism and superconductivity
  Materials for quantum technologies
  Superconductors for quantum technologies and fusion applications
Please get in touch if you think muons might be helpful for understanding materials you’re working on
Review articles –
  I. McClelland et al., Annu. Rev. Mater. Res: https://doi.org/10.1146/annurev-matsci-110519-110507
  G.E. Pérez et al., J. Mater. Chem. A: https://doi.org/10.1039/D2TA07235A
isis_energy_cleangrowth@stfc.ac.uk