## Slide 2: HI-ECN3 RP Aspects
C. Ahdida, O. Pinto, J. Coleman-Smith, P. Vojtyla, H. Vincke
CERN & ISIS collaboration workshop
01-02 June 2026

## Slide 3
BDF/SHiP design optimization
ALARA approach Optimization required to ensure that exposure of personnel to radiation and radiological impact on environment are As Low As Reasonably Achievable
HI-ECN3 design optimization addresses all relevant radiological aspects of the facility covering its full life-cycle
RP studies are based on FLUKA MC studies
All studies will be summarized in the upcoming Technical Design Report
Few selected topics discussed today
Wide range of RP studies

## Slide 4
Target Studies
Prototype Targets
Service Building Considerations
Tritium Diffusion Studies
Outline

## Slide 5
Target Studies

## Slide 6
BDF Target Assembly FLUKA Model
19 W blocks (L144 cm, D25 cm, 19.3 g/cm3, 1.3 tons)
With 1.5 mm Ta cladding
171.25 cm
Tungsten
Tantalum
Inconel, 0.01% Co
Helium (only present during irradiation)
SS, 0.01% Co
25 cm
SS table
Inconel vessel
Inconel holder
Target Assembly materials
The interaction length of the target amounts to 16 λ
ST1A07710 Design
PRELIMINARY

## Slide 7
Residual Dose Rates – 1 month
PRELIMINARY STUDY
Residual dose rates of target assembly
1 month of cool-down
Top view
Cross-sectional view
The spent target will be remotely transferred into a shielded cask
The target will be stored in a dedicated intermediate storage zone in TCC8 for cooldown, prior to transport and waste packaging for disposal
Residual dose rates of target reach ~100 Sv/h at contact to the target vessel
Target area
Spent target intermediate storage area
Target & beam dump

## Slide 8
Residual Dose Rates of Target Assembly
PRELIMINARY STUDY
x
y
z
Residual dose rates of target assembly, no shielding
Various cool-down times
<x,y> [-20;20] cm
<z> [100] cm
Max. DR (mSv/h) at 3 m
Max. DR (mSv/h) at 3 m (top)
Max. DR (mSv/h) at 3 m (upstream)
No safety factor included here, statistical errors
Dose rates are < 10 mSv/h at 3 m for ≥ 5 years of cooling
Statistical uncertainties in parentheses

## Slide 9
Radionuclide Inventory of Target Assembly
LL: Clearance limit for specific activity in Bq/g
LA: Value corresponding to the absolute activity level in Bq of a material above which handling of this material is subject to mandatory licensing
CA: Guidance value for chronic occupational exposure to airborne activity in Bq/m3
PRELIMINARY STUDY
Radionuclide inventory per target assembly region
10 years of cool-down
The greatest statistical uncertainty is <1.4%
The tungsten blocks dominate the overall radionuclide inventory, amounting to a total of 4.5E8 LA
In terms of specific activity, the tantalum cladding is the main contributor
The highest activity concentrations are found approximately within the first third of the target

## Slide 10
Main Contributors to LL and LA
The total H-3 content in the target assembly amounts to 14.74 ± 0.01 Bq
In terms of alpha emitters, the most dominant radionuclide is Gd-148 (74.6 years half-life) with a total of 98.47 ± 0.29 GBq after 10 years. Other alpha-emitters amount to 5.34 ± 0.01 MBq
Comparison to transport classification limits, showing that a transport under LSA-II classification is possible for 5 years of cooling (IP2 certified container
PRELIMINARY STUDY
Main contributors to LL
10 years of cool-down
Main contributors to LA
10 years of cool-down
Statistical uncertainties are below 1.4%

## Slide 11
Preliminary Packaging Proposal
4.2 cm
4.2 cm
Assumed shielding configuration
Including:
KC-T12 container with 12 cm concrete on all sides
Min. 5 cm concrete filling on all sides except the bottom
Additional lead shielding for top and bottom
Additional iron shielding for sides
The waste assembly is defined as the target assembly plus the lead/iron mold
Further filling of free space with sand but excluded for simulations (conservative)
Target length limited to 155 cm
Upstream target side
Bottom target side

## Slide 12
Residual Dose Rates of KC-T12 Package
PRELIMINARY STUDY
x
y
z
Residual dose rates of KC-T12 package, with safety factor 3
Various cool-down times
<x,y> [-20;20] cm
<z> [100] cm
2 mSv/h
0.1 mSv/h
2 mSv/h
0.1 mSv/h
2 mSv/h
0.1 mSv/h
Max. DR (mSv/h) for 10 yrs cooling
Contact: 0.55 (0.03) mSv/h
2 m: 0.05 (0.01) mSv/h
Safety factor 3; stat. errors
Well within 2 mSv/h at contact and 0.1 mSv/h at 2 m (≥10 yrs)
Max. DR (mSv/h) for 10 yrs cooling (top)
Contact: 0.27 (0.02)mSv/h
2 m: 0.03 (0.01) mSv/h
Max. DR (mSv/h) for 10 yrs cooling (downstream)
Contact: 0.73 (0.04) mSv/h
2 m: 0.06 (0.01) mSv/h
Statistical uncertainties in parentheses
Max. DR (mSv/h) for 5 yrs cooling
Contact: 1.11 (0.06) mSv/h
2 m: 0.09 (0.02) mSv/h
Max. DR (mSv/h) for 5 yrs cooling (top)
Contact: 0.54 (0.04)mSv/h
2 m: 0.06 (0.02) mSv/h
Max. DR (mSv/h) for 5 yrs cooling (downstream)
Contact: 1.42 (0.07) mSv/h
2 m: 0.11 (0.02) mSv/h

## Slide 13
Service Building Considerations

## Slide 14
Service Building 754
Service Cell
CV rooms
Handling hall + Buffer area
Hotcell
754
CERN fence
CERN Prévessin site
  CV rooms for He-cooling system of BDF target with filters* and ventilation system of B754 and target area
  Handling hall + buffer area for equipment transfer via airlock zone to service cell, temporary storage
  Service cell for safe packaging and disposal of radioactive equipment (e.g. BDF target), as mandated by host state authorities
B911
Material airlock
Personnel airlock
Telemanipulator area
29.01.2026
EDMS 3406737
*HEPA filters and heat exchanger in underground target area
Claudia AHDIDA et al. HI-ECN3 RP Aspects
14

## Slide 15
Contamination risks during Target Cutting
Cutting process still to be defined in detail, ; current assumption: four cuts, each 1 cm thick
  22 kg of StainlessSteel holder
  3.5 kg of Inconel vessel
Radionuclide inventory of SS holder and Inconel evaluated based on FLUKA + ActiWiz studies
  Assumed Service Cell dimensions:
  Internal surface: 1.3E6 cm2
  Volume: 1.2E9 cm3
Total LA: | 6.0E+05
Total CS: | 3.3E+04
Total CA: | 3.0E+05
Total beta/gamma SurfAct, Bq/cm2: | 1.1E+06
no alpha emitters
Sum of SS316LN holder + Inconel vessel
Inconel vessel only
Most contributing radionuclides: Co-60, Fe-55, Mn-54, Co-58, Sc-46
Resuspended activity in comparison to Swiss Licensing (LA), Surface Contamination (CS) and Air Activity Concentration (CA) Limits, 6 months cool-down*
CS: Guidance value for surface contamination
CA: Guidance value for chronic occupational exposure to airborne activity. Same as Derived Air Concentration (DAC) in ISO17873 norm
LA: Value corresponding to the absolute activity level of a material above which handling of this material is subject to mandatory licensing
Total LA: | 3.9E+05
Total CS: | 1.8E+04
Total CA: | 1.9E+05
Total beta/gamma SurfAct, Bq/cm2: | 9.9E+05
Inconel vessel
SS316LN holder
Neglecting potential contamination of BDF target (W, Ta)
→ Type A work sector classification needed (> 10’000 LA)
29.01.2026
EDMS 3406737
Claudia AHDIDA et al. HI-ECN3 RP Aspects
15

## Slide 16
Radiological Classification of B754
Work sector | Maximum Activity
Normal | LA
Type C | 1E+02 LA
Type B | 1E+04 LA
Type A | Depending on authorization
Resuspended activity for BDF target container cutting of ~6×105 LA
Class A working areas will in addition have a Controlled Radiation Area classification with contamination risk (Limited Stay or High Radiation Area, or temporarily even be a Prohibited Area)
A
Simple Controlled or Limited Stay Radiation Area with Contamination Risk
Work sector classification
Area classification
B911
Supervised Radiation Area
*C. Ahdida, Revised HI-ECN3 service building area classification, EDMS 3237086 v.2
29.01.2026
EDMS 3406737
Claudia AHDIDA et al. HI-ECN3 RP Aspects
16

## Slide 17
ISO 17873 Classification
The proposed classification based on ISO 17873
Service Cell and hot cell with highest Containment Class 4 (ISO 17873)
Telemanipulator zone and laboratory inline with similar areas in ISOLDE / MEDICIS
Classes in-line with recommendations by external consultants
HEPA + charcoal filters
29.01.2026
EDMS 3406737
Claudia AHDIDA et al. HI-ECN3 RP Aspects
17

## Slide 18
2025 Prototype Targets – Contamination Measurements

## Slide 19
2025 Prototype Targets
 | Target 1 | Target 2
 | Integrated POT | Integrated POT
Day 1 (24/09/2025) | 1.6E+13 | -
Day 2 (01/10/2025) | - | 6.8E+13
Day 3 (29/10/2025) | 9.7E+12 | 2.5E+13
Total | 2.563E+13 | 9.326E+13
Test stand in TCC2
Irradiation conditions
Open target vessel after irradiation
Two BDF prototype targets were tests with beam in TCC2
The targets were surrounding by a static He environment with water cooling only for the outside of the target vessel
Contamination measurements were performed and analysed on 16.01.2026, 79 days after irradiation
Information from M. Parkin

## Slide 20
2025 Contamination Measurements
Contamination measurements were performed on all target blocks without any relevant detectable activity with a hand-held device
Two wipe tests were taken inside the target vessels with a surface area larger than100 cm2
The results reported from gamma spectroscopy are as follows:
All measured radionuclides can be produced in SS316LN vessel
CS: Guidance value for surface contamination
If the classification of the material to be transported is exempted, the contamination on the material shall remain below 0.4 Bq/cm² for beta/gamma emitters, and below 0.04 Bq/cm² for alpha emitters.
Target 1 vessel
Target 2 vessel
0.5 Bq → 0.005 Bq/cm2 (1.7E-3 CS)
12 Bq → 0.1 Bq/cm2 (5E-3 CS)
30.01.2026, 93 days cooling

## Slide 21
2026 Prototype Target – Contamination Measurements

## Slide 22
2026 Prototype Target
 | Integrated POT | Avg. intensity (p/s) | Hours of irradiation
Day 1 (10/03/2026) | 8.899E+13 |  | 
Day 2 (18/03/2026) | 9.59E+14 | 8.64E+10 | 3.08
Day 3 (08/04/2026) | 6.96E+14 | 1.93E+11 | 1.00
Day 4 (22/04/2026) | 8.89E+14 |  | 
Day 5 (06/05/2026) | 1.02E+15 | 8.68E+10 | 3.25
Day 6 (24/06/2026) | (planned) |  | 
2026 Prototype Target
Irradiation conditions (to date)
In 2026, a prototype target is actively cooled with helium (up to 16 bar, ~10 g/s He)
Skid technologies identical to final target
Tests ongoing with last irradiation planned for 24/06/2026
Removal of target during the Long Shutdown 3
He cooling skid
Information from M. Parkin

## Slide 23
Beam conditions
Day 2 (18/03)
2 time periods
Time start time end total POT
13:39 16:05 7.315 E+14
16:39 17:18 2.271E+14
Avg. intensity (p/s) 8.64E+10
Hours of irradiation 3.08
Day 3 (08/04)
3 time periods
Time start time end total POT
13:24 14:45 4.21278E+14
15:58 16:33 1.92952E+14
16:43 17:08 8.22499E+13
Day 5 (06/05)
2 time periods
Time start time end total POT
08:49 11:13 7.43843E+14
12:12 13:03 2.71876E+14
Avg. intensity (p/s) 8.68E+10
Hours of irradiation 3.25
Avg. intensity (p/s) 1.93E+11
Hours of irradiation 1

## Slide 24
2026 Contamination Measurements
Once 2026 beam operation finishes, contamination measurements will be performed on the target blocks and vessel as well as critical He cooling system elements (e.g. heat exchanger, HEPA filters)
Future checks for alpha contamination are also foreseen
Target tests are currently still ongoing, however three He-samples were taken shortly after beam operation for Days 2, 3 and 5
The He-samples were contained in a bottle and analyzed via gamma spec
Swagelok 304L-HDF4-400
Internal volume: 400 cm3 ± 5%
Min. wall thickness: 2.4 mm
Material: 304L
He cooling pressure: 13.1 bar
He cooling temperature: 23.5 C
He in cooling circuit: 149 mol, 0.6 kg (assuming 0.28 m3, 280 l)
He in bottle: 0.22 mol, 0.89 g (assuming 420 cm3) 0.15% of total He
Information from F. Dragoni

## Slide 25
He sample analysis – Day 2 and 3
CA: Guidance value for chronic occupational exposure to airborne activity. Exposure to an airborne activity concentration of 1 CA for 40 hours
LA: Value corresponding to the absolute activity level of a material above which handling of this material is subject to mandatory licensing
 |  |  |  |  |  | Decay + shielding attenuation1 corrected |  |  |  |  |  |  |  |  | 
 |  |  |  |  |  |  |  |  |  |  | Extrapolated to total He circuit |  |  |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  | Extrapolated to BDF2 + fully saturated3 |  | 
End of beam operation | Gamma spec. Started | Cooling t (h) | Isotope | Half-life (h) | Activity (Bq) | Activity (Bq) | CA* (Bq/m3) | Multiple of CA | LA (Bq) | Multiple of LA | Activity (Bq) | Multiple of LA | Activity (Bq) | Multiple of LA | Multiple of CA
18/03/2026 17:00 | 20/03/2026 10:34 | 41.3 | I-123 | 13.27 | 0.94 | 2.0E+01 | 8E+04 | 4.8E-02 | 5.0E+07 | 3.9E-07 | 1.3E+04 | 2.7E-04 | 5.8E+06 | 1.2E-01 | 3.1E+00
18/03/2026 17:00 | 20/03/2026 10:34 | 41.3 | Xe-125 | 16.9 | 2.32 | 2.4E+01 | 3E+05 | 1.6E-02 | 3.0E+08 | 8.1E-08 | 1.6E+04 | 5.5E-05 | 8.9E+06 | 3.0E-02 | 1.0E+00
08/04/2026 17:07 | 09/04/2026 09:08 | 16.0 | I-123 | 13.27 | 2.897 | 1.6E+01 | 8E+04 | 3.9E-02 | 5.0E+07 | 3.3E-07 | 1.1E+04 | 2.2E-04 | 6.2E+06 | 1.2E-01 | 1.1E+00
08/04/2026 17:07 | 09/04/2026 09:08 | 16.0 | Xe-125 | 16.9 | 4.081 | 1.5E+01 | 3E+05 | 9.8E-03 | 3.0E+08 | 5.0E-08 | 1.0E+04 | 3.4E-05 | 7.3E+06 | 2.4E-02 | 2.8E-01
*Under atmospheric pressure
Only the relatively short-lived radionuclides I-123 and Xe-125 were identified
Both radionuclides must have been produced in the target, either in the tantalum cladding or the tungsten core material of the target blocks
The measured activities are very low, well below Swiss airborne activity concentration and authorization limits, also when taking radioactive decay, attenuation within the sampling vessel and the total volume of the He cooling circuit into account
Extrapolation to future BDF beam intensity (4E13 p+ / 7.2 s) and radionuclide saturation, would result roughly in 6E6 Bq of I-123 and ~ 9E6 Bq of Xe-125 in the total circuit, which would still remain below 1 LA. It would be above 1 CA, however when taking ODH risks into account (max. He concentration of 1.4% by vol.) the airborne activity can also be considered to be well below 1 CA for an occupational exposure scenario
1Attenuation in 2.4 mm iron
2Rescaling to BDF/SHiP intensity (4E13 p / 7.2 s)
3Considering full saturation in BDF/SHiP operation
Preliminary

## Slide 26
H-3 Diffusion Studies

## Slide 27
BDF tungsten target H-3 content
H-3 activity (Bq)
Total PoT 2×1020 (5 yrs) + 1 month cool-down
Total H-3 Activity Production (Bq) | 
W target | 2.47E+13
He cooling | 4.6E+09
Inhomogeneous H-3 production in the W target due to target dimensions and irradiation profile
Several orders of magnitude lower H-3 production in He than in the W target
Main contribution of H-3 in He cooling circuit due to diffusion
Quantification of H-3 diffusion and related radiological risks
  Conservative assumption that all H-3 produced in tungsten permeates to helium
  Evaluation of H-3 diffusion via SOLIDUSS assuming all H-3 reaching the target surface will desorb to helium
→ 0.02% wrt. W target
Total PoT 2×1020 (5 yrs) + 1 month cool-down
z[4;155]
x[-12;12]
Preliminary

## Slide 28
H-3 content in He cooling
Total H-3 production in 5 years of 24.7 TBq → conservatively assuming all H-3 diffuses to He
He-cooling circuit
Conservative H-3 diffusion
He purification
8 m3 He at 14.5 bar (avg.)
He purification via chemical getters (Entegris®) permanently trapping impurities via chemical absorption
2% of overall flow rate circulated through them
  Achieved purity: H2O, O2 , CO, CO2 , H2 (<100 pptV each), Sulfur compounds (< ppbV)), acting equally on HT, T2 and HTO
High-efficiency air filters (HEPA grade) and heat exchanger (200 °C to 30 °C) are in underground target area
The cooling pipes go from target area to above-ground Service Building
BDF target
H-3 content
A conservative steady state H-3 concentration of 465 pptV was estimated
He cooling, 14.5 bar, 30° C → 200° C
Preliminary
Steady state concentration (pptV)
Production rate of H-3 (mol/s)
Filtration rate of H-3 (mol/s)
A total of 2.3 GBq of H-3 content with a partial H-3 pressure of 6.7E-4 Pa could be present in the circuit

## Slide 29
(Accidental) He release
Assumption of (accidentally) releasing at once the total He (8 m3, 14.5 bar) volume of the cooling system containing 2.3 GBq of H-3 would have the following radiological impact:
  Environmental impact:
    Site-specific dose coefficients for short-term release of HTO (most conservative) are available: 3.11E-18 Sv/Bq (see backup slide)
    A given H-3 release would result in a potential committed effective dose to members of the public of 0.01 uSv → fulfills CERN’s dose optimization objective for the public of <10 uSv/year
  Facility impact:
    A release of the total He (116 m3 at 1 atm) would create an unacceptable ODH risk in the EN-CV rooms (530 m3, 1116 m3)
    ~0.4 CA1 for any accidental releases inside w/o ODH risk (He concentration <1.4% by vol.) → within the given area classification limit
He
He
    It shall be noted that potential contributions from other volatile radionuclides are not considered here
1CA: Guidance value for chronic occupational exposure to airborne activity. Exposure to an airborne activity concentration of 1 CA for 40 hours
Preliminary

## Slide 30
H-3
H-3 permeation through SS304L
H-3 may permeate through the SS304L pipes (3 mm thick)
Conservative H-3 permeation rates* including isotopic correction were evaluated for the given He temperatures
F. Dragoni, BDF target cooling concepts
* Based on 24.7 TBq/year H-3 production in the BDF target leading to 465 pptV
Preliminary
  Cold He (30°C):
    1.4 ∙ 10-15 mol/s, which would result in 47 MBq/year
      The environmental impact with a dose of 0.1 nSv/y is negligible
      The facility impact is negligible given air volumes and ventilation
  Hot He (200°C):
    1.6 ∙ 10-11 mol/s, which results in 0.1 TBq/83 operational days
      The environmental impact with a dose of 0.4 uSv/y is acceptable particularly in view of the conservative assumptions
      No facility impact as hot area not accessible during operation and dynamically confined
H. G. Nelson, J E. Stein, Gas-phase hydrogen permeation through alpha iron, 4130 steel, and 304 stainless steel from less than 100 C to near 600 C, NASA 1973
Notes: Isotopic correction added as experimental data are available for Hydrogen (tritium diffuses more slowly (sqrt of 3) than H in metals
The √3 factor is the isotopic correction used to convert H permeation to T permeation.
This comes from the mass-dependence of diffusivity and solubility.
Sieverts-law permeation equation, corrected to convert hydrogen (H-1) permeation data into tritium (H-3) permeation
Φ0​ → Pre-exponential factor of permeability (from Arrhenius permeability fit for hydrogen).
T temperature in K; p → Permeation coefficient (permeability), also originally from H-1 data
P1​ (higher one with T present) and 𝑃_2 (lower one) represent the partial pressures of the permeating gas (tritium) on the two sides of the membrane or wall
A Permeation area (m²)
D → Wall thickness (m)
The formula computes tritium permeation through a material wall.
It uses hydrogen permeability data, which are more widely available.
Permeation is diffusion-limited, giving the √(𝑃_1 )−√(𝑃_2 )dependence.
The √3 factor corrects the hydrogen data to tritium by accounting for the isotopic mass effect on diffusivity
Permeability is the product of diffusivity and solubility, and it increases exponentially with temperature according to the combined activation energies for diffusion and dissolution
Φ= permeability
𝐷= diffusivity
𝑆= solubility
𝐷_0, 𝑆_0= pre-exponential factors of diffusion and solubility
𝐸_𝐷= activation energy for diffusion
𝐸_𝑆= enthalpy of solution (solubility activation energy)
𝑅= universal gas constant
𝑇= temperature (K)

## Slide 31
H-3 leakage
Furthermore, leaks from the He cooling system may contribute to H-3 releases
The maximum He leakage from all 50 flanged joints was evaluated resulting in 0.28 g/year
This corresponds to a H-3 release of 35 kBq/year
      The environmental impact with a dose of << nSv/y is negligible
      The facility impact is negligible even if released in a single room without considering ventilation
Preliminary
F. Dragoni, BDF target cooling concepts

## Slide 32
H-3 diffusion parameters
W Target Temperatures in °C
 | Bulk | Surface
Max after pulse | 392 | 349
Target avg. after pulse | 243 | 203
Max, time avg. | 387 | 327
Target avg., time avg. | 234 | 193
1 beam pulse of 1 s every 7 s
Temperatures investigated
Reference [2] F. Reiter, G. Gervasini, K. S. Forcey, A Compilation of Tritium-material Interaction Parameters in Fusion Reactor Materials, Commission of the European Communities, 1993
Reference [1] F. Ogallar Ruiz, Evaluation and criticality assessment of radiological source terms to be used for fire risk studies at accelerator facilities, CERN-THESIS-2021-293
Preliminary
Estimation of H-3 diffusion into He with SOLIDUSS [1]
Target temperatures from Ansys calculations (M. Parkin) with most extreme temperatures investigated for diffusion
Diffusion parameters (A, Q) from [2]
[cm2 s-1] frequency factor
[J mol-1] diffusion activation energy
[K] absolute temperature
[J K-1 mol-1] gas constant
Arrhenius equation
Required input
4.1E-3 cm2 s-1,
38E3 J mol-1
4.3E-6 cm2 s-1 @ 665 K (392 C)

## Slide 33
H-3 diffusion parameters
W Target Temperatures in °C
Estimation of H-3 diffusion into He with SOLIDUSS [1]
Target temperatures from Ansys calculations (M. Parkin) with most extreme temperatures investigated for diffusion
Diffusion parameters (A, Q) from [2]
 | Bulk | Surface
Max after pulse | 392 | 349
Target avg. after pulse | 243 | 203
Max, time avg. | 387 | 327
Target avg., time avg. | 234 | 193
1 beam pulse of 1 s every 7 s
Temperatures investigated
Reference [1] F. Ogallar Ruiz, Evaluation and criticality assessment of radiological source terms to be used for fire risk studies at accelerator facilities, CERN-THESIS-2021-293
[cm2 s-1] frequency factor
[J mol-1] diffusion activation energy
[K] absolute temperature
[J K-1 mol-1] gas constant
Preliminary
H-transport properties dashboard Rémi Delaporte-Mathurin
Tungsten, H-3
665 K
Arrhenius equation
Required input
4.1E-3 cm2 s-1,
38E3 J mol-1
4.3E-6 cm2 s-1 @ 665 K (392 C)

## Slide 34
H-3 diffusion estimation
Assumptions
  5 operational periods of 83.3 days with maximum intensity (tot. 2×1020 POT) at fixed high temperature (no T gradient)
  Cool-down periods at 22 °C in between
  Diffusion taken into account for all periods (operation, shutdown) with respective H-3 production right at start of each operational period (conservative)
  Radioactive decay considered (minor effect)
  All radionuclides reaching the target surface diffuse to He (conservative)
Findings
  Total H-3 diffusion in 5 years BDF operation ranges from 21 – 24 TBq (85 – 99 %) depending on the operational T assumed
  Open question: how much of H-3 reaching surface will diffuse to He
Total PoT 2×1020 (5 yrs) + 1 month cool-down
time
Operational period – high temperature
Shutdown period – low temperature
1
2
3
4
5
83 d
83 d
83 d
83 d
83 d
282 d
282 d
282 d
282 d
 | 392 °C | 234 °C | 193 °C | 22 °C
Diffusion per 83.3 d | 94% | 73% | 62% | -
Diffusion per 282 d | - | - | - | 8%
 | 392 °C | 234 °C | 193 °C
Diffusion per 5 years | 99% | 92% | 85%
Diffused H-3 (Bq) | 2.4E13 | 2.3E13 | 2.1E13
H-3 diffusion (t, T)
H-3 diffusion for BDF (operational T)
Operational periods for the BDF target
For all the same shutdown T of 22 °C s assumed
Preliminary

## Slide 35
H-3 diffusion estimation – basic validation
Analytical formula for uniform radionuclide distribution [1] Fraction of atoms Reaching an object’s Surface (FRS)
Surface of object
Volume of object
Diffusion coefficient of interest
Total diffusion time
 |  | 392 °C | 234 °C | 193 °C | 22 °C
SOLIDUSS | Diffusion per 83.3 d | 94% | 73% | 62% | -
 | Diffusion per 282 d | - | - | - | 8%
Analytical formula | Diffusion per 83.3 d | 100% | 73% | 54% | -
 | Diffusion per 282 d | - | - | - | 6%
H-3 diffusion (t, T)
Reference [1] F. Ogallar Ruiz, Evaluation and criticality assessment of radiological source terms to be used for fire risk studies at accelerator facilities, CERN-THESIS-2021-293
Relatively good agreement is observed between the SOLIDUSS predictions and the analytical formula, despite the expected differences arising from the strongly inhomogeneous distribution of H-3 within the BDF target
Preliminary

## Slide 36
Thank you for your attention
Claudia AHDIDA et al. HI-ECN3 RP Aspects
01/06/2026

## Slide 37
Main Requirements for Waste Disposal
FA-MA (ILLW) classification known requirements:
  KC-T12 container is the only large container that PSI currently accepts for large radioactive waste
  A bigger Swiss container exists for nuclear waste, but currently not for industry or research sector. As this may take long time and has cost implications (factor 2), we need to count on KC-T12
  KC-T12 is a concrete container of limited size and weight in which the waste is cemented
  Main dose rate limits
    < 10 mSv/h at 3 m from the target waste assembly
    < 2 mSv/h at contact of the package
  LSA-II or LSA-III classification limit (ADR - Carriage of Dangerous Goods by Road) to be respected1
  Alpha-emitters specific activity limit to be respected on the conditioned waste to avoid alpha-toxic waste classification
Available weight:
15.63 tons minus the weight of the cement filling
Max. available height: 1.68 cm (1.73 m – 5 cm top cement) minus required shielding
Max. available width:
1.16 m (1.26 m – 10 cm side cement) minus required shielding
Container shielding: 12 cm concrete
1. The BDF target assembly is not considered as a combustible solid according IAEA SSG-26 Rev.1 §522.2, and thus the limit of 100 A2 for LSA-II and LSA-III classifications is not applicable
LSA-II
LSA-III

## Slide 38
Alpha Emitters
Gd-148: 99 GBq
Other RN α-emitters: <5.34 MBq
Total mass of waste: 7162 kg
  W Blocks: 1334 kg
  Ta Cladding: 74 kg
  Inconel Holder: 781 kg
  Inconel Pressure Vessel: 159 kg
  Steel Table: 444 kg
  Empty KC-T12: 4370 kg
  Mold: 0 (safety margin)
  Cementation: 0 (safety margin)
  Sand: 0 (safety margin)
Specific activity of alpha emitters of conditioned waste
10 years cooldown
The alpha-emitters specific activity was calculated for the conditioned waste without accounting for the additional mold, cementation and sand filling that would account for a safety margin
The resulting specific activity is below the limit to avoid alpha-toxic waste classification that is
PRELIMINARY STUDY

## Slide 39
Class A working areas will in addition have a Controlled Radiation Area classification with contamination risk (Limited Stay or High Radiation Area, or temporarily even be a Prohibited Area)
A
Simple Controlled or Limited Stay Radiation Area with Contamination Risk
B911
Supervised Radiation Area
Underpressure Cascade Proposal
-230 Pa
-40 Pa 1st / 2nd floor
-120 Pa
-120 Pa
-70 Pa
-60 Pa
-60 Pa
-230 Pa
Hotcell
-60 Pa
-20 Pa
-20 Pa
+30 Pa
0 Pa
0 Pa
-20 Pa
The proposed underpressure cascade follows:
  OUMR (Class A lab)
  ISO 17873
  Ventilation WG recommendations
  Two external consultants
  and is consistent with ISOLDE / MEDICIS approach
Service Cell and hot cell with highest Containment Class 4 (ISO 17873)
Pressure values relative to atmospheric pressure
29.01.2026
EDMS 3406737
Claudia AHDIDA et al. HI-ECN3 RP Aspects
39

## Slide 40
A
Simple Controlled or Limited Stay Radiation Area with Contamination Risk
B911
Supervised Radiation Area
RP Air Monitoring
4 Aerosol monitors (β/γ)
1 Gaseous air activity conc.
b911
1 Punctual bubbler
Class A areas w/ Ventilation Aerosol Monitors (VAM, iCAM by Mirion)
The Target Area and cooling room w/ Air Monitoring Station (AMS)
The exhaust stack shall extend at least 2 m above roof level
Inline gas activity monitor + gamma spec
Notes: 1 Mirrion ICAM per exhaust (~20 kCHF/ICAM). continuous alpha beta monitors. Beta as from a few tens or a hundred keV , calibrated for Sr90
Proper aersol sampling in a long (ideally 8 aerolic diameters after last bend) straight section in exhaust duct
ABPM air monitors in accessible area of next to hot / service cell
BAI 9109-4 Moniteur de mesure bêta des gaz radioactifs - Berthold Technologies GmbH & Co.KG