## Slide 1
Dan Wilcox
Rutherford Appleton Laboratory, UK
For UK team in collaboration with Fermilab LBNF Targetry Project Team, UK Universities, and Culham MRF
NBI 2022
September 20th 2022
LBNF Target Design and Development

## Slide 2: Overview
UK project overview
Target challenges
Prototype target design
  Analysis
  Prototyping
  Irradiated material studies
Future plans and deliverables

## Slide 3: Scope of UK Targetry Contribution
1x Target Exchange System:
1x Instrumented Baffle:
Targets and Connecting Pipework:
1x Prototype Target
1x Production Target
Various Helium Plant Components inc. Blower and Coolers:
Protons
See talk by Eric Harvey-Fishenden, Wed 21st

## Slide 4: UK Project Phases and Status
PRELIMINARY DESIGN
FEATURE PROTOTYPING
FINALIZE UK SCOPE
PHASE-2 PROPOSAL SUBMISSION
Phase 1 (Design Phase)
FINAL DESIGN
MATERIALS RESEARCH
PROCURE/MANUFACTURE/SUPPLY IKC’s
TARGET/HORN INTEGRATION TRIALS
Phase 2 (Construction Phase)
2018
2019
2020
2021
2022
2023
2024
2025
2026
2027
2028
Phase-2 underway as of Apr 2022
M&O (Operations Support)
TARGET STATION COMMISSIONING
  FIRST BEAM
  PRODUCTION OF REPLACEMENT COMPONENTS
Phase 2 funded for the full amount requested
University PI’s have received phase-2 grant award letters

## Slide 5: Recent Press
https://www.ukri.org/news/uk-engineers-build-critical-link-for-global-neutrino-experiment/
https://www.theengineer.co.uk/content/news/uk-engineers-build-critical-link-for-global-flagship-neutrino-experiment

## Slide 6: Comparison with T2K
Parameter | LBNF Design (1 Year Design Life) | T2K Experience (Target 2 History)
Beam Power (MW) | 1.2 | 0.51
Proton Energy (GeV) | 120 | 30
Beam Current (μA) | 10 | 17
Beam Sigma (mm) | 2.7 | 4
Radiation Damage Severity (p/cm^2) | 2.5E+21 | 3.1E+21
Thermal Shock Severity (p/cm^2/pulse) | 1.7E+14 | 2.6E+14
Higher beam power but lower current and smaller beam spot = lower proton fluence and thermal shock than T2K
Longer target will require optimised design of cantilever support
T2K
LBNF
To scale. Core length = 0.9m T2K, 1.5m LBNF
c/o Patrick Hurh (Fermilab)

## Slide 7: Target Engineering Challenges
Protons
Proton beam causes very high heat deposition and radiation damage (several DPA/yr along beam centreline)
1.5m long cantilever – must not touch the inside of the horn
Vessel wall must be thin to prevent pion reabsorption, but strong to contain pressure and support cantilever
Support structure must align the target very accurately relative to the horn and proton beam
Target core temperature jumps by 140°C in 10ms, once every 1.2s – thermal shock and fatigue
Vibrations transmitted from horn to target mount – See talk by Peter Loveridge later today
Materials must be strong and perform well at high temperature:
Nuclear-grade graphite core
Titanium alloy outer container

## Slide 8: Physics Optimisation of Engineering Features
Small effect of varying support fins
Larger effect of increasing target length
Very large effect of changing vessel thickness
Prototype Target
c/o John Back (Warwick University)
Vessel Wall Thickness
Total
Target Length
Size of Support Fins

## Slide 9
 | Grade 2 (CP Ti) | Grade 9 (Ti-3Al-2.5V) | Grade 5 (Ti-6Al-4V) | Ti 15-3 (Ti-15V-3Cr-3Al-3Sn)
Prior Operating Experience | None | None | Used in T2K target | Non-pressure use at T2K
Pressure Code Approval | Listed in ASME | Code route exists | Code route exists | No previous code use
Structural Safety Factor | Lowest | Higher than grade 2 | Higher than grade 9 | Even higher than grade 5
Radiation Damage Tolerance | No data available | Better than grade 5? | Good data and T2K use | Looks best, but needs R+D
Ease of Manufacture | Successful prototype | Difficult to machine | Successful prototype | Welding not yet tested
Ease of Procurement | Widely available | Less widely available | Widely available | Limited availability
Prototype Target Titanium Grade Selection
Note that it must also be possible to weld the selected vessel and window grades together
Ti 15-3 window prototype

## Slide 10: Detailed Target Analysis
Fluid:
Thermal:
Structural:
Fatigue:
Geometry:
Mesh:
Radiation Dose:
Stress Categorisation:
Pressure Code Approval
(FESHM and ASME BPVC)

## Slide 11: ASME BPVC Required Analyses
Categorised stress components
Buckling analysis
Fatigue
First buckling mode with no internal support structures
Goodman equivalent stress amplitude in vessel and windows

## Slide 12: Radiation Dose with Nominal Beam, 1.2MW
DPA is highest in the windows (2.5/yr) and target (0.5/yr)
Peak DPA in any other component is 0.26/yr, in the flow divider tube
Some titanium irradiation data available for up to 0.24 DPA

## Slide 13: Irradiated Titanium Data Summary – Grades 5 and 23
“Fatigue Performance of Proton Irradiated Ti6Al4V Alloy”, Sujit Bidhar, 6th RaDIATE Collaboration Meeting, Dec 10, 2019
Macro-scale Fatigue
Gr5/23
Dose at neck region
0.06~0.24 DPA
Irradiation temp
50C~125C
R=0.2-0.28
Meso-scale Fatigue
Gr23 A&STA, Gr2, 15-3Ti
Meso-scale S-N Curve of unirradiated Ti-6Al-4V
V. Kuksenko, RaDIATE2017
Tensile Testing
Gr5/23, Gr9
“Tensile behavior of dual-phase titanium alloys under high-intensity proton beam exposure…”, T. Ishida et al., Journal of Nuclear Materials, 2020

## Slide 14: Radiation and Fatigue in Titanium
Windows have the highest radiation damage and fatigue of any Titanium component
Upstream Window
tmin = 0.3mm
Dose = 2.5dpa/yr
Tsteady = 115°C
Tmax = 150°C peak
ΔT = 70°C/pulse
ΔσEq = 21MPa/pulse
Downstream Window
tmin = 0.4mm
Dose = 0.7dpa/yr
Tsteady = 150°C
Tmax = 175°C peak
ΔT = 55°C/pulse
ΔσEq = 6MPa/pulse
Extrapolated Endurance Limit for >1E9 Cycles (MPa) | SE (MPa)
Titanium Grade 5 | 360
Derated for 150°C | 315
Derated for 150°C and 0.24DPA | 240
Expected number of beam pulse cycles = 1.5E7 per year

## Slide 15: Radiation and Fatigue in Graphite
First two target segments have highest radiation damage and fatigue of any Graphite component
 | IG-43 Graphite
UTS at room temp (MPa) | 37
Estimated endurance limit (MPa) | 18.5
Equivalent stress amp. (MPa) | 0.95

## Slide 16
Feature Prototyping Highlights

## Slide 17: Target Assembly Procedure

## Slide 18
Quotes received
Production challenges identified at PDR

## Slide 19: Ongoing Prototyping Efforts
Full length target core segment out for quote:
Target core mounting design development:

## Slide 20: Irradiated Material Collaborations
Titanium
Graphite
Highest dose to beam windows:
Titanium irradiation at BLIP:
Meso-fatigue specimens have been shipped to Culham MRF:
Fatigue test in hot cell, using a method developed at Oxford University:
Cracked graphite targets seen at NuMI-MINOS and other facilities:
- Active sample on its way to Bristol University
- Neutron diffraction experiment at ISIS (ENGIN-X) approved
Future Ti irradiations also planned at Birmingham University

## Slide 21: Project Management Integration with Fermilab
UK Phase-2 Gantt:
CAD Integration Schematic:
QA Approach:
Milestones and Deliverables:
Interface Control Documents:

## Slide 22: Conclusions
Phase 1 (Design) complete and closed out. Phase 2 (Construction) fully funded
Close integration with Fermilab team, project management processes well defined
Focus will now be on:
  Construction of a working prototype target
  Irradiated material studies to inform design of future targets
  Refine design, then construct 1st production target

## Slide 24
Backup Slides

## Slide 25: Main Baffle Design
DS Hanger
US Hanger
Duct
Lifting Points
Support Frame
Graphite core segment stack

## Slide 26: Helium Plant Deliverables
v
  1x Positive Displacement Blower
  1x back-up blower (Working Allowance scope opportunity)
  1x Target RAW Cooler
  1x Compressor Pre-cooler
  1x Compressor After-cooler
  1x remote operable gas purity monitoring system
x 3
x 1
x 1(/2)
e.g. Kelvion: Welded Plate and Frame Heat exchanger
e.g. Hiden: HPR-20 benchtop mass spectrometer
Custom machine: identified two potential European Suppliers