## Slide 1: TRIUMF Material Irradiation and PIE – Capabilities and Status
Alexander Gottberg Department Head, Targets and Ion Sources, TRIUMF Adjunct Professor, University of Victoria
ARIEL Program Leader
September 22, 2022

## Slide 2: Canada’s Particle Accelerator Centre is Governed by its 21 Member Universities
Discovery,
accelerated
400 staff, 200 students & post-doctoral researchers
1100 scientific visitors from 39 countries per year
Member Universities
Notes: Comment: 21 member universities. McMaster just joined on April 12th, 2019

## Slide 3
TRIUMF Users come from over 40 countries
In 2019, TRIUMF hosted >1000 Scientific Visitors & Users
Global Reach

## Slide 4: Primary and Secondary Particle Accelerators at TRIUMF
TRIUMF accelerators
520 MeV, 200 kW cyclotron
50 MeV, 100 kW electron linac
Cyclotrons: TR30-1, TR30-2, TR14, TR24, CP42
Heavy ion accelerators, up to 16 MeV/u
520 MeV H- cyclotron
5500 hours per year:
ISOL RIB (50 kW protons)
π and µ (60 kW)
Medical isotopes (50 kW)
Ultra-cold neutrons (20 kW)
Proton therapy studies (50 W)
IAMI
TR24

## Slide 5: TRIUMF’s Proton, Neutron, Pion, Muon Programs
Beamline 1
Nine secondary channels
UCN (Ultra Cold Neutrons) for nEDM measurement
Pions, muons for material and fundamental science
Neutrons for electronics irradiations services
IAMI
TR24
M15
M11
M9
M20
UCN
Cyclotron
NIF

## Slide 6: TRIUMF’s Medical Isotope Factory
Five H- medical cyclotrons
TR30-1, TR30-2, CP42, 250 µA – 1 mA (solid, liquid and gas targets)
  Operated by ATG for
  2M doses annually
  103Pd, 111In, 123I, others…
TR13, <100 µA (solid, liquid and gas targets)
  11C, 18F, 64Cu, 68Ga, others…
TR24, 1 mA (gas, solid, liquid targets)
  Future for IAMI
Protons from 90-500 MeV, 300 µA cyclotron
82Sr / 82Rb production
212Pb, 213Bi, 225Ac production
Exotic medical isotope R&D, fission and spallation with optional isotope separation
Coming 2023
UBC hospital (3 km)
UBC Centre for Brain Health (3 km)
UBC Centre for Comparative Medicine (500 m)
International shipment of 2M patient doses of isotopes and generators
IAMI
TR24

## Slide 7: Radioisotopes for Science
Only purpose build multi-user radioisotope beam facility world-wide
Two independent high-power drivers:
  50 kW, 500 MeV protons
  100 kW, 30 MeV from superconducting e-linac to AETE
Four target stations for >9000 h/y to existing nuclear physics experiments
Symbiotic medical isotope production target system
IAMI
TR24

## Slide 8: TRIUMF Remote Handling
TRIUMF RH specialists assisting in T2K target repair
RH robotics development
Hot cell design, operation and development of systems for operation in kGy – PGy dose fields.
  Mechatronics and robotics development
  Dedicated training programs on prototypes and hot cells
  International collaborations
  Daily shipments of radioactive materials
ARIEL Hot Cell Commissioning

## Slide 9: Material Irradiation Locations
IAMI
TR24
1
6
3
2
7
5
4
8
ISAC, 480 MeV protons, ≤100 µA
ARIEL, 480 MeV protons, ≤100 µA
CTS, 300 keV – 35 MeV electrons, ≤10 mA, µs – s pulses
NBF, 450-480 MeV protons, ~3 nA
PIF, 5-500 MeV, ≤ 10 nA
IPF, 430 MeV protons, ~70 µA
NIF, near-terr. neutrons, 3·106 n/cm2/s
Isotope production cyclotrons, 13-30 MeV, 1-1000 µA

## Slide 10: Overview of Irradiation Conditions at TRIUMF
 | 1. ISAC | 2. ARIEL | 3. IPF | 4. PIF | 5. NBF | 6. NIF | 7. CTS | 8. TR13-30
Particle | Protons | Protons | Protons | Protons | Hydrogen | Neutrons | Electrons | Protons
Energy [MeV] | 470 | 470 | 430 | 5 – 500 | 480 | Terrestrial | 0.3 - 30 | 13-30
Intensity | 5-100 µA | 5-100 µA | 70 µA | 0.1 - 10 nA | 200 nA |  | 10 nA - 10 mA | 1-1000 µA
Time structure | CW | CW | CW | 100 ms - CW | CW | CW | 1 µs - CW | CW
Beam size [mm] | 10 FWHM | 10 FWHM | 12 FWHM | 10 - 70 | 20 x 100 | 200 | 1 - 12 | 20 x 7.5
Flux [/cm2/s] | 1013 - 1015 | 1013 - 1015 | 3·1014 | 105 - 1011 | 6·109 | 2·106 | 1013 - 1019 | 1013 - 1015
Dose rate if out of beam position [kGy/h] | 1 - 106 mixed | 1 - 106 mixed | 1,000 mixed | 1-10 neutrons | 10 neutrons | 1 neutrons | 10,000 gammas | -
Availability [h\y] | 2 x 2000 | 2 x 2000 | 4500 | 1500 | 5500 | 4500 | 500 | 3456
Available integrated [particles\y] | ~3·1021 | ~3·1021 | ~1·1022 | ~3·1016 | 2·1019 | 1016 | 1023 | 1022

## Slide 11: Material Irradiation Locations
IAMI
TR24
ISAC, 480 MeV protons, ≤100 µA
ARIEL, 480 MeV protons, ≤100 µA
CTS, 300 keV – 35 MeV electrons, ≤10 mA, µs – s pulses
NBF, 450-480 MeV protons, ~3 nA
PIF, 5-500 MeV, ≤ 10 nA
IPF, 430 MeV protons, ~70 µA
NIF, near-terr. neutrons, 3·106 n/cm2/s
Isotope production cyclotrons, 30MeV-300uA up to 100mAh
3

## Slide 12: ARIEL e-γ Converter Test Stand
e-
Development motivations
  Thermal stresses (100 kW beam, thermal cycles)
  Radiation damage / radiochemistry
  Irradiations of up to 3 weeks
Experimental setup:
  Water-cooled sample holder
  Power deposition density of up to several MW/cm3
  300 keV beam to avoid activation (30 MeV possible)
300 keV to 30 MeV,
up to 1022 electrons/day, 0.1 – 12 mm FWHM
variable thermal shocks studies

## Slide 13: Material Irradiation Locations
IAMI
TR24
ISAC, 480 MeV protons, ≤100 µA
ARIEL, 480 MeV protons, ≤100 µA
CTS, 300 keV – 35 MeV electrons, ≤10 mA, µs – s pulses
NBF, 450-480 MeV protons, ~3 nA
PIF, 5-500 MeV, ≤ 10 nA
IPF, 430 MeV protons, ~70 µA
NIF, near-terr. neutrons, 3·106 n/cm2/s
Isotope production cyclotrons, 30MeV-300uA up to 100mAh
1

## Slide 14: ISAC targets
Water-cooled heat shields
target container ~2000 °C
(Ø 20 mm, 60 cm3)
500 MeV protons
7 mm FWHM
Target ion source service connections
2932µAh
6599µAh
15969µAh
5750µAh
6003µAh
15197µAh
4710µAh
5769µAh
13891µAh
UCx
Ucx-P2N
UCx
Ta
Ta
SiC
UCx
UCx
C
33315µAh
40573µAh
2021
Target exchange in hot cell every 2-5 weeks
9 – 12 targets per year
PIE on every target
ITE
ITW

## Slide 15: Selected ISAC Target Materials
Axial proton irradiation, used with 500 MeV, up to 100 μA proton driver beams. Target exchanged every 3-5 weeks.
55 mm x
55 mm tantalum fins
2000: Tantalum or niobium foil discs packed within the tantalum target container.
2008: Discs of SiCx, TiCx or ZrCx cast onto exfoliated graphite foils and packed within the tantalum target container.
2013: Discs of UCx cast onto exfoliated graphite foils and packed within the tantalum target container.
2015: Discs of NiO cast onto niobium foils and packed within the tantalum target container.
Target heating (I)
⌀ 20 mm
cylindrical tantalum container
Ion source heating (I)
500 MeV
50 kW p+
Porous materials for optimized release of short-lived radioisotopes on backing foils for high conductive heat transfer into tantalum container
High-power (50 kW) target design
2019: Discs of electro-spun SiC nanoparticles co-spun with carbon fibers and packed within the tantalum container.

## Slide 16: Post-Irradiation Examination and Sample Extraction
Available in ISAC
radiation laboratories:
XRF, SEM, TEM
SPT
Optical microscopy
Pycnometer
2000ºC furnaces, diffusion studies
Emissivity, heat conductivity meas.
Type A and B packaging and shipping
Available in vicinity for activated
samples (< 100 µSv/h):
TEM, SEM, FIB, AFM
XRD
Tensile, impact strength, hardness, corrosion testing
…
UCx sample after irradiation
extraction tools for irradiated materials

## Slide 17: Parasitic irradiations at ISAC
Chart: Distance to beam center (mm)
| 10.5 | 9.5 | 8.5 | 7.5 | 6.5 | 5.5 | 4.4999999999999902 | 3.4999999999999898 | 2.4999999999999902 | 1.49999999999999 | 0.5
Be | 0.00043589 | 0.0006427 | 0.00087723 | 0.0018198 | 0.0041423 | 0.0077838 | 0.010597 | 0.016063 | 0.023387 | 0.028766 | 0.0324
C | 0.0010292 | 0.0015175 | 0.0020712 | 0.0042969 | 0.0097804 | 0.018378 | 0.025022 | 0.037927 | 0.055219 | 0.067919 | 0.0765
Al | 0.0048977 | 0.0072215 | 0.0098567 | 0.020448 | 0.046543 | 0.087459 | 0.11907 | 0.18049 | 0.26278 | 0.32321 | 0.36405
Ti | 0.0075675 | 0.011158 | 0.01523 | 0.031595 | 0.071915 | 0.13513 | 0.18398 | 0.27888 | 0.40603 | 0.4994 | 0.5625
Cr | 0.0086421 | 0.012742 | 0.017392 | 0.036081 | 0.082127 | 0.15432 | 0.21011 | 0.31848 | 0.46368 | 0.57032 | 0.64238
Fe | 0.011107 | 0.016377 | 0.022353 | 0.046371 | 0.10555 | 0.19834 | 0.27003 | 0.40931 | 0.59592 | 0.73297 | 0.82558
W | 0.013712 | 0.020218 | 0.027596 | 0.057249 | 0.13031 | 0.24486 | 0.33338 | 0.50533 | 0.73572 | 0.90492 | 1.0192
Ta | 0.022551 | 0.033251 | 0.045384 | 0.094152 | 0.21431 | 0.4027 | 0.54827 | 0.83106 | 1.21 | 1.4882 | 1.6763
Gy/h
Prog. Nucl. Sci. Technol. 2, 769–775 (2011)
rom Nucl. Energy Technol. 3, 169–175 (2017)
Helium ~10appm/mAh (residual nuclei in FLUKA)
~100appm/DPA-FLUKA
DPA-FLUKA
Analysis of parasitic irradiations by
MonteCarlo simulations

## Slide 18: Hot Cell Based Small Punch Test
Small punch test stand
Mechanical actuator, load cell and LVDT acquired
Sample holder assembled
LVDT
Sample
Punch guide
Punch
Clamping spring
800H samples

## Slide 19: Parasitic irradiations at ISAC 2021-2022
0.1-1 DPA-FLUKA/year
6x1014 480MeV protons/s
100-400 ºC depending on sample material
Close to room temperature

## Slide 20: Out of Beam Samples
Non-irradiated
7.3MGy
45.2MGy
30 seals tested
Remote handling issues during testing
Target operation related issues
New design in 2022 to reduce RH issues.
Radiation resistance of spring energized PEEK seals
Leak rate of irradiated seals

## Slide 21: PEEK
73.8
0
3.6
17.2
0.86
23.91
36.49
(MGy)
Load/thickness^2 (N/mm^2)
Displacement (mm)
Chart: Dose (MGy)
| 0.86 | 1.2 | 1.5999999999999999 | 4.5 | 3.6 | 7.0289313117020891 | 17.2 | 23.512319548509499 | 23.909364247355047 | 30.842203427983403 | 36.489504357333495 | 73.800488246454634 | 0
 | 2.1415 | 2.1647 | 2.0014 | 1.7669 | 1.8122 | 1.5834 | 1.5036 | 1.3284 | 1.5526 | 1.5656 | 1.3852 | 1.3784 | 2.0355
Chart: Dose (MGy)
| 0.86 | 1.2 | 1.5999999999999999 | 4.5 | 3.6 | 7.0289313117020891 | 17.2 | 23.512319548509499 | 23.909364247355047 | 30.842203427983403 | 36.489504357333495 | 73.800488246454634 | 0
 | 243.1129 | 247.669 | 247.4748 | 233.1763 | 246.9406 | 338.8476 | 299.6482 | 319.2557 | 279.3948 | 261.5964 | 206.3101 | 218.3425 | 260.3477
Molecular weight measurements to come

## Slide 22: 2021 & 2022 parasitic irradiation campaign at ISAC
Parasitic target # | Sample materials | Irrad. (μAh) | DPA-NRT
#1-P | Al6061-AlSi10Mg(AM) | 2934 | [0.01-0.025]
#2-P | Al6061-AlSi10Mg(AM) | 33315 | [0.12-0.62]
#3-P | CrMnFeCoNi (Cantor) - SS316L | 40573 | [0.91-3.52]
#4-P | CrMnFeCoNi (Cantor) - SS316L | 11772 | [0.24-1.05]
#5-P | CrFeCoNiCu - CrMnFeNi (Co-less Cantor) | 13891 | [0.32-0.90]
2021
Parasitic target # | Sample materials | Estimated Irrad. (μAh) | Estimated DPA-NRT
#6-P | CuCrZr | 21613 | [0.48-1.87]
#7-P | SS310, 800H | 24290 | [0.54-2.1]
#8-P | cold sprayed Cu alloy | 24290 | [0.54-2.1]
#9-P | Al alloy | 3000 | [0.01-0.055]
#10-P | Cantor, SS316L | 43058 | [0.96-3.73]
#11-P | Al6061 | 43058 | [0.15-0.8]
#12-P | Cantor, SS316L | 8308 | [0.19-0.72]
2022

## Slide 23: Cantor HEA
(111)
(200)
(220)
(311)
(222)

## Slide 24: Cantor HEA and SS316 Pilot irradiation 2021:
DPA-NRT simulated with FLUKA
No temperature effects accounted (from simulation up to 400ºC), online measurements soon
~50 appm He/DPA-NRT
Data from 2 parasitic targets (11,772 µAh (35 days in beam, 2.5 months total time) and 40,573 µAh (79 days in beam, 5 months total time)
Load/thickness^2 (N/mm^2)
Chart: DPA NRT
| 0.2434782608695652 | 0.4760869565217391 | 0.91304347826086951 | 1.0499999999999998 | 1.5941304347826086 | 3.5195652173913041
Cantor HEA | 0.68456 | 0.66748 | 0.65682 | 0.66387 | 0.61675 | 0.5317
SS316L | 0.60464 | 0.60325 | 0.62931 | 0.64361 | 0.62855
SS316L
Cantor HEA
SPT Yield
Max load
Displacement (mm)
0.24
0.47
0.91
1.05
Chart: DPA-NRT
| 0.2434782608695652 | 0.4760869565217391 | 0.91304347826086951 | 1.0499999999999998 | 1.5941304347826086 | 3.5195652173913041
Cantor HEA | 1674.8302 | 1725.5229 | 1560.3709 | 1550.1938 | 1545.5118 | 2210.0216
SS316L | 2166.6511 | 2099.2282 | 1757.349 | 1793.4336 | 1719.5623
 | 5069.3131 | 4935.2587 | 5385.9067 | 4542.0869 | 5529.7679 | 5722.099
 | 6326.5873 | 6707.472 | 5782.3629 | 6341.2653 | 6158.8148
1.59
3.52
DPA-NRT

## Slide 25: Online temperature measurements
Previous attempt
Ideas to experimentally obtain irradiation temperatures, to be implemented Oct-Dec.
Simple design
Welded to dummy sample
RTD measurement

## Slide 26: Thank you Merci
Follow us @TRIUMFLab
www.triumf.ca

## Slide 27: Al alloy
Soon:
ISAC Al6061 beam windows, exchanged every ~7years -> ~0.5Ah -> 6DPA-NRT max in center

## Slide 28
thickness/10
Yield
Max load
Max displacement
Initial slope
Load (N)
Displacement (mm)
(from literature)

## Slide 29: 2021 & 2022 parasitic irradiation campaign at ISAC
2021
CNL collaboration -> 800H and SS310
Ariel beam window -> CuCrZr, Cu AM
Upstream
FWHM=7mm, DPA-FLUKA on Cu(Eth=40eV) @10mAh
2022
Developments ongoing:
Thermocouples
Upstream irradiations
Temperature control (TC + heating elements)
Downstream
Total of 170 SPT samples

## Slide 30: Material Irradiation Locations
IAMI
TR24
2
ISAC, 480 MeV protons, ≤100 µA
ARIEL, 480 MeV protons, ≤100 µA
CTS, 300 keV – 35 MeV electrons, ≤10 mA, µs – s pulses
NBF, 450-480 MeV protons, ~3 nA
PIF, 5-500 MeV, ≤ 10 nA
IPF, 430 MeV protons, ~70 µA
NIF, near-terr. neutrons, 3·106 n/cm2/s
Isotope production cyclotrons, 30MeV-300uA up to 100mAh

## Slide 31: Use of the ARIEL Proton Waste Beam: ARIEL Parasitic Target (2025)
At ARIEL: <70 MeV stopped in target
Pneumatic transfer between 100 µA, 420 MeV proton waste beam and inert gas hot cell
1020 protons per cm2 per week
Routinely available
Additional position for long-term studies in tunable kGy/h – GGy/h dose rates
Parasitic irradiation setup in electron station

## Slide 32: TRIUMF-ISAC
Modular target station
2 symmetric stations operated consecutively
30-100mAh/year/station
480 MeV ≤100 µA

## Slide 33: Material Irradiation Locations
IAMI
TR24
ISAC, 480 MeV protons, ≤100 µA
ARIEL, 480 MeV protons, ≤100 µA
CTS, 300 keV – 35 MeV electrons, ≤10 mA, µs – s pulses
NBF, 450-480 MeV protons, ~3 nA
PIF, 5-500 MeV, ≤ 10 nA
IPF, 430 MeV protons, ~70 µA
NIF, near-terr. neutrons, 3·106 n/cm2/s
Isotope production cyclotrons, 30MeV-300uA up to 100mAh
3

## Slide 34: ARIEL e-γ Converter Test Stand
e-
Development motivations
  Thermal stresses (100 kW beam, thermal cycles)
  Radiation damage / radiochemistry
  Irradiations of up to 3 weeks
Experimental setup:
  Water-cooled sample holder
  Power deposition density of up to several MW/cm3
  300 keV beam to avoid activation (30 MeV possible)
300 keV to 30 MeV,
up to 1022 electrons/day, 0.1 – 12 mm FWHM
variable thermal shocks studies

## Slide 35: Material Irradiation Locations
IAMI
TR24
4
ISAC, 480 MeV protons, ≤100 µA
ARIEL, 480 MeV protons, ≤100 µA
CTS, 300 keV – 35 MeV electrons, ≤10 mA, µs – s pulses
NBF, 450-480 MeV protons, ~3 nA
PIF, 5-500 MeV, ≤ 10 nA
IPF, 430 MeV protons, ~70 µA
NIF, near-terr. neutrons, 3·106 n/cm2/s
Isotope production cyclotrons, 30MeV-300uA up to 100mAh

## Slide 36: NBIF – Neutral beam irradiation facility
H- beam at 450 - 500 MeV EM stripped in highest magnetic field and emerges as a fan of Hº beam ~ 2 cm x 100 cm ~ 1 nA/cm2
1017 p/cm2 per year, 4 GGy
Coil samples to 500 MGy

## Slide 37: Material Irradiation Locations
IAMI
TR24
5
ISAC, 480 MeV protons, ≤100 µA
ARIEL, 480 MeV protons, ≤100 µA
CTS, 300 keV – 35 MeV electrons, ≤10 mA, µs – s pulses
NBF, 450-480 MeV protons, ~3 nA
PIF, 5-500 MeV, ≤ 10 nA
IPF, 430 MeV protons, ~70 µA
NIF, near-terr. neutrons, 3·106 n/cm2/s
Isotope production cyclotrons, 30MeV-300uA up to 100mAh

## Slide 38: PIF Test Area
2 proton beamlines, BL2C and BL1B:
  5 MeV to 500 MeV, 0.1 nA – 10 nA
  Mostly for electronics testing and radiotherapy
Large, uniform beam (easily up to 7 cm x 7cm)
Low flux (~ 108 p/cm2/s), low maximum fluence (<< 1013 p/cm2)
Neutron converters for large area neutron beam

## Slide 39: Possible Irradiation Locations
IAMI
TR24
6
ISAC, 480 MeV protons, ≤100 µA
ARIEL, 480 MeV protons, ≤100 µA
CTS, 300 keV – 35 MeV electrons, ≤10 mA, µs – s pulses
NBF, 450-480 MeV protons, ~3 nA
PIF, 5-500 MeV, ≤ 10 nA
IPF, 430 MeV protons, ~70 µA
NIF, near-terr. neutrons, 3·106 n/cm2/s
Isotope production cyclotrons, 30MeV-300uA up to 100mAh

## Slide 40: Phase 2: IPF (Isotope Production Facility) Targets
T1
T2
IPF
100 µA
~ 70 µA
~ 430 MeV, 70 µA, 12 mm FWHM
Parasitic irradiations
Station available for R&D
Irradiation of up to 6 samples simultaneously
Samples inside a water-cooled container
Thermocouple reading at the sample holder
Has been used for radioisotope release studies
Target containers in target station
Hot cell view

## Slide 41: Material Irradiation Locations
IAMI
TR24
7
ISAC, 480 MeV protons, ≤100 µA
ARIEL, 480 MeV protons, ≤100 µA
CTS, 300 keV – 35 MeV electrons, ≤10 mA, µs – s pulses
NBF, 450-480 MeV protons, ~3 nA
PIF, 5-500 MeV, ≤ 10 nA
IPF, 430 MeV protons, ~70 µA
NIF, near-terr. neutrons, 3·106 n/cm2/s
Isotope production cyclotrons, 30MeV-300uA up to 100mAh

## Slide 42: Neutron Beam Test Area
2·106 neutrons /cm2/s (ISS mission rate simulated in 1 h irradiation)

## Slide 43: Material Irradiation Locations
IAMI
TR24
8
ISAC, 480 MeV protons, ≤100 µA
ARIEL, 480 MeV protons, ≤100 µA
CTS, 300 keV – 35 MeV electrons, ≤10 mA, µs – s pulses
NBF, 450-480 MeV protons, ~3 nA
PIF, 5-500 MeV, ≤ 10 nA
IPF, 430 MeV protons, ~70 µA
NIF, near-terr. neutrons, 3·106 n/cm2/s
Isotope production cyclotrons, 15-30MeV, 300uA up to 100mAh

## Slide 44: Isotope production cyclotrons
15-30 MeV cyclotron for commercial production of radio-isotopes.
300uA up to 100mAh
Opportunistically it can support research activities
Strict control of radionuclide inventories
TR-30
Rigid system:
Beam at 5° for normal operation
Electroplated targets

## Slide 45
Handling and PIE capabilities

## Slide 46
TRIUMF is internationally recognized for its leading role in remote handling, hot cell design, operation and isotope processing. We are eager to co-develop and share expertise.
ARIEL hot cell facility currently being commissioned
ARIEL Hot Cell Facility

## Slide 47: Material Development for High-Power Accelerator Applications
High thermo-mechanical loads from high power driver beams
+
Material aging due to radiation induced defects
Materials development for ARIEL
Complex in-beam geometries
Target station dose rates (damage in insulators and seals ~1MGy-500MGy )
CuCrZr ARIEL beam window
allowing higher power operation
~10DPA-FLUKA/year range
Research on radiation resistant materials
Polymeric materials
HEA alloys
AM manufacturing techniques
Understanding differences between low energy ion, high energy proton and neutron irradiations
Experimental data from parasitic irradiations:
Save beam time
High power beam conditions

## Slide 48: Examples Target Damage Learning Experience
Irradiation damage - misaligned target and protect monitor
After installation of target protection by 4 segment halo monitor.
Be targets lifetime: 1024 p/cm2 800 mA-h
6 positions for targets Be, C, Cu,
Be muon target

## Slide 49: Radiation Damage Issues
300-350 ºC for 1 mm proton beam
Pyrolytic graphite vacuum brazed to TiCuSi foil and soldered to copper saddle
Proc. 2005 PAC
Radiation-cooled thin graphite targets 2 mm at 100 μA lasted for many weeks but eroded at 120 μA and small beam size.
Failure of 1 cm water-cooled graphite target after 1-2 weeks at 120 μA – thermal + radiation damage