## Slide 1: IRRADIATION and characterization for MATERIAL SCIENCE at CIRIL-GANIL FACILITY
Platform for welcoming interdisciplinary researches at GANIL, CIRIL
Research center on Ions, Materials and Photonic, CIMAP
Dr Clara GRYGIEL
IRRSUD beamline coordinator
Deputy director of EMIR&A network
grygiel@ganil.fr

## Slide 2
1983: First experiment
39 years of running
Users: 600 physicists (50% foreigners)
Beam: about 5500 hours per year
2000 hours per year as pilot # High Energy
+ 1000 hours in parallel: Medium Energy
+ 1500 hours in IRRSUD
+ 1000 hours in ARIBE
GANIL campus
SPIRAL2
GANIL + SPIRAL1
2
Average numbers
Run the accelerator facility and Nuclear physics research
Run interdisciplinary physics research
(materials science, astrophysics, atomic physics and radiobiology)

## Slide 3: Beamlines for Interdisciplinary Research
CIRIL platform (J. Rangama, F. Ropars)

## Slide 4: High energies with CYCLOTRONS
IRRSUD
SME
 1 MeV/A
 10 MeV/A
C @ 95 MeV/A
U @ 24 MeV/A
D1
HE
Heavy ions at higher energies (from C to U)
flux up to 1010 ions.cm-².s-1
Rp to some hundred microns
Continuous measurement of flux
Beam sweeping up to 30cm²
4

## Slide 5: Interdisciplinary physics at GANIL Energy range
ARIBE
Swift heavy ions
Electronic excitations
5
surface
Highly charged ions
Potential energy
1500 µm
1013 cm-2
5 µm
> 1015 cm-2
100 µm

## Slide 6
Potential energy deposition EP
ARIBE
energy (MeV/A)
medium energy
high energy
IRRSUD
Gd2Ti2O7 119MeV U
 nm
Capture, decay, emission, sputtering
>> Nanostructure formation
SrTiO3
Xe31+ E = 110 keV
GANIL facility beamlines vs material modifications
LET (keV/µm)
El Said et al, NIMB 269-1234(2011)
Aumayr et al, JPCPM 23-393001(2011)

## Slide 7
1500 µm
5 µm
100 µm
Potential energy deposition EP
ARIBE
energy (MeV/A)
medium energy
high energy
IRRSUD
Defect formation by radiolysis
Collective effect: atomic motions by intense electronic excitations -> extended defects
>> Track formation, disorder, phase transitions, surface nanostructures
Electronic energy loss Se
Sattonnay et al, Acta Mat 60-22 (2012)
Gd2Ti2O7 119MeV U
 nm
Capture, decay, emission, sputtering
>> Nanostructure formation
SrTiO3
Xe31+ E = 110 keV
GANIL facility beamlines vs material modifications
LET (keV/µm)
El Said et al, NIMB 269-1234(2011)
Aumayr et al, JPCPM 23-393001(2011)

## Slide 8
1500 µm
5 µm
100 µm
Potential energy deposition EP
ARIBE
energy (MeV/A)
medium energy
high energy
IRRSUD
Defect formation by radiolysis
Collective effect: atomic motions by intense electronic excitations -> extended defects
>> Track formation, disorder, phase transitions, surface nanostructures
Electronic energy loss Se
Sattonnay et al, Acta Mat 60-22 (2012)
Gd2Ti2O7 119MeV U
<<< µm
 nm
Capture, decay, emission, sputtering
>> Nanostructure formation
SrTiO3
Xe31+ E = 110 keV
Frenkel pairs, Displacement cascades
>> Cavities, bubbles, dislocation loops, segregation, precipitation, amorphization, phase transitions
Nuclear energy loss Sn
GANIL facility beamlines vs material modifications
LET (keV/µm)
El Said et al, NIMB 269-1234(2011)
Aumayr et al, JPCPM 23-393001(2011)

## Slide 9: IRRSUD : Some numbers
9
Rp | 10,4 µm
Se | 4,61 keV/nm
Sn | 0,0079 keV/nm
ENSP surface | 584
36Ar10+
0,98 MeV/A
# 35 MeV
C 1,8g/cc
W 19,35g/cc
Rp | 4,2 µm
Se | 14,24 keV/nm
Sn | 0,0417 keV/nm
ENSP surface | 341
average flux, RT: 5e9 ions/cm².s
In 24H : fluence 4,3e14ions/cm²
at IRRSUD
(Rastered beam on 25cm²)
SRIM
Max: 5e10-1e11ions/cm².s

## Slide 10: In-beam conditions
Temperature
8 - 1300K
Energy: keV up to 0.3 – 100 MeV/A
Incidence
90° - 0°
Gas partial pressure
Online setups for material characterizations:
XRD
ALIX IRRSUD
Emission spectro
Gas release
FTIR
Mass spectroscopy
Sputtering
TOF or catchers
AODO (X-Y TOF SIMS in situ LEED Auger)
Absorption spectro
CASIMIR 15-300K
CESIR RT
DETAIL up to 1400K
FTIR
UV-Vis
External user setups
ex: MiniMecaSiC (CEA-DEN) or Raman (Orléans)
Ions: C to U multicharged
Beam scanning
+ Nuclear materials
10

## Slide 11: Gas release
GRAL
FTIR absorption of the gas mixture
Small hydrocarbons (up to 3 Carbons)
→Track creation at high stopping power in organic compounds
Picq et al, NIM B 151 - 76 (1999)
Dely et al, NIM B 236 - 145 (2005)
CIGAL
mass spectrometry
H2 formation, O2 consumption, CO, CO2
→Gas production during nuclear waste storage of organic compounds contaminated with actinides as Pu (gloves, ...)
11

## Slide 12: Absorption spectroscopy
CASIMIR
15 K - 300 K
→Nitrides
→ Polymers, fundamental mechanims
→ Effects in solids relevant to astrophysics and astrochemistry
CESIR
Room temperature
CHESOI
Special low volume chamber for
rare gas atmospheres (18O2)
Vibrationnal spectroscopy: FTIR, 8000 - 400 cm-1 Electronic spectroscopy: UV-vis 200 – 900 nm
DETAIL
High temperature & FTIR
Up to 1100 °C
Sall et al, EPL 102- 26002 (2013)
Balanzat et al, NIM B 105 - 1 (1995)
Pilling et al, Astronom & Astrophys 509 – A87 (2010)
Melot et al, NIM B 208 - 345 (2003)
12

## Slide 13: Structural - microstructural analyses
X-ray powder diffraction
CHEXPIR, on ME not anymore available
Grygiel et al, RSI 83-013902 (2012)
Sattonnay et al, Acta Mat (2013)
Grygiel et al, Acta Mat 140, 157 (2017)
“ALIX” setup
Only on IRRSUD
grazing incidence diffraction
simultaneous or sequential
→ Phase transition & structural modifications
→ Kinetics studies
13

## Slide 14: Sputtering
High energy
Low energy
Time of flight
Catcher
neutrals
charged particles
AODO
(X-Y TOF SIMS)
UHV
In-situ LEED - Auger
Hijazi et al, NIM B 269 – 1003 (2011)
In-situ Auger
Salou et al, RSI 84-095115 (2013)
Ex-situ analysis by RBS, ERDA, …
Toulemonde et al, NIM B 212 – 346 (2013)
14

## Slide 15: User’s instrumentation
In-situ traction on SiC fibers
Collab Prof M. Schleberger, Uni. Duisburg-Essen, Germany
In-situ UHV AFM
→ Creation of multiple nanodots by single ions, foldings on 2D
Jankowiak et al, NIM B (2013)
Akcoeltekin et al, Nature Nanotech 2 - 290 (2007)
H Lebius, M Schleberger Nature Nanotech 2, 290(2007), New J Phys 10-053007(2008)
E Gruber et al, J. Phys.: Condens. Matter 28, 405001 (2016); 30, 285001 (2018)
15

## Slide 16: Post-Irradiation Experiment techniques
High Resolution X-Ray Diffraction
D8 discover Bruker, Cu anode
4-circles, in-plane geometry
Transmission/Scanning Electron Microscopy and FIB
ARM JEOL 200kV equipped with EELS (Gatan)
HELIOS NANOLAB 660 FIB
PIPS II Gatan
Raman spectroscopy
Atom Force Microscopy
  NX10 Parks Systems
- - and many others…
16
Structural Characterizations:
Surface Characterizations:

## Slide 17: CIMAP-GANIL FACILITY
Access through call for proposals (iPAC, EMIR&A, RADIATE)
Accepted proposals: beamtime during 3 years in backlog
2023: 4/5 months of beamtime (march -> july)
Beamline renovation work: IRRSUD 2022, ME 2023, HE 2024
Cyclotron renovation at GANIL (not yet scheduled)
Beamtime free for scientific collaborations
In-situ and Post-irradiation techniques are available
PIE: various costs depending on techniques (mainly for MEB/FIB/TEM)
4 Beam lines/4 Energy ranges
17

## Slide 18
Director: Dr Nathalie MONCOFFRE
Deputy directors: Dr Marie-France BARTHE
Dr Clara GRYGIEL
IRRSUD and ME beamlines part of EMIR&A

## Slide 19
EMIR&A network
15 accelerators, 11 ion and electron irradiation platforms on 6 sites
From fundamental research to Applications
Irradiation effect in materials and molecules (including radiolysis)
Ion beam analysis
Research Federation (FR) of CNRS, linked mainly to 3 Institutes :
Institute of Physics (INP), Institute of Nuclear and Particle Physics (IN2P3) and Institute of Chemistry (INC)
Research Infrastructure on the MESRI National roadmap

## Slide 20
EMIR&A network

## Slide 21
https://emira.in2p3.fr/
EMIR&A network

## Slide 22
EMIR&A network

## Slide 23
Thank you for your attention
http://cimap.ensicaen.fr/
https://emira.in2p3.fr/
https://www.ganil-spiral2.eu/