## Slide 1: Radiation damage R&D Fermilab Updates
Sujit Bidhar
Target Systems
Sep. 22, 2022
RADIATE Workshop

## Slide 2: Outline
HiRadMat -43 test Beryllium profilometry
Nanofiber target R&D
Graphite ion irradiation Implementation of new technique-
  Transient Grating Spectroscopy to graphite swelling
  LDV (Laser Doppler Vibrometer) to electron irradiated graphite
Titanium fatigue and fatigue tester development
High Entropy alloy

## Slide 3: Beryllium PIE HiRADMat-43
Implemented the increase in yield strength in J-C material model for out of plane deformation simulation
Tensile tests @PNNL
40-45% increase in yield strength due to irradiation
Yield strength :
: Equiv. plastic strain
: Plastic strain rate
: Homologous temperature
A : 432 MPa
B :1280 MPa
C : 0.009
n : 0.5
m : 1.3
Evaluated experimentally by split-Hopkinson pressure-bar test for unirradiated S200FH*

## Slide 4
HRMT 43- Beryllium Array1-288bunch- Irradiated
Chart: Distance across beam center, µm
Beam on 8.37 µsec
Peak energy deposit 6.28e14 w/m3
Peak Temp. 1065 C
Chart: Distance across beam center, µm
Simulation correctly predicted experimentally observed out of plane deformation for irradiated samples
Unirradiated sample shows reverse trend under further investigation

## Slide 5
Temperature distribution at end of beam heating
HiRadMaT 43 Graphite Slug Analysis
strain gage
LDV
Temperature gage
Circumferencial strain
Axial strain
Better result incorporating batched beam structure.
Difference in base line of simulation and experimental result due to sudden beam interaction with strain gage.

## Slide 6: Nanofiber target
Electrospinning Set up
1mm thick nanofiber coat
Production
Sintering
Characterization
XRD
AFM on single nanofiber
Single point indentation
Modulus same as bulk
Modulus mapping
To negate thermal stress wave and high cycle fatigue

## Slide 7: Beam test on nanofiber
Ion irradiation(in-situ TEM)
1 MeV Kr2+ ion
3.25x1015 ions/cm2  5dpa equiv
No measurable change in lattice parameter.
No defects formation.
Nanofiber may offer better resistance to radiation damage.
TEM before irradiation
TEM after irradiation
Thermal shock expt- HiRADMat-43 (CERN)
Proton beam 440 GeV, Beam σ 0.25mm
1.21x1013 protons on nanofiber in 4µsec
Low packing density samples survived.
Holes, crack in higher density samples
Low packing density
High packing density

## Slide 8: Thermal shock simulation on nanofiber mat- HiRADMat -43
Rapid heating of target pressure shockwave for a higher packing density target
Higher packing density reduces airflow induced by beam heating (natural convection) which exerts higher pressure on fibers
3D- fiber level simulation in progress
Low packing density
2
0
4
6
8
10
X106 Pa
High packing density
2D meso scale simulation (ANSYS FLUENT)
Bhattacharya model:
Pressure distribution@ end of beam heating

## Slide 9
Graphite Irradiation Studies with Low Energy Heavy Ions
POCO ZXF5Q
@ Michigan Ion Beam Lab 4.5MeV He++
Irradiation temp. 1000C
Comparable lattice parameter change.
Similar changes in Young’s modulus.
Further verification required:
Compare type of defects and number density of defects
Other physical properties  failure strength, yielding, K,CTE
Can low energy heavy ion mimic high energy proton beam?
Lattice parameter Vs dpa
Modulus Vs dpa

## Slide 10
Pulsed laser beams, 500 ps, λ500nm, few mJ
SAWs
Interference generate periodic pattern
Absorption of the light within the intensity grating
spatially periodic temperature profile
rapid thermal expansion creates two monochromatic, counter-propagating SAWs
Surface Acoustic Wave (SAW) velocity,
Slow decay low stiffness
Spot Size: 50~500 µm
Transient Grating Spectroscopy (TGS) on proton-irradiated Graphite (NTO2)

## Slide 11: Sensitivity of TGS
10% swelling
50% swelling
He filled Frankel defect Lattice swelling and reduction of SAW speed
x
y
Gaussian beam in x direction
sigma 1.1mm
Proton beam 120GeV
Peak Fluence: 8.6x1021/cm2
z
y
TGS is sensitive to slight change in mechanical property.
Along horizontal direction
Along vertical direction
S.Bidhar, NME 2020

## Slide 12: LDV for in-situ target health monitoring
There is clear change in frequency and magnitude of displacement
NTO2 Target Fin
Transient thermal-structural analysis

## Slide 13: LDV on electron-irradiated graphite
Electron Irradiation at SIRIUS (Ecole Polytechnique)
Energy : 2.5MeV
Fluence: 3.4x1019/cm2 ~0.017dpa
Irradiation area : 19x19 mm
10mm
LDV Measurement by Polytec
Excitation : 100 kHz
Piezoelectric at bottom
There is a difference in amplitude and frequency of LDV velocity due to electron irradiation

## Slide 14: Titanium Fatigue- SN Curve- all specimen
R=0.45
Chart: Number of Cycles
| 4151950 | 5398333 | 1 | 4563283 | 65326 | 186679 | 10043672 | 10211769 | 305694 | 76047 | 6615772 | 12706777 | 62711 | 20677025 | 4000000 | 15520861 | 15702552 | 10807028 | 38084707 | 8776335 | 11432914 | 5150226 | 4738577 | 18465211 | 58049 | 4045662 | 2885883 | 69979 | 3838387 | 24528877 | 18898919 | 4666279 | 6698491 | 10843250 | 134201
Smax | 751.9769 | 765.5864 | 0 | 664.5013 | 862.6956 | 849.6029 | 848.7789 | 767.7858 | 808.019 | 852.014 | 830.5354 | 811.1849 | 886.3467 | 950.775 | 0 | 681.4591 | 851.5306 | 645.7454 | 715.4734 | 831.3566 | 831.7085 | 857.7847 | 914.6905 | 0 | 0 | 0 | 935.8618 | 695.7734 | 634.5473 | 952.1824 | 941.6799 | 920.1233 | 807.8382 | 769.3697 | 749.4417 | 646.5289 | 695.7734 | 756.008 | 650.6027 | 699.1283
Non Irradiated
Irradiated
Gr23
Gr5-Batch2
Gr5-Batch3
Gr23
Irradiation reduced fatigue life.
Spread is too much in unirradiated samples.
No. of sample tested are few.
Need to benchmark the results of custom-fatigue tester.

## Slide 15
ASTM B592
Upgrading a commercial bend fatigue tester
ASTM standard sample failure in unexpected mode
Mechanical cut-off switch which only activated when failed catastrophically (safety issues)
Fatigue machine needed some modification
Should have failed here
Instead, failed here
Should have failed here
Extra moment
Limit switch for cut-off
Missouri state university

## Slide 16
Upgrading a Bend fatigue tester
Failure at expected location
Double bearing grip for sample tip
Grip location detached from connecting rod pin
Electronic cut-off switch for automatic crack detection
Prof. Abiodun Fasoro, Univ. Visiting faculty Program
To connecting rod

## Slide 17: Novel Material (Nanofiber, HEAs) Development
Kavin Ammigan was awarded with Early Carrier Award (ECO)
  $2.5M for 5 years
Simulations on radiation damage in HEAs planned to start this year (October) with the hiring of a postdoc
    Alloys consisting of 3 or more principal elements
    Excellent inherent properties including enhanced radiation damage resistance
C. Lu, L. Et al., Nat. Commun., 7 (2016), p. 13564
Reduction in irradiation-induced void distribution in nickel and multi-component HEAs after 3-MeV Ni+ ion irradiation at 773 K
(a) Conventional alloy, (b) High-entropy alloy (Miracle & Senkov, 2016)
(a)
(b)
A. Couet

## Slide 18
Beam parameter: 288 bunches, σ: 0.25mm, POT 3.7x1013 /7.85µsec
Beam time : 4th week of October 2022
List of materials to be tested :
Unirradiated : Graphite (POCO-ZXF5Q, IG430), nanofiber (ZrO2, ZrO2-SiO2, ZrO2-TiO2),Beryllium
(PF60, S200F), Sigraflex , Ti6Al4V, Timet 1100, Ti6246,Ti15-3, DAT54, High
Entropy Alloys, TFGR, pure W, Slugs (Beryllium, Ti6Al4V, NITE)
Irradiated : Graphite (POCO-ZXF5Q, IG430), MoGr, Sigraflex, Beryllium( S200FH, S200F),
Ti6Al4V( Gr 23, Gr5, Gr6), Ti15-3
Instrumentation (strain/ temperature gages) installed ,tested on slugs.
All samples were packed in holders inside array boxes and on their way to CERN
Next HiRADMat test- HRMT-60

## Slide 19
Simulation He bubble in Beryllium Jianqi Xi at Univ of Wisconsin
Raman spectroscopy on Nuclear graphite Eric/Dong Liu at Univ. of Bristol
BLIP irradiated Beryllium PIE  Dave/Andy at PNNL
Profilometry, microhardness of BLIP/HRMT Beryllium  Slava at MRF
High Entropy Alloy (HEA) development  Adrien Couet at Univ. of Wisconsin
Collaboration activities with other institutes
A. Couet
A. Couet
S. Kuksenko
A. Casella
D. Liu

## Slide 20
Thanks for your attention!