## Slide 1: Oxford University
James Marrow
(james.marrow@materials.ox.ac.uk)

## Slide 2: Current Work
Graphite
  Deformation mechanisms in graphite crystals (HOPG) and bulk graphites at elevated temperatures
  Effects of irradiation on graphite crystal deformation
Titanium
  Ultrasonic fatigue testing of meso-cantilevers
  Effects of ion-irradiation

## Slide 3: HOPG: Spherical Indentation
Chart: Displacement (nm)
Chart: Displacement (nm)
(~10 µm diameter
Strong effect of temperature

## Slide 4: HOPG: Spherical Indentation
1 µm
25°C
1 µm
300°C
2 µm
400°C
500°C
3 µm
600°C
1 µm
200°C
2 µm
Strong effect of temperature
all at 50 mN peak load

## Slide 5: HOPG: Spherical Indentation
Chart: Temperature (°C)
| 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 200 | 200 | 200 | 300 | 300 | 300 | 300 | 300 | 400 | 400 | 400 | 400 | 400 | 400 | 500 | 500 | 500 | 500 | 500 | 500 | 500 | 600 | 600 | 600 | 600 | 600
200 to 300 nm | 14.0036 | 14.2499 | 13.9465 | 14.4195 | 14.284 | 16.8343 | 14.0019 | 12.8125 | 13.8322 | 13.424 | 13.8365 | 14.3501 | 13.1755 | 14.4728 | 13.6304 | 13.6971 | 12.7932 | 13.2614 | 9.2773 | 13.2365 | 12.9301 | 12.2525 | 11.1739 | 10.4892 | 10.2804 | 12.7579 | 11.9575 | 6.5186 | 6.8286 | 6.4757 | 6.643 | 6.6373
500 to 600 nm | 14.5817 | 14.7507 | 14.57 | 18.7281 | 14.2965 | 13.5715 | 14.0919 | 13.5735 | 13.7256 | 13.9587 | 14.4523 | 13.7674 | 13.7804 | 6.8475 | 10.2741 | 9.4188 | 8.7628 | 8.4245 | 10.6272 | 6.4462 | 7.4556 | 6.2016
800 to 900 nm | 14.5245 | 14.3731 | 19.3582 | 13.7094 | 14.0362 | 12.6485 | 12.7248 | 13.8622 | 13.7423 | 5.2982 | 7.9666 | 7.3005 | 6.8588 | 9.3166 | 6.7223 | 5.0068
Chart: Displacement (nm)
Strong effect of temperature

## Slide 6: HOPG: Spherical Indentation
1 µm
1 µm
200°C
25°C
100 mN
100 mN
0.5 µm
600°C
50 mN
(a)
(c)
(b)
(i)
(ii)
0.2 µm
25 mN
25°C
Kinking and buckling more prevalent at high temperatures
Postulated mechanism: Effect of temperature on crystal shear modulus C44, relative to C33 and C11
﻿10.1016/j.carbon.2022.01.067
Strong effect of temperature

## Slide 7: Ion-Irradiation (Dalton)
HOPG irradiated to 1 dpa by C2+ ions at: 25°C (RT), 200°C, 400°C and 700°C
Irradiated (RT)
Irradiation decreases modulus!
Continuous stiffness measurement

## Slide 8: Cross-Section TEM (room temp indentations)
Non-irradiated
Irradiated (RT)
Irradiation causes change in kink band size

## Slide 9: Work in Progress
Indentation (and annealing) of irradiated HOPG up to 700°C
Post-indentation cross-sectional TEM (no pop-in)
Bulk Graphite
Imaging
Diffraction
Gilsocarbon (ambient T)
﻿10.1016/j.carbon.2020.03.020
Neutron and X-ray diffraction

## Slide 10: Gen IV Graphite (high T)
Unloaded (RT)
Loaded (RT)
Electrically heated, Mechanically loaded
Diamond Light Source, UK, (Preliminary tests: Nov 2021
Continuation: Dec 2022)
Radiography (3.3 x 2.8 mm)
Disc Compression
  5 mm diameter
  2.8 mm thickness
  SNG742
60 keV monochromatic X-rays
W-powder ‘speckle’
1 mm
~700°C
Strain Mapping by Imaging

## Slide 11
Unloaded (RT)
(00.2)
(00.2)
Raw data (2D diffraction, 100 µm x 100 µm slits
Azimuthal integration
Diffraction
Mapped Area 2.5 mm x 2.5 mm
Stress Mapping by Diffraction
Test specimen
60 keV monochromatic X-rays
Gen IV Graphite (high T)
Work in progress

## Slide 12: Graphite: Conclusion
On-going work to investigate effects of temperature and irradiation on HOPG (‘single’ crystal)
On-going work to investigate effect of temperature on deformation of fine-grained polygranular graphites
Other studies:
  Neutron Bragg edge imaging to investigate crystal reorientation under load
  Crack nucleation and propagation in graphite (in situ µXCT)
  MAX-phase ceramics
    High T indentation, x-section TEM, ion-irradiation
    In situ synchrotron X-ray radiography and diffraction for strain mapping at high temperature

## Slide 13: Meso-scale Mechanical Testing of Proton Beam Window Materials Lazuardi Pujilaksono, Angus J Wilkinson, Jicheng Gong Micromechanics Group, Oxford University

## Slide 14
Proton accelerator

## Slide 15: Ti-6Al-4V window for the proton beam
The proton pulses lead to thermally induced high-cycle fatigue loads on the beam window
Pulsed proton beam

## Slide 16: Driving force
The pulsed proton beam energy will be increased to 1.2 MW in the Long Baseline Neutrino Facility (LBNF)
Will further upgrade from 1.2MW to 2.4 MW in the future
Super-K aims to increase the proton beam power from 500 KW to the 1.3 MW level

## Slide 17: Why meso-scale mechanical tests?
Significantly more specimens
1000 times smaller. Low activity and easy to handle and dispose
Low cost
More flexibility
The size is comparable to the real component
Bulk specimens
Meso specimens
2.7 mm

## Slide 18: Materials
Current proton beam window materials:
Interested materials:
CP-Ti
Ti-6Al-4V with different heat treatment
Beta Titanium including Ti15 and Ti-333
Ti-6Al-4V

## Slide 19: Two batches of irradiated titanium meso-cantilevers
Down stream Ti1: Ti-6Al-4V. This is the same material as the proton beam window at J-PARC. The irradiation level is 0.25 DPA
Down stream Ti2: Expanded the materials from Ti-6Al-4V to CP-Ti and Beta titanium alloys. The irradiation level is 1 DPA.

## Slide 20: 1st batch: Ti-6Al-4V beam window materials, 0.25 DPA
253
260
258
257
258
262
257
260
256
257
252
261
243
255
257
262
259
256
255
259
257
253
260
257
253
Thickness measurements (µm)
48 mm

## Slide 21: 1st batch: specimen design, layout and micro-laser machining
3.4 mm

## Slide 22: 2nd batch of proton irradiated titanium (Part II BLIP irradiation run), 0.95 DPA
250 m = 150 m + 100 m
Four half foils in total
Layer one
Layer two

## Slide 23
Five foils of different titanium materials or heat treatment
 | Material | Thickness (m) | Dimensions (m×m) | Resonant frequency (Hz) | Irradiated?
Foil one | Grade 2 CP-Ti Cold rolling and annealed | 100 | 1000 × 400 | 31113 | Yes
Foil two | Ti15 Solution treated | 100 | 800 × 400 | 30155 | Yes
Foil three | Ti-64 Annealed at 595 ⁰C for 3 hours | 132 | 1000 × 600 | 30160 | No
Foil four | Ti-64 Annealed at 595 ⁰C for 3 hours | 148 | 1000 × 650 | 31207 | Yes
Foil five | Ti-64 | 153 | 1000 × 675 | 31186 | Yes

## Slide 24: 2nd batch, design, layout and micro-laser machining
D 24 mm
116 specimens on a half foil
22 – 27 specimens in the R12 mm hot area
78 specimens without radiation

## Slide 25: Current work on pre-irradiated Ti-6Al-4V materials from RAL
4 cm
2.25 cm
The samples used in this study came from new Ti-6Al-4V beam windows; therefore, the studies we conduct have identical microstructures to real components
Machined into foils
Dummy proton beam windows

## Slide 26
Primary α
Transformed β
Bimodal microstructure of Ti-6Al-4V

## Slide 27: Ti-6Al-4V Meso-cantilevers from dummy beam windows

## Slide 28
Static deflections tests of five proton irradiated materials and make comparison with non-irradiated titanium
Future plan 1: Static meso-cantilever tests, irradiated vs. non-irradiated
 | Material
Foil one | Grade 2 CP-Ti Cold rolling and annealed
Foil two | Ti15 Solution treated
Foil three | Ti-64 Annealed at 595 ⁰C for 3 hours
Foil four | Ti-64 Annealed at 595 ⁰C for 3 hours
Foil five | Ti-64
Load displacement response of a meso-cantilever
Premier nanoindenter

## Slide 29
High cycle fatigue tests of two candidate materials (Ti6Al4V and one other Ti material)
Future plan 2: Ultrasonic fatigue testing of irradiated meso-cantilevers
Meso S-N Curve of Ti-6Al-4V
 | Material
Foil one | Grade 2 CP-Ti Cold rolling and annealed
Foil two | Ti15 Solution treated
Foil three | Ti-64 Annealed at 595 ⁰C for 3 hours
Foil four | Ti-64 Annealed at 595 ⁰C for 3 hours
Foil five | Ti-64

## Slide 30: Future plan 3: Design foils that can be irradiated at the cyclotron irradiation facility (MC40 ) at the University of Birmingham
Help design the foils, enabling irradiation of meso-cantilevers at the cyclotron irradiation facility at the University of Birmingham

## Slide 31: Thanks for your attention!