## Slide 1: Diamond sensors R&D
Alexander Oh
University of Manchester Results and material from the RD42 collaboration.
PPTAP Detectors Workshop

## Slide 2: Development of CVD Diamond for detector applications
Today two main manufacturers of detector grade diamond
  ElementSix Ltd UK
    polycrystalline wafers
    small single crystal diamonds
  II-VI Inc. USA
    large polycrystalline wafers
    development effort underway
Alternative sources
  Diamond on Iridium (DoI) (Audiatec, Germany)
  Hetero-epitaxially grown -> medium area
  Highly oriented crystallites.
5’’ waver
single crystal
DoI, 155ct
poly crystal 5 inch wafer, II-VI Inc.
Notes: 5 inch wafer (dots are 1cm apart)

## Slide 3: Development of CVD Diamond for detector applications
Impressive progress over the last 25 years.
Current state of the art for polycrystalline CVD diamond d ~ 320 mm in 500um thickness
  (~11500 e/MIP)
  commercially available.
  1995: d ~ 50 mm
  2000: d ~ 180 mm
  2020: d ~ 320 mm

## Slide 4: CVD Diamond development goals
removal of surface defects
  few per cm2 → < 1 per cm2
wafer CCD in pCVD
  400 um → 500 um
size of wafers = 15cm (6 inch) diameter state of art
  fixed by microwave frequency (not expected to change)
wafer uniformity
  5% → 2% across whole wafer.
price per cm2
  ~1500USD / cm2 → 800USD /cm2

## Slide 5: Radiation Hardness
Summary of RD42 irradiation results:
*normalized to 24GeV protons
”Back-of-an-envelope calculation, expect Schubweg of: l ~ 16mm at 1017 cm-2 protons_24 GeV_eq
*
Notes: 800 MeV proton update: https://indico.cern.ch/event/505107/contributions/1182410/attachments/1272791/1887710/RD42Meeting-May2016-800MeVResults.pdf
l = l_0 / (l_0 * k * Phi + 1)

## Slide 6: High Rate tests
neutron irradiated pCVD
Flat to better than 2% up to 10-20 MHz/cm2. Exploring systematics of O(1%)
Notes: ICHEP2020: July 29, 2020

## Slide 7: Carrier lifetime challenge – 3D diamond detectors
After large radiation fluence all detectors are trap limited
Mean free paths (schubweg) λ< 50μm
Need to keep drift length (L) smaller than mfp(λ)
Build 3D detectors to reduce transit time.
Huge progress made in fabrication of 3D diamond detectors in the last 10 years.

## Slide 8
  Lasered graphitic structures in pCVD (’10)
  Single crystal with column structure (‘11)
  Pico second laser for improved graphitic electrodes (‘12)
  Several Prototypes tested at Diamond Light Source CERN test beam RBI proton beam
  Clinical Photon beam
  Femto second laser processing and TCAD simulation (’13,’14)
  Phase modulated laser processing (’15,’16)
  Polarised & Phase modulated laser processing (’17,’18)
  Prototypes with poly and single crystal diamond (2019 ++.
3D diamond? (2008)
UK made leading contributions to 3D Diamond detectors

## Slide 9: 3D diamond prototypes
CMS and ATLAS pixel prototypes tested:

## Slide 10: 3D diamond prototypes
CMS and ATLAS pixel prototypes tested:
HV=-55V
Eff. > 99.2%
RD42 Preliminary

## Slide 11: 3D diamond detectors challenges for the future
Optimise graphitisation process for 3D diamond production in terms of:
  Resistivity: currently at (1 - 0.1Wcm) aim for <0.1Wcm.
  Processing speed: currently O(10um/s), aim to speed up and/or parallel processing of wires.
  Wire thickness / uniformity: Little data available, needs more research effort.
Optimization of internal electric field
  Geometry: Recently internal cage structure optimise E field.
  Will explore the full potential (see later slides).
Radiation hardness:
  Need to check predictions with latest devices.
  25um cells in 3D.

## Slide 12: Resistivity challenge
Laser wave front shaping helps to decrease resistivity.
Dependence on processing parameters being studied.
More research needed to lower resistivity.

## Slide 13: Carrier lifetime challenge – 3D diamond detectors
Low field regions might effect transit time.
Preliminary simulations show not a concern due to diffusion.
More work needed to quantify impact of radiation damage.

## Slide 14: 3D diamond detectors: Radiation challenge
Few radiation hardness data available, but promising:
  Compare signal loss in 3D pixels to published results from planar
  3D sensors collect twice as much charge when unirradiated
  3D sensors see 5±10 % reduction in signal at 3.5 x1015
  Planar sensors see 45±5 % reduction for 3.5 x1015
3D cell size: 50um x 50um
Notes: 0.88 normalisation

## Slide 15: 3D diamond detectors Geometry challenge
Laser processing allows any geometry, including horizontal wires.
  Exiting possibility to optimise the electric and weighting field.
  Small cell sizes realizable, wire diameter at abut 1mm.
  Simulation studies currently ongoing.
Future research in this area:
  Optimise geometry
  Wire processing
  cell sizes <(25mm)2
  Simulation – Prototyping – Characterization.

## Slide 16: 3D diamond detectors Simulation challenge
Lack of build-in models, especially pCVD and traps / polarisation in current TCAD tools being addressed.
Need effort to improve simulations:
  polycrystalline CVD diamond, grain boundaries.
  graphitic wire simulation
  radiation damage
  new geometries
3D diamond simulation examples from RD42

## Slide 17: 3D diamond detectors Devices in future experiments
The BCM’ phase-2 project of ATLAS will feature a small area 3D diamond detectors.
  Prove technology readiness for small cells.
  Stepping stone for larger area application.
3D diamond detector
planar diamond detector
Notes: https://www.google.com/search?q=bcm%27+atlas&client=firefox-b-d&ei=ySSAYI6yKY6Ai-gP2tKnuA8&oq=bcm%27+atlas&gs_lcp=Cgdnd3Mtd2l6EAMyBggAEBYQHjoHCAAQRxCwAzoECAAQHjoICAAQFhAKEB5QoxFYmRpgjxtoAXACeACAAU-IAYwEkgEBN5gBAKABAaoBB2d3cy13aXrIAQjAAQE&sclient=gws-wiz&ved=0ahUKEwjOutmKtY_wAhUOwAIHHVrpCfcQ4dUDCA0&uact=5

## Slide 18: 3D diamond detectors Possible FCC devices
3D seems to be a viable option to enhance radiation tolerance.
Radiation hardness requirement and resulting l dictate cell size.
Cell size determined by wire-diameter (1mm) and cell capacitance.
(25mm)2 or even below seems feasible.
  Loss of efficiency small at 1017 peq mm drift path vs l=18 mm
  Leakage current not an issue.
Main technological challenge for large scale application is the scaling of wire production.

## Slide 19: Summary
Polycrystalline CVD diamond.
  Collection distance 25% increase.
  Decrease price by 50% (happens with larger use as in Si).
Radiation tolerance.
  Go to smaller cell size.
  True 3D field electrodes (internal cages) offer huge potential to optimize electric field distribution to minimize drift time.
  Also offer possibility of gain in diamond.
Processing of 3D graphitic wires in diamond.
  Reduce resistivity.
  Scale production capability.
The UK has made leading contributions to this field.
  Exploring funding routes to sustain effort.

## Slide 20: Discussion

## Slide 21: BACKUP

## Slide 22: Diamond properties
  Low dielectric constant  low capacitance
  Low leakage current  low noise
  Room temperature operation
  Fast signal collection time
Property________________ Diamond____ Silicon
band gap 5.47 1.12
mass density [g/cm3] 3.5 2.33
dielectric constant 5.7 11.9
resistivity [Wcm] >1011 2.3e5
breakdown [kV/cm] 1e3...20e3 300
e mobility [cm2/Vs] 1700 1400
h mobility [cm2/Vs] 2100 440
therm. conductivity [W / cm K] 10..20 1.5
radiation length [cm] 12 9.4
Energy to create an eh-pair [eV] 13 3.6
ionisation density MIP [eh/mm] 36 89
ion. dens. of a MIP [eh/ 0.1 ‰ X0] 450 840
  MIP signal ~2 smaller at same X0
  Efficiency < 100% (pCVD)

## Slide 23: FCC first layer requirements
Unprecedented particle flux and radiation levels
10 GHz/cm2 charged particles
1018 cm-2 1 MeV-n.eq. fluence for 30ab-1
Rate & Radiation challenge
@ r=2.5cm

## Slide 24: Radiation Hardness
Irradiated polycrystalline and single crystal CVD diamond.
  Protons 25MeV, 70MeV, 300MeV, 800MeV, 24GeV
  Pions 300MeV
  Neutrons ~1MeV (TRIGA reactor)
Signal response tested in test-beam.
  120 GeV proton
  pad, strip and pixel-detector pattern, E = ±2V/mm
  Samples pre-exposed to Sr90 to fill traps (aka pumping)
  Require track on active area, no threshold on strip signals.
  Build signal of five highest contiguous signals within 10 strips around the track.
Notes: To be included in these k_factor determinations we have
to get the same signal (to within 5%? 10%?) for both polarities,
and then we plot the average of the two. All reference measurements
are at 1000V, typically on a (500+/-20) micron thick sensor.

## Slide 25: Radiation Hardness
“Charge Collection Distance” (CCD) is measured.
Traps reduce the life-time of charge carriers, or “Schubweg” (l).
  Relation between CCD and l:
damage constant
particle fluence
Radiation damage is fitted
with simple damage model:

## Slide 26: Radiation Hardness (planar)
Scaling to 24 GeV protons
  Universal scaling for all particle types with fluence.
  Poly and single crystal diamond show consistent damage constants.
  Predictions are possible for any particle type and fluence.
https://www.research-collection.ethz.ch/handle/20.500.11850/222412
Notes: kl = 0.67 ± 0.04 ×10-18 cm2mm-1

## Slide 27: Radiation Hardness: Signal Uniformity

## Slide 28: High Rate tests
Tests the pulse height as function of particle rate.
Test single and poly crystalline diamond.
Irradiated and un-irradiated.
100um
Notes: ICHEP2020: July 29, 2020

## Slide 29: High Rate tests
Raw Data from 10 MHz/cm2 Flux
Notes: ICHEP2020: July 29, 2020

## Slide 30: 3D diamond detectors: Characterization challenge
TPA demonstrated.
More accurate ionization profiles possible using same beam shaping techniques as in production of wires.
Research needed to fully exploit technique for characterizations.
https://www.research-collection.ethz.ch/handle/20.500.11850/445547
Notes: https://www.research-collection.ethz.ch/handle/20.500.11850/445547