## Slide 1: Sense and Sensitivity
XinRan Liu
The University of Edinburgh
Confronting the radiological screening challenges for next-generation rare event detectors

## Slide 2
Overview
Currently DM + 0vbb Landscape
1
2
3
G3 + 0vbb Backgrounds Requirements
Current Material Assay Techniques
4
R&D Upgrades
Notes: Throughout my time in particle physics the issue of how to make early career scientist feel at ease as well as standout in ever growing collaborations has always been one of my highest concerns.
For these reasons, I joined the LZ E&I committee since its approval by the EB and IB in 2018 and was proud to hold the position as the first chair at the start of 2020. As part of my time as chair I oversaw the formation of the the early career committee - LZ-GETUP with some 90+ members.
In considering the critical role the LZ-GETUP committee would play and wanting to establish a solid foundation upon which the committee can flourish, I met with the chair of SNOWMASS Early career and other early career committees from DUNE and ATLAS to share best practice. I also represented LZ in APS-Inclusion, Diversity and Equity Alliance workshops.
After I stepped down as chair of the E&I committee it was a logical transition to drive forward LZ-GETUP. I was elected as the IB representative a role created to increase communication with the IB in both directions: Firstly for early career members to understand what decisions were made and how, and 2 for IB to be able to hear from junior members on those decisions as well as issues junior members considered important.
For goal #1, my part was simply listening to the IB meetings, taking notes on the discussions, and then relaying the notes to LZ-GETUP members in a timely manner, highlighting items that I thought would be of broad interest.
For goal #2, I was expecting more resistance in making our opinions heard, but in practice, I think that simply having an LZ-GETUP representative in the IB meetings made all IB members more aware that they should be working to be more inclusive of all opinions when making decisions. This resulted in the IB soliciting our opinions by asking us to provide individual feedback on a number of issues. Personally, I see this as an even better outcome than expected.
I am also a member of the working group for the EDI committee at the University of Edinburgh - School of Physics and Astronomy.
Finally over the past year I have worked closely with the IOP to produce promotional material to encourage nominations for early career medal and prizes. As treasurer of the IOP APP group I am also asking the IOP to allow us to create new awards for early career contribution to EDI and Public Engagement.

## Slide 3
Liquid Xenon Experiments
LUX
PANDAX-II
XENON1T
250 kg
(100 kg)
580 kg
(362 kg)
2,000 kg
(1,042 kg)
3.4x10-46 cm2
2.5x10-46 cm2
7.7x10-47 cm2
2013
2016
2017
2.6x10-48 cm2
1.4x10-48 cm2
2022 + 3 live years
2022 + 5 live years
LZ
XENONnT
7,000 kg
(5,600 kg)
5,900 kg
(4,000 kg)
Typical detector improvements:
Mass
Detector components
Detection and analysis methods
Improve background
PandaX – 4T
6 x10-48 cm2
202x + 5 live years
4,000 kg
(2,800 kg)

## Slide 4
Current Landscape

## Slide 5
NO unicorns in this magical forest
Maybe here?
Current Landscape

## Slide 7
Liquid Xenon Experiments
LUX
PANDAX-II
XENON1T
250 kg
(100 kg)
580 kg
(362 kg)
2,000 kg
(1,042 kg)
3.4x10-46 cm2
2.5x10-46 cm2
7.7x10-47 cm2
2013
2016
2017
2.6x10-48 cm2
1.4x10-48 cm2
2020 + 3 live years
2020 + 5 live years
LZ
XENONnT
7,000 kg
(5,600 kg)
5,900 kg
(4,000 kg)
Darwin/G3
1x10-49 cm2
2023 + 7 live years
50,000 kg
(40,000 kg)
Typical detector improvements:
Mass
Detector components
Detection and analysis methods
Improve background
PandaX – 4T
6 x10-48 cm2
2020 + 5 live years
4,000 kg
(2,800 kg)

## Slide 8
Detector recipe:
Neutrinoless Double Beta Decay

## Slide 9
The earth is unfortunately a radioactive planet and in the case of Dark Matter and , the ‘signature’ of each process are similar to that of natural radioactivity.
The Challenge

## Slide 10
The Challenge
Requirements for next generation dark matter and 0vbb experiments:
  Upgrade HPGE to reach < 10 μBq/kg levels
  Increase radon emanation throughput with greater sensitivity
  Improve surface alpha radioassay sensitivities
  Improve ICPMS sensitivity to < ppt/ppq levels
  Coordinated international efforts to cross calibrate existing facilities and continued improvements.
Golden rule: Everything is radioactive, quantify
panic level via screening.

## Slide 11
The Solution
Mass Spectrometry, NAA
Gamma-ray Spectroscopy
Radon Emanation
Optical Microscopy
Alpha detectors

## Slide 12
One Lab To Rule Them All
Boulby UnderGround Screening (BUGS) Facility
A jewel in the crown of the Boulby Underground Laboratory
Facility designed to become a centre of excellence for material assay and cleanliness
Class 1,000 cleanroom
New nitrogen system to produce large quantities.
Minimal Rn reduction required, ~2.5 Bq/m3 ambient
Hugely important to current and future rare event search material selection

## Slide 13
Gamma-ray Spectroscopy
The ambitious programme to reboot and expand the UK underground screening facility launched in 2013.
2013
2016
Starts with refurbishment of the existing p-type coax – renamed Lunehead
In 2016 added 3 S-ULB detectors in purpose-built castles.
In 2021 S-ULB SAGe well detector commissioned
2022

## Slide 14
Radon Removal System
A radon removal system was designed and built, capable of removing the radon from the carrier gas by up to 10 orders of magnitude depending on the gas.

## Slide 15
Germanium Detector Background
Belmont
160% (3.2kg) p-type

## Slide 16
Germanium Detector Background
Belmont
160% (3.2kg) p-type
214Pb at 352 keV – 150x reduction

## Slide 17
Germanium Detector Background
Able to hit ~100 μBq/kg with Belmont and Roseberry
New S-ULB SAGe well added, detector only shielded on 16/08/21!
Detector | Relative Efficiency or type | Count rate (/kg/day) |  |  |  | 
Detector | Relative Efficiency or type | 351 keV (214Pb) | 609 keV (214Bi) | 238 keV (212Pb) | 1461 keV (40K) | 2615 keV (208Tl)
Roseberry | BE6530 | 0.15(7) | 0.15(7) | 0.8(3) | 0.8(2) | 0.2(1)
Chaloner | BE5030 | 5(1) | 4(1) | 7(1) | 8.4(14) | 2.1(5)
Belmont | 160% | 0.7(2) | 0.4(1) | 0.13(6) | 1.0(2) | 0.3(1)
Merrybent | 100% | 2.5(3) | 1.8(3) | 0.3(1) | 1.9(3) | 0.8(2)
Lunehead | 100% | 5.6(5) | 4.7(4) | 8.3(5) | 9.1(6) | 2.0(3)
Lumpsey | SAGe-Well | 104(2) | 60(2) | 166(3) | 7.0(6) | 12(1)
1.1(7)
1.3(3)
1.1(7)
1.7(7)
0.7(2)

## Slide 18
XIA UltraLo 1800 – Alphas
As of 2021, two XIA UltraLo-1800 surface alpha counters running at Boulby – Kettleness & Ormesby.
Installed liner to reduce detector backgrounds.
Factor three improvement compared to surface lab due to more cosmics which can mimic background events.
Sample | Duration (hrs) | Alphas | Surface Area (cm2) | Emissivity (⍺/khr/cm2) | Activity (mBq/m2)
Background (SS Tray) | 168 | 342 | 1800 | 1.24 ± 0.07 | 6.88 ± 0.38
Background (PTFE Liner) | 168 | 103 | 1800 | 0.38 ± 0.04 | 2.12 ± 0.22
PNNL Copper | 168 | 13 | 707 | 0.13 ± 0.04 | <0.72 ± 0.22

## Slide 19
Electroforming Copper
STFC awarded funding for ‘scope, feasibility and costing’ study of establishing an electroplating facility in Boulby.
  Lead by NEWS-G and ECuME experience.
Survey ongoing to assess UK interest.
https://www.surveymonkey.co.uk/r/7JLT2DW
Still open and takes <2 minutes.
This is highly complementary to the BUGS facility and existing detectors.

## Slide 20
Boulby Radon Emanation System

## Slide 21
The Boulby Radon Facility - Sensitivity
Sensitivity based on the performance of the UCL system, but there are several changes.
  New detector has lower background by factor 4.
  New detector must use nitrogen instead of helium, demonstrated comparable detection efficiency.
  The new system is entirely constructed by swagelok with integrated external components.
Large Volumes of gas at ~ 5 μBq/m3
Radon Emanation ~ 100 μBq per sample

## Slide 22
Cold Radon Emanation Facility
The worlds first cryogenic radon emanation system.
2 emanation chambers available:
A 2.7 L chamber, operational at several fixed temperatures.
A 200 L chamber, which can be cooled and stabilised at temperatures down to ~77 K.
  Allows measurements of whole detector components.
  Enables studies of emanation rate as a function of temperature.
Goal: to deliver a world-leading sensitivity <0.1 uBq/kg to 222Rn emanated from materials at temperatures of *relevance to rare-event searches.
*e.g., LXe & LAr temperatures.

## Slide 23
ICPMS
Dedicated low-background facility at UCL inside a class 6 cleanroom.
Fast: 1-2 samples/day
Sensitivity of 10 ppt for 238U & 232Th
Requires expertise in sample preparation.

## Slide 24
Outlook
“Yesterday’s discovery is today’s calibration…”
(R. Feynman)
“… and tomorrow’s background”
(V. Telegdi)
We have started R&D programme.
We would like to establish BUGS as a center of excellence for screening and cleanliness and the UK as the world leader in material assay.
We need to develop new assay techniques
  Multi-array HPGE in coincidence
  Cold Radon Emanation
  Improved surface and bulk alpha sensitivity - new detectors
  Watch this space!

## Slide 25: Thank you for listening!
Any Questions?