## Slide 1
Overview
Current and future activities in HEP detectors at RAL PPD
1
03/07/19
E. Giulio Villani, RAL

## Slide 2: PPD past Silicon Projects
HEPAPS CMOS MAPS sensor
  0.25um CIS TSMC/IBM
  Developed ‘ad hoc’ radiation models
DNW CMOS MAPS
  Patented Triple Well for Charge collection
MI3
  Intelligent imaging
TPAC for CALICE
  50x50 um pixels tracking ECAL for ILC
  0.18um MAPS based Si-W ‘TeraPixel’ system
  Deep PW for improved CCE
  Extensive beam and laser test
Cherwell MAPS sensor (25x25um)
  0.18um CMOS Not rad hard
  Prototype for tracking and digital calorimetry
  Charge collection by diffusion
  Tested and Paper out soon
CHESS-2
  Testing rad hard HV-CMOS sensors
AIDA 2020
  TCAD simulations for the development of CMOS detector models
Most (all) current HVCMOS structures share the same topology initially proposed by us

## Slide 3: PPD current Silicon Projects
OverMOS 1, 1.1, 2.0 MAPS prototype sensor
  Rad Hard Pixel Monolithic HR-CMOS
  Multiple structures and substrates
  Neutron irradiation
  3D TCAD modelling
DECAL MAPS sensor (50x50um)
  0.18um Rad Hard Pixel Monolithic HR-CMOS
  40MHz global shutter
  Charge Collection by drift
  Configurable with in-pixel electronics
  For digital calorimetry and outer tracking at FCC
  In publishing stage
CMOS dosimetry
  0.18um SL CMOS FG based dosimeter
  Aimed at biomedical applications
  Sensitivity to 1 rad gamma doses
M1
STI

## Slide 4: PPD future Silicon Projects
RD50 Schottky for radiation damage investigation
  RD50 proposal for epi Schottky fabrication
  Aimed at radiation damage investigation of P epi for CMOS TCAD modeling
  Design, fabrication, testing, analysis at RAL
Low Gain Avalanche Detectors (LGAD)
  Investigation of LGAD for Phase II ATLAS/CMS Upgrade
  Candidates for LHC-b Upgrade
  General applications as Ultra Fast Detectors (UFDs) in future HEP experiments
  Joint collaboration with Te2V, Oxford, Birmingham

## Slide 5: SW Tools
Synopsys TCAD simulations
We routinely use 4 – 5 machines simultaneously
Process fabrication simulations
Opto-electrical-thermal devices 3D simulations
Radiation damage modelling
SRIM simulations
Ions transport in matter
Radiation damage
Orcad – PCB design and SPICE simulation
Electronics and PCB layout
Maple for math modelling
Radiation damage modelling
Impact ionization studies
Physics of detectors
MoBo

## Slide 6: Lab equipment
Pulsed 3 wavelength (‘Trilite’) laser with 1um minimum beam spot accuracy and <1um XYZ motorized stage for sensor testing
TCT laser
Radioactive sources (90Sr, 55Fe, 60Co)
Peltier cooled CAs
Keithley Semi-Conductor analyzer CS4200 with HV – CV - PG units
Thermal camera
Environmental chambers
N2 cooling system for live sample testing
3-D printers
Laser Cutting facility
Impedance analyzer
DAQ facilities (ATCA, HSIO, ATLYS, ITS-DAQ, NI DAQ)
Excellent working relationships with international facilities
90Sr
TCT
Trilite

## Slide 7
OVERMOS is a CMOS MAPS project demonstrator fabricated using:
TJ 180 nm Hi-res 18 um thick epitaxial layer 1kOhm –cm
Small ( 3.5x3.5 um2) n-collecting nodes
Multi diode arrangements within pixel
CMOS DPW  originally proposed for DECAL of ILC
  OVERMOS description
N++
P-Epi
P++-Sub
DPW
SiO2
18 μm
03/07/19
E. Giulio Villani, RAL
Particle track

## Slide 8
A TCAD modelling of fabrication process of OVERMOS has been developed to investigate and predict its performances
OVERMOS devices have been n-irradiated to  [1e13,5e13,1e14,5e14,1e15]
Pixel 4
P++
N++
40um
40um
  OVERMOS description
03/07/19
E. Giulio Villani, RAL

## Slide 9
XY stage 1um accuracy
AMPTEK A250CF
LeCROY WR
  OVERMOS Laser Test
  2.04  0.17 mV/fC
T = 21°C
DUT
Nd:YAG Trilite Laser
  mV
  fC
Trigger (Q-sw)
03/07/19
E. Giulio Villani, RAL

## Slide 10
  Laser energy settings, measured with Pd10-pJ:
  ~ 25  1.8 pJ @ 1064 nm
  50Hz rate
15 m
  OVERMOS Laser Test
  ~ 7.8 ns Laser pulse width,
  Shutter size set to 5 x 5 um2
  Beam size ‘destructive’ test
03/07/19
E. Giulio Villani, RAL

## Slide 11
2
3
4
5
1
7
8
9
10
6
12
13
14
15
11
17
18
19
20
16
22
23
24
25
21
OVERMOS Laser scan 5 x 5 um2 beam size
25 points, repeated over entire pixel area to give map of collected charge
The dynamics of charge collection of three points (7,10,25) is compared with TCAD simulations for non-irradiated and irradiated devices
Vbias = 10V
  OVERMOS Laser Test
Cu shielded OVERMOS
OVERMOS
40 m
40 m
03/07/19
E. Giulio Villani, RAL

## Slide 12
<Q> = 492.1 [fC] Collection time: 44.60.36 ns
Hit 25
OVERMOS Laser scan 5 x 5 um2 beam size
10 non – irradiated pixels Laser Test results
  OVERMOS Laser Test
<Q>= 153.4 [fC] Collection time: 57.60.52 ns
<Q>= 166.34 [fC] Collection time: 53.50.31 ns
Hit 10
Hit 7
=0
<Qc>=267
03/07/19
E. Giulio Villani, RAL

## Slide 13
=1e13
<Qc>=147
=5e13
=5e14
=1e14
Qc [fC]
<Qc>=143
<Qc>=109
<Qc>=79
m
  OVERMOS Laser Test
=1e15
<Qc>=68
Qc [fC]
Qc [fC]
Qc [fC]
Qc [fC]
m
m
m
m
03/07/19
E. Giulio Villani, RAL

## Slide 14
  OVERMOS Laser Test
=1e13
=1e14
=5e13
=5e14
=1e15
=0
Laser TRG
Kinematics of charge collection - fC
03/07/19
E. Giulio Villani, RAL

## Slide 15
  TCAD simulation
Simulations workflow
Process simulation 5500 secs
Process simulation – SDEVICE
4000 secs
Layout editing
DC/CC/OPT simulation
>200k secs
Running on WS Intel Xeon Gold 5122 4 Core Processor, 3.6GHz, 16GB 2.4GHz RAM, 240GB SSD 6Gb/s
03/07/19
E. Giulio Villani, RAL

## Slide 16
Pixel .gds
A simplified TJ CMOS fabrication process of OVERMOS has been implemented in SPROCESS
Around 15 simulated steps, which include epitaxial growth on Si bulk, SiO2 thermal growth, N/P implant, etching, thermal annealing, metal deposition, contacts placement
Si bulk
Epitaxial growth
SiO2 thermal growth
Mask layout 1
P implants
Strip resist
Mask layout 2
N implants
Strip resist
Mask layout 3
XP implants
Strip resist
SiO2 etching
Al patterning dep
contacts
  TCAD simulation
03/07/19
E. Giulio Villani, RAL

## Slide 17
  TCAD simulation
For DC studies only ¼ pixel is simulated
For CC studies using Laser light, an extra PolySi box surrounds the pixel, with high SRV to simulate non-reflecting boundaries (added as an SDE directive within SPROCESS)
Thermally grown 8.1 nm SiO2 for interface traps effects
Thick deposited SiO2 for better Delaunay meshing/optical attenuation/reflection (will implement STI next)
Emulation of CoSi2 silicide for optical attenuation in non-NS regions (will implement silicide growth next)
SiO2
PolySi
03/07/19
E. Giulio Villani, RAL

## Slide 18
  TCAD simulation
  HPTM
A factor 1.66 has been applied to gint to account for n irradiation
03/07/19
E. Giulio Villani, RAL

## Slide 19
VB
CB
  TCAD simulation
* Effects of Interface Donor Trap States on Isolation Properties of Detectors Operating at High-Luminosity LHC, DOI: 10.1109/TNS.2017.2709815
Fixed oxide-charge (Oxch) density and interface traps (Oxint) included
Interface traps distributed among 3 energy levels, Gaussian ,  = 70meV
Ratio Oxint/Oxch ~ 0.9
Simulations 1.2e11 Oxch
Xsection 1E-15 cm^-2
1.2e11 Oxch
[0.007,10,10 ]
hN eN eN
SiO2
SiO2
DLN=30
03/07/19
E. Giulio Villani, RAL

## Slide 20
  TCAD simulation IV
TCAD
TEST
DC IV plots up to BV
<IV>[10] measured OVERMOS + 
IV TCAD Oxch 1.2e11, OxINT 1.1e11
 | Ileak_[A] @10V | Ileak_TCAD[A] @10V | % | aBV[V] | BVTCAD[V]
0 | 1.0e-12 | 0.85e-12 | 15 | 50.8 | 54.79
1e13 | 7.5e-12 | 1e-11 | -33.3 | 52 | 54.6
5e13 | 6.72e-11 | 7.47e-11 | -11.1 | 51.2 | 54.7
1e14 | 2.1e-10 | 2.06e-10 | 1.9 | 52.4 | 54.7
5e14 | 6.21e-10 | 1.18e-9 | -90 | 53.6 | 54.8
1e15 | 1.43e-9 | 1.83e-9 | -28 | 54.4 | 54.8
aBV defined as V: (I/V)max
0 
1e13 
5e13 
1e14 
5e14 
1e15 
Vbias for CCE
03/07/19
E. Giulio Villani, RAL

## Slide 21
  TCAD simulation CC
TCAD
TEST10
Qcoll | Test | TCAD | %
<Qh7> | 492 | 556 | -13
<Qh10> | 166 | 131 | 21
<Qh25> | 153 | 166 | -8.4
Tcoll10-90 | Test | TCAD | %
<tcollh7> | 44.6 | 45.2 | 1.3a
<tcoll10> | 53.5 | 59.9 | 12b
<tcoll25> | 57.6 | 68 | 18c
ahit7 with CA delay subs: 9.1% bhit10 with CA delay subs: 17.7% chit25 with CA delay subs: 23.3%
Laser Hit
03/07/19
E. Giulio Villani, RAL

## Slide 22
  TCAD simulation
Qcoll | Test | TCAD | %
<Qh7> | 309 | 529 | -71
<Qh10> | 165 | 113 | 31
<Qh25> | 110 | 143 | -30
Laser Hit
Qcoll | Test | TCAD | %
<Qh7> | 282 | 437 | -54
<Qh10> | 132 | 75 | 43
<Qh25> | 106 | 82 | 22
1e13
5e13
Q [fC]
t [ns]
t [ns]
Q [fC]
03/07/19
E. Giulio Villani, RAL

## Slide 23
  TCAD simulation
Qcoll | Test | TCAD | %
<Qh7> | 265 | 373 | -40
<Qh10> | 82 | 51 | 37
<Qh25> | 65 | 53 | 18
Qcoll | Test | TCAD | %
<Qh7> | 263 | 301 | -14
<Qh10> | 38 | 24 | -36
<Qh25> | 27 | 23 | -14
1e14
5e14
Laser Hit
t [ns]
Q [fC]
t [ns]
Q [fC]
03/07/19
E. Giulio Villani, RAL

## Slide 24
  TCAD simulation
Qcoll | Test | TCAD | %
<Qh7> | 246 | 257 | -4
<Qh10> | 21 | 24 | -14
<Qh25> | 10 | 17 | 70
Laser Hit
1e15
t [ns]
Q [fC]
03/07/19
E. Giulio Villani, RAL

## Slide 25
RD50- Radiation Hard Semiconductor devices for very high luminosity colliders
PPD joined RD50 in Dec 2016
03/07/19
E. Giulio Villani, RAL

## Slide 26
03/07/19
E. Giulio Villani, RAL

## Slide 27
03/07/19
E. Giulio Villani, RAL
PPD contribution

## Slide 28
  RD50 funding request
We propose to fabricate a number of Schottky and n+p diodes on p-type epitaxial (50um thick) silicon wafers, of doping concentration as they are normally used in CMOS MAPS devices, to investigate radiation bulk damage in CMOS sensors
1. RAL PPD, UK 3. JSI, Slovenia
2. IHEP, China 4. University of Birmingham, UK
The purpose is to gain a deep understanding of radiation damage in such structures with a view to develop reliable damage models that can be implemented in TCAD device simulators (Synopsys or Silvaco).
We will purchase 6 inch wafers, 25 x 5 doping levels (1e13, 1e14, 1e15, 1e16 and 1e17 cm-3 ), total 125 wafers.
The remaining wafers, upon agreement, could be distributed among other groups and/or RD50 institutes interested in participating in this project, whether at device design and/or at device test level

## Slide 29
Wafers purchase through IHEP
Schottky devices fabrication and modelling will take place at RAL, UK
N+P junctions fabrication at Carleton University, Canada
Neutron irradiation and tests at JSI
‘Unofficially’ told that the submission has been successful – waiting from confirmation from CERN
  RD50 funding request

## Slide 30
  LGAD
New end-cap timing detector: HGTD
LGAD could be used for PID using TOF in nuclear physics
They are potentially useful in pCT, for hadron therapy

## Slide 31
  LGAD
Few vendors can produce LGAD with throughput needed for large area detector
Proposal with T2EV (UK based company with long history of space science imaging devices) for production of epi-based LGAD on low resistivity substrate

## Slide 32
Conclusions
RAL PPD has many years of experience in CMOS HEP detectors development
Tangible international impact on CMOS HEP community
Very well positioned to continue and contribute even more to such activities
New projects include additional RD50 contribution and LGAD developments

## Slide 33
Neutron detectors using semiconductors usually rely on secondary radiation emitted from neutron interaction.
This is normally achieved by coating a charged particle sensitive device with a film converting neutrons to secondary charged particles, either via nuclear reactions (A) or as energetic recoils from elastic scattering (B).
Converter
Si detector
A: α and Li produced by neutron capture in 10B-converter Due to kinematic constraints, only one of the ions might reach the detector
n
α
Li
-
-
-
-
-
-
Converter
Si detector
n
Li
α
-
-
-
-
-
-
-
-
n
p
B: p produced by neutron elastic scattering in CH2 converter
CMOS neutron imaging

## Slide 34
CMOS neutron imaging
Programming (i.e. e- / h+ injection) is achieved via FN tunneling
The stored charge affects the conductivity of the N/P MOS
FG
+
-
h+
e-
F [V/cm]
Φ [V]
STI
FG

## Slide 35
CMOS neutron imaging
The process of n detection is then performed via 10B neutron capture in the CFLASH/NVM dielectric and subsequent discharge of the FG
Sensitive layer coincides with conversion layer
FG
-
-
-
-
-
-
-
-
-
-
-
-

## Slide 36
A number of CFLASH sensors were tested in February, 2018, for sensitivity to slow neutrons. The facility used was the Vesuvio spectrometer, at ISIS (RAL).
5 sensors were placed inside the tank in the beam, while additional 3 were left outside, exposed to the gamma background.
The output of the sensors was monitored in real time while they were being exposed to the neutron flux.
In-beam sensors
N-beam path
off-beam sensors
CMOS neutron imaging

## Slide 37
CMOS neutron imaging
In-beam sensors output Average slope ≈ 1.7 μV/s +/- 1σ
Off-beam sensors output remained practically unchanged over 12 hrs
A value of K = 50, corresponding to a B doping level of around 5E18 – 1E19 would give expected results comparable to measured ones.
Average dose received during the n test: 2.12E-3 cGy/s
Expected results: 4.7*K*1E-5 cGy/s

## Slide 38
CMOS neutron imaging
In-beam sensors output
Comparison with ISIS current log file shows flattening of the cells output coincide with beam off condition