## Slide 1: RF panel : WG1 bulk Nb
Maud BAYLAC, Laura MONACO, Catherine MADEC

## Slide 2: What was performed
Identification of the labs (9) and contact persons
  CEA : T. Proslier / E. Cenni / G. Devanz
  CERN : F. Gerigk / W. Venturini
  CNRS-IJCLab : D. Longuevergne / A. Miyazaki
  DESY : H. Weise / D. Reschke
  ESS : P. Pierini / H. Danared / M. Lindros
  Hamburg univ.: M. Wenskat
  HZB : J. Knobloch / O. Kugeler
  INFN : D. Sertore (Milano LASA) / C. (LNL) / A. (Padova)
  STFC : P. McIntosh
Survey performed (June) and analysed
  Answers missing ESS and DESY
TOPIC |  | Info/data from your lab |  |  |  | Explainations on expected info/data | Explainations on expected info/data
Main R&D achievements |  |  |  |  |  |  | 
 |  | Single/multi-cell | Frequency | Shape | Project |  | 
 | for prototypes | ? | ? | ? | ? |  | if possible, indicate corresponding project
 | for series | ? | ? | ? | ? |  | if possible, indicate corresponding project
Future R&D |  |  |  |  |  |  | 
 | project names | ? |  |  |  |  | if possible, list involvment in future projects (FCC, ILC, LHeC …)
Material |  |  |  |  |  |  | 
 | Fine grain | ? |  |  |  |  | indicate yes/no, if possible give some details, specifications, actual techniques and future plans
 | Medium grain | ? |  |  |  |  | indicate yes/no, if possible give some details, specifications, actual techniques and future plans
 | Large grain | ? |  |  |  |  | indicate yes/no, if possible give some details, specifications, actual techniques and future plans
 | Additive manufacturing | ? |  |  |  |  | indicate yes/no, if possible give some details, specifications, actual techniques and future plans
Processing techniques |  |  |  |  |  |  | 
 | surface polishing | ? |  |  |  |  | cold EP, mechanical polishing, electrolytic plasma polishing, rotational BCP
 | surface treatment | ? |  |  |  |  | nitrogen infusion and doping
 | heat treatment | ? |  |  |  |  | two-step baking processes, Mid-T baking
 | cleanliness | ? |  |  |  |  | robotisation/cobotisation
Field emission |  |  |  |  |  |  | 
 | diagnostics during tests | ? |  |  |  |  | indicate type of diagnostics during tests, on test facilities
 | diagnostics during operation in cryomodule | ? |  |  |  |  | indicate type of diagnostics used during operation, in cryomodule
 | recovery within cryomodules | ? |  |  |  |  | indicate type of technique (plasma processing, CO2 …) used to recover from field emission
Infrastructures/tools in your lab |  |  |  |  |  |  | 
 | cavity preparation | ? |  |  |  |  | indicate types of infrastructres, tools in your lab for shaping, welding, surface and annealing treatments, tuning, processing assembly in clean room,…
 | cold RF testing | ? |  |  |  |  | indicate types of infrastructres, tools in your lab
 | cryomodule assembly | ? |  |  |  |  | 
 | cavity testing in cryomodule | ? |  |  |  |  | 
Manufacturer |  |  |  |  |  |  | 
 | cavity | ? |  |  |  |  | indicate your manufacturer for bulk Nb cavity

## Slide 3: Data surveyed
Goals : reduce operational cost (Q0 ↑) and capital cost (Eacc ↑)
Data surveyed
  Main R&D achievements, for series and for prototypes
    Cavity type (single/multi-cell, frequency, shape)
    Project
  Future R&D
    Project name, cavity type
  Material
    Fine, medium or large grain, additive manufacturing
  Processing techniques
    Surface polishing
    Surface tratment
    Heat treatment
    Cleanliness
  Field emission
    Diagnostics during tests, diagnostics during operation
    Recovery within cyromodules
  Infrastructures / tools
    Cavity preparation, cold RF testing, cryomodule assembly, cavity testing in cryomodule
  Manufacturers
Higher Eacc
ILC – higher Eacc  smaller linac (= lower capital cost)
MC – quick acceleration (vs m-lifetime)
FCC – fewer cavities  smaller RF installation
Higher Q0
FCC, ERL, ILC – lower RF losses, cryogenic power minimised.
Others: Reproducibility, cost, industrial manufacturing

## Slide 4
About 10 labs : CERN, CEA, HZB, IJCLab, INFN (LASA, LNF, Padova), univ. Hamburg, STFC
Frequencies (and harmonics) : 1.3 GHz (3.9 GHz), 802 MHz (401 MHz), 704 MHz (352 MHz), 650 MHz (325 MHz)
Most R&D on elliptical cavities
  single-cell to develop the preparation protocole, to be further applied on multi-cells
Preparation protocole composed of a wide variety of techniques
  Surface polishing : (cold, metallographic) electropolishing (EP), high pressure rinsing (HPR), (rotational) buffered chemical processing (BCP)
  Surface treatment : N-doping
  Heat treatment : low/mid/2 step temperature baking, H degassing
Heavy infrastructures required
  Clean rooms ISO4 required for preparation
  Cavities are tested vertically (easier testing) and at low power  dedicated infrastructures
  Diagnostics used during tests to characterize cavity performances and field emission
Main R&D on bulk cavities in Europe : some key points

## Slide 5: Goals to be adressed in the report
MEMORANDUM ON THE INFO TO COLLECT FROM THE EUROPEAN TEAMS Each WG to report on the progress (timeline) on the survey of each national team in their European reference community on:
Areas of specific expertise/strength/weakness (within the WG theme)
Table of main devices, their specs
Current R&D activities in HEP, and outside HEP (improving the RF field on performance, reliability, energy efficiency, cost)
Available infrastructures
Interest in future HEP activities
Current FTEs involved
Current collaborations with other Institutions
Needed infrastructures, insufficient infrastructures.
Overlaps/Affinity with R&D carried out in others labs  to be deduced from the data surveyed
Current budget (which source of funds)
Which activity would they expand on, in case of extra-funds/additional personnel
Green : input provided by survey
Blue : possible through new survey
Red : seems tricky
eg : CEA will not communicate its budget

## Slide 6: Follow up consultation
Additional survey to complete the existing data set with
  Needed infrastructures, insufficient infrastructures
  Current collaborations with other Institutions
  Overlaps/Affinity with R&D carried out in others labs
  Current FTEs involved
  Current budget (which source of funds)
  Which activity would they expand on, in case of extra-funds/additional personnel
Agenda
  Survey to be launched asap to get and process the data by mid october
NB : Meeting is not compatible with agenda of the report (mid oct)