## Slide 1: Outcome of the Post-Irradiation Examination of the baseline design prototype target and Nb-cladding R&D for the Beam Dump Facility (BDF) at CERN 16th International Workshop on Spallation Materials Technology (IWSMT16) Oxfordshire, UK, 28th October – 1st November 2024
Tina Griesemer1, Rui Franqueira Ximenes1, Marco Calviani1, Ana Fontenla1, Stefano Sgobba1, Gonzalo Izquierdo1, Oscar Sacristan De Frutos1, Stefan Hoell1, Adria Terricabras1, Ignacio Aviles Santillana1, Giuseppe Mazzola1, Luigi Salvatore Esposito1, Matthew Alexander Fraser1, Richard Jacobsson1, Alexey Rempel2, Marco Kaiser2, Thomas Brehm2, Roman Kuchar2, William Kyffin3,4, Thomas Dutilleul3, Jack Callaghan5, Abdullah Mamun5
2024/10/31
CERN, Geneva, Switzerland
Framatome, Erlangen, Germany
Nuclear AMRC, Sheffield, UK
University of Sheffield, Sheffield, UK
Bangor University, Bangor, UK

## Slide 2: Content
The HI-ECN3 project and BDF/SHiP
Target requirements
Baseline design
Post-Irradiation Examination of a prototype target
Nb-cladding R&D studies
Conclusions & outlook (1)
Follow-up of IWSMT15 talk
Rui F. Ximenes - Post-Irradiation Examination of the prototype production target materials of the Beam Dump Facility (BDF)
& Beam Dump Facility production target at CERN and advanced cladding technological R&D
@ IWSMT16, is complementary to
Michael William Parkin - Alternative designs for the Beam Dump Facility (BDF) production target and in-beam test plans at CERN
.
.
.
Main difference from last year: BDF/SHiP is presently an approved experiment posed for beam commissioning in 2031 & an alternative target design is being explored

## Slide 3: TCC8 & ECN3
Outcome of the PIE of the baseline design prototype target & Nb-cladding R&D for the BDF at CERN | IWSMT16
Transfer Tunnel (TT) 20
TDC2: TT20 splitters
TCC2:
T2 / T4 / T6 / TAX
ECN3
TCC8: T10 / TAX
→ K12
SPS LSS2
CCC
EHN1
EHN2
TDC8
TT83 (P4)
TT85 (P42)
TDC85
P42 Beam Dump (TIDVG4)

## Slide 4: Beam Intercepting devices towards ECN3
EHN1
EHN2
ECN3
SPS
TT22
TT21
LSS2
TT24
P4
TCC8
P4:6
P42
Other BIDS: Collimators, Masks, etc  To be defined
Target + beam windows
P42 commissioning Dump (TIDVG4)
T4 XTAX
TT20 TED
TBSE
TCSC
T4 Target
NA-CONS
HI-ECN3

## Slide 6: NA62 in ECN3 (Today)
ECN3
B918
B911
TCC8
Existing
Access Shaft
48 m2
T10 target, K12 beamline and NA62 experiment to be dismantled in LS3
T10
Target
K12 beam line
T10
XTAX
Outcome of the PIE of the baseline design prototype target & Nb-cladding R&D for the BDF at CERN | IWSMT16

## Slide 7: BDF/SHiP Target & Complex (Future ~ 2031)
New
Service Building
~ 500 – 700 m2
ECN3
Beam Dilution System
New
Access Shaft
(material only)
88 m2
TCC8
Existing
Access Shaft
48 m2
B918
B911
New Target Complex
containing the Beam Dump Target
13 x TZM blocks (580 mm)
5x W blocks (780 mm)
Baseline Design  To be improved during TDR
WP4
WP3
WP2
WP5+SHiP
WP4
WP6,WP7 +al.
350 kW-class Target

## Slide 8: BDF/SHiP Target
SPS Beam Dump Facility: Comprehensive Design Study, https://doi.org/10.23731/CYRM-2020-002
SHiP Experiment - Comprehensive Design Study report, https://cds.cern.ch/record/2704147
R. Jacobsson
Beam Dump Target / SHiP Target
  Fully absorbe all p+, maximize production of charm and beauty hadrons & re-absorption of pions, muons and kaons
High energy → production of charmed and beauty mesons
High ppp & POT → overcome small prod cross-section of extra rare events of hidden particles
High ρ, Z & A → Maximize p+ interaction
Short λ → Force absorption of K & π to reduce muon & neutrino background

## Slide 9: BDF Target Designs overview
Baseline Design (CDR) – Water cooled, W + TZM cladded w/ Ta2.5W .
Pursued during the conceptual design phase
Prototype + test with beam + Post irradiation examination
Still some safety aspects to be addressed
Could be further optimized for physics
https://doi.org/10.1103/PhysRevAccelBeams.22.113001
Alternative designs currently being studied in the TDR
Enclosed compact
Cu + W Target
Removes water from beam
Keeps physics performance
Reduces decay heat
Increases T and stress
W Helium cooled Target
Removes water from beam
Better physics performance
Reduces decay heat & residual stresses
Conceptually different system!
Baseline-based concepts: with W rolled material, Nb-cladded Target, thin Ta cladding…
BDF Baseline Target Design

## Slide 10: BDF Target baseline design
Water-cooled, Ta-cladded TZM + W Core
  TZM: Absorbs most of the power. Higher strength, better creep resistance, higher recrystallisation temp wrt Mo.
  W: Good radiation damage resistance. Best for physics.
  Ta2.5W: To avoid corrosion-erosion of the core materials
  Cooling: 22 bar, 5 m/s, ~660l/min, ~305kW of heat.
Manufacturing
  Forged TZM and sintered W (single blocks)
  Diffusion bonding with cladding via Hot Isostatic Pressing
https://doi.org/10.1103/PhysRevAccelBeams.22.113001
Target Core with reasonable physics performance & that allows diluting (longitudinally) the energy deposition
13 x TZM blocks (Z=42, ρ=10.2g/cm3)
(580 mm)
5x W blocks (Z=74, ρ=19.3g/cm3)
(780 mm)
D250 mm
BDF Baseline Target Design

## Slide 11: Post-Irradiation Examination of a prototype target
Post-irradiation examination of a prototype tantalum-clad target for the Beam Dump Facility at CERN, T. Griesemer, R.F.Ximenes et al, https://doi.org/10.48550/arXiv.2410.01964 (submission to PRAB)

## Slide 12
Notes: Instrumentation (temperature and strain) of 4 most critical blocks
Total 14 hours of beam in 3 days → 2.4 × 1016 PoT

## Slide 13
Prototype Beam tests
Validate manufacturing and test operation at identical temperatures & mechanical stresses.
Reduced diameter (80 mm) prototype.
Tested in 2018 on a dedicated slow extraction (SX) testbench in the T6 primary beam line in TCC2 at CERN. Total of 2.4 × 1016 p+
https://doi.org/10.1103/PhysRevAccelBeams.22.123001
BDF Baseline Target Prototype + PIE
Beam parameters
Operational conditions
Notes: Instrumentation (temperature and strain) of 4 most critical blocks
Total 14 hours of beam in 3 days → 2.4 × 1016 PoT

## Slide 14: PIE activities & samples
Thermal diffusivity
Interface Shear
Bulk Tensile
Microstructural
Non-destructive
I. Film Dosimetry
II. Metrology & Microscopy
III. Ultrasonic Testing
V. Microstructural Characterization
IV. Specimen Extraction
VI. Mechanical Characterization
VII. Thermal Characterization

## Slide 15: PIE – Nondestructive testing
II. Metrology and Microscopy
Better cleaning of lubricant necessary
Strong turning grooves in the centre
→ No relevant geometrical changes nor swelling and no corrosion, cracks, or melting visible
1 mm
1 mm
I. Film Dosimetry
II. Metrology and Microscopy
III. Ultrasonic Tests
III. Ultrasonic Tests
→ No signs of damages in the bonding interface!
I. Film Dosimetry
→ BTV and gafchromic imaging consistent (< 1mm)
→ Blow up of the beam downstream.

## Slide 16: PIE – Microstructure analysis
Cracks in irradiated W Block
Testing of unirradiated W Block
V. Microstructural Characterization

## Slide 17: PIE – Microstructure analysis
Cracks in irradiated W Block
Dye penetrant testing (PT) show superficial cracks (1&3) and Crack 2 was not detected
Testing of unirradiated W Block
PT Testing indicated cracks in unirradiated W
SEM shows similar cracks as in irradiated sample
TZM: → Tantalum & TZM → No damages)
W: → Cracks → Beam-induced?
Cracks did not exist before EDM cutting (UT Testing)
No differences between unirradiated and irradiated microstructure
Reason: Cracks superficial, release of high residual stresses during EDM cutting, brittle W (porosity & fully recrystallized). Attributed to quality of sintered W
EBSD and SEM images show cracks inside W → No delamination of the interface
V. Microstructural Characterization

## Slide 18: PIE - Shear testing
VI. Mechanical Characterization
Shear testing
Irradiated TZM-Ta2.5W
Un-irradiated TZM-Ta

## Slide 19: PIE - Shear testing
VI. Mechanical Characterization
Shear testing
Irradiated TZM-Ta2.5W
  Ta clad: Higher shear breaking strength than bulk Ta (150 MPa) (un-irradiated block)
  Ta2.5W clad: Close to shear breaking strength of bulk Ta2.5W (215 MPa) (irradiated, w/ and wo Ta foil)
Fracture in shear neck region
  1 at the interface, 3 in the Tantalum
  80-750um extension (slightly higher in un-irradiated)
Un-irradiated TZM-Ta

## Slide 20: PIE - Shear testing
Un-irradiated W-Ta
Irradiated W-Ta
VI. Mechanical Characterization
Shear testing

## Slide 21: PIE - Shear testing
Fracture outside necking indicating very brittle W (both irradiated and un-irradiated) – weaker than interface itself
Small extension before fracture
14S2 fracture before test
Un-irradiated W-Ta
Irradiated W-Ta
VI. Mechanical Characterization
Shear testing

## Slide 22: PIE - Shear testing
Both Intragranular fracture & no distinct fracture on both irradiated and un-irradiated
TZM block
W block
VI. Mechanical Characterization
Shear testing
Uniform fracture, always on Ta and Ta2.5W (with and without Ta foil)

## Slide 23: PIE: Mechanical testing
VI. Mechanical Characterization
Tensile testing
Hardness testing
Unirradiated
Irradiated
Unirradiated
Irradiated
RT
200 °C
Tensile Testing TZM
Tensile Testing W
200 °C
Irradiated
Unirradiated
RT
RT
200 °C
Unirradiated
Irradiated

## Slide 24: PIE: Mechanical testing
Tensile Testing
W
Tensile specimens very error prone for brittle material such as W
→ 4-pending test better
TZM : Lower mechanical properties of irradiated samples → low PoT → no irradiation damage
→ No differences in microstructure detected → No faults in testing set up found
Unirradiated
Irradiated
Unirradiated
Irradiated
RT
200 °C
Vickers Hardness [HV 0.5]
TZM, Ta, Ta2.5W: as annealed materials
W as fully recrystallized
No differences unirradiated and irradiated
Thermal Testing
Two-layered specimens of core and cladding material from irradiated Block #4 and #14
Negligible thermal contact resistance of all interfaces
No dependencies of proximity to beam impact axis or usage of Ta interlayer detected
No irradiation effects detected ( compared to prior studies)
VI. Mechanical Characterization
Tensile testing
Hardness testing

## Slide 25: Nb-cladding R&D studies
Exploring diffusion bonding of niobium and its alloys with tungsten and a molybdenum alloy for high-energy particle target applications, T. Griesemer, R.F.Ximenes et al, https://doi.org/10.48550/arXiv.2410.01988 ,
(submission to JMR&T)

## Slide 26: Nb-cladding R&D
Selection of Nb-alloys:
Promising LOCA improvement
Compliant with Thermo-mechanical conditions
Likely HIP “bondable”
  Phase diagrams: Good solubility no critical intermetallic phases
  Diffusivity: as much diffusivity into W and Mo as Ta.
  Ductility: Nb identical to Ta
*by courtesy of Bangor University
Temperature after LOCA
Assuming htc=1W/m2.K
Decay heat power
Nb-cladded baseline target

## Slide 27: Nb alloy cladding R&D - Prototype capsules
I. EBW of Capsules
II. Helium Penetrant Test
III. 1st HIPing Cycle (1200 °C)
VII. Thermal Characterization
IV. 2nd HIPing Cycle (1400 °C)
VI. Cutting & OM at interface
VIII. Mechanical Characterization
W | TZM Nb
W | TZM Nb1Zr
W | TZM C103 (Nb10Hf1Ti)
W Ta
26 mm
1 mm
50 mm
30 mm
10 mm
Welding lip
Capsule Geometry
Capsules after EB welding
HIPing Furnace at Nuclear AMRC
1st batch after HIPing
Single failed UT capsule fell apart when cut open
Successfully bonded capsule
OM to visually check the bonding interface
→ Bonding visually ok
OM of Nb//W
V. Ultrasonic Testing

## Slide 28: Nb-cladding R&D
Thermal diffusivity specimens
  Excellent thermal contact has been confirmed for all Niobium alloys (Nb, Nb1Zr, C103)
Tensile specimens
  Interface strength for Nb alloys higher for TZM than W
  TZM core :
    Ta foil + HIP: High increased the strength
    C103 did not bond without the foil
  W core
    Higher variation, but it seems no foil increases interface strength
SEM: Increase of successful diffusion bonding / maximum stresses
I. EBW of Capsules
II. Helium Penetrant Test
III. 1st HIPing Cycle (1200 °C)
VII. Thermal Characterization
IV. 2nd HIPing Cycle (1400 °C)
VI. Cutting & OM at interface
VIII. Mechanical Characterization
V. Ultrasonic Testing
*by courtesy of Bangor University
However, long-lived Nb isotopes pose challenges for waste disposal
Nb-cladded baseline target

## Slide 29: Conclusions & outlook

## Slide 30: Conclusions & outlook
PIE of the BDF Ta-clad prototype
Manufacturing a prototype, testing it with beam and analysing it afterwards is a mandatory QA loop for high power targets like BDF.
BDF’s baseline design is sound, and the cladding technology is compliant with thermo-mechanical conditions.
The sintered tungsten is likely a bad choice. Baselining a better-quality W is mandatory.
Nb cladding R&D
On paper, Nb is a great cladding candidate for W.
HIP cladding Nb-alloys on W and TZM is possible.
For BDF, we still need to validate it with beam and address its waste disposal .
Following HI-ECN3 project approval and start of TDR phase
Sound baseline design, yet with potential for optimization and with some caveats to be addressed.
Multiple alternative designs explored in view of mitigating water radiolysis, decay heat and improve physics performance. He-cooled target most promising option. Being explored in detail.

## Slide 32: WP3 – Target & BIDs: Planning (key dates)
TDR phase
TDR phase (main activities) – (2024-mid 2026)
Target (& BIDs) conceptual design followed by detailed design
Prototype(s) Target Design, construction and beam tests
Material studies, R&D and Procurement
Production phase – (2026 – 2030)
Detailed Design phase
Procurement & production of components and systems
Tests/dry-run, installation activities
Material tests/PIEs
Production phase
Commissioning & operation

## Slide 33: BDF Target Prototype removal (2020)
Unplug-in  Transport to the bunker  Unscrew downstream flange  Instrumentation wire cut & flange removal  Extraction half-shells core assembly  Unscrew half-shells  Removal top half-shell & first glimpse of the target blocks
BDF target assembly

## Slide 34: BDF Target Prototype removal (2020)
Identification of the blocks and angular orientation with respect to the beam with a marker  Removal of the target blocks for the post irradiation examination (PIE) campaign  Storage of the extracted blocks in a shielded container

## Slide 35: Ta2.5W cladding – LOCA
Potentially degradation of the material through oxidation with LOCA.
→ Campaign to assess the onset for extensive oxidation and formation of volatile oxides
Thermogravimetric analyses (TGA) performed for Ta2.5W, TZM and W in the range of 400-800 C under active and inert atmospheres.
Visual inspection of the samples before and after oxidation for different temperatures.
Ta2.5W
TZM
W
Raw sample
800 C at 2 C/min
800 C at 40 C/min
400 C at 10C/min x 7 days
800 C at 2C/min
Inert
Atmosphere
(argon 6.0)
Active
Atmosphere
(50% argon: 50% air)
400 C
500 C
600 C
700 C
r1 = 10
r2 = 2
r3 = 40
[C/min]
r1 = 10
r2 = 2
r3 = 40
[C/min]
Notes: Small mass gain for Ta2.5W at 400C with inert argon (with some impurities)
Clear oxide layer at 500 C