## Slide 1
Investigation of some operational properties of the new-style ISIS TS-1 target
David Findlay
ISIS, RAL
IWSMT-16
Abingdon
28 October 2024 – 1 November 2024

## Slide 2
ISIS Spallation Neutron and Muon Source
TS-1 target
TS-2 target

## Slide 3
use proxies to monitor target thermal performance and structural integrity
But when running, we actually see nothing

## Slide 4
2.53 cm
0.85 cm
TS-1 W target 10 plates
TS-2 W target solid cylinder
4.0 µC, 3.2 kJ per pulse, 10 pps
4.5 µC, 3.6 kJ per pulse, 40 pps
Heat per unit area:
TS-2 / TS-1 = (4.0 / 4.5) / (0.852 / 2.532)  8
Chart: Radial position, cm
| -5 | -4.8 | -4.5999999999999996 | -4.4000000000000004 | -4.2 | -4 | -3.8 | -3.6 | -3.4 | -3.2 | -3 | -2.8 | -2.6 | -2.4 | -2.2000000000000002 | -2 | -1.8 | -1.6 | -1.4 | -1.2 | -1 | -0.8 | -0.6 | -0.4 | -0.2 | 0 | 0.2 | 0.4 | 0.6 | 0.80000000000001004 | 1.00000000000001 | 1.2000000000000099 | 1.4000000000000099 | 1.6000000000000101 | 1.80000000000001 | 2.0000000000000102 | 2.2000000000000099 | 2.4000000000000101 | 2.6000000000000099 | 2.80000000000001 | 3.0000000000000102 | 3.2000000000000099 | 3.4000000000000101 | 3.6000000000000099 | 3.80000000000001 | 4.0000000000000098 | 4.2000000000000099 | 4.4000000000000101 | 4.6000000000000103 | 4.8000000000000096 | 5
TS-1 | 0.004504 | 0.0061176 | 0.0082061 | 0.010871 | 0.014222 | 0.018375 | 0.023447 | 0.029546 | 0.036769 | 0.045191 | 0.054851 | 0.065748 | 0.077833 | 0.090994 | 0.10506 | 0.11979 | 0.13489 | 0.15001 | 0.16475 | 0.1787 | 0.19141 | 0.20249 | 0.21154 | 0.21826 | 0.22239 | 0.22378 | 0.22239 | 0.21826 | 0.21154 | 0.20249 | 0.19141 | 0.1787 | 0.16475 | 0.15001 | 0.13489 | 0.11979 | 0.10506 | 0.090994 | 0.077833 | 0.065748 | 0.054851 | 0.045191 | 0.036769 | 0.029546 | 0.023447 | 0.018375 | 0.014222 | 0.010871 | 0.0082061 | 0.0061176 | 0.004504
TS-2 | 1.6542e-15 | 2.4931e-14 | 3.3636e-13 | 4.0624e-12 | 4.3921e-11 | 4.2509e-10 | 3.6829e-09 | 2.8564e-08 | 1.9832e-07 | 1.2326e-06 | 6.8577e-06 | 3.4155e-05 | 0.00015228 | 0.00060777 | 0.0021715 | 0.006945 | 0.019884 | 0.050963 | 0.11693 | 0.24015 | 0.44154 | 0.72672 | 1.0707 | 1.4122 | 1.6674 | 1.7623 | 1.6674 | 1.4122 | 1.0707 | 0.72672 | 0.44154 | 0.24015 | 0.11693 | 0.050963 | 0.019884 | 0.006945 | 0.0021715 | 0.00060777 | 0.00015228 | 3.4155e-05 | 6.8577e-06 | 1.2326e-06 | 1.9832e-07 | 2.8564e-08 | 3.6829e-09 | 4.2509e-10 | 4.3921e-11 | 4.0624e-12 | 3.3636e-13 | 2.4931e-14 | 1.6542e-15
Nucl. Instr. Meth. A 889 (2018) 113–117

## Slide 5
Comparison of ISIS neutron-producing targets – all Ta-clad W
Single input and single output manifolds — all water cooling channels in parallel
New-style TS-1 target
Old-style TS-1 target
Three input and output manifolds
TS-2 target

## Slide 6
Checking operational performance of ISIS targets
— structural — thermal
Structural — integrity of Ta cladding?
breach?
Z
N
Water Ta W

## Slide 7
Gamma-ray detector
Cooling water
Shielding on trolleys
Target
Target services area
Gamma spectrometry measurement after end of each user cycle
TSA1, no W-187 seen, neither in old-style nor new-style target
 Ta cladding intact
TSA2, W-187 seen  breach in Ta cladding
Both TSA1 and TSA2, Ta-182 seen — simply erosion of cladding

## Slide 9
Complicated spectrum, many overlapping lines
analyse smoothed second derivative of spectrum, whereby
background is effectively eliminated, and structure inconsistent with the expected widths of gamma-ray peaks is removed
Nucl. Instr. Meth. A 1046 (2023) 167708
Start with most likely isotope
Look up ENDF/B decay lines
Calculate smoothed second derivative of entire spectrum assuming energy-dependent HPGe detector efficiency energy-dependent attenuation in material between source and detector energy-dependent FWHM of peaks
Fit to smoothed second derivative of measured spectrum
From energies of missed peaks, add other isotope(s)
Iterate

## Slide 11
Can’t measure gamma-ray spectrum from every component in target services area
Instead, rely on an effective thickness of material between effective source position and HPGe detector — determined by data themselves
Get absolute activities of radionuclides
Involves approximations, obviously, but faute de mieux
TSA2, TS-2 target services area

## Slide 12
From activities eroded from target,
and from calculated activities in target (MCNPX, etc.),
get masses of material eroded
TS-1 target, old-style: erosion consistent with zero from measurement statistics
TS-1 target, new-style: ~25 mg/year from cladding only
TS-2 target: ~1 g eroded during target lifetime, from and through cladding
Nucl. Instr. Meth. B 521 (2022) 7–16

## Slide 13
Checking operational performance of ISIS targets
— structural — thermal
Decay heat measured in old-style TS-1 target Nucl. Instr. Meth. A 933 (2019) 8–11 — consistent with MCNPX calculations
(basically switch off coolant flow and measure increasing plate temperatures)
Decay heat in new-style TS-1 target Provisionally scheduled for Christmas 2024 / New Year — need ~2 weeks uninterrupted

## Slide 14
New-style TS-1 target
Single input and single output manifolds — all water cooling channels in parallel
 important to know water is going through all cooling channels
ANSYS + similar Put in power dissipations, thermal conductances, etc. Get out temperatures
Prompt heat deduced from thermocouple temperatures
We have tried to put in observed temperatures get out power dissipations and thermal conductances
Not easy to ‘reverse’ ANSYS

## Slide 15
Beam off
To get power dissipation and heat transfer coefficient to coolant independently for each plate, need to analyse temperature transients

## Slide 16
, ,
Plate 1
Plate 10
Coolant
Thermal sink
Plate
Plate 9
Plate
Plate
, , : thermal conductances
Plate 2
Solve coupled differential equations and fit to data
But for fast decays, plates really aren’t ‘point’ masses

## Slide 17
Better: run ANSYS for each plate for whole range of heat transfer coefficients to coolant for decay of steady state when beam switched off
get temperatures plates internal heats set of ’s time
interpolate to get ’s as continuous functions of , and
fit to measured plate temperatures

## Slide 18
Plate 1 power omitted — thermocouple anomaly
— not fully understood — but not serious problem operationally
Plate 10 power discrepancy — operationally insignificant
But plates 2–9 agree well with FLUKA and MCNPX
Nucl. Instr. Meth. A 1059 (2024) 168986 A 1067 (2024) 169701

## Slide 19
Heat transfer coefficients essentially consistent with design ‘good water cooling’ value of 2 W/cm²/°C
Nucl. Instr. Meth. A 1059 (2024) 168986
Overall, apart from a couple of small anomalies, new-style TS-1 target is working well
[End]

## Slide 20
Thermocouple 1 anomaly
Thermocouples 2–9
Beam on, 40/32 pps
Beam to 40 pps

## Slide 21
Thermocouple 1 — three different decay time constants

## Slide 22
/2
, ,
Plate 1
Plate 10
Window
Coolant
Thermal sink
Plate
Plate 9
Plate
Plate
Plate 1 thermocouple
, , and : thermal conductances

## Slide 23
W
Ta
Ta
Thermocouple
Water
Pressure
vessel
Thimble
Not to scale!

## Slide 24
Plate 1 anomaly in TS-1 target not serious operationally because
  ~700 milliamp-hours clocked up, and no problem
  from plate 2 temperature, downstream side of plate 1 must be being cooled
  endoscopic examination revealed no blockages