## Slide 1
Conceptual Study of Post Irradiation Examination (PIE) Facility at J-PARC
Shigeru SAITO1, Shinichiro MEIGO1, Shunsuke MAKIMURA2,
Yukinori HIRANO1, Kazuyoshi TSUTSUMI1 and Fujio MAEKAWA1
1J-PARC Center, JAEA
2 J-PARC Center, High Energy Accelerator Research Organization (KEK)

## Slide 2
Contents
1. Introduction
2. Test items and required instruments
3. Facility layout plan
4. Construction plan, R&D
5. Summary

## Slide 3: 1. Introduction - Current concept of the proton irradiation facility -
H- beam from Linac
400 MeV, 250 kW,
625 μA, 500 μs, 25 Hz
Pb-Bi
Sample specimens （SS･T91）
400 MeV, 250 kW
PBW
Water or He cooling
Irradiation samples
(Accelerators)
Proton beam
Irradiation samples (fusion & fission)
TEF-P
PIE facility
PIE of irradiated samples
Chemical processing for RI production
PIE specimens
PIE specimens
LBE target
Materials irradiation
high-energy accelerator facilities including ADS
fusion and fission reactors
Soft error testing of semi-conductor devises
RI production
Proton beam applications
Four important areas of application have been identified.
A part of the proton beam is branched with flexibly changing its intensity and pulse width.
MLF
HD
NU
J-PARC’s existing facilities
Overseas facilities

## Slide 4: - Post irradiation examination (PIE) facility -
・Post irradiation examination (PIE) facility is under consideration and to be constructed near the proton irradiation facility at J-PARC.
・The needs for this PIE facility are
(1) PIE of irradiated samples
(2) Chemical processing for RI production
https://jopss.jaea.go.jp/pdfdata/JAEA-Technology-2023-025.pdf
(in Japanese)
・As for PIE, there is a need to accept irradiated samples from other facilities in J-PARC and samples irradiated by accelerators in Japan and overseas.
・As for RI production, alpha-emitter Ac-225 considered effective for prostate cancer, is a promising candidate.
・In this study, list the instruments and equipment needed to carry out these tasks, consider whether they are feasible on the current site, and prepare a layout plan for the facility.

## Slide 5: - Hot cells in the facilities -
Sample preparation cell
Capsule disassembly
Specimen Removal
RI Target Removal
Specimen preparation
Target assembly for re-irradiation
Target station
Target Maintenance Cell
Target Replacement
Target dismantling
Coupon cutting
0 cm
MSM
Target
trolley
PBW
PM
Proton beamline
Crane
Large component handling room
Truck yard
Cask
Target
Target head
Irradiation test plate holder
Proton irradiation facility
irradiation capsule
Small Cell
Gamma scan
Measuring dimensions
PIE facility
Various cells, GB, etc.
Sample fabrication and processing
Post irradiation testing
Mechanical strength test
Surface observation
Microstructure observation
Analysis, etc.
RI separation and purification
Irradiated specimens from overseas accelerator facilities
Specimens/RI target (via underground pit)
From other J-PARC facilities
Irradiated targets
irradiated coupons
Other PIE facilities

## Slide 6: 2. Test items and required instruments - Test items -
1. Specimen preparing
1.1 Cutting machine
1.2 Milling machine
1.3 Notching machine
1.4 Grinding machine
1.5 Dimensional measuring instruments
1.6 Silicon oil bath
2. Mechanical properties testing
2.1 Tensile and compression test
2.2 Fatigue test
2.3 Creep test
2.4 Charpy impact test
2.5 SP (small punch) test
2.6 Hardness test
2.7 Nano-indentation
3. Surface observation
3.1 Cutting machine
3.2 Resin-filling equipment
3.3 Grinding machine
3.4 Optical microscope
3.5 Metallurgical microscope
3.6 Scanning electron microscope （SEM）
3.7 Field emission scanning electron
microscope （FE-SEM）
4. Microstructure observation
4.1 Electrolytic polishing
4.2 Focused ion beam（FIB）
4.3 Transmission electron microscope
（TEM）
5. Graphite testing
5.1 Density measurement
5.2 Thermal diffusivity measurement
6. LBE analysis
6.1 Transpiration method
6.2 Thermal chromatography
7. Other equipment
7.1 Gas analysis
PIE
Specimen for Charpy, SP, fatigue and creep.
Testing in LBE
Observation of LBE corrosion under irradiation
Hadron and Neutrino target
Important for ADS R&D
DBTT shift
Ac-225 production
1. Dismantling of sealed containers
2. Dissolution of Th
3. Separation and purification
4. Weighing and sorting
5. Storage and shipping

## Slide 7: - Specimens from the proton irradiation facility -
Testing | Specimen | Irradiation dose | Atmosphere | Ttest | Number
Tensile | Plate （SS-J3） | High（14-20 dpa） Middle（7-14 dpa） Low（-7 dpa） | Inert gas | Tirr* | >36 （Each dose 6×3×2 conditions）
 |  |  | LBE | Tirr | 
SSRT** | Plate （SS-J3） | Middle（7-14 dpa） Low（-7 dpa） | Inert gas | Tirr | >16 （Each dose 4×2×2 conditions）
 |  |  | LBE | Tirr | 
Fatigue | Plate with round section | Middle（7-14 dpa） Low（-7 dpa） | Inert gas | Tirr | >36 （Each dose 9×2×2 conditions）
 |  |  | LBE | Tirr | 
Creep | Plate with round section | Middle（7-14 dpa） Low（-7 dpa） | Inert gas | Tirr | >24 （Each dose 6×2×2 conditions）
 |  |  | LBE | Tirr | 
Testing | Specimen | Irradiation dose | Atmosphere | Ttest | Number
Charpy impact | □3.3 mm | Middle（7-14 dpa） Low（-7 dpa） | Air | -196°C –250°C | >20 (Each dose 10×2）
SP (Small punch) | φ3.0 mm □4.0 mm | High（14-20 dpa） Middle（7-14 dpa） Low（-7 dpa） | Air | -196°C –250°C | >36 (Each dose 12×3）
Hardness test | Resin-filled | High（14-20 dpa） Middle（7-14 dpa） Low（-7 dpa） | Air | RT | TBD
nano-indentation | Resin-filled | High（14-20 dpa） Middle（7-14 dpa） Low（-7 dpa） | Air | RT | TBD
*: Irradiation temperature
**: Slow strain rate tensile test
Tensile/SSRT
Fatigue
Charpy
TEM/SP

## Slide 8: - Test items common to metal samples and LBE-
 | Specimen | Purpose | Number
Optical microscope Laser microscope | 3×7×2 mm | Corrosion surface observation | > 30（Beam injection window, irradiation sample plate, etc.）
Metallurgical microscope | Resin-filled | Metallographic observation | Some mechanical strength specimens
SEM | Tested specimen | Fracture surface observation | All mechanical strength specimen
FE-SEM | Resin-filled | Corrosion cross-sectional observation Elemental analysis | > 30 (Beam injection window, irradiation sample plate, etc.）
 | Specimen | Purpose | Number
TEM | Electrolytic polishing, FIB* | Microstructural Observation | > 30
Gas analysis | > 10 mg | Determination of transmutation gas | TBD
*: Focused ion beam
FIB
TEM
SEM
Analysis | Sample | Information | Number
γ-ray measurement | g | Nuclides and their amounts | TBD
Transpiration method | mg | Evaporation behavior | TBD
Thermo-chromatography | g | Adsorption behavior | TBD

## Slide 9: - Components, materials and testing items planned for PIE (J-PARC MLF, Neutrino) -
Component | Size | Material | Testing | Number
Hg target vessel | φ50×2.5 mmt, 50 g | SUS316L | Tensile, microhardness, surface observation, TEM, gas analysis | 4 /year
Proton beam window | φ50×2.5 mmt, 15 g | A5083 | Tensile, microhardness, surface observation, TEM, gas analysis | 2 /2years
Moderator vessel | φ50×2.5 mmt, 15 g | A6061-T6 | Tensile, microhardness, surface observation, TEM, gas analysis | １ /year
Moderator vessel | φ50×2.5 mmt, 15 g | A5083 | Tensile, microhardness, surface observation, TEM, gas analysis | １ /year
Moderator vessel | φ50×2.5 mmt, 17 g | Ag-In-Cd A5083 | Tensile, microhardness, surface observation, TEM, gas analysis | １ /year
Muon target | φ40×20 mmt, 45 g | Graphite | Compression, microhardness, surface observation, TEM, gas, thermal diffusivity, dimensional change, ultrasonic conduction | 1 /3years
Muon target | φ40×20 mmt, 80 g | SiC/SiC composite | Compression, microhardness, surface observation, TEM, gas, thermal diffusivity, dimensional change, ultrasonic conduction | 1 /3years
Component | Size | Material | Testing | Number
Beam window | φ40×0.3 mmt, 1.8g | Ti-6Al-4V | Microhardness, surface observation, TEM, radiochemical analysis | 2 /5years
OTR | φ50×50 μmt | Ti-15V-3Cr-3Sn-3Al | Microhardness, surface observation, TEM, radiochemical analysis | 2 /5years
SSEM | 2~5 mm ×5 μmt | Pure Ti | Microhardness, surface observation, TEM, radiochemical analysis | ～10 /5years
Neutrino target | TBD | Isotropic graphite | TBD | 1 /5years
2 m
MLF target
Graphite IG-430U
26 mmf x ~900 mm
Ti alloy
(BW=0.3 mm)
Neutrino target
Muon target

## Slide 10: - Components, materials and testing items planned for PIE (J-PARC Hadron) -
Component | Size （Before cutting） | Material | Testing | Number
Ti window （50 kW target upstream） | φ265×2～20 mmt 3.3 kg | Ti-6Al-4V | Tensile, Microhardness | 1 /3 years
Ti window （50 kW target downstream） | φ440×4～24 mmt 9.9 kg | Ti-6Al-4V | Tensile, Microhardness | 
Be window (90kW target upstream） | φ300×6 mmt 0.8 kg | Pure Be（S-200F） | Tensile, Microhardness | １ /6 years
Be window (90kW target downstream） | φ455×8 mmt 2.4 kg | Pure Be （S-200F） | Tensile, Microhardness | 
Al window for SY vacuum partition (2016 replacement) | φ230×0.1 mmt 11 g | Pure Al （A1060-H18） | Tensile, Microhardness, Elemental analysis | 
Al window for SY vacuum partition (2018 replacement) | φ260×0.1～35 mmt 2.1 kg | Al alloy （A7N01-T6） | Tensile, Microhardness, Elemental analysis | 
COMET Phase 1.5 target | φ20 mm× 400 mm, 400 g | SiC/SiC composite | Tensile, microhardness, surface observation, TEM, gas analysis, thermal diffusivity | 2 in total
COMET Phase 2 target | φ20 mm× 160 mm, 1 kg | W alloy | Tensile, microhardness, surface observation, TEM, gas analysis, thermal diffusivity | 2 in total
COMET target

## Slide 11
- Process flow diagram -
Specimens
storage cell
Mechanical strength testing
Specimens
Solid wastes
Specimen processing
Specimens
Solid wastes
Surface observation
Hardness testing
SEM, FE-SEM
Specimens
Solid wastes
Microstructural
Observation
Charpy impact
SP test
Specimens
Specimens
Specimens
Wastes management systems
Exhaust
Cooling water
Cooling water
Cooling water
Cooling water
Etching waste
Cooling water
Etching waste
Stack
Exhaust
Gas
analysis
Specimens
LBE analysis
Specimen
storage cell
LBE handling cell
Pre-treatment of LBE
Samples
Solid wastes
Wastes management systems
Exhaust
Samples
Solid wastes
Liquid wastes
Stack
Exhaust
LBE Analysis
Metal specimens
Using these flows as a reference, the layout of the facility was studied to ensure efficient flow lines for irradiated samples and waste.

## Slide 12: - Process flow diagram of Ac-225 production -
Dissolution of Th
Th target
Wastes containing Th
Wastes management systems
Exhaust
Separation of Ra and Ac
Dissolved solution
Radiation and
weight measurement
Ac-225
Sealed in container
Solidified and stored
Ra-225
Liquid wastes
Shipment to pharmaceutical manufacturers
Ac-225
Stack
Exhaust
Ac-225 extraction decayed from Ra-225
Proton irradiation facility
Under ground pit
Extraction of Ra
Ac-225, 227
Ac-225
Solidified and stored
Dissolved solution
α-γ concrete cell
A. K. H. Robertson, et.al., “232Th-spallation-produced 225Ac with reduced 227Ac content”, Inorg. Chem. 2020, Vol. 59, No. 17, 12156−12165. DOI:10.1021/acs.inorgchem.0c01081
Milking

## Slide 13: The equipment required for post irradiation testing
The equipment required for post irradiation testing
The equipment required for the separation and purification of Ac-225
Test items | Type of cells, lab, etc. | Number
Receiving and storage specimens | β-γ concrete cell（120ｃｍ） | 1
Mechanical strength testing | β-γ concrete cell（90ｃｍ） | 4
Specimen processing | β-γ concrete cell（90ｃｍ） | 1
Surface observation | Iron cell（15ｃｍ） | 2
Graphite samples testing | Iron cell（15ｃｍ） | 1
Activated LBE handling | Iron cell（15ｃｍ） | 1
Preparation for chemical method | Lab, hood with lead shielding | 1
Electropolishing, FIB, TEM observation | Lab, hood with lead shielding | 1
Impurity analysis for LBE | Lab, GB with lead shielding | 1
Thermal diffusivity measurement and density measurement of graphite | Lab, equipment with lead shielding | 1
Maintenance and modification of testing and analysis equipment | Lab | 2
Test items | Type of cells, lab, etc. | Number
Receiving, separation and purification, weighing, fractionation, storage | α-γ concrete cell（90ｃｍ） | 1
6 β-γ
concrete cells
4 iron cells
6 labs
1 α-γ
concrete cell

## Slide 14: 3. Facility layout plan - Facility design restrictions -
① Proposed construction site for the PIE facility.
② Irradiation samples from the proton irradiation facility are transported through the underground tunnel.
③ Irradiation samples from other facilities in J-PARC are transported from the truck yard.
④ Samples and wastes to be transported to other PIE facilities are taken out from the truck yard.
Underground tunnel
Truck approach position
5 m down, 50 m x 32 m. Close to WASTEF.
Exterior view of WASTEF
WASTEF operation room
Slope
Cliff

## Slide 15: - Facility layout plan -
Storage pit
Isolation room
Isolation room
Waste storage
β-1
β-2
α-1
β-3
β-4
β-5
β-6
F-1
F-2
F-3
F-4
L-1
L-2
L-3
L-4
Service area
Staff room
Radiation control room
women's restroom
Stairs
Control room
MSM Maintenance room
Control Room
Stairs
EV
Truckyard
Operation room
Corridor
Entrance
5 m
Men's restroom
Staff room
Mechanical property tests
-Tensile, fatigue, creep
Separation and purification of medical RIs
FIB
TEM
SEM/FE-SEM
DBTT shift
-Charpy impact test
-Small punch (SP) test
Specimen preparation and processing
High-power target materials from J-PARC and other facilities in Japan and overseas
Analysis of activated LBE
50 m x 32 m
Ground floor

## Slide 16: - B1F -
5 m
Hot machinery room
Hot machinery room
Cold machinery room
Emergency power supply room
Sampling room
Low-level liquid waste storage tank room
High-level liquid waste storage tank room
αγ liquid waste storage tank room
Fire extinguishing system room
Storage pit
Stairs
Stairs
B1F
50 m x 32 m
Liquid waste storage tank rooms
Hot machinery rooms
Cold machinery rooms, etc.

## Slide 17: - 2nd and 3rd floor -
5 m
Cold machinery room
Stairs
Stairs
EV
L-1
Cold mock-up room
L-5
L-6
Workshop
Staff room
Staff room
Staff room
Staff room
5 m
Cold machinery room
Stairs
EV
Meeting room
Meeting room
Meeting room
C402
Staff room
Staff room
Staff room
Staff room
2nd floor
3rd floor
Staff rooms, workshop, cold mock-up room
Cold machinery room
Labs, etc.
Staff rooms, Meeting rooms
Cold machinery room

## Slide 18: - Location of the proton irradiation facility and PIE facility -
Plane view
Elevation view
Proton irradiation facility
PIE facility
Proton irradiation facility
PIE facility
Proton beam
LBE target
17.8 m

## Slide 19
4. Construction plan, R&D
- Road map -
Facility Operation
Facility Construction
Irradiation Facility
1
5
10
PIE facility
Material Irradiation
Irradiation and PIE
RI Medicine
Space use
Phase 2
Construction of new irradiation facility
Soft error
Roadmap of the Materials Division of the Atomic Energy Society of Japan
Phase 1
DX and AI implementation for upgrading
Soft error test
RI production
JAXA Roadmap
Gateway construction completed
Enhanced space stay technology beyond Mars
Space equipment test
Needs for facilities
Full-scale operation
operation
10 → 250 kW
Facility Construction
Facility Design
Facility Design
Year

## Slide 20: - Development of PIE technique -
Desk-top electrical discharge machine,
Sankyo Engineering, Inc.
Specimen preparation machines
Accessible by MSM
Main unit and control unit should be separate.
Cutting machine
Disk while cutter
EDM→Wires should be automatically replaceable.
Milling machine with rotating jig
for fatigue and creep specimen with round section preparation
Mock-up test
Notching machine for Charpy specimen preparation
Wire cutting
Disk grinding
Grinding machine for SP (small punch) specimen preparation
Performed on MEGAPIE specimens

## Slide 21: - Development of PIE technique -
Tensile/Fatigue testing machine, Instron, linear type 5 kN
Tensile, fatigue and creep test in LBE
Accessible by MSM
Setting of test specimen and strain gauge
Installation of oxygen sensor →Ｈorizontal type
Testing machine in LBE
Accessible by MSM
Main unit and control unit should be separate.
Test in LBE
LBE bath
No lagging material
Coating
Level gauges(H&L)
Cover
Flange
Rod
Rod
Oxygen Sensor
T.C.
Drain tank
Jigs and specimen
Specifications for the specimen preparation machines and testing machine are under considering with reference to the experience of STIP and MEGAPIE.

## Slide 22: 5. Summary
Based on the PIE flow, test items, RI separation and purification process, etc., we determined the space required and examined the layout, which we believe is feasible in the current space.
The next issues are as follows,
  -Specification review of hot cells
  -Revision of the proposed building layout
  -Space for piping, cables and ventilation ducts, etc.
  -Development of PIE technique with unirradiated sample
This facility will contribute greatly to research on ADS materials and accelerator materials.

## Slide 23
Thank you!