## Slide 1: Status of the STS Target Segment Manufacturing R&D
Justin Mach Senior Target Systems R&D Engineer
with Aaron Jacques, Yongjoong Lee, Joel Montross, Thomas Muth, Joseph Tipton
October 28th – November 2nd, 2024
16th International Workshop on Spallation Materials Technology, Abingdon, UK

## Slide 2: Outline
STS target foot assembly and risks
Manufacturing R&D overview
Full-scale HIP demonstration
Initial HIP bonding results
Copper swelling risk
Potential thermal interface alternative
Open questions
Summary

## Slide 3: Target foot: key elements & risks
HIP bonding (1-step)
Copper to tungsten/tantalum
Copper to Inconel
Prediction of the post-HIP residual stress state
HIP bonding challenged by small radii, length, and wedge shape
Inconel CTE ~ 3X tungsten CTE
Water channels
Water flow
~300 mm

## Slide 4: Target foot assembly

## Slide 5: Mfg. R&D input to aid preparation for final design approval
 |  | R&D Requirements |  |  |  |  | 
 |  | Measure material interfaces’ properties vs. bonding pressure | Predict material interfaces’ bonding pressure | Develop HIP / confirm residual stress prediction is conservative | Fabrication review & approval | Confirm (observe) material interface bonding | Confirm (measure) as-manufactured Inconel properties
Design Deliverables | Analysis confirms material interfaces pass requirements | VHP coupon samples (Q1 FY25) | Full-scale HIP simulation (Q3 FY24 – Q3 FY25) |  |  |  | 
 | Analysis confirms Inconel FOS > 1 |  |  | Small-scale prototypes & simulation (Q3 FY24 – Q3 FY25) |  |  | 
 | Verify design & analysis |  |  |  | Full-scale fabrication (Q1-Q2 FY25) | Full-scale destructive examination (Q2-Q3 FY25) | Full-scale material testing (Q3-Q4 FY25)
in progress
not started
Production

## Slide 6: Near full-scale HIP test assembly fabrication in process
Simplified core and water passages to enable faster fabrication and HIP results by end of 2024

## Slide 7: HIP simulation reveals heat transfer assisted by residual compressive interface pressure post-HIP (regardless of bond quality)
Dark Blue ≥ 100 MPa
Tension
Dark Red ≥ 100 MPa
Compression
1. Heat up
2. Pressure on
(hold)
3. Cool down
“shrink fit”
4. Pressure off
“spring back”
(bonded)
FEA model view is looking down at a center cross-section of a rear edge (one of more difficult regions to bond)
4. Pressure off
“spring back”
(unbonded)
High compression on all radiused surfaces remains even without bonding
Grey ~ 0 MPa

## Slide 8: HIP simulation reveals heat transfer assisted by residual compressive interface pressure post-HIP (regardless of bond quality)
Unbonded interfaces
¼ symmetry model (tungsten and Inconel removed for clarity)
Bonded interfaces
Dark Blue ≥ 100 MPa
Tension
Dark Red ≥ 100 MPa
Compression
Grey ~ 0 MPa

## Slide 9: In general, stress state is similar (regardless of bond quality) – Inconel in tension, tungsten in compression
Bonded interfaces
Unbonded interfaces
¼ symmetry (solid tungsten block used for spallation material)
[Pa, ±400 MPa]
Hydrostatic stress

## Slide 10: Small-scale HIP test articles – 4/7-mm Inconel shells
Piece parts
EB weld development
(note: tungsten core not used, copper buckled during assembly)
Pre-HIP
Post-HIP
60-66 mm
7 mm shell
tungsten
Inconel 718
OFHC copper

## Slide 11: Typical HIP cycle – 950 °C, 200-300 MPa, 2.5 hour hold time

## Slide 12: Mk1 4-mm thick Inconel – 1st cut reveals a mechanically tight structure
oblique cut angle to reduce damage from sectioning
Tungsten damage from sectioning
Initial observations:
Appears mechanically tight everywhere
Inconel/copper appear well bonded
Tungsten cracking caused by sectioning  residual stress relaxation and redistribution upon cutting
Expectations from simulation predictions correspond to failure location and direction
tungsten
718 Inconel
OFHC copper
(polishing and metallography in process)

## Slide 13: Post-cut maximum principal stress prediction shows vertical crack / damage away from W-Cu interface most likely  prediction matches behavior
In-plane of pancake forging (likely to be stronger direction)
Unconstrained (anything between forging axis and in-plane  likely to be weaker direction)
No damage
Max. principal stress orientation
Max. principal stress orientation
[Pa]
Tungsten face
Tungsten face

## Slide 14: Delaminations visible at W-Cu interface (after 2nd cut)
(expected with additional destructive examination due to residual stress relaxation and redistribution)

## Slide 15: Post-HIP copper and Inconel 718 appear tightly bonded in corner (most difficult place to bond)
Differential Image Contrast (creates depth of field)
Large grained copper post-HIP
Initial hardness HRF 80 (~1/2 hard Cu, ~250 MPa 0.5%YS)
Post-HIP hardness HRF 48 (~as hot-rolled, ~70 MPa 0.5%YS)

## Slide 16: Diffusion across bond line with multiple alloys present (shear/thermal testing in process)
Inconel
Cu
Cu
Inconel
VHP bonded shear sample testing in process
25 mm

## Slide 17: Copper Swelling
Li M. and Zinkle S.J. (2012) Physical and Mechanical Properties of Copper and Copper Alloys. In: Konings R.J.M., (ed.) Comprehensive Nuclear Materials, volume 4, pp. 667-690 Amsterdam: Elsevier.
Proton irradiation campaign by Yong Joong Lee to investigate effects of He implantation & DPA damage
What is the lower bound Cu swelling temperature for STS?
180 °C? Less?
~0.6% Δρ / dpa / 100 appm He
STS – Cu:
~1 dpa / yr
~50 He-appm / dpa
Typical pure metal swelling temperature is ~1/3 Tm [°K], which is 180 °C for Cu

## Slide 18: Early design iteration shows copper swelling can reduce fatigue FOS to << 1
Copper swelling zone

## Slide 19: Can Ta replace Cu and eliminate the swelling risk?
W
Ta
Inconel 718
Ta
Inconel 718
Tungsten cracked during cooldown  interface bonds strong enough to resist delamination at edge stress concentrations
Ta
Inconel 718
W
Vacuum hot press:
950 °C, 120 MPa, 2.5 hours
W
Ta
Inconel 718
Significant creep in Ta & 718
27 x 27 mm

## Slide 20: Achieved ~7 μm diffusion band between Ta and IN718
SEM investigation in progress
~7 μm
Ta
IN718
Notes: There is a diffusion band of ≈ 7 µm that is being evaluated in the SEM

## Slide 21: Thermal interface: open questions
Should we be concerned about copper swelling if the predicted copper temperature is < 180 °C?
Are there known issues with diffusion bonding Ta and Inconel 718?
How do diffusion bonded interface properties change with irradiation?
or Ta?

## Slide 22: Summary
Target foot manufacturing R&D is focused on verifying HIP process produces bonded interfaces
Small-scale HIP results confirm mechanically tight tungsten-copper interface and diffusion bonding at copper-Inconel interface
Copper swelling risk has motivated research on use of tantalum as an alternative thermal interface material
Results forthcoming on interface strength, heat transfer, and residual stresses