## Slide 1
HUMAM1, Susumu HATAKEYAMA2, Masatoshi KONDO3
Study on Electromigration Effect
on corrosion and mass transfer
in High-temperature Liquid Metal Pool
16th International Workshop on Spallation Materials Technology
October 31st, 2024
1 School of Environment and Society, Institute of Science Tokyo, Japan
2 School of Engineering, Institute of Science Tokyo, Japan 3 Institute of Integrated Research, Institute of Science Tokyo, Japan
Yoshiki Kitamura1 is going to present on behalf of Mr. Humam.

## Slide 2
Introduction
Liquid lead (Pb) and its alloy have been proposed as a spallation target of accelerator driven systems (ADSs), a coolant of fast reactors (FRs) and a tritium breeder of fusion reactors. The chemical compatibility of liquid Pb with structural materials is one of the important issues to be addressed.
Corrosion behaviors of austenitic steels
in heavy liquid metal coolants (HLMCs) Pb and LBE
Austenitic steels could cause a selective leaching of Ni and Cr in liquid LBE(C. Shroer et al., Corrosion Science 2014), since the solubility of these elements in liquid LBE was quite large at high temperature.
The corrosion of austenitic steels in HLMC was mainly influenced by the temperature, flow velocity and oxygen concentration (G. Ilincev et al., Nucl. Eng. Des. 2006).
M. Kondo et al. JNST (2006 )
316 specimen after exposure
to flowing LBE
Fe
Fig. 1 Cross-sectional SEM/EDX analysis of 316 specimen after exposure to flowing LBE
Depletion of Ni and
penetration of LBE
Oxide
layer

## Slide 3
Electron stream in ADS and Fusion reactors
The electron stream through the interface between liquid metals and structural materials can be produced according to the proton irradiation in ADSs and the α-particle irradiation in fusion reactors.
Electromigration (EM) and its effect on corrosion and mass transfer in high-temperature liquid metals
Electromigration phenomenon in liquid metals was reported. That technology was applied for the coating of micro patterned structures (For example, I. Dutta et al. (2009)).
I. Dutta et al.
Appl. Phys. Lett. 94, 184104 (2009)
Fig. 2 Time-lapse photographs of a molten stream emanating from a Ga bead placed on a Cu stripe on Si, and traveling from right to
left, along the current direction.
However, the effect of electromigration on the material corrosion in liquid metal pools was not clarified so far.

## Slide 4
Purpose of present study
To clarify the effect of electromigration on the material corrosion in liquid metal Pb by means of electromigration experiment in high-temperature liquid Pb pool.
To clarify the theoretical model of electromigration in high-temperature liquid metals.

## Slide 5
Experimental apparatus
used for electromigration test
Outer vessel
Thermocouple
Test capsule
(crucible)
Ar gas
Specimen
Staging
63
43
33
304
Crucible (Al2O3 SiO2)
304 specimen
(Electron down stream)
Liquid Pb pool
Ar
Heater
Insulator
TC
(Test temp.)
Ф20
Outer vessel
Ar gas
304 specimen
(Electron
up stream)
Copper wire
Staging
Test material: 304 austenitic steel
(Fe-18Cr-12Ni)
Liquid metal: Pb
(approximately 100 g: 10cc)
V/S ratio: approximately 2.5 ×10-2
Two 304 specimens were installed. The current flowed through the specimen and liquid Pb.
Cover gas: Ar gas
The temperature inside the vessel was monitored by thermocouple.
Fig. 3 Experimental apparatus used for electromigration test

## Slide 6
Temperature | 773 K
Test material | 304 (Fe-18Cr-12Ni)
Liquid metal | Pb
Test current density (electromigration) | 3.7 A/m2
Test duration | 250 hours
Specimens are cleaned using a solution with a mixture of acetic acid, ethanol, and 30% H2O2 (1:1:1).
The 304 specimens (tested in upstream and downstream) were observed and analyzed by SEM/EDX, FE-SEM, Auger and EBSD.
Static corrosion tests were also performed without electron current flow.
Experimental conditions of electromigration test in liquid Pb
Table 1 Experimental conditions

## Slide 7
Experimental results
The 304 specimens installed in upstream and downstream revealed different morphology. The surface morphology was different from that after simple static immersion
304
304 specimen
(Electron downstream)
304 specimen
(Electron upstream)
Electron stream
(Electrical current)
Cavity
50 μm
1 μm
Fig. 4 SEM surface tilt image of dimple-like structure on 304 specimen installed in electron downstream
Fig. 5 SEM surface tilt image of precipitations on 304 specimen installed in electron upstream
The morphology of the specimen installed
in electron downstream side is explained in next slide.
Simple static immersion
(304/Pb, 773 K, 250 hr)
Fig. 6 SEM surface image of of 304 specimen tested without electrical current flow.
50 μm

## Slide 8
(a) Fe mapping
50 μm
Depleted region
Matrix region
Morphology of 304 specimen (electron downstream side)
Dimple-like structures were observed on the electron downstream side.
The ferritization of specimen surface was caused by the depletion of Ni in the dissolution corrosion process. (The thickness was approximately 55 μm)
The penetration of Pb elements into the test material was detected according to the results of EDX and AES analysis indicated
Some cavities were also detected on the corroded surface. These cavities were located along the grain boundaries.
304
Resin
(b) Cr mapping
(c) Ni mapping
Cr depletion
Ni depletion
Fe enrichment
Cavities
Fig. 7 EDX mapping analysis on 304 specimen installed in electron downstream side.
Grain boundary
Cavities
Fig. 8 EDX mapping analysis on 304 specimen in stalled in electron downstream side.
Ferritization
Fig. 9 AES Pb mapping analysis on 304 specimen in stalled in electron downstream side. (Tilting angle: 30 degree)
Pb penetration

## Slide 9
Experimental results
304
304 specimen
(Electron downstream)
Liquid Pb pool
304 specimen
(Electron upstream)
Electron stream
(Electrical current)
Cavity
50 μm
1 μm
The 304 specimens installed in upstream and downstream revealed different morphology.
Fig. 4 Dimple-like structure on 304 specimen installed in electron downstream
Fig. 5 Precipitations on 304 specimen installed in electron upstream
The morphology of the specimen installed
in electron upstream side is explained in next slide.

## Slide 10
Morphology of 304 specimen (electron upstream side)
50 μm
304
(a) Fe mapping
Resin
(b) Cr mapping
(c) Ni mapping
Precipitations
Cr depletion
Ni depletion
Fe enrichment
Ni enrichment
(partly)
Cr enrichment
(partly)
Fig. 10 EDX mapping analysis on 304 specimen installed in electron upstream side.
Precipitations were detected on the electron upstream side.
The ferritization of specimen surface was caused by the depletion of Ni in the dissolution corrosion process.
The Cr and Ni enrichment regions were partly detected in the ferritized region. These regions are located along the grain boundaries of ferritized region
Fig. 12 EDX mapping analysis on 304 specimen in stalled in electron upstream side.
Fig. 11 Surface cross sectional FE-SEM COMPO image of specimen installed in electron upstream side.
Cr and Ni rich region
(Fe was not included)
Precipitations
10 μm

## Slide 11
Electromigration is a mass transport phenomenon of metal atoms driven by electrical current.
: Electrostatic force : Electron-wind force : Electron-wind charge number : Electrostatic charge number/valence : Mass of free electron ) : Relaxation time | : Effective charge number : Electron charge : Electric field : Current density : Number density of defects
Forces in electromigration
The electron stream through the metal will be scattered by the metal ions. The momentum transfer will drive the metal atoms to migrate along the direction of the electron stream.
Theoretical model of electromigration in liquid Pb pool (1)
Fig. 13 Forces working on liquid metal atoms and momentum transfer between liquid metal atoms and electrons

## Slide 12
The direction of the electromigration is determined by the liquid metal element.
Electron-wind force is more dominant than electrostatic force in liquid Pb.
Force: Upstream to downstream
Electron-wind force dominant
Force: Downstream to upstream
Electrostatic force dominant
Theoretical model of electromigration in liquid Pb pool (2)
Pb
Fig. 14 Direction of migration of liquid metal atoms

## Slide 13
Cr and Ni dissolved from 304 specimen installed in the downstream side according to the dissolution corrosion.
Pb atoms were pushed onto the 304 specimen surface in the down stream side.
Cr and Ni atoms could migrated along the direction opposite to the electron migration as they escaped from the Pb migration.
Theoretical model of electromigration in liquid Pb pool (3)
The dissolution corrosion could be promoted by the electromigration effect. The Pb penetration into 304 matrix was also promoted by the electromigration effect. (The removal of Pb penetrated could form the cavities)
Cavities
Fig. 15 Effect of electromigration on corrosion and mass transfer in liquid Pb

## Slide 14
  The metal elements on the grain boundary could be pushed into liquid Pb by the electrons. Some pores could be then formed.
The migration of Pb atoms to the downstream side caused the migration of dissolved elements and impurities from downstream side to upstream side.
Some metallic impurities could move into the pores.
Oversaturation of elements on the upstream side resulted in the formation of precipitations.
Theoretical model of electromigration in liquid Pb pool (4)
Fig. 16 Effect of electromigration on corrosion and precipitation in liquid Pb

## Slide 15
The electrical resistance is higher in grain boundary than in grain bulk area.
Electrons will mainly go through the bulk area, which will promote the damage on the grain bulk area.
The difference in the attack rate on the grain bulk and grain boundary will result in the formation of the dimple-like structure.
Theoretical model of electromigration in liquid Pb pool (5)

## Slide 16
The corrosion behavior of 304 steel in liquid Pb pool was promoted by the electromigration which was installed in the downstream side of electron stream. Different rate of attack between the grain bulk and grain boundary area will result in the formation of dimple-like structure.
The migration of liquid Pb will cause the secondary migration of dissolved elements to the upstream of electron stream. This effect could promote the dissolution corrosion in the down stream side. The secondary migration of dissolved elements and impurities will lead to the formation of precipitations on the specimen surface located in the electron upstream side.
Acknowledgement: Dr. Hamaji from NIFS for discussion, Minho O sensei from Tokyo Institute of Technology for help in SEM and EDS analysis, Materials Analysis Division Open Facility Center Tokyo Institute of Technology for help with XRD analysis, Hokkaido University for AES/EBSD and STEM analysis.
Conclusions
Humam’s e-mail : humam.h.32a6@m.isct.ac.jp

## Slide 17
XRD analysis
Supporting Data

## Slide 18
4. Results
Static corrosion test
10 μm
100 μm
No formation of precipitations, cavities, or dimple-like structures were found.
Some surface areas are corroded and exfoliated.
Corrosion damage is less severe with a mass loss of 0.002 g.
100 μm
Cr
Upstream | Downstream
Precipitation layer ~13.80 μm | No precipitation layer
Depleted region ~49.26 μm | Depleted region ~55.06 μm
Flat | Dimple-like structures
Cavities were formed | Precipitations diffused into cavities/pores

## Slide 19
[1] M. Spychalski et al., “Tungsten Langmuir probes from JET-with the ITER-Like Wall: Assessment of mechanical properties by nano-indentation,” Phys. Scr., vol. 96, no. 12, 2021.
The divertor in JET-ILW is rectangular, as shown on the right.
The effective area of the diverter is complicated, but it can be approximated as approximately the same as the area of the rectangle, 0.1 A / (0.6 x 0.2 cm) = 0.83 A/cm2