## Slide 1: Applying a Pressure System Safety Code to Spallation Target Design
29 October 2024
IWSMT-16
Joseph B. Tipton, Jr. & Justin Mach
Second Target Station (STS) Project
Notes: Image - 2021-P09584: Aerial overview of the Spallation Neutron Source, SNS, and the future location for the SNS Second Target Station, September 30, 2021. This image has been reviewed by an ORNL Releasing Official and is approved for public release, September 26, 2022.

## Slide 2: Agenda: This talk shows the challenges of applying the ASME BPVC and ways it has focused design efforts
Can’t use a factored load methodology due to rotating loads
Code fatigue curves bake-in mean stress & margins
Good final design means simulating manufacturing stresses
To the Code, the HIPed target is like one giant weld
Philosophical questions for consideration

## Slide 3: Philosophical question: Is it even a pressure vessel since it can run to failure and is replaceable?

## Slide 4: Philosophical question: Is it even a pressure vessel since it can run to failure and is replaceable?
Target segment is below ASME/BPVC volume minimums

## Slide 5: Philosophical question: Is it even a pressure vessel since it can run to failure and is replaceable?
Target segment is below ASME/BPVC volume minimums
PHAR/SAD/ASE process required by DOE O 420.2 ensures a level of safety greater than the protection afforded by the ASME/BPVC

## Slide 6: Philosophical question: Is it even a pressure vessel since it can run to failure and is replaceable?
Target segment is below ASME/BPVC volume minimums
PHAR/SAD/ASE process required by DOE O 420.2 ensures a level of safety greater than the protection afforded by the ASME/BPVC
Structural failure of the target segment would not present a safety hazard.

## Slide 7: Philosophical question: Is it even a pressure vessel since it can run to failure and is replaceable?
Target segment is below ASME/BPVC volume minimums
PHAR/SAD/ASE process required by DOE O 420.2 ensures a level of safety greater than the protection afforded by the ASME/BPVC
Structural failure of the target segment would not present a safety hazard.
Pressure safety and worker safety are provided through the core vessel.

## Slide 8: Philosophical question: Is it even a pressure vessel since it can run to failure and is replaceable?
Target segment is below ASME/BPVC volume minimums
PHAR/SAD/ASE process required by DOE O 420.2 ensures a level of safety greater than the protection afforded by the ASME/BPVC
Structural failure of the target segment would not present a safety hazard.
Pressure safety and worker safety are provided through the core vessel.
Akin to B31.3 concept of safeguarding through “barricades or shields”

## Slide 9: Philosophical question: Is it even a pressure vessel since it can run to failure and is replaceable?
Target segment is below ASME/BPVC volume minimums
PHAR/SAD/ASE process required by DOE O 420.2 ensures a level of safety greater than the protection afforded by the ASME/BPVC
Structural failure of the target segment would not present a safety hazard.
Pressure safety and worker safety are provided through the core vessel.
Akin to B31.3 concept of safeguarding through “barricades or shields”

## Slide 10: Target design relies on HIP that imparts significant residual stresses. It’s as if the entire target foot is a weld.

## Slide 11: Target design relies on HIP that imparts significant residual stresses. It’s as if the entire target foot is a weld.
Stainless Steel Heel
Inconel Shroud
Cu Clad
W
Ta
Coolant
Target
Foot
Target Leg

## Slide 12: Target design relies on HIP that imparts significant residual stresses. It’s as if the entire target foot is a weld.
T = 700°C
T = 30°C;
(then Water Pressure )
T = 30°C
T = 30°C + PulseΔT
Shift x = -0.75mm
Beginning-of-Life (BOL) Fatigue Analysis Methodology

## Slide 13: Target design relies on HIP that imparts significant residual stresses. It’s as if the entire target foot is a weld.
T = 700°C
T = 30°C
T = 30°C
Shift x = -0.75mm
Manufacturing Residual Stresses

## Slide 14: Rotating loads create unforeseen problems with elastic-plastic static analysis.

## Slide 15: Rotating loads create unforeseen problems with elastic-plastic static analysis.
ASME BPVC.VIII.2 Part 5 “Design by Analysis”
Stress categorization
Stress linearization for singularities
Elastic-Plastic Method
Thermoelastic-plastic curves with hardening
Load & Resistance Factor Design (LRFD)
Convergence = Acceptance
Elastic Method

## Slide 16: Rotating loads create unforeseen problems with elastic-plastic static analysis.
ASME BPVC.VIII.2 Part 5 “Design by Analysis”
Stress categorization
Stress linearization for singularities
Elastic-Plastic Method
Thermoelastic-plastic curves with hardening
Load & Resistance Factor Design (LRFD)
Convergence = Acceptance
Elastic Method

## Slide 17: Rotating loads create unforeseen problems with elastic-plastic static analysis.
ASME BPVC.VIII.2 Part 5 “Design by Analysis”
Elastic Method
Stress categorization
Stress linearization for singularities
Limit-Load Method
Elastic-Plastic Method
Thermoelastic-plastic curves with hardening
Load & Resistance Factor Design (LRFD)
Convergence = Acceptance

## Slide 18: Code fatigue curves bake-in mean stress and stress margins.

## Slide 19: Code fatigue curves bake-in mean stress and stress margins.
Start with SN curve fit to data
NUREG/CR–6909

## Slide 20: Code fatigue curves bake-in mean stress and stress margins.
Start with SN curve fit to data
Adjust curve down to include max possible mean stress (no hardening)
Mean Stress
Alternating Stress
NUREG/CR–6909

## Slide 21: Code fatigue curves bake-in mean stress and stress margins.
Start with SN curve fit to data
Add margin as worst of x12 cycles or x2 stress
Adjust curve down to include max possible mean stress (no hardening)
Mean Stress
Alternating Stress
NUREG/CR–6909
NUREG/CR–6909

## Slide 22: Code fatigue curves bake-in mean stress and stress margins.
Inconel 718 (Solution Annealed)

## Slide 23: Code fatigue curves bake-in mean stress and stress margins.
"These ASME curves are not useful for predicting the cycle life of equipment. They are used to specify a permissible design life which includes a large factor of safety.“
https://www.pveng.com/origins-of-the-asme-fatigue-life-curves-post/
Inconel 718 (Solution Annealed)

## Slide 24: Code fatigue curves bake-in mean stress and stress margins. Instead we utilize…

## Slide 25: Code fatigue curves bake-in mean stress and stress margins. Instead we utilize…
Nominal S-N Curves
SS316L nominal curve
IN718(SA) with grain size

## Slide 26: Code fatigue curves bake-in mean stress and stress margins. Instead we utilize…
Nominal S-N Curves
SS316L nominal curve
IN718(SA) with grain size
High Fidelity FEA
Manufacturing (HIP, machining, welding)
Start-up (pressure, quasi-steady state)
Pulse & Response

## Slide 27: Code fatigue curves bake-in mean stress and stress margins. Instead we utilize…
Nominal S-N Curves
SS316L nominal curve
IN718(SA) with grain size
High Fidelity FEA
Manufacturing (HIP, machining, welding)
Start-up (pressure, quasi-steady state)
FEA Fatigue
Critical Plane Theory
Ductile/Brittle Fatigue Models
Pulse & Response
Goodman Mean Stress Correction

## Slide 28: Code fatigue curves bake-in mean stress and stress margins. Instead we utilize…
Nominal S-N Curves
SS316L nominal curve
IN718(SA) with grain size
High Fidelity FEA
Manufacturing (HIP, machining, welding)
Start-up (pressure, quasi-steady state)
FEA Fatigue
Critical Plane Theory
Ductile/Brittle Fatigue Models
Pulse & Response
Goodman Mean Stress Correction
FFOS (Fatigue Factor-of-Safety)

## Slide 29: Residual stresses drive the design performance. Final design simulations need HIP, machining, and welding fidelity.

## Slide 30: Residual stresses drive the design performance. Final design simulations need HIP, machining, and welding fidelity.
Solid shroud through HIP
Reduced stresses after cooling passage drilling

## Slide 31: Residual stresses drive the design performance. Final design simulations need HIP, machining, and welding fidelity.
Solid shroud through HIP
Reduced stresses after cooling passage drilling
Permanent Cover – High Stresses after HIP
Cover added after HIP & machining – Reduced Stresses

## Slide 32: Commercial pressure safety codes don’t fit spallation targets…

## Slide 33: Commercial pressure safety codes don’t fit spallation targets…
…but they can guide good target design.