## Slide 1: Status and Plan of Materials and the Radiation Damage Analysis in FRIB
Eiichi Wakai (FRIB, Michigan State University) T. Kanemura,(FRIB), S. MILLER (FRIB), J. WEI (FRIB), S. MAKIMUA(J-PARC), T. ISHIDA (J-PARC), K. Ammigan(Fermilab)
November 1, 2024

## Slide 2: Radiation Damage – General Phenomena and Design Requirement for lifetime
Phnomena | Temp. (K) | Displacement Damage
Radiation hardening and embrittlement | < 0.35 - 0.4TM | >0.1 dpa
Irradiation creep | <0.40 - 0.45TM | >10 dpa
Volumetric swelling from void formation | 0.3-0.6 TM | >10 dpa
Phase instability from radiation-induced precipitation | 0.3-0.6 TM | >10 dpa
High temperature He embrittlement | >0.45 - 0.5 TM | >10 dpa
Radiation-induced amorphization | >0.18 TM (graphite) | >0.5 – 10 dpa
0 K
Melting point (TM)
1
0.5
0
Radiation-induced amorphization in Graphite
High temperature He embrittlement (aggregated at grain boundaries)
Irradiation creep
Radiation hardening and embrittlement
Volumetric swelling from void formation
Phase instability from radiation-induced precipitation
Al-193oC
Cu-405oC
Ti-698oC
Graphite-1778oC

## Slide 3: Materials for High-Power Targetry System
Material | Melting Point (oC) | Crystal structure at RT | Threshold displacement energy (eV)
Al | 660 | FCC | 27(*4), 16.5(*5)
Graphite | 3800 - 3950 | Hexagonal | 60 (*1), 24 at 0 dpa (*2, *3) and 12 at 1dpa (*2), 69 (*4), 25(*5)
Cu | 1084 | FCC | 33(*4), 19(*5), 30 (*6),
Ti | 1668 | HCP | 19(*5), 21 (0.3-0.5 MeV electron), 31 ( 0.5-2.5 MeV) (*7)
Ti-64 Alloy |  | HCP+BCC | 66 (in α-phase), 46 (in β-phase) (*8)
*1: UK Nuclear Industry Standard
*2: (For pristine graphite, the best estimate of Ed is 24 eV. Ed decreases with increasing irradiation damage, dropping by nearly a factor of 2 at a dose of one displacement per atom. For a fully disordered amorphous-carbon structure, Ed is around 5 eV. )
*3: IAEA Techdoc-1154 in 2000, Irradiation damage in graphite due to fast neutrons in fission and fusion systems.
*4: Y. Iwamoto, S. Meigo, S. Hashimoto, Estimation of reliable displacements-per-atom based on athermal recombination-corrected model in radiation environments at nuclear
fission, fusion, and accelerator facilities, Journal of Nuclear Materials 538 (2020) 152261
*5: H.H. Anderson, The Depth Resolution of Sputter Profiling, Appl. Phys. 18, 131--140 (1979).
*6: A.Yu. Konobeye, U. Fischer, Yu.A. Korovin, S.P. Simakov, Evaluation of effective threshold displacement energies and other data required for the calculation of advanced atomic displacement cross-sections, Nuclear Energy and Technology 3 (2017) 169–175.
*7: G. Sattonnay, et al., Determination of displacement threshold energies in pure Ti and in c-TiAl alloys by electron irradiation, J. Nucl. Mater. s 275 (1999) 63-73.
*8: Ankit Roy, et al., Insights into radiation resistance of titanium alloys from displacement cascade simulations, J. Nucl. Mater. Volume 586, 2023, 154695.
Threshold displacement energy (Td) is the minimum kinetic energy that an atom in a solid needs to be permanently displaced from its site in the lattice to a defect position

## Slide 4: Void Swelling Resistance
Jinlong Du, Suihe Jiang, Peipei Cao, Chuan Xu, Yuan Wu, Huaqiang Chen, Engang Fu & Zhaoping Lu, Superior radiation tolerance via reversible disordering–ordering transition of coherent superlattices, Nature Materials 22, pages442–449 (2023)
Superior radiation tolerance of superlattice steel containing high-density Ni(Al,Fe) NPs. Comparison of b and c shows that the superlattice steel exhibits much stronger void swelling resistance than 9Cr ODS steel. a, Void swelling in superlattice steel compared with that of typical conventional austenitic steels, ferritic–martensitic (F-M) steels and ODS steels (Supplementary Information gives detailed descriptions). The coloured areas are guides to the eye. The inset (zoomed-in view of the dashed rectangular box) shows that superlattice steels exhibit zero void swelling compared with several typical ODS steels. b, TEM micrograph of the superlattice steel after average radiation damage of 2,350 dpa within the investigated region at 500 °C, and no voids were observed. c, TEM micrograph of 9Cr ODS steel after average radiation damage of 840 dpa at 500 °C, and numerous voids were observed. The images in b and c were recorded in underfocus with a defocus distance of −2.0 μm
500oC

## Slide 5: FRIB (Facility for Rare Isotope Beams)
Michigan State University's research in nuclear physics has made it one of the top universities in the USA.
It can accelerate ions from protons to uranium to 200 MeV/u(Currently at the 20 kW level. In the future (5 years later) 400 KW) FRIB is conducting research mainly in nuclear physics, but it will also pursue isotope production.

## Slide 6: Background FRIB (Facility for Rare Isotope Beams)
Thomas Glasmacher, Alexandra Gade, Georg Bollen & Jie Wei, The Facility for Rare Isotope Beams: Providing New Opportunities for Science, Nuclear Physics News, Vol. 34, No. 3, 2024, pp.5-12.
a) Single-slice graphite target inside the water-cooled copper enclosure; (b) thermal image of a 10.4kW, 177MeV/u 238U beam on the target rotating at 500 revolutions per minute; (c) intermediate mini-channel beam dump and (d) rotating beam dump.
FRIB facility graphic showing layout of all areas

## Slide 7: FRIB Rump-up Schedule
EPOCH | 1 |  | 2 |  | 3 |  | 4 |  | 5 |  | 6
Beam Power | 10 kW |  | 20 kW |  | 50 kW |  | 100 kW |  | 200 kW |  | 400 kW
ARTEMIS, light ion beams from gas |  |  |  |  |  |  |  |  |  |  | 
ARTEMIS, heavy ion beams from metal |  |  |  |  |  |  |  |  |  |  | 
High Power ECR, gas beams |  |  |  |  |  |  |  |  |  |  | 
High Power ECR, metal beams |  |  |  |  |  |  |  |  |  |  | 
Intermediate power charge selector in FS1 |  |  |  |  |  |  |  |  |  |  | 
High power charge selector in FS1 |  |  |  |  |  |  |  |  |  |  | 
Post-stripper chicane |  |  |  |  |  |  |  |  |  |  | 
Additional beam collimation in FS2, BDS |  |  |  |  |  |  |  |  |  |  | 
Dual charge state heavy ions upstream of the stripper (velocity equalizer) |  |  |  |  |  |  |  |  |  |  | 
Rotatable target, 1 slice |  |  |  |  |  |  |  |  |  |  | 
Rotatable target, multi-slice |  |  |  |  |  |  |  |  |  |  | 
Post-target shield |  |  |  |  |  |  |  |  |  |  | 
Beam dump 6º slant (S-shape) |  |  |  |  |  |  |  |  |  |  | 
Beam dump 6º slant (S-shape), better cooling |  |  |  |  |  |  |  |  |  |  | 
Rotatable beam dump, 1-mm wall |  |  |  |  |  |  |  |  |  |  | 
Rotatable beam dump, 0.5-mm wall |  |  |  |  |  |  |  |  |  |  | 
Medium power ladder wedge system with adjustable slits (hands on) |  |  |  |  |  |  |  |  |  |  | 
High power wedge system (remote handling) |  |  |  |  |  |  |  |  |  |  | 
PPS upgrade with fast ionization chambers |  |  |  |  |  |  |  |  |  |  | 
As increasing beam power, materials and devices receive radiation damage and the related phenomena.
The analysis of the status of property changing of materials/devices needs to check for safety longer operation.
Some Subjects for the Power Upgrades:
Higher design standards and manufacturing techniques like ISIS
Highly inspection of materials and device (including development) before operation
PIE of the devices (inside and outside FRIB ) after operation
Simulated irradiation experiments using MIBL and the others
Collaborative researches
Intense Working teams for high-power targetry systems

## Slide 8
How challenging is FRIB?: Areal Heat Density (W/m2)
0.1
1
10
100
1,000
(MW/m2)
0.01
0.001
Hot Plate
Pressure vessel in light-water reactor
FRIB:
10-400 GW/m2
IFMIF
（Design Phase）
10,000
100,000
Present
Operation (20 kW)
in beam with 1 mm diameter
J-PARC and SNS - Proton beam
ITER
Transient heat flux of plasma
in Fusion reactor
Nozzel of Rokket Engine
Grand surface
Surface of the Sun
Neutrino Facility in J-PARC (Beam window)

## Slide 9: FRIB Target and Beam Dump (including plan)
Ion Beam
T. Glasmacher, A. Gade, G. Bollen & J. Wei, The Facility for Rare Isotope Beams: Providing New Opportunities for Science, Nuclear Physics News, Vol. 34, No. 3, 2024, pp.5-12.
Present Beam Bump (20 kW operation)
Next Step Beam Bump (more than 50 kW)
Target (graphite)
From M.Avilov, HPTW-2018, June 4th - 8th 2018.
Ti-alloy shell thickness 0.5 mm to reduce power deposition in the shell
600 rpm and 70 cm diameter to limit maximum temperature and amplitude of temperature changes
60 gpm water flow to provide cooling

## Slide 10: World’s Accelerator Device Employing or Planning Ti-6Al-4V Alloy
LBNF target container and beam window
J-PARC Neutorino’s beam window
CERN LHC Main beam dump beam window
MSU-FRIB beam dump
ILC 14MW main beam dump (water) beam window
10
FNAL LBNF Neutrino Target
Previous design: MSU-FRIB Water Cooling Rotating Beam Dump, 300 kW, 7dpa/yr
LHC Main Dump Window
for Run-3
ILC Water Main Dump
Window
Information By Taku Ishida (J-PARC)
Neutrino Facility in J-PARC (Beam window)

## Slide 11: Device List of high-power targetry system of FRIB (Uranium beam case) (including conceptual design evaluation)
 | Device | Beam-intercepting material | Beam power at device (power at target) | Thermal load (Uranium) Deposited Power |  | Type | DPA (irrad. period) | Implanted ion concentration
Linac (FS1) ~ 20 MeV/u | Charge stripper | Graphene sheet | 2.5 kW (20 kW) | 94 W |  | Rotating solid | 9 dpa (1 week) | N/A
 |  | Liquid lithium | 50 kW (400 kW) | 1360 W |  | Liquid film w/o window | N/A | N/A
 | Charge selector | Glidcop AL-15 (Cu alloy) | 2.5 kW (20 kW) | 500 W |  | Static solid, water cooled | 3000 dpa (1 week, at peak) | 10 at% (1 week)
 |  | Graphite (planned) | 13 kW (100 kW) | 3 kW |  | Rotating solid | 80 dpa (1 week at peak) | 0.07 at% (1 week)
 |  | TBD (liquid metal) | 50 kW (400 kW) | 10 kW |  | Liquid film w/o window | N/A | N/A
Target Hall ~ 200 MeV/u | Target | Graphite | 400 kW (400 kW) | 100 kW |  | Rotating solid | 8 dpa (2 weeks) | N/A
 | Beam dump | CuCrZr | 15 kW (20 kW) | 15 kW |  | Static solid, water cooled | 12 dpa (1 week) | 0.02 at% (1 week)
 |  | Water in thin-wall Ti shell | 37.5 kW (50 kW) | 300 kW |  | Rotating liquid water/ window | 7 dpa in shell (1 year) | N/A
Urgent Issue Device
Notes: Charge stripper suffers the severest condition (beam focused on thin film, high dE/dx due to low energy).
Target will have a similar thermal load but have advantage of thickness (rigid). Graphite is ok.
Beam dump and charge selector for high power operations will be liquid due to Bragg peak.

## Slide 12: Beam Dump Ti Alloys - Irradiation Damage Behavior
Under RaDIATE Collaboration,
several Ti alloys have been examined.
(1) How long can Ti-64 withstand irradiation?
(2) Are there any titanium alloys that are superior in the irradiation environment?

## Slide 13: BLIP Irradiation of BLN Results under RaDIATE Collaboration
Tensile Property
Stress
range
0.25DPA
0.95DPA
Strain (%) ＝ Elongation÷Gauge length
0
10
5
15
0
250
500
750
1000
Stress (MPa)
After irradiaiton
：0.0％
Before
Irradiation
Uniform Elongation
7.0%
Entirely Brittle
1250
Hardening
Confidential
Ti-15V-3Cr-3Sn-3Al
Solution-Treatment and Aged (STA)
0.25DPA
0.95DPA
Unirr.
1.5％ uniform elongation after irradiation
Tensile Property of irradiated Ti-64 and Ti-15-3

## Slide 14: Radiation damage effect of Ti-64 (annealed) by high energy protons
Immediately after irradiation, at about 0.1 DPA, Ti-6Al-4V is radiation hardened and loses ductility
Formation of dense nano-sized a-type defect clusters in the main α(HCP)-phase: main cause of irradiation hardening and embrittlement.
Radiation-induced ω phase formed in β(BCC)-phase
T.Ishida, E.Wakai et al. J. Nucl. Mat. 541 (2020) 152413
Stress
range
0.25DPA
0.95DPA
Strain (%) ＝ Elongation÷Gauge length
0
10
5
15
0
250
500
750
1000
Stress (MPa)
After irradiaiton
：0.0％
Before
Irradiation
Uniform Elongation
7.0%
Entirely Brittle
1250
Hardening
Confidential
｛110｝b
<0001>w
// <11１>b
Z= <110>b
//<1120>w
-
I-FFT
Atomic column imaging
By M.Olszta, D.Edwards(PNNL)
ｇ=0111
a-type loops only
ZA<113>b
（0.23dpa）
Unirr.
0.95 dpa
Z＝ <113>b
β phase
(BCC)
ω phase
（Hexagonal non-CPed）
α phase
(HCP)

## Slide 15: Radiation damage effect of Ti-15-3 (STA) by high energy protons
Ti-15V-3Cr-3Sn-3Al
Solution-Treatment and Aged (STA)
0.25DPA
0.95DPA
Unirr.
1.5％ uniform elongation after irradiation
Uniform Elongation (%)
(dpa)
Complete loss of UE (Ti64)
Preserve a few % UE
(Ti-15-3 STA)
(dpa)
Yield Strength (MPa)
Ti-6Al-4V
Ti-15-3STA
Hardening
(Ti-64)
β
α
ZA<113> β
α
β
ZA<1120> α
Ti-15-3STA shows only slight hardening and retains ductility after irradiation at ～1 dpa.
Fine, highly distorted β+α phase structure reduces irradiation effects.
No irradiation-induced damage was found.
Diffuse streaks characteristic of ω-phase precursors. Irradiation did not grow the ω phase.
0.95DPA
Confidential
Confidential

## Slide 16: Higher dpa - Low energy Ion Irradiation Experiment
Materials： KSW KS15-3-3-3 (Ti-15V-3Cr-3Sn-3Al) sheet material manufactured by Kobe Steel, Ltd. undergoes a two-step (low → high temperature) aging treatment (ST2A)
  Unaged (ST), aged (STA) and Ti-64 annealed (A)
  Mechanical polishing on strip-shaped specimens ⇒ Electropolishing to remove the machined layer.
Irradiation： 2.8MeV-Fe2+ion beam at HIT facility, Univ.Tokyo
  ~1x10-3 dpa/s, up to ~11 dpa, damage peak at 1.2 μm depth
  Under room temperature (RT) and 300℃
  Masking produces unirradiated areas on the same specimen
Nano-indentation： Shimadzu Co. DUH-211S
  Berkovich-type, indentation with 150 nm depth×120 times (10μm intervals)
  Compare irradiated and un-irradiated areas
Microscopic observations on radiation damage signatures：
  Focused Ion Beam (FIB) sampling and thin lamellae production
  Electropolishing and/or gentle milling by low-energy Ar ion to remove FIB damage layers and surface oxide layer
  Transmission Electron Microscope: JEOL Ltd. JEM-2100F・JEM-ARM200F・ FEI TITAN3G2 60-300, CTEM/STEM/HREM/EELS/EDS
16

## Slide 17: Nano-Hardness (Irradiation at RT)
In Ti-64, irradiation hardening as large as 1 GPa is observed.
For Ti-15-3, STA material shows some hardening, but ST material without aging treatment (100% metastable β-phase) shows almost no irradiation hardening.
10 μm
Ti-15-3ST
100% β
Ti-64
78% α/ 22% b
Ti-15-3STA
53% b / 47% α
Radiation Hardening

## Slide 18: Ti-15-3ST2A (irradiated at 300℃) nano-hardness
Both Ti-64/Ti-15-3 showed a slight hardening
Radiation Hardeing: 1GPa（Ti-64） >> 0.2GPa（Ti-15-3ST2A）
Ti-6Al-4V, A
Nano-hardness (GPa)
Ti-15-3 ST2A
Nano-hardness (GPa)
Ti-64, A
Ti-15-3, ST2A

## Slide 19: Materials Challenge (High Entropy Ti-Based Alloy) For Application
 | Ti | V | Cr | Zr | Ta | Al | W
Ti-HEA No. 1 | 30 | ● | ● | ● | ● |  | 
Ti-HEA No. 2 | 20 | ● | ● | ● | ● |  | 
Ti-HEA No. 4 | 30 | ● |  | ● | ● | ● | 
Ti-HEA No. 5 | 30 | ● | ● | ● |  |  | ●
(at%)
Ti-based alloys by cold crucible levitation melting (CCLM) in the NIMS (National Institute for Materials Science)
After CCLM melting, normalizing treatments were done at 1200oC for 5 hrs in air, and hot rolling tests were examined for four Ti-HEA.

## Slide 20: Advanced Materials Challenge (High Entropy Ti-Based Alloy) For Application
500
1000
0
1500
0
500
1000
1500
Temperature (oC)
Yield Strength (MPa)
NbMoTaW
(O.N. Senkov)
Inconel 718
Our data (Ti-HEA)
0.1/s
0.01/s
VNbMoTaW
(O.N. Senkov)
Ref. O.N. Senkov et al. / Intermetallics 19 (2011) 698-706
E. Wakai, T. Ishida, K. Furuya, et al., (to be published）
Preliminary
Seeking the possibility of titanium alloys that can be used at higher temperatures (depending on time schedule and resource)
The best titanium alloys, which can be used industrially for long periods of time, have a maximum temperature of up to 600°C (such as DAT54).
Ti-based HEA can be over the Inconel 718 strength.
Compression Tests at high temperature in a vacuum performed in NIMS Facility of Japan
Ti-HEA

## Slide 21: Fe-Mn-Cr-V-Al-C HEA
Chart: 
| 0 | 0.1 | 1
Displacement Damage (dpa) | 6.03 | 5.64 | 5.62
(a)
300oC Irradiation
Chart: 
| 0 | 0.1 | 1
 | 5.27 | 4.96 | 6.02
Nano-hardness (GPa)
(b)
500oC Irradiation
σy = MαGb(Nd) 0.5
Δσy(MPa) = 3.06 ΔHv (kg/mm2)
ΔHv (GPa) = 0.937 ΔHN (GPa),
Dislocation loops with burgers vector of (1/2)<111> type formed in the irradiated Fe-based HEA irradiated at 300oC to 1 dpa under 100 appm He/dpa by Fe3+ and He+ ions. The pictures of (a) bright-field image, (b) weak beam dark-field image, and (c) diffraction pattern were taken from near 011 pole using g=211.
Fe+He ion irradiation
100appmHe/dpa
100appmHe/dpa
E. Wakai et al, Materials Characterization, 2024.
300oC Irrad. case

## Slide 22: Advanced Materials Challenge (High Entropy W-Based Alloy) For Application
Our data (W-HEA)
W-rich W-Fe-Si-V-Cr HEA
Preliminary
Seek higher strength for high temp. application (in metallic materials)
E. Wakai, H. Noto, et al., (to be published）

## Slide 23: Next Step-1 plan for 50 kW (Mid. 2025) and 100 kW operation
Since the beam dump plans to produce isotopes in water, materials with good water corrosion resistance and excellent resistance to irradiation damage are essential.
The thin-walled vessel to receive the beam must be thinner than 1 mm to prevent heat generation under the unprecedented beam load (105 MW/m2), which exceeds that of a fusion reactor divertor, and must be rotatable.
Materials that meet these requirements are limited, and Ti-15-3 material will be selected as a candidate; Ti-15-3 alloy has excellent press workability at room temperature, and thermal processing and optimal heat treatment using this alloy should be performed to take advantage of its characteristics.
Creep evaluation is essential for the long time of 6,000 hours of use, depending on the temperature, but at high temperatures. In titanium alloys, industrially available commercially available materials (e.g., DAT54) have a maximum temperature of 600°C.
FRIB Beam Dump Design Requirement - Basic
- This draft plan is still a private plan and will be discussed within the FRIB. -

## Slide 24: Next Step-2 plan for 50 kW (Mid. 2025) and 100 kW operation
After these, we plan to evaluate the exact dpa and other parameters (the calculated annual damage due to the beam burst was about 7 dpa, but we also plan to evaluate the dpa due to neutrons produced by the reaction between energetic particles and water).
In addition, nuclear heating due to radio-activation will be calculated.
Based on these processes, thermal stress analysis will be carried out, and the conventional design will be modified and updated to achieve the optimum shape for design and fabrication.
In addition, it would be safer to evaluate irradiated materials in bulk materials as much as possible.There are evaluations of thermal fatigue and fatigue with pulsed ions, the former for cycles in the 108 range, while the latter is considered to be a shock wave of low stress, but it will be subjected to fatigue over gigacycles.
FRIB Beam Dump Design Requirement - dpa cal., nuclear heating effect, and others
Wolverine:
3 MV Tandem particle accelerator
Maize:
1.7 MV Tandem particle accelerator
400 KV Ion
Implanter
In-situ TEM
Water corrosion
- This draft plan is still a private plan and will be discussed within the FRIB. -

## Slide 25: Next Step-3 plan for 50 kW (Mid. 2025) and 100 kW operation
PIE and materials characterization are planned to be proceeded in order to correctly understand the state of before and after irradiation in damage of used devices.
Titanium 15-3 is known to have good availability of thin sheets but poor availability of bulk materials, so we will either find a company that can obtain it or fabricate it at a facility such as NIMS in Japan.
Since there are only a limited number of places and facilities where thermal load tests exceeding 100 kW can be performed, it is necessary to proceed with the evaluation of thermal load experiments using electron beams up to 300 kW, such as those at NIFS in Japan.
Since ion irradiation at low energies can be performed to high dpa in a short time, it will be important to promote further material selection.
FRIB PIE and related exams for assignment evaluation
Wolverine:
3 MV Tandem particle accelerator
Maize:
1.7 MV Tandem particle accelerator
400 KV Ion
Implanter
In-situ TEM
Water corrosion
- This draft plan is still a private plan and will be discussed within the FRIB. -

## Slide 26: Summary
The Facility for Rare Isotope Beams (FRIB) is a scientific user facility for nuclear science. FRIB’s superconducting radio frequency (SRF) linear heavy-ion accelerator can accelerate all the ions from hydrogen up to uranium to energies above 200 MeV/u.
FRIB currently operates at a primary beam power of 10 kW 20 kW. Then in particular, the function of the beam dump is planned to include isotope production in water.
The status and private draft plan of urgent devices of the FRIB have been shown, and the radiation damage analysis of Ti alloys and advanced materials are mainly analyzing and should be developing for the application of beam dump in FRIB, etc.
To proceed from 20 kW to over 50 kW, the development of beam dump is urgent issue and thermal fatigue effect (2x108 cycles) due to rotation and evaluation of the synergistic effects of irradiation and water (corrosion), etc. are very important.

## Slide 27: Acknowledgments
We are very thanks to the members of engineering and research teams of FRIB.
The PIE after BLIP irradiation was performed in PNNL and we are grateful to Drs. D. Edwards, D. Senor, A. Casella (PNNL) for their work and P. Hurth (Fermilab) for his coordination in the RaDIATE collaboration.
In low energy ion irradiation experiment of University of Tokyo, we are grateful to Dr. S. Kano and Prof. H. Abe.
In the microstructural analysis, we are grateful to Prof. T. Shibayama (Hokkaido University), Prof. K. Furuya (Hachinohe College) and Dr. A. Hasegawa and Y. Nakayama (National Institute of Materials Science) for their support and discussion.
In compressive tests at high temperature, we are grateful to Ms. N. Motohashi and Mr. S. Kuroda (NIMS), and Dr. Y. Noto (NIFS) for several related tests under a collaboration study.
A part of this work was supported by JSPS Grants-in-Aid for Scientific Research (21H04668, 21H04480), MEXT‘s Nanotechnology Platform (JPMXP09A21HK0074) and NIFS general collaboration program. A part of this work was also conducted at the Hokkaido University and NIMS as a program of “Nanotechnology Platform” and “ARIM” and NOF of NIMS in the Ministry of Education, Culture, Sports, Science and Technology (MEXT), Japan, and the Japan-US Science and Technology Cooperation Program （High Energy Physics）

## Slide 28
Back-up Slides

## Slide 29: Updated Fabrication Test of Beam Window in J-PARC (Neutrino Facility)
T.Ishida, E.Wakai et al. J.Nucl. Mat. 541 (2020) 152413
Recent New Fabrication Test in J-PARC
Beam Window of Neutrino Facility of J-PARC under collaboration of UKRI
0.5 mm thickness in minimum

## Slide 30
Beam profile monitor receiving a small amount of proton beam at J-PARC
Post Irradiation Exam of 50μm-thick Ti-15V-3Cr-3Sn-3Al (Ti-15-3) alloy foils
T.Ishida, E.Wakai et al.
Nucl. Mater. En. 15 (2018) 169-174
Ti-1: 1.4×1020pot
0.12 peak DPA ＠RT
Very low density of defect clusters No significant changes on micro-Vickers hardness
“15-3 Ti alloy may have a high resistance for radiation damage due to nanoscale precipitates working as point defect sink cites”
Radiation Damage Tolerance of Metastable β-phase Ti-15-3(ST)
2D concentration map of Ti varied 79-69at% with amplitude less than 5nm
A high density of nano-clusters of ω phase precursor (athermal ω phase)
stable after irradiation

## Slide 31: Phase transformation of ω phase precursor in metastable β phase of Ti-15-3 ST (irrad. at RT)
Loop formation starts
No loops
E.Wakai, S.Kano, T.Ishida et al. JIMM 2022 Autumn Meeting
E.Wakai et al., HPTW2023, Riken, Nov.7.2023
Hardness measurements using a nano-indenter show that irradiation hardening of about 1 GPa appears in Ti-64, whereas almost no irradiation hardening is observed in Ti-15-3 ST, indicating that it is expected to have high irradiation resistance.
The distribution of radiation damage was found to be depth-dependent from the incident surface, with no dislocation loops observed up to a region of ~ 6 dpa.
The diffraction pattern analysis revealed no clear spots due to the ω phase, but nano-sized atomic disorder, which may be precursors of the ω phase , was observed, and the diffuse streaks seemed to become stronger with increasing dpa. The streaks seem to weaken with further dpa.
Correlation possibly exists between dislocation loop formation and ω phase transformation
＋0.2GPa
Tentative
Tentative
Tentative
Tentative

## Slide 32: Nano-hardness change of Ti-64 (irradiated at RT) & TEM observation
Nanoindentation hardness increases at 1 dpa and remains constant up to 11 dpa.
This is because the number density of nano-size defect clusters in the dominant α phase saturates at 1 dpa.
α-phase
b-phase
T.Ishida, S.Kano, E.Wakai et al, J. Alloys and Compounds 995 (2024) 174701 / arXiv:2405.00517 [cond-mat.mtrl-sci]
Dark contrast in red/yellow,
light contrast in blue/purple
[]
[]
I-FFT Filtered
In contrast, in the β phase, there are very few dislocations and no phase transformations.
In the I-FFT image of HREM, regular lattice disorders uniformly distributed in the β-phase corresponding to the precursor of the ω-phase are observed.
Why does this structure have a sink effect ?
Cf. E.Sukedai et al.(2019) https://doi.org/10.2320/matertrans.ME201910

## Slide 33: Graphite Radiation Damage - Amorphous below 500oC
Tetsuo Tanabe , et al., Radiation damage of graphite - degradation of material parameters and defect structures, Phys. Scr. T64,1996, pp.7-16.
For pristine graphite
Filip Vukovic, Jean-Marc Leyssale,Philippe Aurel,Nigel A. Marks, Evolution of Threshold Displacement Energy in Irradiated Graphite, PHYSICAL REVIEW APPLIED 10, 064040 (2018)
Graphite Structural Change
Amorphous is induced by irradiation below about 500oC
The best estimate of Ed is 24 eV. Ed decreases with increasing irradiation damage, dropping by nearly a factor of 2 at a dose of one displacement per atom. For a fully disordered amorphous-carbon structure, Ed is around 5 eV
(Very careful: 60 eV is adopted in UK Nuclear Industry Standard)

## Slide 34
Total displacements: 229,664/Ion
(Total Vacancies: 229,664/Ion, Replacement collision: 0/Ion)
Ion longitudinal = 6.32 mm
Ti = 1mm thickness
Density=4.51 g/cm3
Water = 10 mm thickness
Density=1.0 g/cm3
Ion 238.05 amu, 47.6 GeV
Total displacements: 231,663/Ion
(Total Vacancies: 231,663/Ion, Replacement collision: 0/Ion)
Ion longitudinal = 7.63 mm
Ti = 0.5mm thickness
Density=4.51 g/cm3
Water = 10 mm thickness
Density=1.0 g/cm3

## Slide 35
Ducted fume food
Mechanical Testing (long time test for fatigue)
Mechanical Testing (short time for tensile or )
Mechanical Testing (long time test for creep)
True-stress and strain
Mechanical and Corrosion Testing (water)
Nano-Indentation Testing
Work desk
Work desk
Shelves
Optical Microscope
Laser Microscope
SEM/EDS/EBSD
Heat Furnace
X-ray Reflation Diffraction
Hardness
Cutting, Polishing
Arc Melting
4-terminal electric resistivity
Ultra sonic test
Shelves
Work desk
Optical Microscope
Ultra-sonic vibration
Materials Testing (draft private)Plan