## Slide 1: Gas Production in the Proton Beam Window and Target Vessel at SNS
Wei Lu, Franz X. Gallmeier & David McClintock
Oak Ridge National Laboratory, Oak Ridge TN, USA
16th International Workshop on Spallation Materials Technology (IWSMT-16)
Abingdon, Oxfordshire, UK
Oct. 29 2024

## Slide 2: Contents
SNS and its proton beam windows & targets
Measurements at the Harp and constructions of proton beam profiles
Cross section calculations for the gas production
Gas productions at PBWs 6&7 and Target 12
Summary

## Slide 3: Current Status of SNS
Completion of PPU (Proton Power Upgrade) project this summer
SNS is now operating at 1.3 GeV and 1.7 MW and will reach the designed full capacity of 2 MW in 2026
1.7 MW
1.3 GeV

## Slide 4: SNS FTS Target-Moderator-Reflector System
Consists of PBW, mercury target, IRP (Inner Reflector Plug) and ORP (Outer Reflector Plug)
IRP, an Al-6061 structure cooled by heavy water, hosts four moderators (3 cryogenic hydrogen moderators and 1 ambient water moderator), beryllium reflector and stainless steel (SS) shielding
ORP, a SS structure cooled by heavy water, consists of SS shielding
PBW is located ~2.35 m upstream of the target nose tip

## Slide 5: SNS Mercury Target Module
Water-cooled shroud
Mercury vessel
Both water-cooled shroud and mercury vessel nose are double-walled
Water-cooled shroud
  1.52 mm SS
  3.56 mm water
  1.78 mm SS
3.05 mm helium
Mercury vessel
  3.05 mm SS
  2.03 mm mercury
  3.05 mm SS

## Slide 6: Proton Beam Windows at SNS
PBWs 1-5 & 7
PBWs 6 & 8 (current)
Uninstalled PBW 6
Effective Al thickness
is 3.4 mm

## Slide 7: Gas Production Measurements in Plan
Measurements of hydrogen and helium productions on PBWs 6&7 and Target 12 are planned
PBW 6 (Al-6061)
PBW 7 (Inconel-718)
Target side
Accelerator side

## Slide 8: Gas Production Measurements in Plan
4 specimens in each disk for PBW 6 and 12 specimens in each disk for PBW 7 & Target 12. 3 disks for PBWs 6&7 and 1 disk for Target 12
Either inductively coupled plasma–mass spectroscopy (ICP-MS), or thermal ionization mass spectroscopy (TIMS) will be applied
Analytical Chemistry Laboratories (ACL) at the Chalk River Laboratories (CRL), Canada
Target 12 after sample cutting
Machining map for PBW 6
Machining map for PBW 7 & Target 12

## Slide 9: Measurements at the Harp at SNS
W. Blokland, HIGH BEAM INTENSITY HARP STUDIES AND DEVELOPMENTS AT SNS, Proceedings of 6th International Particle Accelerator Conference (IPAC-15), Richmond, Virginia, USA , May 3-8, 2015
Harp is located at 7.192 m from the PBW
Consists of 30 tungsten (100 um) wires for each of the horizontal, vertical, and diagonal planes.
Designed to measure the position, profile and peak current density of the passing proton beam
No magnets downstream of the harp

## Slide 10: Fitting Harp Measurements
Harp measurements have limited space resolution and show variations due to electronic signals
They are hence fitted:
a > 2

## Slide 11: Predicting Beam Profile and Direction at PBW
Since it is free drifting downstream of the harp, the beam size downstream could be predicted by the measurements at the harp and magnets upstream by the RTBT Wizard
The direction of the beam is determined by the expansion/converging of the beam footprint

## Slide 12: Fitted Harp Measurements

## Slide 13: Fitted Harp Measurements

## Slide 14: SNS Operation History
Target 12
PBW 6 (Aluminum)
PBW 7 (Inconel)
Beam power
Beam energy

## Slide 15: Target 12
Average proton energy: 939.5 MeV
Total energy during operation: 4492.5 MWhr

## Slide 16: PBW 6
Average proton energy: 1002.2 MeV
Total energy during operation: 15892.6 MWhr

## Slide 17: PBW 7
Average proton energy: 996.8 MeV
Total energy during operation: 15239.1 MWhr

## Slide 18: Calculations of Gas Production Cross Sections
Recalculation of hydrogen and helium production cross sections
  recent updates of INC models
  many mass spectroscopy techniques capable to distinguish isotopes of hydrogen and helium
Elemental targets:
  C, Mg, Al, Si
  Ti, V, Cr, Mn, Fe, Co, Ni, Cu, Zr, Nb, Mo, Ag, Sn
  Ta, W, Au, Hg, Pb, Bi, U
Particle transport code, MCNP6
  CEM03.03
  INCL4

## Slide 19: Calculation Methods for Gas Production Cross Sections
Htape3x not maintained and not correctly working in MCNP6
Production cross sections
  Tally all particles produced
  GENXS card
Residual cross sections
  Tally productions stay within the target
  Thin targets of 1 mm was used
  AARE (Activation in Accelerator Radiation Environments) code
    Prepares MCNP output for nuclide inventory calculation codes, supports
      CINDER(90/2008)
      SP-FISPACT
      ORIHET3
    Applications in burn-up, activation and transmutation analysis
    V-1.0 released by RSICC and V-2.0 is to be submitted
    Reference: Gallmeier, F. and Wohlmuther, M., AARE_ACTIVATION SCRIPT VERSION 2.0 USER GUIDE, ORNL/TM-2018/1036, Oak Ridge National Laboratory, Oak Ridge, TN 2018

## Slide 20: Hydrogen and Helium Cross Sections Calculations - CEM03.03 vs INCL4
INCL4 is not capable to produce light nuclides in transmutation
CEM03 shows synthetic tuning for certain energies
CEM03 is close to realistic transmutation productions

## Slide 21: Hydrogen and Helium Cross Sections Calculations - Production vs Residual Cross Sections
For helium, the difference between production and residual C.S. is not significant ~10% or less
For hydrogen, the difference depends on the target and energy, usually ~ a factor of 2
Issue of residual C.S. is geometry dependent

## Slide 22: Hydrogen and Helium Cross Sections Calculations - Fractions of Isotope contributions
Contributions of hydrogen and helium isotopes are energy and target dependent
Similar for incident protons and neutrons
Generally,
  Proton ~60 – 80%
  Deuteron ~20 – 30%
  Triton ~5 – 10%
  Helion ~20 – 30%
  Alpha ~70 – 80%

## Slide 23: Hydrogen and Helium Cross Sections - 1 GeV protons
Targets | Hydrogen (barn) | Isotope contributions (%) |  |  | Helium (barn) | Isotope contr. (%) | 
 |  | P | D | T |  | He3 | He4
Al | 1.81 | 72.6 | 22.9 | 4.5 | 0.43 | 21.7 | 78.3
Fe | 3.88 | 72.2 | 22.8 | 4.9 | 0.68 | 23.6 | 76.4
W | 8.01 | 60.8 | 28.7 | 10.4 | 1.40 | 15.7 | 84.3
Targets | Hydrogen (barn) | Isotope contributions (%) |  |  | Helium (barn) | Isotope contr. (%) | 
 |  | P | D | T |  | He3 | He4
Al | 0.71 | 62.2 | 30.8 | 7.0 | 0.40 | 18.9 | 81.1
Fe | 2.30 | 67.9 | 26.1 | 6.1 | 0.64 | 21.8 | 78.2
W | 5.12 | 55.9 | 31.4 | 12.7 | 1.31 | 14.2 | 85.8
Production cross section
Residual cross section

## Slide 24: Displacement Productions at Target 12
Inner most
Outer most
Displmax = 10.3
dpa
Displmax = 7.6
dpa
Displmax = 8.7
dpa
Displmax = 6.7
dpa

## Slide 25: Displacement Productions at Target 12
Inner most
Outer most
Contrmax =39 %
Contrmax =47 %
Contrmax =53 %
Contrmax =59 %

## Slide 26: Helium Productions at Target 12
Inner most
Outer most
Hemax = 915
appm
Hemax = 919
appm
Hemax = 915
appm
Hemax = 913
appm

## Slide 27: Helium Productions at Target 12
Inner most
Outer most
Contrmax =93 %
Contrmax =95 %
Contrmax =96 %
Contrmax =98 %

## Slide 28: Hydrogen Productions at Target 12
Hmax = 3582
appm
Inner wall of MV
Contrmax =88 %

## Slide 29: Helium and Hydrogen Productions at PBW 6
Inner most
Outer most
Contrmax =99 %
Contrmax =99 %
Hemax = 2133
appm
Hemax = 3576
appm
Displmax = 4.42 dpa

## Slide 30: Helium and Hydrogen Productions at PBW 7
Upstream
Outer most
Hemax = 3948
appm
Hemax = 3945
appm
Displmax = 18.8 dpa
Hmax = 15182
appm
Hmax = 15299
appm
Upstream
Downstream
Downstream
Displmax = 19.6 dpa
Proton contribution 95-99%

## Slide 31: Peak Gas Productions and Uncertainty
 | Avg. proton energy (MeV) | Total energy received (MWhr) | Peak radiation damage productions |  | 
 |  |  | Displacement (dpa) | Helium (appm) | Hydrogen (appm)
Target 12 | 940 | 4493 | 10.3 | 919 | 3582
PBW 6 | 1002 | 15893 | 4.4 | 2133 | 3576
PBW 7 | 997 | 15239 | 19.6 | 3948 | 15299
Proton beam profile
  measurements of Harp: tungsten wire signal variation ~10%
  beam profile fitting: RMS estimate < 5%
Calculations of cross sections
  CEM03 was benchmarked to experimental measurements
  generally ~20%

## Slide 32: Summary
With the anticipation of preparing specimens for measurements, the gas productions for PBWs 6&7 and Target 12 were calculated
  Peak helium productions are 2133 appm for aluminum PBW 6 and 3948 appm (19.6 dpa) for Inconel PBW 7, both reached the tentative radiation damage limit of the material
The incident proton beam profiles were carefully constructed from the Harp measurements and averaged over the operation time
The gas production cross sections were updated with more recent INC models and isotope production cross sections
  CEM03 is reasonable in predicting transmutation productions rather than INCL4 though with synthetic tuning
  Different than helium cross section, the hydrogen residual cross section is geometry dependent
  It is better to calculate hydrogen production with the real geometry using the AARE modified MCNP6 code rather than using its cross sections