## Slide 1
15th April 2024
Sayani Biswas
SONAR 1 workshop (virtual)
Usage of MuDirac in µ-XES experiments
Muonic X-ray Emission
Spectroscopy
µ-
Cu
Ag
Au
Sn
O
Pb

## Slide 2
Outline
µ-XES experiments at ISIS
How MuDirac is being used
Possible inclusions in MuDirac
ISIS
Rutherford Appleton Laboratory

## Slide 3
CHRONUS
µ-XES experiments at ISIS
Target Station 1 (TS1)
Target Station 2 (TS2)
C, 45°
10mm
Currently, we perform the
µ-XES experiments in port 4
20 ms (50 Hz)
TS1
TS2
320 ns

## Slide 4
µ-XES experiments at ISIS
C, 45°
10mm
Currently, we perform the
µ-XES experiments in port 4
Decay-channel
Muon momentum range:
17 MeV/c – 120 MeV/c
(currently 90 MeV/c)
A. D. Hillier et al, Phil. Trans. R. Soc. A (2019)

## Slide 5
µ-XES experiments at ISIS
- beam
Sample
Ge X-ray detector
0.1-10 MeV
Ge X-ray detector
0.1-10 MeV
Ge X-ray detector
low energy
Ge X-ray detector
low-energy
C, 45°
10mm
Currently, we perform the
µ-XES experiments in port 4
MuX setup (under development)

## Slide 6
- beam
Sample
µ-XES experiments at ISIS
Ge X-ray detector
0.1-10 MeV
Ge X-ray detector
0.1-10 MeV
Ge X-ray detector
low energy
Ge X-ray detector
low-energy
A. D. Hillier et al, Microchemical Journal (2016)
- beam
Fe
500μm
Zn
500μm
Cu
500μm
Ag
1000μm
1) Proof-of-concept sample:

## Slide 7
µ-XES experiments at ISIS
- beam
Sample
Ge X-ray detector
0.1-10 MeV
Ge X-ray detector
0.1-10 MeV
Ge X-ray detector
low energy
Ge X-ray detector
low-energy
denarius of Julia Domna
3rd century (211-217 CE)
190 µm
51(1)% Ag
49(1)% Cu
B. V. Hampshire et al, Heritage (2019)
2) Roman silver coins:

## Slide 8
1
2
3
Position | Name of area | Simulated gold thickness
1 | Altar | 1-50 μm
2 | Zachary body | 15.0(5) μm
3 | Angel body | 16.0(5) μm
M. Cataldo, PhD thesis (2024)
- beam
Sample
Ge X-ray detector
0.1-10 MeV
Ge X-ray detector
0.1-10 MeV
Ge X-ray detector
low energy
Ge X-ray detector
low-energy
µ-XES experiments at ISIS
3) Baptistery gate of Florence:

## Slide 9
µ-XES experiments at ISIS
- beam
Sample
Ge X-ray detector
0.1-10 MeV
Ge X-ray detector
0.1-10 MeV
Ge X-ray detector
low energy
Ge X-ray detector
low-energy
Diverse science areas (measured so far using MuX)
  Cultural Heritage
      Bronze Age artefacts
      Mary Rose artefacts
      Swords
      Cannon Balls
      Sundials
      Coins
      Mirrors
      Statues
      Florence baptistery gates (gates of paradise)
  Solar cells
  Piezoelectric devices
  Li batteries
  Steel, corrosion and carbon composition
  Meteorites
  Biomaterials

## Slide 10
How MuDirac is being used
GUI of periodic table using PyQt6

## Slide 11
How MuDirac is being used
GUI for elemental analysis
using PyQt5
Most users are not familiar with large facilities, let alone muons
Need simple to use and intuitive software
EVA (Elemental Visualisations and Analysis):
  Easy to visualise data
  Automatic correction
  Easy to identify elements
    Peaks
    Machine Learning (to be added)
  Simple/basic analysis
  Easy to extend

## Slide 12
How MuDirac is being used
GUI for elemental analysis
using PyQt5
Easy GUI
Automatically sets up
SRIM/TRIM
Adds momentum spread
Scans momentum
Easy plotting of results
Plots individual components
Saves results

## Slide 13
How MuDirac is being used
Machine Learning offers the potential for a ‘black box’
Deep learning to classify the elemental composition
Trained on standard samples
  Pure
  Taking pure samples and ‘mixing them’
Works surprisingly well –
  Work for Cu Sn real data
  And for noisy data
Element | Train acc (%) | Val acc (%)
Ag | 99.98 | 99.96
Al | 99.89 | 99.83
Au | 99.93 | 99.92
B | 99.90 | 99.85
C | 99.90 | 99.86
Cu | 99.97 | 99.94
Fe | 99.87 | 99.80
In | 99.97 | 99.90
Pb | 99.91 | 99.88
Si | 99.90 | 99.75
Sn | 99.93 | 99.92

## Slide 14
Possible inclusions in MuDirac
Intensities of muonic X-rays -> probably already underway
Gamma rays
Muon capture probabilities
Inclusion of oxidation state of the element

## Slide 15
Acknowledgements
Adrian Hillier, all instrument scientists in the MuSR group, and engineers/technicians in
cryogenics, electronics & instrumentation group.
Beth Hampshire - Department of Physics, Warwick University and the ISIS Neutron and Muon Facility
Massimiliano Clemenza, Milan-Bicocca, Italy
Matteo Cataldo, Milan-Bicocca and ISIS Neutron and Muon facility
Don Paul - Department of Physics, Warwick University
Katsu Ishida – RIKEN, Japan
The Matt’s STFC Technology
Simone Sturniolo, Leandro Liboro SCD STFC
Keith Butler, SCD STFC Machine Learning