## Slide 1: Superconducting Thin Film Coating for Radio Frequency Cavities (TF-SRF) at STFC/DL/CI
Main goal:
  to enable STFC for the superconducting thin film coated cavity production and testing
Main objectives:
  Developing coating technology for superconducting thin films (STF)
    Deposition of Nb, Nb3Sn, NbTiN, V3Si, Mg2B, … and SIS structures
      Deposition targets for planar deposition (Nb3Sn, NbTi, V3Si, Mg2B)
    Thin film characterisation
    AC/DC superconductivity evaluation
  Developing cavity deposition expertise
    Copper cavity production
    Cavity polishing and cleaning
    Building deposition facilities
    Optimising deposition parameters
      Deposition targets for cavity deposition in form of tubes or rods: Nb3Sn, NbTi, V3Si, Mg2B
  SRF testing at DL
    1.3 GHz (and 6 GHz) cavity testing as 1st step
    Scaling up to a routine cavity coating and testing
    Multicell cavities
Possible topics
for STFC-DAE collaboration

## Slide 2: Copper cavity preparation
Copper cavity production:
  Half-cell by machining or hydroforming, copper tubes and 316LN flanges,
  Seamless cavity production
    then EB welding
Chemical polishing:
  SUBU5 solution,
  Electropolishing (EP)
Cavity shipping:
  With flanges, filed with N2

## Slide 3: Deposition targets
For planar deposition:
  Materials: Nb3Sn, NbTi, V3Si, Mg2B…
  Diameter 50 mm and 100 mm
For cavity deposition:
  Materials: Nb3Sn, NbTi, V3Si, Mg2B…
  A tube diam. 10-20 mm and length of 0.5-1 m
  or a road diam. 2-5 mm and length of 0.5-1 m
For NEG deposition:
  Materials: alloys of
    Ti-Zr-V, Ti-Zr-Hf-V, Zr-Hf-V, with or w/o Cu or Ag,
    Zr-Cu, Zr-Ag
  or a road diam. 1-3 mm and length of 1-2 m

## Slide 4: International collaborations
Thin film deposition
PVD: DC, pulsed, HIPIMS…
Film characterisation
SEM, FIB, AFM,
Real cavity measurement
Cavity deposition
(PE)CVD, (PE)ALD
XPS, XRD, RBS, TEM…
Superconducting RF properties evaluation
Superconducting properties measurement
RRR, Hc, Hfp, Hsh, …
QPR at CERN
QPR at HZF
HW cavity at ASTeC
Nb, NbN, Nb3Sn, MgB2, SIS, etc.
Surface preparation
Cleaning, etching,
Polishing, passivating
DC magnetic susceptibility,
Field penetration
Nb film laser treatment
I.FAST WP9: Innovative superconducting cavities (01/05/2021-30/04/2025)
The main emphasis is on applying the result of ARIES to RF cavity deposition and testing
Film deposition
SEM image of a NbN thin film
DC magnetisation
QPR
Test cavity
1.3 GHz cavity for STF deposition
ARIES WP15: (01/05/2017-30/04/2021)
The main emphasis is on a systematic study of correlation between

## Slide 5: Other ways of collaboration
ASTeC vacuum solution group is well equipped and experienced to train:
  a visiting scientist (postdoc) – recommended duration is 6 months or longer
  PhD student (registered at any Indian University) – recommended duration is at least 12 months
Topics:
  Vacuum system design and operation (for accelerators and in general)
  Vacuum science
  Non-evaporable getters
  Low SEY
  Thin film coatings and characterisation
  Thin film SRF