## Slide 1
Thin film SRF perspectives in UK
Oleg B. Malyshev
ASTeC/CI
On behalf of a TF SRF team at STFC Daresbury Laboratory

## Slide 2
Introduction
Present state

## Slide 3
Bulk Nb: monopoly since > 50 years
Nb/Cu applications at low accelerating field only until recently
  Figures of merit:
    Eacc  BRF  BSH limitation = magnetic transition
    Q0  1/RS limitation = thermal transition
    Duty cycle (=> 100%): limitation = cryogenic power
    (particle speed /light speed): influences design
  At f < 3 GHz: cavities are mainly limited by BRF!!!
Q0
Eacc
Nb : Limits @ 2 K, 1.3 GHz :
Eacc ~ 55 MV/m (± 5 MV/m)
(Geometry : B/Eacc ~ 4.2 mT/(MV/m))
Rs = RBCS + Rrés.
High field dissipations
quench
P = const, ↑
Investment +
Power consumption
Q0 ↑ Costs ↓
Investment
Eacc ↑ Costs ↓
E Field
B Field
Epeak
Bpeak
0
max.field
Courtesy of C. Antoine (CEA, France)
Aimed performance
Present state
Notes: SC cavity are intensively used for accelerating charged particles, but bulk Nb cavities are ay their performance limit Eacc  BRF  BSH and Q0  1/RS .
We aim to increase both Eacc and Q0. for this we have to look for new solutions.

## Slide 4: Superconductors considered for SRF
Material | TC (K) | BSH (mT)@ 0 K
Pb | 7.1 | 100
Nb | 9.2 | 219,0
NbTi | 9.2-10 | 
NbTiN | 10.6-11.8 | 
V3Si | 17.0 | 
NbN | 17.3 | 214,0
Nb3Sn | 18.3 | 425,0
Nb3Al | 18.5-19.1 | 
MgB2 | 39.0 | 170,0
Pnictides: Ba0.6K0.4Fe2As2 | 38.0 | 756,0
Cuprates: YBaCuO | 93.0 | 1050,0
High TC => High Q0
High HSH => High Eacc … in theory
Courtesy of C. Antoine (CEA, France)
Notes: We are looking for non-Nb SC materials with higher Tc to increase Q0 and higher BSH to increase Eacc.
These materials are under considerations in present

## Slide 5: International collaborations
Thin film deposition
PVD: DC, pulsed, HIPIMS…
Film characterisation
SEM, FIB, AFM,
Real cavity measurement
Cavity deposition
(PE)CVD, (PE)ALD
XPS, XRD, RBS, TEM…
Superconducting RF properties evaluation
Superconducting properties measurement
RRR, Hc, Hfp, Hsh, …
QPR at CERN
QPR at HZF
HW choked cavity at ASTeC
Nb, NbN, Nb3Sn, MgB2, SIS, etc.
Surface preparation
Cleaning, etching,
Polishing, passivating
DC magnetic susceptibility,
Field penetration
Nb film laser treatment
I.FAST WP9: Innovative superconducting cavities (01/05/2021-30/04/2025)
15 partners from 9 countries
The main emphasis is on applying the result of ARIES to RF cavity deposition with non-Nb STF and SRF testing
Film deposition
SEM image of a NbN thin film
DC magnetisation
QPR
Choked cavity
1.3 GHz cavity for STF deposition
ARIES WP15: (01/05/2017-30/04/2021)
9 partners from 6 countries
The main emphasis is on a systematic study of correlation between
Notes: Internationally the TF SRF community is quite small, organised with good working relations and collaborations,
For example, UK team was involved in ARIES… read
When the collaboration has expanded within IFAST project …. read

## Slide 6: Superconducting Thin Film Coating for Radio Frequency Cavities (TF-SRF) at STFC/DL/CI
Main goal:
  To enable STFC for the superconducting thin film coated cavity production and testing
Main objectives:
  Developing coating technology for superconducting thin films (STF)
    Deposition of Nb, Nb3Sn, NbTiN, V3Si, Mg2B, … and SIS structures
    Thin film characterisation
    AC/DC superconductivity evaluation
  Developing cavity deposition expertise
    Copper cavity production (incl. EB welding)
    Polishing and cleaning of copper cavities
    Building deposition facilities
    Developing deposition targets
    Optimising deposition parameters
  SRF testing at DL
    1.3 GHz (and 6 GHz) single cell cavity testing as a 1st step
    Scaling up to a routine cavity coating and testing
    Multicell cavities
Notes: The UK team has the mail goal: read the slide
For this there 3 main objective:

## Slide 7
A path towards the goal
(1) Superconducting thin film development

## Slide 8: Copper surface preparation
Mechanical polishing
Fine mechanical polishing
  diamond turning (for flat samples) at STFC
  tumbling
Chemical polishing:
  SUBU5 solution
  Electropolishing (EP)
Laser polishing
  not proved yet
Combination of different techniques
In present, relying on IFAST partners: INFN/LNL and IJCLab
Needs to be developed at STFC
Notes: In present, only small planar samples can be polished in-house, we have to rely on our collaborations.

## Slide 9: Thin Film Deposition in VISTA
VISTA laboratory
Stablished and coordinated by R. Valizadeh (ASTeC)
CI collaborators: Prof J. Bradley and Dr V. Danak (Liverpool University)
Participants: : J. Conlon, C. Benjamin, S. Simon
Chemical Vapour Deposition (CVD)
Physical Vapour Deposition (PVD)
PVD deposition
Hybrid Physical Chemical Vapour Deposition (HPCVD) Facility
PVD deposition
Notes: To facilitate our aims we have VISTA laboratory where we built various deposition facilities based on a few types PVD, CVD and HPCVD

## Slide 10: Thin film development
Techniques:
  PVD: DC, pulsed, HIPIMS…
  (PE)CVD, (PE)ALD – under development
  Combined: PCVD – under development
Materials:
  Nb
  Nb3Sn, NbTiN, V3Si, NbN, MgB2, etc.
  SIS structures
Deposition facilities
  For planar samples
  For QPR samples
A sample during the Nb deposition
Courtesy of R. Valizadeh (STFC)
A QPR sample during and after the Nb TF deposition
Courtesy of R. Valizadeh (STFC)
Notes: We have significant progress with thin film development:
read

## Slide 11: Thin Film Characterisation in VISTA
Stablished and coordinated by R. Valizadeh (ASTeC)
CI collaborators: Prof J. Bradley and Dr V. Danak (Liverpool University)
Participants: J. Conlon, C. Benjamin, S. Simon, A. Hannah, G. Stenning
Auger
FEI inspect S50 SEM
Auger, XPS
Courtesy of R. Valizadeh
More characterisation facilities are available through collaborations with
The Materials Characterisation Laboratory at ISIS (RAL)
CI universities
Other UK universities
International collaborations
Notes: Various Thin Film Characterisation facilities for analysing TF composition, structure, morphology, etc. available in VISTA and in other labs through collaboration within UK and internationally.

## Slide 12: Thin film characterisation - 1
X-section SEM of Nb3Sn deposited on Cu
X-section SEM of Nb3Sn with a Nb underlayer as double structure on Cu
Courtesy of R. Valizadeh (STFC)
Film crystal structure with EBSD analysis of planar Nb on copper
XRD analysis of NbTiN deposited on copper
Notes: Various TF characterisation techniques are employed for this.
read

## Slide 13: Thin film characterisation - 2
High resolution SEM of ion milled X-section of SIS multilayer structure (Nb/AlN/Nb3Sn) deposited on Ta.
(b) EDX chemical mapping of the X-section. Courtesy of R. Valizadeh (STFC)

## Slide 14: Thin film characterisation – 3
XPS analysis of NbTiN representing Nb and Ti chemical state)
XPS: Composition and chemical analysis
Layer t (1e15at/cm2) t (nm) r(1e22at/cm3) Nb Sn O Al
1 7644.333 1497.201 5.106 75.0000 25.0000 0.0000 0.0000
2 15920.986 2855.270 5.576 100.0000 0.0000 0.0000 0.0000
3 898207.563 76119.281 11.800 0.0000 0.0000 60.0000 40.0000
RBS analysis of Nb3Sn on sapphire
SIMS depth profile of Nb on copper
Film composition and Depth profile

## Slide 15: Superconducting Properties Evaluation
CryoLab
Coordinated by O.B. Malyshev (ASTeC)
CI collaborators: Prof G. Burt (Liverpool University)
Participants: D. Seal, L. Smith, T. Sian, D. Turner, N. Leicester, K. Marks, J. Conlon,
S. Pattalwar, A. May, K. Dumbel, J. Wilson, G. Stenning
Magnetic field penetration facility
RRR/Tc
+ 3 other experiments
RS measurements with
a 7.8 GHz choked cavity and
a 6 GHz split cavity
CrabLab
Notes: Superconducting Properties Evaluation are performed on 3 in-house designed and built facilities in Cryolab and Crablab

## Slide 16: Thin film DC superconducting properties - 1
RRR and Tc measurements: (a) Cryostat, (b) insert, (c) sample holder
Resistance measurements for a V3Si on sapphire
sample indicating the 10, 50 and 90 % transition points
Courtesy of L. Smith (STFC)
Notes: First Superconducting property is whether the film is superconducting is performed by measuring RRR and Tc as shown in this slide

## Slide 17: Thin film DC superconducting properties - 2
Courtesy of E. Seiler (IEE, Slovakia)
PPMS (Physical Property Measurement System)
  Virgin DC magnetisation curve: Ben(~Bc1 perp), [Bp, Bc2]
The Materials Characterisation Laboratory at ISIS (RAL)
IEE-SAS (Bratislava, Slovakia)
Nb/Cu
Determination of the characteristic field Hen from the virgin magnetization curves
Hen for non-Nb STF produced within ARIES WP15
Notes: Physical Property Measurement Systems allow to study the characteristic field Hen from the virgin magnetization curves

## Slide 18: Thin film DC superconducting properties - 3
Magnetic field penetration facility for the planar samples
  TF samples can be compared in conditions similar to ones in the cavity
    DC magnetic field parallel to the surface
    Magnetic field applied from one side of the sample (similar to an SRF cavity)
  Applied and penetrated field measured by Hall probe sensors
  ,
    i.e. SC is in Meissen state when
Courtesy of L. Smith (STFC)
Notes:   A unique Magnetic field penetration facility deigned and built at DL allows to TF samples be compared in conditions similar to ones in the cavity. Read green

## Slide 19: Thin film RF superconducting properties
A radiofrequency (RF) cavity and cryostat dedicated to the measurement of superconducting coatings at 7.8 GHz (CrabLab/DL/STFC)
  Operation with a closed-cycle refrigerator:
    Tcavity = 4.0 K and Tsample = 4.0 K
  Low power (1.0 W) measurements with an emphasis
  on fast turn-around time (~2 days for each sample).
  Flat Sample – a disk diam. 90 - 130 mm
An example of 𝑅s(𝑇s) measurements for Nb and Nb3Sn TF planar samples with the choked cavity.
Sample
Sample Plate
Cavity Plate
Courtesy of D. Seal (STFC/LancU)
Notes: Another unique facility allows to test planar samples at the RF conditions at 7.8 GHz.
The advantage of this system:
A simple sample – a disk of 100-mm diam
on fast turn-around time (~2 days for each sample).
An example of Rs(Ts) for Nb and Nb3Sn

## Slide 20
A path towards the goal
(2) Superconducting thin film coated RF cavity
Notes: All our finding must be finally lead to RF cavity deposition and testing

## Slide 21: Development of 6 and 1.3 GHz cavity coating
Cylindrical Magnetron has been built
Nb thin film depositions on cylindrical and cavity shaped surfaces are ongoing
Cylindrical magnetron in low power (DC) sputtering mode
Plasma dominated by argon emission
Cylindrical magnetron in high power (HIPIMS) sputtering mode
Plasma dominated by niobium emission

## Slide 22: 6 GHz split cavity
An idea suggested by G. Burt (CI)
The cavity cut is along the electric field lines, i.e. electric current is not crossing the cut
Easy to coat with either conventional planar magnetron or in tubular geometry used for RF cavities
Easy to inspect
Two 6 GHz cavities were Nb coated and tested at 4.2 K  T  11 K
Split cavity mounted on the cold head for cryogenic measurements
Surface resistance Rs as a function of temperature
for Nb thin films coated split cavity
Nb thin films coated split cavity
Courtesy of N. Leicester (STFC/LancU), T. Sian, and J. Conlon (STFC/LancU)
A split cavity during thin film deposition
Notes: Another unique project is exploring a longitudinally split cavity.
Read

## Slide 23: 1.3 GHz cavity testing
Aiming a high power test
  Required fully operational by end of 2023
    Main Delivery for IFAST WP9: a non-Nb SC coated prototype testing (by March 2025)
  Cryostat and insert:
    Cryostat is available
    New insert is designed, parts manufactured, assembling in process
  Copper cavity:
    will be provided by I.FAST partners: Piccoli and LNL/INFN
    looking for UK industry as well
    Coating with STF at STFC/DL
  Clean room for assembling the cavity – TBD
  RF amplifier – under development
  Bunker and cryogenics:
    SuRF lab infrastructure is available
Notes: Finally, the deposited cavity must be tested
Read

## Slide 24: Superconducting Cavity Evaluation in SuRF lab
SRF bunker
He liquefier and
LHe storage Dewar
Clean room and assembly area
Courtesy of T. Sian
This STFC/DL infrastructure
is being used for the full power SRF testing of >160 cavity modules for ESS and
will be used for SRF testing of PEP-II cavities
This infrastructure can be used in future for the full power SRF testing of superconducting thin film coated RF cavities
Notes: Large infrastructure already exist in STFC/DL for Superconducting Cavity Evaluation .
Read

## Slide 25: Future for TF-SRF cavities in UK
Development
Single layer coating:
  Nb
  Nb3Sn, NbTiN, V3Si, Mg2B
Multilayer coatings
  SS, SIS, SISIS…
Multicell cavity coating
Split cavity development
Low and high power RF testing at STFC/DL
Possible applications
RF loaded test in CLARA
  Multicell cavities
  Split cavity
  LHe-free cryo-cooling
UK-XFEL
ISIS-II
…
Possible involvement in international projects (e.g. ILC, FCC…)
Notes: The future development will be following these stages: read
Ultimately, the RF civilities should be used for future machined : read

## Slide 26: Conclusions
A significant progress since the programme started in 2014
Developing coating technology for superconducting thin films: an ongoing systematic study of correlation between deposition parameters and superconducting properties:
  Mastering Nb deposition
  Ongoing
  Development in non-Nb films: Nb3Sn, NbTiN, V3Si, Mg2B…
  Ongoing
  Developing deposition targets for non-Nb films
  Ongoing
  Deposition of SIS structures (e.g. Nb3Sn/AlN/Nb/Cu)
  Ongoing
  Thin film characterisation: SEM, FIB, XPS, XRD, AFM, RBS…
  Ongoing
  DC/AC superconductivity evaluation with in-house built and commercially available facilities
  Ongoing
  RF superconductivity evaluation with 7.8 GHz choked cavity test for planar samples
  Ongoing
Developing cavity deposition expertise
  Copper cavity production (incl. EB welding)
  Looking for industry partners
  Polishing and cleaning of copper cavities
  In plans (industry or in-house)
  Building and commissioning deposition facilities
  Ongoing
  Optimising deposition parameters for 1.3 and 6 GHz cavities
  Ongoing
  Plasma characterisation
  In progress
  Developing deposition targets
  In progress
SRF testing at DL
  6 GHz split cavity low power testing
  Ongoing
  Full power testing facility for 1.3 GHz cavity
  Nov. 2023
  Scaling up to a routine cavity coating and testing
  In plans - 2025
  Multicell cavities
  In plans - 2028
Applying TF-SRF cavities
  UK projects: UK-XFEL and ISIS-II
  In plans - 2025
  International projects, for example: FCC
  In plans – 20??
Notes: In conclusion you cab see that UK team is progressing well in TF development with a number of ongoing activities.
We are in a progress towards a single cavity coating and testing
And we have a vision to the future development and applications

## Slide 27: Acknowledgments
STFC/ASTeC:
  R. Valizadeh, C. Benjamin, L. Smith, A. Hannah, T. Sean, J. Conlon, F. Goudket, S. Wilde, S. Pattalwar, N. Pattalwar, A. May, P. Smith, J. Wilson, K. Dumbel, …
STFC/ISIS:
  G. Stenning
Liverpool University:
  J. Bradley, V. Danak, S. Simon, F. Lockwood Estrin, F. Walk
Lancaster University:
  G. Burt, H. Marks, D. Turner, D. Seal, N. Leicester
CEA:
  C. Antoine, …
CERN:
  A. Sublet, W. Venturini, G. Vandoni, M. Taborelli, …
IEE:
  E. Seiler, R. Ries and F. Gömöry
IJClab:
  D. Longuevergne and O. Hryhorenko
INFN
  C. Pira, E. Chyhyrynets, …
HZB:
  O. Kugeler, S. Keckert, D. Tikhonov, …
RTU
  A. Medvids, P. Onufriev …
Siegen University
  M. Vogel, A. Zubtsovskii …
…